Emergent Magnetism at Transition Metal-Nanocarbon Interfaces

F. Al Ma’Maria,b, M. Rogersa, S. Alghamdia, T. Moorsoma, S. Leec, T. Prokschad, H. Luetkensd, M. Valvidarese, G. Teobaldif,g, M. Flokstrac, R. Stewartc, P. Gargianie, M. Alia, G. Burnella, B.J. Hickeya and O. Cespedesa,1

aSchool of Physics and Astronomy, University of Leeds, Leeds LS2 9JT, UK.; bDepartment of Physics, Sultan Qaboos University, P.O. Box 36, 123 Muscat, Oman; cSchool of Physics and Astronomy, SUPA, University of St Andrews, St Andrews KY16 9SS, UK; dLaboratory for Muon Spin Spectroscopy, Paul Scherrer Institut, 5232 Villigen, Switzerland; eALBA Synchrotron Light Source, E-08290 Barcelona, Spain; fStephenson Institute for Renewable Energy, Department of Chemistry, University of Liverpool,Liverpool  L69 3BX; gBeijin Computational Science Research Centre, Beijing 100193 China.

1Corresponding author email address: o.cespedes@leeds.ac.uk

Charge transfer at metallo-molecular interfaces may be used to design multifunctional hybrids with an emergent magnetization that may offer an eco-friendly and tunable alternative to conventional magnets and devices. Here, we investigate the origin of the magnetism arising at these interfaces by using different techniques to probe 3d and 5d metal films such as Sc, Mn, Cu and Pt in contact with fullerenes and RF sputtered carbon layers. These systems exhibit small anisotropy and coercivity together with a high Curie point. Low energy muon spin spectroscopy in Cu and Sc-C60 multilayers show a quick spin depolarization and oscillations attributed to non-uniform local magnetic fields close to the metallo-carbon interface. The hybridization state of the carbon layers plays a crucial role, and we observe an increased magnetization as sp3 orbitals are annealed into sp2 graphitic states in sputtered carbon/copper multilayers. X-ray magnetic circular dichroism (XMCD) measurements at the carbon K-edge of C60 layers in contact with Sc films show spin polarization in the lowest unoccupied molecular orbital (LUMO) and higher * molecular levels, while the dichroism in the * resonances is small or non-existent. These results support the idea of an interaction mediated via charge transfer from the metal and dz- hybridization. Thin film carbon-based magnets may allow for the manipulation of spin ordering at metallic surfaces using electro-optical signals, with potential applications in computing, sensors and other multifunctional magnetic devices.

Interfaces are critical in quantum physics, and therefore we must explore the potential for designer hybrid materials that profit from promising combinatory effects. In particular, the fine tuning of spin polarization at metallo-organic interfaces opens a realm of possibilities; from the direct applications in molecular spintronics and thin film magnetism to biomedical imaging or quantum computing. This interaction at the surface can control the spin polarization in magnetic field sensors, generate a magnetization spin filtering effects in non-magnetic electrodes or even give rise to a spontaneous spin ordering in non-magnetic elements such as diamagnetic copper and paramagnetic manganese.(1-11)

The impact of carbon-based molecules on adjacent ferromagnets is not limited to spin filtering and electronic transport, but extend to induced changes in the metal anisotropy, magnetization, coercivity and bias.(12-14) Charge transfer and d(metal)-π(carbon) orbital coupling at the interface may change the density of states, spin population and exchange of metallo-carbon interfaces.(4, 15, 16) The interaction between the molecule and the metal depends strongly on the morphology and specific molecular geometry.(17, 18) It may lead to a change in the density of states at the Fermi energy N(EF) and/or the exchange-correlation integral (Is) as described by the Stoner criterion for ferromagnetism.(19, 20) The coupling can even extend through a non-magnetic metallic layer that carries the exchange information from a ferromagnetic substrate to an organic layer.(21)

The emergent magnetism measured in Cu/ and Mn/C60 multilayers extends as well to other transition metals close to complying with the Stoner criterion such as Sc and Pt –see table 1. We grow our films via DC or RF sputtering and in-situ thermal evaporation (SI Appendix, section 1). Although we could expect that metals closer to the Stoner criterion would present higher magnetization, it is apparent that the magnetic properties of the sample are strongly determined by the charge transfer and coupling between the carbon molecules and the metal. This is the case of Sc as compared to Cu; although Sc is very close to fulfilling the condition for ferromagnetism, it is also a material very prone to oxidation. Furthermore, the Fermi energy and the structure of Sc are not particularly well matched to those of C60. Copper, on the other hand, has a good dz- coupling, close lattice matching and the potential to transfer up to 3 electrons per fullerene cage, and this may result in the higher observed magnetization. The fullerenes may also be replaced by other nanocarbon allotropes with mixed sp2 and sp3 hybridization, such as RF-sputtered amorphous carbon (aC) layers. These films have the advantages of being smoother, cheaper than fullerenes and easily compatible with conventional metal sputtering, making them more suitable for potential industrial applications in the future. However, the resulting magnetization as measured using a superconducting quantum interference device -vibrating sample magnetometer (SQUID-VSM; see SI Appendix, Section 1) is on average 20-40% lower than when using C60, although they preserve the same trend observed in C60 multilayers, i.e. higher magnetization and coercivity when using copper films.

| System | Magnetisation (emu/cc metal) | Coercivity (Oe) |
| --- | --- | --- |
| Cu/C60 | 67±10 | 90±5 |
| Sc/C60 | 17±7 | 75±10 |
| Mn/C60 | 18±2 | 75±5 |
| Pt/C60 | 14±4 | 65±10 |
| Cu/aC | 35±5 | 95±10 |
| Sc/aC | 14±7 | 75±5 |

Table 1: Magnetic properties of different nanocarbon hybrids with 2-3 nm thick metal layers and the structure Si(substrate)/Ta(3)/Nanocarbon/Metal/Nanocarbon. All materials are deposited in the same chamber without breaking vacuum and with a base pressure ≤2×10-8 mbar. Metals are grown via DC magnetron sputtering, C60 is thermally evaporated and amorphous carbon (aC) is RF sputtered from a graphite target.

The magnetization of Cu and Mn – C60 multilayers has been measured to be dependent on the metallic film thickness, with a peak at 2-5 nm. However, the magnetic moment in Sc/C60 samples is roughly constant. For aC/Cu samples, a factor 2 higher moment is measured between ~2-5 nm, but this difference is not as large as for Cu/C60, where the moment is a factor 6 higher for Cu layers 2-2.5 nm thick than for layers of 3-4 nm. (4) This would be expected if the magnetic contribution is mostly due to the interfacial region, resulting in a surface magnetization of ~0.05 emu/m2 in C60/Sc and 0.1 emu/m2 in aC/Cu (see fits in Fig. 1A). The presence of a magnetic moment for films below ~1 nm in Sc/C60 seems indicative of a good wetting of the C60 by the Sc film, leading to continuous films or large superparamagnetic islands with high susceptibility at room temperature. Copper films grown on C60, on the other hand, tend to form islands that fill the rifts formed on the uneven molecular film (RMS roughness of ~1-2 nm compared to ≲0.5 nm for sputtered metals) before forming a continuous layer. The effect of the metal film thickness in the total roughness of the hybrid multilayer is also related to the formation of clusters. As seen in figure 1B, samples with thin metal layers are smoother than equivalent samples with thick metal layers, which may have an impact on the magnetization.

Pt and Sc-C60 samples result in a relatively weak magnetization and low coercivity Hc. According to the Stoner-Wohlfarth model,(22, 23) the coercive field in the easy axis, Hc, should be equal to K/Ms, where K is the magnetocrystalline uniaxial anisotropy and Ms is the saturation magnetization. For superparamagnetic systems with random crystal orientations, this equation is modified so that Hc drops with temperature till it reaches a zero ideal value for single magnetic domains at the blocking temperature TB: (24)

HC≈KMs1-TTB                    (1)

Zero field cooled-field cooled (ZFC-FC) measurements of thin Sc multilayers (<1nm) show a thermal hysteresis not characteristic of ferromagnetic materials, but rather of superparamagnets or spin glasses below their blocking temperature (Fig. 1C).(25) The magnetic anisotropy derived from the fit of the coercive field to equation (1) is very small, ≲500 J/m3 –similar to that of permalloy (Fig. 1D). On the other hand, the blocking temperature is very high, some 885 K, corresponding to a grain size of 20 nm (K·V≈TB). Thicker Sc(2nm)/C60 films display shape anisotropy with saturation fields of 5 kOe (10 kOe) at 300 K and 12 kOe (17 kOe) at 2 K  for in-plane fields (out of plane), respectively. The sample saturation magnetization at low temperatures is not reached until fields of >10 kOe are applied for both in-plane and out-of-plane measurements. The atomically rough interface may give rise to weakly coupled magnetic moments with random orientation that do not align easily in smaller fields. That can lead to the observed behavior at low temperatures and the zero field cooled/field cooled measurements for ultra-thin films (<2 nm) with enough random dipolar fields.

Density functional theory (DFT) simulations show that the magnetization is more concentrated at the interface for aC/Cu than for C60/Cu samples, resulting in a slower decay of the interface magnetic moment with the metal layer thickness (see SI Appendix, Section 2). This effect is linked to a higher magnetic contribution of the carbon layers in the case of aC compared to C60 (Figure 1F). Up to 95% of the moment in Cu/C60 is computed to be in the metal, with the remaining 5% in the C60, but for Cu/aC the moment in the carbon can be as high as 40% of the total. The calculated Stoner product of the exchange integral (Is) with the density of states at the Fermi level (DOS(EF)) is also smaller for aC/Cu than for C60/Cu, which agrees with the lower measured magnetization (Figure 1G).

Figure 1: (A) Magnetometry in Si//Ta(3)/C60(15)/Sc(t)/C60(15)/Al and Si//Ta(3)/aC(5)/Cu(t)/aC(5)/Al multilayers, lines are fit to a constant interfacial magnetic moment. B Sample roughness measured via atomic force microscopy (AFM) vs. number of layers (N) when each film thickness is kept constant (blue dots; line fit to N2) or when the total multilayer thickness is kept constant (green squares; line fit to asymptotic decay). Both curves should intercept at N=4, but different AFM tips shift them with respect to each other by 1-2 Å. (C) ZFC-FC characteristic measured at 100 Oe for a 0.2 and a 2 nm Sc samples normalized to the low temperature FC moment. The measurement shows thermal hysteresis typical of systems such as superparamagnets and spin glasses. (D) The coercivity of thin Sc films with C60 increases upon cooling following the dependence for superparamagnetic systems but with a high blocking temperature of 885 K. (E) C60/Sc(2)/C60 samples have a high saturation field that increases at low temperatures and with fields perpendicular to the sample. (F) The simulated contribution of the carbon atoms (MC) to the total magnetic moment (Mtot) for different carbon allotropes and densities shows that the magnetism in the carbon layers is more significant for aC/Cu than for C60/Cu. The as-sputtered aC has a density of ~1.7 g/cc, whereas for annealed graphitic films it is ~2.3 g/cc (G) The simulations predict as well a larger Stoner product Is×DOS(EF) for C60/Cu than for most aC/Cu systems, in line with the experiments that show larger moments in C60-metal samples (Table 1).

In order to investigate the magnetic order at the interface and the propagation length of the effect, we use low energy muon spin rotation (μSR) to provide a magnetic profile of the sample.(26-29) Here, a beam of almost fully polarised positive muons (μ+) is moderated to keV energies so that their tunable stopping range is of the order of tens to hundreds of nm. The time evolution of the muon spin polarization is a highly sensitive probe of the local magnetism. This is measured through the detection of the anisotropically emitted decay positrons, preferentially emitted along the muon’s spin direction at the moment of the decay (see SI Appendix, section 2 for further detail).  We use this technique to probe two Sc-C60 and Cu-C60 samples whose structure includes a thin Sc film of 2 nm (2.5 nm for Cu-C60) and a thick Sc film of 5 nm (15 nm for Cu-C60). Nanoscaling of non-magnetic metals has been shown to give rise to spin ordering.(30-33) The thin films should give rise to a strong magnetic signal, whereas for the thicker films, the interfacial magnetization should be quenched or diluted by the bulk properties of the metal. Full sample structures and muon stopping profiles are shown in figures 2A-B.

The muon spin spectroscopy measurements in Sc-C60 and Cu-C60 multilayers show similar properties. At 250 K, both samples have an exponential decay of the polarization at zero field and at remanence that may be due to the presence of local magnetic fields with dynamic or topological variations.(34, 35) The amplitude of this signal can be modelled as a function of the contribution of each individual layer in the samples. We find that the C60 interfaces with thin metal layers have a much stronger contribution to the depolarization; e.g. for the Sc-C60 sample only 2% of the muons stopped in the top C60 layer (in contact with Au and thick Sc) contribute to the fast exponential decay vs. 60% of those stopping in the bottom C60 layer close to the thin Sc film -see boxes in Figs. 2C-D. Similar fast exponential decay terms can be observed in antiferromagnetic or ferrimagnetic systems with spin canting, which would explain the low remanent magnetization observed in these samples.

The presence of local hyperfine fields may also be evidenced by a zero-field precession signal at 250 K of ~1.1 MHz in Sc/C60 and ~0.4 MHz in Cu/C60. Due to the lack of screening electrons in the molecular semiconductor, muons couple with electrons in C60 to form the bound state muonium (+-e-).(36, 37). Two muonium states are known in C60: i) the exohedral muonium radical with anisotropic hyperfine coupling which is observable below 100 K where the C60 rotational modes are frozen, and ii) the endohedral muonium state with a large (vacuum muonium like), isotropic hyperfine coupling. At 250 K the zero-field precession of the exohedral muonium state is not observable due to the fast C60 rotation. The isotropic endohedral muonium state should not cause a zero-field precession in the MHz range. However, charge transfer from the transition metal to the C60 may cause a deformation of the cage as it is observed for the C60 spin triplet state.(38) This deformation may result in a slightly anisotropic hyperfine coupling of the endohedral muonium state which then gives rise to the observed precession frequency in the MHz range, similar as it has been observed in C70.(39)

The difference in the zero-field precession frequencies could then be related to different charge and spin states as a function of the transition metal used as a substrate. The frequencies of oscillation shift in remanence after an applied magnetic field of 300 Oe, and the amplitude of the signal is once again stronger when probing the bottom Sc or Cu/C60 interface (Fig. 2E). Fig. 2F (top) shows the change in the precession amplitude attributed to field inhomogeneities. This can be related as well with the random orientation of local dipoles in small fields due to film roughness. The oscillation frequency of the muons in an applied transverse external field of 140 Oe is also increased for implantation energies corresponding to thin Cu layer due to the additional local field (Fig. 2 F-bottom).

Below 100 K, it is possible to observe the zero-field muonium precession frequencies of the exohedral radical state in the range of 1-9 MHz. The fact that the muonium oscillation frequencies are clearly observable implies that the magnetization must be localized close to the Cu layers; otherwise the internal fields would shift/destroy these modes in C60. Their amplitude can be used to probe the magnetic properties of the sample at 20 K (Figs. 2G-H). Given the number of particles implanted in C60, the muonium signal should increase to reach a maxima at 8 keV (Sc-C60) or at 18 keV (Cu-C60). However, the signal remains roughly constant, indicative of magnetic fields perturbing the muonium signal at the higher implantation energies towards the bottom layers.

Figure 2: Muon stopping profile for (A) multilayer with the structure  Si//Ta(3)/C60(20)/Sc(2)/ C60(50)/Sc(5)/C60(20)/Au(10) (Sc-C60) and (B) multilayer with the structure Si//Ta(3)/C60(25)/Cu(2.5)/ C60(50)/Cu(15)/C60(25)/Au(25) (Cu-C60) –film thickness in brackets in nm. All measurements at 250 K unless otherwise indicated. The amplitude of the slowly relaxing component in the muon precession is reduced as we approach the thin metal films in (C) Sc-C60 and (D) Cu-C60, indicating the presence of a depolarization term. Lines are fits to the percentage of muons implanted at each layer contributing to the decay. Schematics show this contribution for each multilayer in a red colour scale.  In remanence, the decay is faster but the contributions remain proportionally the same. The magnetic contribution of the bottom metal-C60 interfaces leads to a drop of the muon decay asymmetry at 10-12 keV (Sc-C60) or 18 keV (Cu-C60).  (E) Top: Muon oscillation amplitude at zero field in Sc-C60 (1.1 MHz). Bottom: in remanence with two contributions (1.1 and 0.8 MHz). Lines are a fit to the layers contribution, with the bottom metal and C60 layers having the largest input. (F) Oscillation amplitude (top) and frequency (bottom) for the muon precession in Sc-C60 with an applied transverse field. Muonium oscillation intensity (1.2, 7.8 and 9 MHz) at 20 K compared to the percentage of muons implanted in C60 layers for (G) Sc-C60 and (H) Cu-C60. Local magnetic fields at the bottom layers reduce the muonium signal.

The orbital hybridization and molecular coupling with the metal are essential to the charge transfer and emergent magnetism. C60 films degrade in ambient conditions due to light induced oxidation, which leads to a decay of the magnetization in a few days if the structures are not protected (Fig. 3A). The concentration of oxygen in C60 exposed to atmospheric conditions drops when heated in vacuum at 400 K, reaching near pristine levels by 450 K.(40) The magnetism at Sc/C60 interfaces follows this de-oxygenation trend, with increased magnetization after heating to 400-500 K. At higher temperatures, the C60 is desorbed from the metallic substrate, leading to a reduced magnetization (Fig. 3B).

For RF sputtered carbon, annealing alters the orbital states, bonding and structure of the layers. We use Raman spectroscopy to track these changes via two vibrational modes: the D band due to the breathing of benzene rings, and the G band due to the stretching of the C-C bond (E2g mode at the -point).(41, 42) As the annealing temperature is increased, the G band shifts to higher frequencies; from 1520 to 1615 cm-1. The intensity of the D band (ID) with respect to the G band (IG) gets progressively higher; ID/IG increases from ~0.6 in as-deposited films to ~2 after annealing at 875 K for one hour (Fig. 3C). The Raman changes are evidence for the conversion of amorphous carbon into nanocrystalline graphite and the change of orbital hybridization from sp3 to sp2.(41-43) In as-deposited films, the estimated percentage of sp3 orbitals from the ID/IG ratio and G peak position is ~15-20%, but at 875 K the percentage has dropped to zero. Above 875 K, graphitic nanocrystals expand until they form full graphite sheets. This leads to the G peak shifting back to lower frequencies and the ID/IG ratio decreasing again. In addition to these well characterized changes, above 875 K there is the formation of a new peak at 1275 cm-1 that we have labelled as D*. This peak is at a frequency below those conventionally assigned to the D band in graphite for a 532 nm source even in strain/stressed samples (1340-1380 cm-1).(44) This shift could be due to charge transfer and reduction of the carbon atoms.

The structural changes result in a reduced magnetization but increased coercivity (Fig. 3D), with a net enhancement in the B×H energy product (SI Appendix, section 3). These results are reproducible for samples annealed in-situ (i.e. heated inside the SQUID at 50 mtorr He atmosphere using an oven probe) and ex-situ (annealed in an external oven under vacuum and then re-measured). The solubility of carbon in solid Cu above 1100 K for 72 h –i.e. at higher temperatures and for longer times than those used in our experiment, is below 5 atomic ppm.(45) Although the solubility of RF sputtered aC in thin films of Cu could be different than in bulk, we do not observe any sign of interdiffusion.

Figure 3: Degradation, annealing and carbon hybridization effects. (A)  Time decay of the magnetization in Cu/C60 multilayers. In samples with several layers, the bottom interfaces are protected from chemical degradation by the top layers, and the magnetization decay is slow. (B) By annealing, the magnetization of a Si//C60(15)/Sc(3nm)/C60(15) sample can be enhanced or the degradation compensated. (C) Raman spectra of RF sputtered amorphous carbon on Cu after annealing. At 475-775 K, the G peak moves to higher frequencies and decreases in intensity relative to the D peak. At 875 K and above, the G peak increases again and the D peak has a replica at 1275 cm-1. (D) Evolution of the magnetization and carbon structures during the annealing process. Lines are a guide to the eye. Schematics show the sample structure changes derived from the Raman spectra.

An independent measurement of the magnetization contribution of the carbon material is provided by soft X-ray Absorption Spectroscopy (XAS), exploiting its inherent chemical specificity when the X-ray photon energy is tuned at the carbon K-edge electronic transition. It can therefore be used to assess the presence of magnetic ordering in a given element separately from the contribution of other layers or impurities using X-ray Magnetic Circular Dichroism (XMCD).(46) The K edge XMCD can only probe orbital polarization due to the zero angular momentum of the 1s core shell.(47, 48)  In figure 4 we present results in the near edge X-ray fine absorption spectroscopy (NEXAFS) and XMCD at the carbon K-edge of a Sc-C60 sample under a 1 T applied magnetic field along the X-ray beam direction, incident at a 45 degree angle on the film. The edge structure of C60 on the metal surface is complex, and at room temperature it includes features at 284 (LUMO), 286.2, 286.7 and 287.5 eV (excited LUMO+1, +2, +3) in the * antibonding region. (49, 50) The positions of these peaks are lower in energy than for pure C60, which has previously been observed for fullerene films in contact with other conducting magnetic substrates.(51, 52) The * region is above the ionization potential and the modes are less defined, producing wider peaks. The HOMO-LUMO transition (h1u-t1u) in C60 is optically forbidden, although it is weakly present via vibrational excitations.

In XMCD spectra at room temperature, the first unoccupied states at the LUMO (t1u-t1g levels) appear as magnetically ordered with the positive X-ray polarization having lower electron yield current –we refer to this as negative dichroism, observed here in the absence of magnetic material. Conversely, the following peaks around 287.5 eV (LUMO+2,+3) have positive dichroism. In contrast to this spin polarization for * states, the * antibond orbitals are weakly or not polarized, see figure 4. Similar results with a negatively polarized LUMO and positive higher * states can be obtained in samples with other Sc film thicknesses and under other experimental configurations (SI Appendix, section 4). The measurements show a time dependence due to charging effects and/or radiolysis, but the sign of the dichroism is changed when the Xray polarization is reversed or a negative magnetic field is applied.

There is a small peak some 5.5 eV above the LUMO, at 289.5 eV. This energy is too high for a charged LUMO * state. However, the resonance is too narrow and well defined for a * state. Also, the peak becomes much stronger at low temperatures, indicating a quantum state difficult to observe at 300 K. We hypothesize that these characteristics may be interpreted as due to a delocalized superatom molecular orbital (SAMO), previously measured using low temperature scanning tunneling microscopy in C60 deposited on a metal surface.(53) The highest relative photo-ionization cross section would correspond to the s-wave orbital,(54) but here the energy gap to the LUMO is closer to values observed in microscopy for p- or d-wave orbitals. Another possibility is that this peak constitutes a carbon core exciton (CEx) close to the ionization potential.(55, 56) XMCD measurements show this state to have the same polarization direction as the LUMO. In addition to this prospective magnetically polarized SAMO, two non-polarized states become visible at low temperatures: the metal-coupled charged carbon state at 282-283 eV, and the peak due to aggregated or graphite-like C60 at 285.3 eV.

In conclusion, we have shown evidence for the universality of the emergent magnetism in metal-nanocarbon interfaces and its magnitude in different materials. Our results give evidence that it is indeed possible to have spin-polarized states at a metallic interface with molecular carbon even in the absence of magnetic materials. This is of critical importance in the design and measurement of organic spintronic devices and magnetic field sensors, where these interfaces can be used as spin filters. Furthermore, given changes in polarization at the different energy levels, a gate voltage may give us tuning access to spin up/down configurations or new quantum configurations, such as spin-polarized superatom orbitals or polarons. The possibility of tailoring the magnetic properties of transition metal-nanocarbon hybrids by using molecular interfaces opens as well tantalizing possibilities - for example in non-corrosive magnets, bio-compatible hybrid nanoparticles, metal recovery and in magnetic memories where the information is controlled via charge transfer with electro-optic irradiation.(5, 6)

Figure 4: X-ray spectroscopy of C60 grown on a Sc 4 nm film collected at room temperature (top) and at 2 K (bottom). The measurements are done under an applied 1T perpendicular magnetic field in the total electron yield mode (TEY) and a 45º beam incidence. The NEXAFS show the typical structure of C60 –suggested modes in the bottom panel. Both measurements show magnetic dichroism, indicating the presence of a considerably large orbital polarization in the C60 density of states -even in the absence of a magnetic substrate. Note that XMCD measurements at low temperatures are multiplied by a smaller factor and that there is an additional, negatively polarized peak provisionally assigned to a superatom molecular orbital (SAMO) or core exciton (CEx).

ACKNOWLEDGMENTS. We thank the Engineering and Physical Sciences Research Council (EPSRC) in the UK for support through grants EP/P001556/1, EP/J01060X/1, EP/I004483/1 and EP/M000923/1. XAS/XMCD experiments were performed in the BOREAS beamline at the ALBA synchrotron (proposals ID2014071101 and ID2015091530). MV wishes to acknowledge Mineco grant FIS2013-45469-C4-3-R. The SR experiments were performed at the Swiss Muon Source SS at the Paul Scherrer Institut, Villigen, Switzerland. SA thanks Taibah University for support with a PhD scholarship. Use of the N8 POLARIS (EPSRC EP/K000225/1) and ARCHER (via the UKCP Consortium, EP/K013610/1 and EP/P022189/1). High Performance Computing facilities is gratefully acknowledged.

1.	Djeghloul F, et al. (2016) High Spin Polarization at Ferromagnetic Metal-Organic Interfaces: A Generic Property. Journal of Physical Chemistry Letters 7(13):2310-2315.

2.	Barraud C, et al. (2010) Unravelling the role of the interface for spin injection into organic semiconductors. Nature Physics 6(8):615-620.

3.	Raman KV, et al. (2013) Interface-engineered templates for molecular spin memory devices. Nature 493(7433):509-513.

4.	Al Ma'Mari F, et al. (2015) Beating the Stoner criterion using molecular interfaces. Nature 524(7563):69-U128.

5.	Atodiresei N & Raman KV (2014) Interface-assisted spintronics: Tailoring at the molecular scale. Mrs Bulletin 39(7):596-601.

6.	Moodera JS, Koopmans B, & Oppeneer PM (2014) On the path toward organic spintronics. Mrs Bulletin 39(7):578-581.

7.	Carmeli I, Leitus G, Naaman R, Reich S, & Vager Z (2003) Magnetism induced by the organization of self-assembled monolayers. Journal of Chemical Physics 118(23):10372-10375.

8.	Vager Z & Naaman R (2004) Bosons as the origin for giant magnetic properties of organic monolayers. Physical Review Letters 92(8).

9.	Naaman R & Vager Z (2010) Cooperative Electronic and Magnetic Properties of Self-Assembled Monolayers. Mrs Bulletin 35(6):429-434.

10.	Crespo P, et al. (2004) Permanent magnetism, magnetic anisotropy, and hysteresis of thiol-capped gold nanoparticles. Physical Review Letters 93(8).

11.	Hernando A, Crespo P, & Garcia MA (2006) Origin of orbital ferromagnetism and giant magnetic anisotropy at the nanoscale. Physical Review Letters 96(5).

12.	Moorsom T, et al. (2014) Spin-polarized electron transfer in ferromagnet/C60 interfaces. Physical Review B 90(12).

13.	Bairagi K, et al. (2015) Tuning the Magnetic Anisotropy at a Molecule-Metal Interface. Physical Review Letters 114(24).

14.	Gruber M, et al. (2015) Exchange bias and room-temperature magnetic order in molecular layers. Nature Materials 14(10):981-+.

15.	Raman KV & Moodera JS (2015) MATERIALS CHEMISTRY A magnetic facelift for non-magnetic metals. Nature 524(7563):42-43.

16.	Cespedes O, Ferreira MS, Sanvito S, Kociak M, & Coey JMD (2004) Contact induced magnetism in carbon nanotubes. Journal of Physics-Condensed Matter 16(10):L155-L161.

17.	Warner M, et al. (2013) Potential for spin-based information processing in a thin-film molecular semiconductor. Nature 503(7477):504-+.

18.	Serri M, et al. (2014) High-temperature antiferromagnetism in molecular semiconductor thin films and nanostructures. Nature Communications 5.

19.	Stoner EC (1938) Collective electron ferromagnetism. Proceedings of the Royal Society of London Series a-Mathematical and Physical Sciences 165(A922):0372-0414.

20.	Janak JF (1977) UNIFORM SUSCEPTIBILITIES OF METALLIC ELEMENTS. Physical Review B 16(1):255-262.

21.	Gruber M, et al. (2015) Spin-Dependent Hybridization between Molecule and Metal at Room Temperature through Inter layer Exchange Coupling. Nano Letters 15(12):7921-7926.

22.	Stoner EC & Wohlfarth EP (1947) INTERPRETATION OF HIGH COERCIVITY IN FERROMAGNETIC MATERIALS. Nature 160(4071):650-651.

23.	Stoner EC & Wohlfarth EP (1948) A MECHANISM OF MAGNETIC HYSTERESIS IN HETEROGENEOUS ALLOYS. Philosophical Transactions of the Royal Society of London Series a-Mathematical and Physical Sciences 240(826):599-642.

24.	Candela GA & Haines RA (1979) METHOD FOR DETERMINING THE REGION OF SUPERPARAMAGNETISM. Applied Physics Letters 34(12):868-870.

25.	Knobel M, et al. (2008) Superparamagnetism and other magnetic features in granular materials: A review on ideal and real systems. Journal of Nanoscience and Nanotechnology 8(6):2836-2857.

26.	Schulz L, et al. (2011) Engineering spin propagation across a hybrid organic/inorganic interface using a polar layer. Nature Materials 10(1):39-44.

27.	Morenzoni E, et al. (1994) GENERATION OF VERY SLOW POLARIZED POSITIVE MUONS. Physical Review Letters 72(17):2793-2796.

28.	Morenzoni E, et al. (2002) Implantation studies of keV positive muons in thin metallic layers. Nuclear Instruments & Methods in Physics Research Section B-Beam Interactions with Materials and Atoms 192(3):254-266.

29.	Prokscha T, et al. (2008) The new mu E4 beam at PSI: A hybrid-type large acceptance channel for the generation of a high intensity surface-muon beam. Nuclear Instruments & Methods in Physics Research Section a-Accelerators Spectrometers Detectors and Associated Equipment 595(2):317-331.

30.	Yamamoto Y, et al. (2004) Direct observation of ferromagnetic spin polarization in gold nanoparticles. Physical Review Letters 93(11).

31.	Niklasson AMN, Mirbt S, Skriver HL, & Johansson B (1997) Quantum-well-induced ferromagnetism in thin films. Physical Review B 56(6):3276-3280.

32.	Cespedes O, Wheeler M, Moorsom T, & Viret M (2015) Unexpected Magnetic Properties of Gas-Stabilized Platinum Nanostructures in the Tunneling Regime. Nano Letters 15(1):45-50.

33.	Hong SC, Lee JI, & Wu R (2007) Ferromagnetism in Pd thin films induced by quantum well states. Physical Review B 75(17).

34.	Graf MJ, et al. (2003) Onset of antiferromagnetism in UPt3 via Th substitution studied by muon spin spectroscopy. Physical Review B 68(22).

35.	Nakano T, et al. (2009) Fast muon spin relaxation in ferromagnetism of potassium clusters in zeolite A. Physica B-Condensed Matter 404(5-7):630-633.

36.	Duty TL, et al. (1994) ZERO-FIELD MU-SR IN CRYSTALLINE C-60. Hyperfine Interactions 86(1-4):789-795.

37.	Kiefl RF, et al. (1992) MOLECULAR-DYNAMICS OF THE MUONIUM-C60 RADICAL IN SOLID C-60. Physical Review Letters 68(17):2708-2712.

38.	Filidou V, et al. (2013) Probing the C-60 triplet state coupling to nuclear spins inside and out. Philosophical Transactions of the Royal Society a-Mathematical Physical and Engineering Sciences 371(1998).

39.	Prassides K, et al. (1992) MU-AT-THE-COST-OF-C70 - MONITORING THE DYNAMICS OF FULLERENES FROM INSIDE THE CAGE. Journal of Physical Chemistry 96(26):10600-10602.

40.	Werner H, et al. (1994) REACTION OF MOLECULAR-OXYGEN WITH C-60 - SPECTROSCOPIC STUDIES. Journal of the Chemical Society-Faraday Transactions 90(3):403-409.

41.	Ferrari AC & Robertson J (2004) Raman spectroscopy of amorphous, nanostructured, diamond-like carbon, and nanodiamond. Philosophical Transactions of the Royal Society a-Mathematical Physical and Engineering Sciences 362(1824):2477-2512.

42.	Ferrari AC & Robertson J (2001) Resonant Raman spectroscopy of disordered, amorphous, and diamondlike carbon. Physical Review B 64(7).

43.	Ferrari AC & Robertson J (2000) Interpretation of Raman spectra of disordered and amorphous carbon. Physical Review B 61(20):14095-14107.

44.	del Corro E, Taravillo M, & Baonza VG (2012) Nonlinear strain effects in double-resonance Raman bands of graphite, graphene, and related materials. Physical Review B 85(3).

45.	Lopez GA & Mittemeijer E (2004) The solubility of C in solid Cu. Scripta Materialia 51(1):1-5.

46.	Barla A, et al. (2016) Design and performance of BOREAS, the beamline for resonant X-ray absorption and scattering experiments at the ALBA synchrotron light source. Journal of Synchrotron Radiation 23:1507-1517.

47.	Ohldag H, et al. (2007) pi-Electron ferromagnetism in metal-free carbon probed by soft x-ray dichroism. Physical Review Letters 98(18).

48.	Guo GY (1996) What does the K-edge x-ray magnetic circular dichroism spectrum tell us? Journal of Physics-Condensed Matter 8(49):L747-L752.

49.	Shinohara H, Sato H, Saito Y, Tohji K, & Udagawa Y (1991) CARBON K-SHELL X-RAY ABSORPTION NEAR-EDGE STRUCTURE OF SOLID C-60. Japanese Journal of Applied Physics Part 2-Letters 30(5A):L848-L850.

50.	Kondo D, et al. (2002) Unoccupied molecular orbitals of C-60 molecules adsorbed on Si(001)-(2 x 1) and Si(111)-(7 x 7) surfaces studied by NEXAFS. Surface Science 514(1-3):337-342.

51.	Tran TLA, et al. (2011) Hybridization-induced oscillatory magnetic polarization of C-60 orbitals at the C-60/Fe(001) interface. Applied Physics Letters 98(22).

52.	Wong PKJ, et al. (2013) Electronic and magnetic structure of C-60/Fe3O4(001): a hybrid interface for organic spintronics. Journal of Materials Chemistry C 1(6):1197-1202.

53.	Feng M, Zhao J, & Petek H (2008) Atomlike, hollow-core-bound molecular orbitals of C-60. Science 320(5874):359-362.

54.	Bohl E, et al. (2015) Relative Photoionization Cross Sections of Super-Atom Molecular Orbitals (SAMOs) in C-60. Journal of Physical Chemistry A 119(47):11504-11508.

55.	Ma Y, et al. (1993) CORE EXCITONS AND VIBRONIC COUPLING IN DIAMOND AND GRAPHITE. Physical Review Letters 71(22):3725-3728.

56.	Saito Y, Shinohara H, & Ohshita A (1991) ELECTRON-ENERGY LOSS SPECTRUM NEAR CARBON K-EDGE IN SOLID C-60. Japanese Journal of Applied Physics Part 2-Letters 30(6B):L1145-L1147.

57. 	Associated data to this manuscript can be found at http://doi.org/10.5518/179