Fiber Utilization in Pervious Concrete: Review on Manufacture and Properties

Jie Li 1, Jun Xia1,*, Luigi Di Sarno2, Guobin Gong1

# Abstract

Impermeable structures rise from the ground to replace the original natural permeable structure, which caused urban runoff, flooding, and heat island effects to appear frequently. As a new type of material that can be exploited as a sponge city, the performance of pervious concrete PC needs to be improved as soon as possible. Referring to fiber in conventional concrete, whether the application of fibers to PC can improve its performance needs to be identified. This article conducts a comprehensive review including manufacture, performance, and mechanism based on published articles about fiber-reinforced pervious concrete (FPC) for fiber utilization in pervious concrete. This article recommended the manufacturing method, which includes mix design, mixing procedure, compaction, and curing method. Based on the experimental data provided by the existing literature, a comprehensive analysis was carried out to provide the best solution for adding fibers, which includes the type, length, aspect ratio, and volume fraction of the fibers. In addition, the research status of the five types of fibers in the five basic indicators in PC is summarized to explore visible research gaps, which are compressive strength, flexural strength, splitting tensile strength, porosity, and permeability.

Keywords: Compressive strength, Flexural strength, Splitting tensile strength, Porosity, Permeability, Pore characterization, and Durability.

|  | σ | Compressive strength |
| --- | --- | --- |
|  | σ0 | Compressive strength at zero porosity |
|  | p | Porosity |
|  | E | Elasticity modulus (Pa); |
|  | γ | Fracture surface energy (J/m2) |
|  | A | Half length of an internal crack (m) |
|  | K | Empirical constants |
|  | fca | Factor of type of aggregate |
|  | fe | Factor of exposure to acidic environment |
|  | fa | Factor of age |
|  | fT | Factor of temperature |
|  | C | The cement content of mix, expressed as fraction |
|  | rm | Mean distribution radius |
|  | FM | Fineness modulus (FM) |
|  | dMFS | Mean free spacing |
|  | dn | Number averaged pore size |
|  | ϕA | Porosity |
|  | Sp | Specific surface area of pores |
|  | Γ3D | Three-dimensional pore distribution density |
|  | d | Aggregate size |
|  | d0 | Smallest aggregate size |
|  | wc | Water-cement ratio |
|  | k | Permeability of pervious concrete (mm/s) |
|  | i | Hydraulic gradient |
|  | g | Acceleration of gravity |
|  | h | Hydraulic load |
|  | hf | Final hydraulic load |
|  | WFT | Water film thickness (mm) |
|  | PFT | Paste film thickness (mm) |

# Introduction

An important reason for the deterioration of freshwater resources is the impervious coverage of urban areas, replacing original permeable natural structures [1]. The paucity of the drainage system for heavy rain loads would cause urban flooding in impermeable areas [2]. In addition, the impermeable structure would maintain excessive heat to augment the heat island effect [2, 3]. The pervious concrete (PC) has been introduced to ameliorate this phenomenon, with enough connected pores to allow water to pass through [3]. The prominent permeability of PC would contribute to drainage and deliver beneficial effects on ‘Sponge City’ that boost rainwater management [4]. However, it would palpably deteriorate its strength due to pores. The limited application of PC is ascribed to the checks and balances of strength and water permeability [5]. Therefore, PC is usually used in light traffic load areas such as pavement or parking lots [6].

Pervious concrete is three-phase material, which includes paste, aggregates, and pores. The forming mechanism could be explained by aggregates enveloped by scarce pastes and forming a pore structure. The aggregates are bonded by the hydration of paste and together to provide strength in synergy. The general porosity varies from 15% to 30%, contributing to permeability. The typical compressive strength is an essential factor of about 2.8 MPa to 28 MPa [7].

The prior research mainly focuses on compressive strength and its relationship with permeability [8-10]. However, flexural and splitting tensile strength are equally crucial when PC is applied in pavement design, especially in permeable bricks or plates [11-13]. Recently, researchers were inclined to explore novel methods to improve PC performance, and referred fiber addition was considered an effective solution. The strength and permeability prediction model mentioned before shall adjust to consider the addition of fibers [14]. The length, aspect ratio, and elasticity of modulus of fibers would be considered as a parameter that affects its properties. Since the introduction of fiber-reinforced pervious concrete (FPC), the variety and interest are gradually increasing. Different types of fibers were explored, which have widely divergent characterization. The addition fiber embraced various types and could be broadly classified into five primary groups [15]: Synthetic, Natural, Carbon-based, Metallic, and Inorganic, as shown in Table 1.

The research timeline of fibers in PC is shown in Figure 1. The timing of the emergence of new fiber types is summarized. According to the published articles, the FPC first occurred in 2006. Kevern’s team [16-19] proposed that polypropylene fiber (PP) could be added to PC. It concluded that fiber addition increased compressive strength and contributed to permeability due to the improvement of void continuity. The polypropylene fiber addition in PC was investigated from then on with different lengths, aspect ratios, content, and modulus of elasticity, formed integrated research in 2006-2008, and found the compressive, permeability, and durability could be improved. After that, Natural fiber was also introduced into the PC system. In 2010-2011, Schaefer [20, 21] investigated one type of natural fiber, which is Cellulose microfiber in PC, and found that the PC with cellulose fiber would perform good mechanical properties and have less effect on permeability. In addition, Shu and Wu [22, 23] explored polypropylene fiber's effects on the abrasion resistance of PC. In subsequent studies, new types of fibers were continuously introduced. In 2012, Rehman [24]found that carbon fiber has higher tensile strength than PP and would perform better than PP in PC.

In 2014, Bonicelli [25] compared four types of synthetic fiber: polyolefin fiber, polypropylene fiber, and polyethylene fiber, with 12mm and 18mm lengths. It was found that only 18mm polyethylene fiber would improve the performance of the PC. Metallic fiber and inorganic fiber were introduced into the PC system. Hesami [26, 27] compared three fiber types: steel fiber, polyphenylene sulfide fiber, and glass fiber, and observed that steel fiber has enhanced compressive strength with respect to others. In addition, glass fiber exhibit augmentedsplitting tensile strength and polyphenylene sulfide fiber posseses improvedflexural strength. In 2015, Nayak [28] proposed that polyester could also be used in PC and found that it can improve overall mechanical properties, including compressive, flexural, and splitting tensile strength. In addition, Kerven [29] proposed that macro polypropylene fiber could be used in PC with considerable length and found no significant effects on mechanical properties and would decrease the permeability.

In 2016, some sustainable recycled materials were introduced. Kim [30] proposed two types of synthetic fibers made from recycled polypropylene fiber. These two types of fiber increased compressive strength and slightly increased infiltration ability. Moreover, Rangelov [31] proposed cured carbon fiber composite materials (CCFCM), which could be one kind of fiber made from carbon fiber composites. Each element contains a dense network of carbon fibers bonded by the thermoset resin. It would contribute to the mechanical properties of PC but may slightly decrease the porosity. In 2018, Aliabdo [32] compared rubber fiber and polypropylene fiber, and found that rubber fiber would decrease the mechanical properties but increase the permeability of PC. Avishreshth [33] used steel fiber with different shapes in PC and observed that the mechanical properties could be improved but decreased permeability. Zhong [34] proposed that Polyvinyl Chloride Fibers (PVC) is also a choice used in PC, but there needs to be evidence or exploration on the effects of PVC addition. In addition, Akand [35, 36] investigated the effectiveness of treated PPF through various chemical treatment and found that acid treatment was an optimum choice. Huang [37] proposed that Polyvinyl Alcohol fiber (PVA) would contribute to compressive and splitting tensile strength in 2019, but studies on permeability were not available.

Since 2020, various new types of fibers have been introduced. Ali [38] explored the effect of Waste Polyethylene terephthalate (WPF) fiber in PC. It could increase PC's permeability and flexural strength but deteriorate to compressive strength. Dai [39] compared the effects of addition with soft and hard polypropylene and basalt fiber in PC. It found that basalt could increase compressive strength but decrease the permeability of PC. Oni [40] compared three types of ultra-high performance fiber in pervious concrete brick, including Kevlar fiber (KF), PVA, and ultra-high molecular weight polyethylene fiber (UHMWPE ). Furthermore, it found that these three types of fiber would perform deterioration on mechanical properties except PVA and KF would increase the flexural strength. Three of them would increase the permeability.

Steel fiber notably improved ultra-high performance concrete and the same as for PC, which Hesami [27] referred to. It is conducive to the mechanical properties of PC but deteriorates freshwater resources due to evident corrosion. Therefore, copper-coated steel fiber and amorphous metallic fiber (AMF) were introduced. Zhu [41] studied the addition of copper-coated steel fiber in PC and found improved mechanical properties but reduced permeability. In addition, Park [42] found that adding Amorphous metallic fiber (AMF) would contribute to compressive strength and permeability simultaneously, and AMF would trigger water in the pore to evaporate quickly.

Moreover, Juradin [43] introduced one type of natural fiber, which is Hemp fiber in PC, it would decrease permeability. However, when the vibrated compacted method is used, the mechanical properties could be increased compared to the hammer compacted method. Mechrabi [14] proposed one type of macro-fiber, which is barchip fiber. It would increase the mechanical properties but need more studies about the effects on the permeability of PC. Wen [44] investigated that Polyacrylonitrile fiber (PANF) could improve compressive strength and permeability but decrease the flexural strength of PC. Juradin [45] introduced waste cloth strips in PC obtained from waste cotton T-shirts. For the large size of aggregates, the waste cloth strips would improve compressive strength but decrease permeability. Park [46] investigated natural fiber, kenaf fiber, which includes 45-57% cellulose, 22% hemicellulose, 8-13% lignin, and 3-5% pectin. It decreases the compressive strength of the PC.

It is worth noting that there is no unified experimental test method when exploring fibers' influence on PC in the literature mentioned. The size of the samples would affect the results and present differences, especially for detecting water permeability. In the earliest experiments on the strength prediction of pervious concrete, the specimen size of compressive strength was 150 by 300 mm cylinders [47] or 100 by 200mm cylinders [48, 49], which is referred to ASTM C39 [50] for conventional concrete. With the popularity of pervious concrete, the test methods of permeable concrete in each country refer to the test methods of conventional concrete in their own countries and propose the corresponding sample size. Existing major standards could be classified by three countries: the UK [51-54], the US [50, 55-61], and the Chinese [62-65]. These standards use different sample sizes for each property testing method. Table 2 below summarizes the sizes used by different standards. This article summarized and compared fiber effects in various literature with the same sample size and obtained a comparable conclusion.

Due to the desire to develop pervious concrete with excellent performance, the aggregate sizes used in the articles exploring fibers in PC are primarily distributed in the 5-10mm to balance hydraulic and mechanical properties. Several PC proportions combined 10~20mm partial particle size to optimize the aggregate particle size to obtain denser packing [26, 27, 66-68] or introduce fine aggregates to improve the overall performance [14, 66, 68, 69]. Dai [39] proposed that graded aggregates are more beneficial to the compressive strength of PC than single-size aggregates due to higher specific surface area. Liu [70] discovered that the average pore size would increase by adding 10-15mm aggregates and found that the pore distribution would be less homogeneous. Therefore, the compressive strength decreased with increasing 10-15mm aggregate content. In addition, to investigate the effects of different aggregates, Furkan Ozel [71] compared basalt, limestone, travertine, and pumice aggregates and found that pumice presented poor performance than others. Besides, recycled aggregates are an alternative method to replace natural aggregates. Although it will cause performance loss, PC performance is up to standard and more sustainable [32, 41, 67, 72].

The water-cement ratio should also be an essential factor in FPC. According to the review of these articles, water/cement (w/c) ratio is usually distributed between 0.2~0.4. Hesami [26] investigated PC, including rice husk ash and fibers, and found similar trends in each mechanical strength with different w/c, and w/c was optimized at 0.33. Zhu [41] found that the w/c would affect the fiber effects. Research on the influence of fiber content on permeability showed different trends at different w/c, which is similar to the conclusion of Liu [73]. Bonicelli [25] explored the w/c range from 0.27-0.35 and found that the smaller the water-cement ratio, the more pronounced difference in permeability. In addition, Tang [74] used an orthogonal test method to study the impact of w/c on the flow value of paste and the compressive strength of PC. It is found the impact is significant and the significance was higher than fiber content. On the contrary, Wen [44] confirmed that the significance of w/c is lower than fiber content in the orthogonal experiment.

Most of the research on pervious concrete focused on the results in the laboratory, while some other researchers have produced prefabricated permeable bricks and plates to control the quality of the finished product. The production process of permeable bricks is non-sintered, which is more environmentally friendly and energy-saving than sintered bricks. In addition, the pervious concrete production process differs between the laboratory and the in-situ. Therefore, permeable concrete in situ cannot deliver laboratory results. The laboratory is predominantly compacted by rodding and vibration instead of the road roller used for on-site construction. Therefore, the fibers in the finished product were also explored [40, 75].

In addition to paying attention to mechanical properties, resistance to freeze-thaw damage is also essential. Compared to conventional concrete, due to the existence of pores, the internal stress would be significant for the structure when the water freezes. Song [76] pointed out that the performance difference between aggregate and ITZ and expansion stress lead to deboning of aggregate and cement interface, which are the main culprits for the deterioration of pervious concrete under F-T conditions. Taheri [77] pointed out that a PC's pore structure would have no potential energy to bear the volume expansion due to water freezing when it is nearly saturated. In order to improve the freeze-thaw resistance of pervious concrete, some literature proposed improved methods, which include SCMs substitution [78], sand [18], AEA [79], latex [79, 80], and fiber addition. Kevern [18] investigated sand addition or substituting a portion of the coarse aggregate mixture and observed superior durability to the control mix. In addition, PC prepared with fly ash and silica fume delivered densified micrograph and enhanced the durability of PC [81]. Bilal [78] found that sand addition and SCM replacement with proper compaction enhanced the durability of the PC. For conventional concrete, proper air-entraining agent (AEA) addition would enhance the durability because it would have better F-T resistance when the void spacing factor is maintained at around 200 micrometers [82]. Wu [79] examined mixtures with AEA and found AEA provided improvement as that for ordinary concrete. The reason is mixtures with better uniformity due to AEA addition.

Besides, the effects of fiber addition on durability were studied. Wu [79] explored mixtures with PPF fiber and found that embedded fibers enhanced cracking resistance and mitigated the F-T damage. Amade and Rogge [83] used cellulose fiber in PC and found an impressive improvement in splitting tensile strength and F-T resistance by providing thermal expansion and contraction resistance. It is due to less fiber agglomeration appearing for tiny fibers. Wu [84] investigated hooked steel fiber and basalt fiber enhancement on F-T resistance and observed an improvement between the cementation layer and aggregates due to fiber addition. Han [75] compared carbon fiber, glass fiber, and polypropylene fiber addition in pervious concrete bricks and found that glass fiber had better-improved F-T resistance than carbon fiber due to the chemical bond force between glass fibers and cement. Fiber length and volume fraction would also affect durability. Kevern [29] found that short PPF fiber with 38mm had minor damage or no effect on durability at the lower dosage rate but performed better enhancement at a high dosage rate. Regardless of dosage, long PPF fibers with 50mm improved freeze-thaw resistance by around 30%. Kevern [16] focused on the effects of PPF fiber with short and long lengths and sand addition on durability. It observed that fiber addition with 0.03% or 0.1% by volume enhanced freeze-thaw resistance, which is the same as a mixture with sand. However, there is no significant difference between the effects of long and short fiber addition on durability. Wang [80] compared the freeze-thaw resistance of mixtures with sand, latex, and PPF fibers with different volume fractions. It is observed that there is an increase in F-T resistance due to fiber addition. However, the enhancement decreases as the volume fraction increases, but is still higher than the control mix. In addition, 7% sand delivered excellent improvement, but adding 10% latex showed a decreasing trend. Nassiri [85] explored the effects on the durability of PC with CCFCM addition and observed that 1% and 2% volume fractions of CCFCM enhanced F-T resistance, and 2% performed the highest resistance. The impact of fiber on durability would be different for different proportions of paste. Zhong [34] examined fiber effects on the durability of PC in three different matrices and observed that appropriate content of fiber addition improved the durability for ultra-high-strength matrices (UHSM) but minor enhancement for normal strength (NSM) and high-strength matrices (HSM). The reason may be that fiber enhancement for HSM and NSM could not remedy the deterioration of PC due to F-T damage. For crack growth, some articles have carried out 3-D laser scanning for local cracks. Liu [70] pointed out that basalt fiber with 20 mm in PC enhanced F-T resistance due to the bridge connection of fiber, which delayed the propagation of cracks. In addition, mixtures with fiber had a more homogeneous pore distribution. Zeng [86] illustrated the effect on crack permeability and crack surface topography of PC under freeze-thaw damage by camera recording and 3-D laser scanning. It defined the crack roughness by computational method to explore the effects of steel fiber addition. The mechanism of enhancement on freeze-thaw resistance due to steel fiber addition was observed: bridging cracks by fiber, reducing crack width, and reducing the damage due to freezing water by increasing closed pores volume. In addition, the predicted model was established to estimate the crack permeability by the material permeability parameter and the roughness number of the crack surface. Yang [87] examined PPF in PC and found it enhanced material toughness, thus producing more effective bonding between the fibers and the paste. Another explanation was that multidirectional fibers established more extensive pathways to escape water to avoid water retention.

To summarize, this article summarizes published literature, extracting available information. The manufacturing methods are classified, and the optimum or appropriate method is proposed, which includes mix design, mixing procedure, compacting, and curing method. In addition, it discusses different types of fibers' effects on mechanical and physical properties, identifying available and reasonable research gaps. This study will serve as an effective improvement plan for the subsequent research on fiber addition in PC. Compared with the PC prediction model without fiber summarized in the article, a reasonable predicted model for fiber is identified for subsequent research.

# Mixing, compacting, and curing method

## Mixing design for fiber and mixing procedures

The content of fiber addition in the PC should be specified. As shown in Table 3, there are generally six different fiber quantification methods in the mix design. The predominate approach is quantified by weight or volume fraction of PC (Type 1 and 2). Some of the researchers regard fiber as part of the cement paste and thus use cement replacement ratio, either by weight or by volume (Type 3 and 4). While some other researchers added fibers based on the skeleton aggregates, thus quantifying the fibers based on the  weight or volume of aggregates (Type 5 and 6). Type 4 and 6 are preferred to use due to they consider fiber volume in PC.

Pervious concrete has a unique structure, and its mixing process differs from conventional concrete. The PC needs to consider the state of materials to ensure that its paste can be evenly distributed on the surface of the aggregates. The suitable paste should have uniformity and cohesion to avoid segregation. Therefore, it is necessary to choose an appropriate mixing process. In addition, the process would be slightly changed based on the typical PC due to the existence of fibers to ensure that the fibers can be evenly distributed to exert the optimized effect. The literature showed that different mixing procedures of FPC could be divided into three primary categories, as shown in Table 4 [14, 16, 33, 38, 40, 42, 44-46, 67, 69, 70, 72, 73, 80, 84, 85, 88-93]: Consider Fibers in Pastes, Fibers in Aggregates, and Fibers as Additives. For the ‘Fibers in Pastes’ and ‘Fibers in Aggregates’ options, the fibers could either be dry or wet when added to mixing. In addition, the time to add fiber should be identified in pre-mixing or post-mixing. For the ‘Fibers as Additives’ option, there are four types of mixing procedures: the One-time feeding method, the Secondary feeding method, the Cement-wrapped stone method, and the Dispersion method. The different types of mixing procedures almost finish in the range between 2.5 minutes and 15 minutes, except the time for the ‘Fibers in pastes’ dry method takes up to 30 minutes. Appropriate processes can be selected according to the fiber types and mixed design principles.

## Compacting and curing method

The compacting methods in the existing literature are usually laboratory-based procedures. The compacting methods used in works of literature are summarized in Table 5. ASTM C09.49 and UNI EN 12697-30 [94, 95] proposed Method 1, specifying using a standard Proctor hammer to compact. It could control the compact energy by controlling the number of blows, and each blow would perform constant compact energy. Method 2, 3, and 4 were generally used in FPC, and some literature combined different times of rodding and vibration times for different numbers of layers. These combinations would perform full compaction or sometimes over-compacted due to excessive vibration, thus causing segregation. In addition, Method 5 is normally used in pavement construction. Bar vibration performed excellent compaction in practical applications for conventional concrete, but it usually leads to over-compaction for PC. Besides, Method 6 would be used to fabricate pervious concrete bricks or blocks. It can perform controllable compaction energy but requires the weighting of each material feed. The curing method could be divided into three categories, as shown in Table 6, and the most common method is water curing at 22-25℃. The moist curing by a film covering is usually for in-situ construction.

The mixing procedure, compacting, and curing methods affect the properties of PC, especially the fiber quantification and compacted methods that determine the effectiveness of fibers in FPC. The literature review shows there are no commonly adopted procedures and empirical criteria are usually used to judge the appropriateness of the final mixed materials.

# The effects of fiber addition on Mechanical and Physical Properties

## Compressive Strength

In conventional concrete, fibers are distributed homogeneously in the paste to form a bridging action, thereby enhancing the strength of the entire system. However, the distribution of fibers in PC would be affected by the pore size and distribution, resulting in different enhancement from conventional concrete. Furthermore, different specimen sizes may have a considerable impact on the performance. Most specimens' sizes were referred to ASTM C39 [50] and GB/T 50081-2019 [64], and the sizes are divided into four main categories, namely CY D100H200, CY D150H300, CU 150, and CU 100, in which CY refers to cylinder specimens while CU refers to cubic specimens. ASTM C39 stipulates that the correction coefficient should adjust samples with L/D less than 1.75. The same L/D of CY D100H200 and CY D150H300 and higher than 1.75. GB/T 50081-2019 stipulates that the specimen size is CU 150 and CU 100. Therefore, Cylinders and Cubes were separated in this article.

The effect of fibers on the compressive strength (CS) of PC varies because it also depends on the proportions of mixtures, mixing process, curing condition, compaction method, and especially target porosity for PC. Fig. 2 and 3 illustrate the improvement index for CS versus the volume fraction for synthetic and carbon-based fiber in cube and cylinder samples. The improvement index for compressive strength is obtained by comparing the FPC's performance with PC control mixtures. Different types of fiber quantifications were converted into volume fractions of fibers in a mixture for comparison.

For synthetic fiber in PC, as shown in Figure 2, the volume fraction is mainly distributed between 0~1.6% in Cylinder specimens, and up to 47% improvement can be achieved by using PPS fiber with 0.27 w/c [26]. With the increase of volume fraction, the changing trend of improvement index on compressive strength is different, some literature has minor effects [16, 80], some presented decreasing trend [20, 21, 67, 96], some delivered an increasing trend [30, 90], and some would be increased first and then decreased [29, 66, 68]. Alemu [90] discovered that PVA  addition would deteriorate CS significantly. However, the deterioration extent would be reduced with increasing PVA contents. On the contrary, the deterioration extent would be increased with increasing WPF contents [67]. In addition to deterioration, enhancements are also reported. Kevern [29] found that the improvement index first increased and then decreased with the PPF volume fraction increasing for two different lengths, but Schaefer [20, 21] found that the enhancement was reduced with increasing of volume fraction. Fiber length also affects enhancement. Schaefer [20, 21] explored the PPF with various length and volume fraction and observed a decreasing due to length increasing which also found in Dean’s [16] and Pils’s research [66]. However, Kevern [29] observed that longer PPF length would contribute to the enhancement extent at a medium volume fraction, but would minor deteriorate to the improvement extent at a relatively higher volume fraction. In Cubes specimens, the volume fraction is mainly distributed between 0~2.0%, but a few articles have studied fibers with a large volume fraction [32]. Juradin [43] investigated PPF addition in PC and achieved up to 112.05% by using vibration compacting method. Most of the literature results showed that the improvement index of compressive is decreasing after increasing as volume fraction increasing [32, 39, 41, 72, 97], and can identify an optimal volume fraction which would be affected by various factors. However, Ali [38] found the deterioration in compressive strength would be gradually exacerbated with volume fraction incremental increase of PET fiber.

There are limited studies on carbon-based fiber. Nassiri's team has conducted corresponding research on cured carbon fiber composite material (CCFCM) from 2016-2021[5, 31, 85, 98, 99], and adopted cylinder specimens. The other is pure carbon fiber [43, 100, 101], and cubes specimens were exploited. In cylinders specimens, the Nassiri team explored the complete volume fraction distribution and four different lengths of fibers and found that the enhancement effect was insignificant. In cubes specimens, the distribution of research on pure carbon fiber is relatively discrete, with a volume fraction of up to 5%. Most literature showed positive effects, of which the highest reached 124.1% improvement with vibration compaction [43], which is higher than 7.2% with wooden rodding.

The research on Metallic fiber in PC is unexpectedly less than that of synthetic fibers even though it shows an excellent enhancement effect in conventional concrete. For Metallic fibers, the volume fraction is distributed between 0 and 2%. In cylinders, Lee [102] explored the impact of volume fraction on CS under different mix proportions. The results showed that 1% of steel fibers performed a negative enhancement for each paste strength, and 2% had an excellent effect, which is up to 50.44% improvement. In cubes, steel fibers delivered a minor enhancement effect.

The improvement index of inorganic fiber delivered a positive contribution, mainly glass and basalt fiber. In cubes specimens, the volume fraction of inorganic fiber has a limited distribution between 0~0.5%, and the highest amelioration can reach 102.41% with glass fiber [43]. It was reached due to generating a dense system by vibration compaction, while wooden rodding has only 40.5% enhancement. Singh [97] found the enhancement on compressive strength first increase and then decrease with the increases of volume fraction of glass fiber. Wang [92] explored basalt fiber in PC with different diameters, lengths and volume fractions. It was found out that the CS improvement would decrease with volume fraction and diameter increasing, and increase with increasing in length. Wu [103] delivered different results and found that the enhancement would first increase and then decrease with the increasing volume fraction. In the comparison of the data of Wu’s [103] and Wang’s [92], the longer basalt fiber would achieve better improvement than the shorter basalt fiber. In cylinders specimens, the highest enhancement was achieved by lower w/c [26]. Lee [102] found proportions of paste and aggregate size would affect the enhancement of glass fiber addition. It observed higher paste strength would contribute to the improvement but still delivered a decreasing trend with volume fraction increasing. On the contrary, the PC containing a large aggregate size would perform an increasing trend of CS enhancement index with the volume fraction of fiber increasing.

The studies on natural fiber showed that it is unsuitable for PC systems [20, 21, 43, 46]. There is no in-depth exploration of its fiber length, aspect ratio, or contents.

To summarize, most types of fibers in PC affect compressive strength insignificantly, with almost a range of enhancement at 0~40%. The inorganic fiber would be an optimized choice to improve CS because it can achieve better enhancement at a small volume fraction. The size and shape effect of FPC needs further exploration when comparing different specimens.

## Flexural Strength

According to ASTM C78 [57] and BS EN 12390-5 [54], 100x100 specimens with minimal 350 mm span were selected for investigation. The addition of fiber has almost positive effects on flexural strength (FS), except for some inorganic and synthetic fibers whose strength is weak. Figure 4 shows the effects of fiber volume fraction on flexural strength improvement for each type of fiber.

For Synthetic fiber, the volume fraction distribution is concentrated at 0-2% and achieved the highest enhancement up to 175.3% by inspecting the ultimate displacement of mid-span. The impact of Synthetic fiber on flexural strength is usually positive, except for WPF [14, 67, 69] and rubber fiber [32], whose tensile strength is low. For the same fiber type, different proportions of PC mixture will cause changes in the optimal volume fraction of fiber. With the increase of the volume fraction, the improvement index first increases and then decreases [41, 66, 68, 97]. In addition, Waste PET and PVA fiber also showed the same pattern [38, 72]. Hesami [26] discovered that w/c would affect the FS improvement and observed that the proper water-cement ratio could realize full potential of fibers. In addition, the highest improvement index was 69% at the optimal level of Rice Husk Ash (RHA). Fiber length is another important factor for the same type of fiber. Zhao [91] compared the different fiber lengths ranging from 6mm to 12mm and observed that 12mm fiber has slightly better enhancement than 6mm on flexural strength. For natural fiber, few studies have conducted in-depth research on its addition and few about its impact on PC's flexural and splitting tensile strength.

For carbon-based fiber, the volume fraction is distributed between 0~5%. Carbon fiber is a high-performance fiber and research length is only 12mm. Singh [100] explored an incremental increase volume fraction of carbon fiber, delivering a trend of first increase and then decrease. Nassiri [85, 98, 99] conducted a relatively comprehensive work on 0~5% volume fraction and 0~12mm length of CCFCM. It was observed that the smaller the fiber length, the higher the FS improvement. In addition, the volume fraction of CCFCM fiber has little effect on the improvement index.

For metallic fiber, a maximum improvement of 115.7% for FS was achieved [71]. The volume fraction is distributed between 0~2% with 0~70% improvement. Similarly, there are few studies on fiber length and aspect ratio on comparison transversely, most of which focus on the volume fraction of fiber. Zhu [41] investigated the CCSF and observed an increasing trend with increasing volume fraction, and the same pattern is found in Ozturk’s [68] research. Lee [102] explored SF with different paste strengths and particle sizes and found SF in normal-strength paste delivered higher improvement than SF in the high-strength paste. In addition, it is observed that the enhancement on FS for a mixture containing large aggregate size decreased with increasing volume fraction. Avishreshth [33] found that fiber shape is an essential factor for enhancing mechanism, and the hooked-end steel fiber improved more than crimped steel fiber. However, the improvement index decreased at a higher volume fraction of hooked-end fiber because its shape is easy to agglomerate.

Inorganic fiber's volume fraction is distributed between 0~0.5%, and the optimum improvement of 64% was achieved [26]. Lee [102] explored that GF in different proportions would present various effects. The GF showed various effects due to fiber addition with the same length and volume fraction in different proportions. The FS improvement would increase with increasing VF in high-strength paste, but it is the opposite in normal-strength paste. It confirms the statement mentioned before that different proportions would change the optimum for the fiber volume fraction.

To summarize, almost fiber in mixtures enhanced the flexural strength of PC, primarily distributed in the improvement index of 0~100%. Synthetic and metallic fiber contribute to the flexural strength of PC by using a small volume fraction. Therefore, they are the optimum choice for improving the flexural strength of PC.

## Splitting Tensile Strength

BS EN 12390-6 [53] and ASTM C496 [56] regulated that the standard sample size is CY D150H300. For cylinders, the results with the different sizes perform no difference. Therefore, the cylinder samples were selected for investigation and a few articles that used cube specimens was also explored. There is a comprehensive research on carbon-based and synthetic fiber about its volume fraction, while inorganic fiber focuses on a limited range. Figure 5 shows the effects of fiber volume fraction on splitting tensile strength (ST) improvement for each type of fiber.

For synthetic fiber, its improvement effects are between 0 and 50%, and most of the research is concentrated between 0 and 1%. Similar to the results obtained by FS, fibers’ optimal volume fraction is changed according to the proportions of the paste. Kevern [29] compared two different fiber lengths with three different contents, and found that improvement of the length with 56 mm PPF is more significant than that with 38mm, and obtained up to 47.06% improvement. Therefore, the results displayed a trend in which the longer length of the synthetic fiber showed better enhancement. Pils [66] discovered that adding PPF fiber will reduce the splitting tensile strength, which may be due to its high diameter and low aspect ratio.

For carbon-based fiber, the enhancement on ST is similar to that on FS. The optimum improvement of CF is up to 39.39% [43]. In addition, Singh [100] found a similar trend and enhanced extent on ST with FS due to carbon fiber addition. Nassiri's team [31, 85, 98, 99] also focused on splitting tensile strength and found that CCFCM enhanced ST based on different volume fractions, lengths, and aspect ratios. The impact of fiber length on ST differs from that on FS, and a longer length does not necessarily deteriorate the improvement of ST.

For metallic fiber, the volume fraction distribution is 0~2%, and the research is mainly for 30~60mm steel fiber. Hesami [26] found that a maximum increase of 41% was achieved with a w/c of 0.27 at RHA optimum levels. Fiber shape would also affect the enhancement of fiber. Avishreshth [33] compared hooked end and crimped steel fiber and found the hooked end performed better but easy to form fiber agglomeration due to higher volume fraction.

For inorganic fiber, the research scope is relatively limited, the volume fraction is distributed between 0 and 0.4%, and its length is distributed between 6 and 12mm. Juradin [43] explored the glass fiber with a smaller volume fraction of 0.18%  and the flexural strength was enhanced 62.121% by using the vibrating compacted method. In addition, Hesami [26] illustrated that glass fiber performed the best when w/c was 0.4, which is different from polypropylene and steel fibers. The fiber type will also affect the optimal volume fraction of fiber due to different tensile strength and elasticity of modulus.

In the cubes sample, inorganic fiber was intensively investigated, with varying volume fractions, lengths, and aspect ratios. Wang [92] analyzed the effects of different volume fractions, different fiber lengths, and different diameters of basalt fiber on ST and used the entropy method to predict the optimum percentage of basalt fiber. It found that the enhancement of ST increased with the increase of volume fraction and length of the fiber until reaches the optimal performance, then the ST enhancement index will decrease.

In conclusion, fiber usually can improve the splitting tensile strength of PC, except for some synthetic fiber. Inorganic, synthetic, and metallic fiber can effectively improve the splitting tensile strength at low dosages, but inorganic fiber provides a higher level of enhancement, for both cylinder and cube specimens, therefore, is an optimal solution.

## Pore characterization

The addition of fiber affects pore structure in PC (including shape, characteristic sizes, size distribution, porosity, connectivity, and tortuosity). Therefore, it would affect the properties of the PC. Such a mechanism is more complicated than conventional concrete due to macro pores.

When fibers are mixed into PC as additives, it enhances the strength of the paste, thereby strengthening the bond between the aggregate and the paste interface. However, fiber addition would interfere pore structures, thus affecting the properties of the PC. Rehder [96] proposed that improvement fibers would be better at higher porosity. Due to the increased number of pores, the spacing between pores is reduced and thus increasing the possibility of pores being bridged by fibers. Liu [70] examined fiber addition and observed that the average pore size of the sample was reduced by fiber. In addition, Tran [67] illustrated that pore volume and size decreased due to trapped fiber between coarse aggregates covered with paste. In addition, fiber shape would affect its pore structure. Kim [30] found that twisted fibers of PC had more pores than flat fibers. Moreover, the incorporation of fiber affects the distribution of pores. By adding basalt fibers, Liu [70] discovered that pore size distribution was more uniform than the control mix. The reason may be that adding fibers prevents the paste from segregation, thereby obtaining a uniform pore structure [90]. In addition, Wen [44] mentioned that the fiber dispersed in the paste could fill and reduce capillary pores to obtain a uniform PC distribution.

## Porosity

Most of the existing research adopted ASTM C1754 to measure the open porosity. The addition of fiber has two aspects of effect on porosity. One is that fiber would intrusion the distribution of aggregates, which contributes to the pore enlarging. The enlargement is usually related to the elasticity of the modulus of fiber. On the other hand, adding fiber may occupy the void space and reduce the porosity. The existence of these two possibilities causes the fluctuating impact of fiber addition on porosity, with both increases and decreases. Figure 6 summarizes the relationship between the volume fraction for each type of fiber and the enhancement of compressive strength.

Regarding synthetic fiber, the volume fraction is distributed between 0~2%, the fiber length is distributed between 0~60mm, and the aspect ratio is mainly distributed between 0~600. Schaefer [20, 21] used fiber with a volume fraction of 0.099% to the detriment of about 35.889% of PC’s porosity, but porosity increases with VF increasing. Nassiri [85] explored the PPF with Schaefer's similar length and compared the effect of CCFCM. It found that 0.5% PPF would lead to a 64% enhancement in porosity, the highest enhancement. Therefore, the porosity would increase with the increasing volume fraction of PC with the same fiber length. Dean [16] incorporated PPF with 19.1mm and 50mm, including that the porosity increased first and then decreased as the fiber volume fraction with the same length increased. In addition, it was observed that the porosity increased with fiber length increasing when the volume fraction was at a lower level about 0.033% volume fraction. On the contrary, the porosity decreased with fiber length increasing when the volume fraction was at a higher level about 0.099% volume fraction. Similarly, PPF with 38mm and 56mm lengths also performed similarly [29]. There was a significant positive correlation between the volume fraction of waste PET fiber with 40mm and porosity [38].

There are a few related literature for carbon-based fiber, and the main types are pure carbon fiber and CCFCM.  Singh [100, 101] used carbon fibers in PC and observed reduced porosity, and it decreased with increasing volume fraction of fibers. Nassari team [31, 98] tested  CCFCM reinforced PC with various volume fractions, lengths, and aspect ratio ranges. It was concluded that CCFCM with short length would first detriment to and then contribute to porosity with volume fraction increasing, which is different from synthetic fiber.

For metallic fiber, Mehrabi and Toghroli [14, 69] evaluated the porosity of PC with 35mm SF at 1% and 2% addition and observed that the porosity increased with the volume fraction increases. Three different PC proportions mixed with 1% and 2% SF with 30mm also showed similar conclusions [102]. However, SF with 50mm and 60mm end up with opposite conclusions [33]. Therefore, it could be observed that the porosity increases with VF increasing when the fiber length is relatively small and decreases with VF increasing when the fiber length is relatively large.

For inorganic fiber, the effect on the porosity is usually unfavorable. The studies on basalt fiber concluded that the porosity would decrease with increasing VF [92, 100, 103]. In addition, Wang [92] investigated various lengths and diameters and concluded that the porosity would increase with fiber diameter and length. Similarly, glass fiber addition was concluded with a similar regular conclusion [97]. However, Lee [102] investigated glass fiber with three different proportions, and the results showed that the porosity increased with VF increasing for the proportions with a maximum particle size of 3.03mm, which differed from PC with 3 mm aggregates. Therefore, it shows that the influence of fiber addition on porosity would be the combined action of fiber properties and external media.

## Permeability

Permeability is a unique characteristic of permeable concrete that is different from conventional concrete, allowing water to flow through permeable concrete to reach the bottom layer in a unit of time. Various testing methods rely on specimens with different shapes and sizes. The permeability testing method is divided into three methods: the constant head method (CHM), the falling head method (FHM) in the laboratory, and the infiltration method in the field. The falling head test is a type of convenient method for engineering. Zhang [104] pointed out that the results from the falling head would be more excellent than the constant head method’s, about 100%~300%. It has better fitting with porosity but has less accuracy due to the rapid drop in water level, which is manually recorded. However, it would cost less time than CHM. On the contrary, Sandoval [105] compared the advantages and disadvantages of the two methods and found that the falling head permeability test could not detect significant differences between the studied materials and would cost much more time. In addition, it cannot assess the actual hydraulic potential of the material, but the constant head permeability test can estimate these parameters. The CHM was used in the laboratory with superior accuracy, while actual engineering would tend to use the FHM. Abdelhady [106] summarized the permeability of 549 samples, which used the constant head method, but the difference in specimens’ size was not considered. Table A.1 in Appendix summarizes the permeability test method and sample size.

Fiber has different effects on the permeability results obtained by different methods. Juradin [43] studied four types of fiber addition effects on permeability with CH and FH test methods and observed that the permeability coefficient obtained by CH would be 16% lower than that from the FH test method. In addition, the enhancement due to fiber addition detected by FH is more significant than CH. Therefore, different results are obtained due to the use of different methods, as shown in Figure 7.

In the constant head test method, the impact of fiber on the permeability is primarily minor or unfavorable. Synthetic fiber's volume fraction is distributed between 0 and 0.4%. Xiao [72] examined the permeability of PC with PVA fiber and found the effects due to adding fiber is minor. It also observed that the permeability would decrease first and then increase with the volume fraction increasing. Tran [67] revealed that WPT fiber addition would harm the permeability and decrease with the volume fraction increasing. Zhu [41] explored thick and thin PPF with different lengths and concluded that the permeability of thick PPF increased and thin PPF decreased with increasing volume fraction. Besides, Juradin [43] identified that the compacting method matters. PC specimens including PPF, HF, CF, and GF were tested, and it was observed that the fiber in PC with a denser system presented more deterioration to the permeability. However, adding fibers produces a significant enhancement in the permeable brick. Oni [40] investigated KF with 6mm, PVA with 18mm, and UHMWPE fiber with 12mm and observed a significant enhancement in permeability, which is up to 211.29%, 17.742%, and 94.355%, respectively. For inorganic fiber, the impact on permeability is primarily unfavorable. Basalt fiber was studied by Wu [103], and observed a reduction of permeability as the volume fraction increased from 0.075% to 0.302%. Similar findings were examined in Wang's research [92]. The permeability of PC with basalt fiber would decrease as the fiber volume fraction increases and increases with the fiber's length and diameter increase. In addition, Liu [70] conducted 0.2% BF with 20mm would slightly contribute to permeability.

In the falling head test method, the influence of fiber addition is also minor or insignificant. For synthetic fiber, Kevern [16] identified PPF with 19.1mm and 50 mm effects on the permeability of PC and detected minor volume fraction change caused significant deviation, which is first increasing and then decreasing. In addition, the PPF with 50mm caused lower permeability than 19.1mm at the same volume fraction level. Similarly, Zhao [91] explored  PPF with 3,6,12 mm and observed that the length increase was detrimental to the permeability increase of PC. Ali [38] investigated waste PET fibers with eight levels of volume fraction and observed permeability raised with the volume fraction increasing up to 70.02 % at the 2% volume fraction. On the contrary, Pils [66] concluded that permeability increased with the volume fraction increasing. For metallic fiber, the volume fraction is distributed between 0.5% and 2.0%, the length is distributed between 0-60mm, and the aspect ratio is distributed between 40-70, which lacks research on high aspect ratio. The effects of steel fiber addition are generally minor for the permeability of PC [14, 33, 69]. Besides, Lee [102] inspected PC with different strengths of paste and particle size and observed that the contribution for high-strength paste was higher than normal-strength paste and would be higher in PC containing a large aggregate size. The shape of steel fiber does not affect the permeability when the volume fraction keeps the same, and its’ permeability decreases with the volume fraction increasing [33]. For inorganic fiber, the result is different from steel fibers, and the permeability increases with the increase of fiber volume fraction. The conclusion changes when high-strength paste is used instead of low-strength paste [102].

# Correlation between physical and mechanical properties

Prior investigations showed that porosity is the essential factor affecting strength, and the two are inversely related [107]. Based on such a relationship, predictive models have been proposed. The mathematic laws used in these Empirical models are either linear, power, exponential or logarithmic. Roy [108] proposed that the strength of porous materials limitations could be described by the following equations:

|  | σ=σ0exp-bp | Eq. 1 |
| --- | --- | --- |
|  | σ=2EγπA | Eq. 2 |

in which, σ is the compressive strength (MPa); σ0 is the compressive strength at zero void (MPa); p is the void ratio or porosity (%); E is the the elasticity modulus (Pa);  γ is the fracture surface energy (J/m2); and A is the half length of an internal crack (m).

Some empirical models have been proposed, and a viable fitness has been obtained based on Eq.1 [109, 110]. In addition, the theoretical models were extended by considering the critical stress of brittle material that incurred crack propagation, as shown in Eq.2. The accurate theoretical model is obtained by exploring the relationship between elasticity modulus and fracture surface energy and porosity [111-113]. These proposed models are further improved to summarize empirical prediction equations under specific conditions, which are considered different factors and theories shown in Table 7, such as w/c ratio, aggregate size, aggregates/binders ratio, the internal pore structure, and binder strength [107, 114, 115].

In addition, pervious concrete's permeability is also affected by porosity [116], but mostly are empirical models, as shown in Table 8 [117-124]. It has been proved that paste film thickness (slurry layer thickness) is also a determinate factor [124]. The correlation between them may change due to fiber addition, and thus worth further exploration.

## Porosity & Strength

Fiber addition for FPC would affect the relationship between porosity and compressive strength. Dai [39] found that the correlation becomes higher due to the incorporation of single or multiple admixtures, including the addition of fiber, probably because the adhesion admixture creates the fresh cement paste more homogeneous and dense. Mehrabi [14] explored the mixtures with recycled aggregates and additional additives such as nano-clay and pumice powder. Two different volume fractions and three types of fibers were tested. The enhancement of STF was observed to be higher than WPF, and MF deteriorated the compressive strength at the porosity ranging between 20% and 25%. Five basic mathematic laws that govern the relationship between porosity and compressive are plotted, as shown in Fig 8. The addition of fiber changes the upper and lower limits of the model. As shown in Figure 8 a), incorporating WPF increased the correlation, and incorporating MF decreased the correlation. For the same kind of fiber, mixtures with different fiber content delivered significant differences. Figure 8 b) showed that adding 1% volume fraction of STF would contribute to the correlation, but a 2% volume fraction would decrease the correlation. In addition, the MF showed significant correlation deterioration when fiber was added 2%, as shown in Figure 8c). The high dosage of fibers leads to fiber agglomeration, which leads to uneven distribution and reduces the goodness of the fitting. However, WPF showed higher consistency with mixtures and contributed to correlation, as shown in Figure 8 d). It may be due to the WPF being less intrusive to mixtures.

Singh [97, 100, 101] explored the four types of fibers and observed that porosity increases if VF increases. Meanwhile the compressive strength of PC decreases. Therefore, CS may be shown a decreasing trend even though fiber would enhance compressive strength. Although compressive strength decreases with the fiber contents increasing, all four fibers enhanced compressive strength overall, and carbon fiber shows an excellent reinforcing effect. In addition, the correlation between porosity & CS is more significant in basalt fiber and glass fiber addition mixtures, which indicates that the paste distribution is relatively stable for these two mixtures with inorganic fibers, as shown in Figure 9. Moreover, fiber collaboration with different aggregates led to different correlations, indicating that the pores formed by different aggregates would affect fiber distribution, thus causing different trends, as shown in Figure 9 a) and b).

Different types of fibers affect the correlation differently between porosity and compressive strength, as shown in Figure 10. With the increase of VF of PET fiber [38], its fitting curve showed excellent fitting. The increase in fiber volume fraction did not significantly impact the uniformity of its paste. On the contrary, adding PVA fibers resulted in a poor correlation [72]. The results obtained by adding two types of fiber showed that fiber length is essential. The effect on compressive strength is due to the combined action of porosity and fiber enhancement. Adding 12 mm PVA would reduce the porosity of PC, and porosity increases with the increased fiber contents. However, the 40mm long PET fiber continuously increased porosity with increased fiber contents. Therefore, the relationship between porosity and compressive strength for those two fibers with different lengths show opposite trends

## Porosity & Permeability

The incorporation of fibers would affect the permeability of PC [30], and there are two primary explanations. Some researchers claimed that fiber addition filled a portion of macro pores, thus decreasing the permeability [73, 103]. Liu [70] found that the incorporation of fibers filled some tiny pores and occupied part of the large pores between the coarse aggregates, thereby reducing the average pore size and interconnected porosity and reducing permeability. Similarly, Tang [125] proposed that PVA fiber extended to pores, occupying part of the pore space and decreasing permeability. On the other hand, the interface between fiber and paste would be a flow path when the volume fraction of fiber is relatively high. Zhu [41] proposed that the adhesion between the fiber and the cement substrate is relatively poor; water can easily enter the interface between the fiber and the paste under pressure, increasing the connected porosity. Tang [125] investigated that the PVA fiber cannot be wrapped entirely at a high volume fraction, which leads to the decrease of the bond between the aggregates, forming a permeable pathway in the PVA-Aggregates and PVA-Cement bond.

Since the fiber addition affects the porosity and the microstructure of the pore, the relationship between porosity & permeability may also be different from PC without fiber. Mehrabi [14] compared mixtures with two different volume fractions of the three types of fibers and observed that Equations (2) and (5) provided appropriate empirical relations. It is found that fiber addition has less influence on the relationship between porosity and permeability. However, some experimental results exceed the limit of these two proposed models, as shown in Figure 11. Therefore, a new prediction model is necessary.

Wu [23] investigated latex and PPF fiber addition effect on PC properties with two aggregate groups with different gradations, as shown in Figure 12 a). It was found that a mixture with fiber displayed a higher correlation between permeability and porosity than without fiber, indicating a more homogeneous and dense paste. However, Harry Rodin [98] explored different fiber volume fractions and found that the mixture with low VF presented a higher correlation between permeability and porosity than the control mix. The correlation decreased with increasing VF, even lower than the control mix at the highest dosage. The reason may be that the increase in fiber content leads to an increase in the possibility of fiber agglomeration, which causes uneven distribution of paste. In addition, the correlation between permeability and porosity is related to water-cement ratio. Hesami [26] pointed out that the correlation between porosity and permeability would be affected by w/c of mixtures, as Figure 12 b) shows. In addition, PC with different fiber types performed distinguishing results due to various w/c. The correlation decreased with w/c increasing for PPS and Glass fiber but showed an opposite trend for steel fiber. The explanation would be that mixtures with PPS and Glass fiber reached an optimum state for fiber distribution, and there would be confusion due to water addition. On the contrary, the mixtures with steel fiber need more water to distribute fiber, thus contributing to raised correlation.

## Permeability & Strength

Some articles have studied the relationship between compressive strength and permeability for the addition of fiber and found that the change of compressive strength and permeability presented a linear relationship with the increase of fiber volume fraction as shown in Figure 13. Ali [38] explored the effects of various volume fractions of waste PET and found the correlation between permeability and compressive strength is high and perfectly fitting. However, the permeability and flexural strength correlation are rather scattered. Xiao [72] examined mixtures with different volume fractions of PVA fiber, and observed a similar trend with Ali but has a large slope. The flexural strength was also highly related to permeability. In addition, the fiber shape would also affect the correlation between properties. Avishreshth [33] discovered that mixtures with crimped steel have a higher correlation than hooked-end steel fiber due to difficulties of distribution for hooked-end fiber.

Fiber type is an essential factor in the correlation between permeability and strength. Different fiber types due to their various elasticity of modulus thus affect the distribution of fiber, and would show different correlations. Singh [97, 100, 101] investigated the BF, CF, PPF, and GF in PC, and observed the significant enhancement by adding carbon fiber, but the higher variability appeared due to fiber content increasing. As shown in Figure 14, the basalt fiber and glass fiber had a relatively high correlation between permeability and compressive strength, implying relatively stable for paste distribution. However, the carbon fiber and PPF caused large fluctuations, which made the correlation low.

In summary, the correlation between properties of PC would be affected by fiber addition, which includes fiber confusion in mixtures decreased correlation, or increased correlation due to the homogeneous and dense paste. This effect is generally due to the difference caused by different fiber properties. Further research on the influence of fiber properties on it is needed.

# Enhancement mechanism of fibers in pervious concrete

Depending on whether the modulus of elasticity of fiber is higher or lower than that of the matrix, Wen [126] classified the FPC into two categories. In conventional concrete, the former would contribute to the initial hardening stage and the latter to the crack situation [126]. However, the enhancement for PC would be different due to the existence of pores. Besides the distribution of fiber and interlocking force between fiber and matrix, the interference to pores would be considered, which is a crucial factor affecting the PC's mechanical and physical properties.

According to various references, the research range for each fiber parameter is identified for each type of fiber, as shown in Figure 15. The overall distribution of fiber properties could be referred to investigate the research gap. The best scenario for fiber enhancement and the limit for this scenario would be summarized for five main fiber types: Synthetic, Carbon-based, Metallic, Inorganic, and Natural fibers. For Natural fiber, fewer articles are referred to indicating that Natural fiber is unsuitable for PC systems but also needs to be more noticed. Figure 15 shows the parameter range for each type of fiber, including fiber length and aspect ratio. Table 9 summarizes the optimum range of fiber on different properties for all four types of fibers based on published papers. In addition, the best scenario for each type of fiber is identified based on Table 10; as shown in the Table, the limit for each best scenario is listed, and the research gap is identified.

# 6. Conclusion

Pervious concrete is a viable measure for water resource management as a new type of material. However, due to the existence of pores, its application range is limited. Therefore, fiber-reinforced pervious concrete has been developed to enhance the performance. There has yet to be a specific standard or comprehensive theory framework to explain the enhancement mechanism. Through the literature review and analyses, the following conclusions can be reached.

- The appropriate mix design scheme should be identified for specific application to determine whether the fiber is considered as pastes, aggregates or additives in the system, ensuring that the fibers can be evenly distributed in the paste and attached to the aggregates' surface.

- It is recommended to use a standard hammer compacting specified by ASTM C09.49, in order to control the compacted energy each time and avoid paste segregation.

- Compared with conventional concrete, synthetic fiber is more widely used in FPC than metallic fiber, even though metallic fiber has a higher performance contribution. It may be because of its corrosiveness and tendency of causing water pollution. The volume fraction of Inorganic fiber in FPC is concentrated at 0~0.5%, a small adding level. The distribution of its fiber length range is relatively wide. The research scope of carbon-based fiber is relatively limited. The research on CCFCM is relatively comprehensive, but few studies on CF and focus only on shorter fibers and lower volume fractions. In addition, there needs to be more research on natural fiber.

- Fiber addition would interfere pore structures of PC and affect the properties of PC.

- Adding fiber affects the average pore size and pore distribution, thus affecting the properties of the PC. The impact on the porosity due to fiber addition is divided into two aspects, which include intrusion of the distribution of aggregates and occupying the void space, resulting in fluctuations in results.

- The effect on properties of PC due to fiber addition varies, it is affected by factors such as water cement ratio, proportions, compacted method, fiber shape, fiber volume fraction, and fiber length.

- Inorganic fiber focus on enhancing compressive strength and splitting tensile strength of PC, and it can achieve remarkable results with a smaller volume fraction. In addition, metallic and synthetic fiber would be an optimal choice for improving the PC's flexural and splitting tensile strength. The difference from conventional concrete is that the distribution of fibers in concrete cannot be fully utilized, and some fibers may be exposed to the pore and the external environment. Therefore, distinguishing different fiber types shall consider different elasticity modulus of fiber and the matrix, as well as chemical stability of fibers in the aqueous environment. The optimal addition scheme of fiber for each type of fiber has obtained based on existing literature.

- Fiber enhances the strength of the paste as an additive. However, the strength of the PC would be decreased or increased. The strength would be increased because the possibility of pores being bridged by fibers. On the other hand, the strength would decrease due to the addition of fiber leading to increased pores and the number of defects.

- Fiber would fill a portion of macro pores to decrease average pore size and interconnected pores, thus reducing permeability. However, a flow path would be formed to increase the permeability due to weak bonds between fiber and paste.

- The correlation between porosity & permeability and porosity & strength would be affected by the fiber type, water cement ratio, and fiber volume fraction. It depends on the homogeneity of the mixtures due to fiber addition. Adding too much fiber will lead to uneven distribution of paste, and adding a small amount is beneficial to increase viscosity and avoid segregation.

Future research should focus on the mechanism of fiber in PC. In addition, a full-scale experiment that comprises fiber volume fraction and the number of fibers calibrated by fiber length and diameter would be of great relevance to prove, through scaling-up, the augment performance of PC. The predicted model could be identified due to fiber addition and, further, consider the hybrid fiber system. In addition, after identifying the fiber system, the aggregate grading can be optimized considering sustainability.

# List of References

1.	Tang, Y.T., et al., Aligning ancient and modern approaches to sustainable urban water management in China: Ningbo as a “Blue-Green City” in the “Sponge City” campaign. Journal of Flood Risk Management, 2018. 11(4).

2.	Li, Q., et al., Comprehensive performance evaluation of LID practices for the sponge city construction: A case study in Guangxi, China. J Environ Manage, 2019. 231: p. 10-20.

3.	Chen, J., et al., Alleviating urban heat island effect using high-conductivity permeable concrete pavement. Journal of Cleaner Production, 2019. 237: p. 117722.

4.	Guan, X., J. Wang, and F. Xiao, Sponge city strategy and application of pavement materials in sponge city. Journal of Cleaner Production, 2021. 303: p. 127022.

5.	AlShareedah, O. and S. Nassiri, Pervious concrete mixture optimization, physical, and mechanical properties and pavement design: A review. Journal of Cleaner Production, 2021. 288.

6.	Chandrappa, A.K. and K.P. Biligiri, Pervious concrete as a sustainable pavement material – Research findings and future prospects: A state-of-the-art review. Construction and Building Materials, 2016. 111: p. 262-274.

7.	Zhong, R., Z. Leng, and C.-s. Poon, Research and application of pervious concrete as a sustainable pavement material: A state-of-the-art and state-of-the-practice review. Construction and Building Materials, 2018. 183: p. 544-553.

8.	Debnath, B. and P.P. Sarkar, Characterization of pervious concrete using over burnt brick as coarse aggregate. Construction and Building Materials, 2020. 242: p. 118154.

9.	Kuo, W.-T., C.-C. Liu, and D.-S. Su, Use of washed municipal solid waste incinerator bottom ash in pervious concrete. Cement and Concrete Composites, 2013. 37: p. 328-335.

10.	Tan, Y., Y. Zhu, and H. Xiao, Evaluation of the Hydraulic, Physical, and Mechanical Properties of Pervious Concrete Using Iron Tailings as Coarse Aggregates. Applied Sciences, 2020. 10(8): p. 2691.

11.	China, M.o.H.a.U.-R.D.o.t.P.s.R.o., Permeable paving bricks&permeable paving flags. 2011.

12.	El-Hassan, H. and P. Kianmehr, Pervious concrete pavement incorporating GGBS to alleviate pavement runoff and improve urban sustainability. Road Materials and Pavement Design, 2016. 19(1): p. 167-181.

13.	Shanableh, A., et al., Sustainability assessment and physical characterization of pervious concrete pavement made with GGBS. MATEC Web of Conferences, 2017. 120.

14.	Mehrabi, P., et al., Effect of pumice powder and nano-clay on the strength and permeability of fiber-reinforced pervious concrete incorporating recycled concrete aggregate. Construction and Building Materials, 2021. 287: p. 122652.

15.	Ravichandran, D., et al., Influence of fibers on fresh and hardened properties of Ultra High Performance Concrete (UHPC)—A review. Journal of Building Engineering, 2022. 57: p. 104922.

16.	Dean, S.W., et al., Pervious Concrete Mixture Proportions for Improved Freeze-Thaw Durability. Journal of ASTM International, 2008. 5(2).

17.	Kevern, J., Mix design development for Portland cement pervious concrete in cold weather climates. 2006.

18.	Kevern, J., et al., Mix Design Development for Pervious Concrete in Cold Weather Climates. 2006.

19.	Kevern, J.T. Advancements in pervious concrete technology. 2008.

20.	Schaefer, V.R. and J.T. Kevern. An Integrated Study of Pervious Concrete Mixture Design for Wearing Course Applications. 2011.

21.	Schaefer, V.R., et al. Pervious Concrete Overlay Design, Construction and Performance. 2010.

22.	Shu, X., et al., Performance comparison of laboratory and field produced pervious concrete mixtures. Construction and Building Materials, 2011. 25(8): p. 3187-3192.

23.	Wu, H., et al., Laboratory Evaluation of Abrasion Resistance of Portland Cement Pervious Concrete. Journal of Materials in Civil Engineering, 2011. 23(5): p. 697-702.

24.	Rehman, H.A.A. SOME PROPERTIES OF FIBER REINFORCED NO FINE CONCRETE. 2012.

25.	Bonicelli, A., et al., Evaluating the effect of reinforcing fibres on pervious concrete volumetric and mechanical properties according to different compaction energies. European Journal of Environmental and Civil Engineering, 2014. 19(2): p. 184-198.

26.	Hesami, S., S. Ahmadi, and M. Nematzadeh, Effects of rice husk ash and fiber on mechanical properties of pervious concrete pavement. Construction and Building Materials, 2014. 53: p. 680-691.

27.	Hesami, S., et al., Evaluation of Polyphenylene Sulfide and Steel Fibers on Mechanical Properties of Pervious Concrete Pavement. International journal of pavement research and technology, 2014. 7: p. 218-222.

28.	Nayak, B.H., K.S.B. Prasad, and M.P. Kumar, An Experimental Study on Strength Characteristics of Pervious Concrete by Partial Addition of Glass Fiber and Polyester Fiber. International Journal of Engineering Research, 2015. 4(10): p. 545-549.

29.	Kevern, J.T., D. Biddle, and Q. Cao, Effects of Macrosynthetic Fibers on Pervious Concrete Properties. Journal of Materials in Civil Engineering, 2015. 27(9).

30.	Kim, Y.J., A. Gaddafi, and I. Yoshitake, Permeable concrete mixed with various admixtures. Materials & Design, 2016. 100: p. 110-119.

31.	Rangelov, M., et al., Using carbon fiber composites for reinforcing pervious concrete. Construction and Building Materials, 2016. 126: p. 875-885.

32.	Aliabdo, A.A., A.E.M. Abd Elmoaty, and A.M. Fawzy, Experimental investigation on permeability indices and strength of modified pervious concrete with recycled concrete aggregate. Construction and Building Materials, 2018. 193: p. 105-127.

33.	Avishreshth, P.P. Bansal, and T. Chopra, Characterization of Steel Fiber Reinforced Pervious Concrete for Applications in Low Volume Traffic Roads, in Urbanization Challenges in Emerging Economies. 2018. p. 93-102.

34.	Zhong, R. and K. Wille, Influence of matrix and pore system characteristics on the durability of pervious concrete. Construction and Building Materials, 2018. 162: p. 132-141.

35.	Akand, L., M. Yang, and X. Wang, Effectiveness of chemical treatment on polypropylene fibers as reinforcement in pervious concrete. Construction and Building Materials, 2018. 163: p. 32-39.

36.	Akand, L. and M. Yang, Micromechanical modelling of pervious concrete reinforced with treated fibres. Proceedings of the Institution of Civil Engineers - Construction Materials, 2023. 176(1): p. 2-12.

37.	Huang, J., Wang, F., Cui, H., Zhou, J., Xia, X. , Influence of Different Preparation Technology on the Dispersion of PVA Fiber in Recycled Aggregate Pervious Concrete. BULLETIN OF THE CHINESE CERAMIC SOCIETY, 2019. 0(3).

38.	Ali, T.K.M., et al., Properties of eco-friendly pervious concrete containing polystyrene aggregates reinforced with waste PET fibers. Innovative Infrastructure Solutions, 2020. 5(3).

39.	Dai, Z., et al., Multi-modified effects of varying admixtures on the mechanical properties of pervious concrete based on optimum design of gradation and cement-aggregate ratio. Construction and Building Materials, 2020. 233.

40.	Oni, B., J. Xia, and M. Liu, Mechanical properties of pressure moulded fibre reinforced pervious concrete pavement brick. Case Studies in Construction Materials, 2020. 13: p. e00431.

41.	Zhu, H., et al., Study on the Permeability of Recycled Aggregate Pervious Concrete with Fibers. Materials (Basel), 2020. 13(2).

42.	Park, J.H., et al., Effect of eco-friendly pervious concrete with amorphous metallic fiber on evaporative cooling performance. J Environ Manage, 2021. 297: p. 113269.

43.	Juradin, S., et al., Impact of fibre incorporation and compaction method on properties of pervious concrete. Materiales de Construcción, 2021. 71(342).

44.	Wen, F., et al., Physical Properties and Seepage Characteristics of Optimized Fiber-Reinforced Permeable Concrete. Journal of Materials in Civil Engineering, 2021. 33(5).

45.	Juradin, S., et al., Pervious Concrete Reinforced with Waste Cloth Strips. Sustainability, 2022. 14(5).

46.	Park, S., et al., Effect of the rheological properties of fresh binder on the compressive strength of pervious concrete. Journal of Materials Research and Technology, 2022. 17: p. 636-648.

47.	Meininger, R.C., No-Fines Pervious Concrete for Paving. Concrete international, 1988. 10: p. 20-27.

48.	Crouch, L., et al., Estimating Pervious PCC Pavement Design Inputs with Compressive Strength and Effective Void Content. 2006.

49.	Mulligan, A.M., Attainable compressive strength of pervious concrete paving systems. 2005.

50.	Materials, A.S.f.T., Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens. 2021.

51.	Publication, B.S., Testing methods for pervious concrete, in Part 2: Density and void content. 2018.

52.	Publication, B.S., Testing hardened concrete, in Part 3: Compressive strength of test specimens. 2019.

53.	Standards, B., Testing hardened concrete, in Part 6: Tensile splitting strength of test specimens. 2009.

54.	Pubilication, B.S., Testing hardened concrete, in Part 5: Flexural strength of test specimens. 2019.

55.	Materials, A.S.f.T., Standard Test Method for Density and Void Content of Hardened Pervious Concrete (Withdrawn 2021). 2021.

56.	Materials, A.S.f.T., Standard Test Method for Splitting Tensile Strength of Cylindrical Concrete Specimens. 2017.

57.	Materials, A.S.f.T., Standard Test Method for Flexural Strength of Concrete (Using Simple Beam with Third-Point Loading). 2022.

58.	Institute, A.C., ACI 522R-10: Report on Pervious Concrete. 2011, American Concrete Institute.

59.	Materials, A.S.f.T., Standard Test Method for Permeability of Granular Soils (Constant Head). 2022.

60.	Materials, A.S.f.T., Standard Test Method for Infiltration Rate of In Place Pervious Concrete. 2020.

61.	Materials, A.S.f.T., Standard Test Methods for Measurement of Hydraulic Conductivity of Saturated Porous Materials Using a Flexible Wall Permeameter. 2016.

62.	Standards, B.L., Technical specification for porous concrete pavement. 2021.

63.	China, M.o.H.a.U.-R.D.o.t.P.s.R.o., Technical specification for application of pervious recycled aggregate concrete. 2016.

64.	China, M.o.H.a.U.-R.D.o.t.P.s.R.o., Standard for test methods of concrete physical and mechanical properties. 2019.

65.	China, M.o.H.a.U.-R.D.o.t.P.s.R.o., Technical specification for pervious cement concrete pavement. 2009.

66.	Pils, S.E., et al., Pervious concrete: study of dosage and polypropylene fibers addiction. Revista IBRACON de Estruturas e Materiais, 2019. 12(1): p. 101-121.

67.	Nhat Ho Tran, T., et al., Microparticle filtration ability of pervious concrete mixed with recycled synthetic fibers. Construction and Building Materials, 2021. 270.

68.	Ozturk, O. and N. Ozyurt, Sustainability and cost-effectiveness of steel and polypropylene fiber reinforced concrete pavement mixtures. Journal of Cleaner Production, 2022. 363.

69.	Toghroli, A., et al., Evaluating the use of recycled concrete aggregate and pozzolanic additives in fiber-reinforced pervious concrete with industrial and recycled fibers. Construction and Building Materials, 2020. 252.

70.	Liu, R., et al., Influence of Pore Structure Characteristics on the Mechanical and Durability Behavior of Pervious Concrete Material Based on Image Analysis. International Journal of Concrete Structures and Materials, 2020. 14(1).

71.	Furkan Ozel, B., Ş. Sakallı, and Y. Şahin, The effects of aggregate and fiber characteristics on the properties of pervious concrete. Construction and Building Materials, 2022. 356.

72.	Xiao, Q., et al., Characterization of PVA Fiber-Reinforced Pervious Concrete with Blended Recycled Ceramic Aggregates and Natural Aggregate. Advances in Materials Science and Engineering, 2022. 2022: p. 1-10.

73.	Liu, R., et al., Physical and mechanical properties of pervious concrete with multi-admixtures. Magazine of Concrete Research, 2021. 73(9): p. 448-463.

74.	Tang, C.W., C.K. Cheng, and C.Y. Tsai, Mix Design and Mechanical Properties of High-Performance Pervious Concrete. Materials (Basel), 2019. 12(16).

75.	Han, H., et al., Performance improvement of non-sintering permeable brick with the addition of fibers at a low content. Journal of Building Engineering, 2021. 43.

76.	Song, H., J. Yao, and J. Xiang, The role of aggregate and cement paste in the deterioration of the transitional interface zone of pervious concrete during freeze-thaw cycles. Case Studies in Construction Materials, 2022. 16.

77.	Taheri, B.M., et al., Experimental evaluation of freeze-thaw durability of pervious concrete. Journal of Building Engineering, 2021. 33.

78.	Bilal, H., et al., Influence of silica fume, metakaolin & SBR latex on strength and durability performance of pervious concrete. Construction and Building Materials, 2021. 275.

79.	Wu, H., et al., Experimental investigation on freeze–thaw durability of Portland cement pervious concrete (PCPC). Construction and Building Materials, 2016. 117: p. 63-71.

80.	Wang, K., V. Schaefer, and J. Kevern, Development of Mix Proportion for Functional and Durable Pervious Concrete. 2023.

81.	Nazeer, M., K. Kapoor, and S.P. Singh, Strength, durability and microstructural investigations on pervious concrete made with fly ash and silica fume as supplementary cementitious materials. Journal of Building Engineering, 2023. 69.

82.	Institute, A.C., Guide to Durable Concrete. 2008, American Concrete Institute.

83.	Brown, A.G.A., D.B. Mobley, and M.B. Peters. DEVELOPMENT OF HIGH QUALITY PERVIOUS CONCRETE SPECIFICATIONS FOR MARYLAND CONDITIONS. 2013.

84.	Wu, Y., et al., The Strength and Elastic Modulus of Pervious Concrete Considering Pore and Fiber during Freeze–Thaw Cycles. Sustainability, 2022. 14(23).

85.	Nassiri, S., et al., Mechanical and durability characteristics of pervious concrete reinforced with mechanically recycled carbon fiber composite materials. Materials and Structures, 2021. 54(3).

86.	Zeng, W., et al., Effect of steel fiber on the crack permeability evolution and crack surface topography of concrete subjected to freeze-thaw damage. Cement and Concrete Research, 2020. 138.

87.	Yang, Z., Freezing-and-Thawing Durability of Pervious Concrete under Simulated Field Conditions. Aci Materials Journal, 2011. 108: p. 187-195.

88.	Zhai, H.-X., et al., Study on the Preparation and Performance of a Prefabricated Pervious-Cement-Based Concrete Pavement Slab. Symmetry, 2022. 14(7).

89.	Singh, A., et al., Glass and carbon fiber reinforced polymer composite wastes in pervious concrete: Material characterization and lifecycle assessment. Resources, Conservation and Recycling, 2022. 182.

90.	Alemu, A.S., et al., Practical considerations of porosity, strength, and acoustic absorption of structural pervious concrete. Case Studies in Construction Materials, 2021. 15.

91.	Zhao, J., Yang, X., Li, H., Ma, Y., Effect of Chopped Fibers on the Performance of Pervious Concrete. Journal of Building Materials, 2019. 22(2).

92.	Wang, W., et al., Experimental Study on the Performance of Basalt Fiber Modified Pervious Concrete Based on Entropy Method. Advances in Materials Science and Engineering, 2022. 2022: p. 1-18.

93.	Wang, W., et al., Numerical simulation of strength of basalt fiber permeable concrete based on CT technology. Case Studies in Construction Materials, 2022. 17.

94.	Aggregates, C.C.o.C.a.C., ASTM C09.49 for Pervious Concrete. 2008.

95.	Unificazione, E.N.I.d., Bituminous mixtures - Test methods - Part 30: Specimen preparation by impact compactor. 2019.

96.	Rehder, B., K. Banh, and N. Neithalath, Fracture behavior of pervious concretes: The effects of pore structure and fibers. Engineering Fracture Mechanics, 2014. 118: p. 1-16.

97.	Bright Singh, S. and M. Murugan, Effect of aggregate size on properties of polypropylene and glass fibre-reinforced pervious concrete. International Journal of Pavement Engineering, 2020. 23(6): p. 2034-2048.

98.	Rodin, H., et al., Enhancing Mechanical Properties of Pervious Concrete Using Carbon Fiber Composite Reinforcement. Journal of Materials in Civil Engineering, 2018. 30(3).

99.	AlShareedah, O., et al., Field performance evaluation of pervious concrete pavement reinforced with novel discrete reinforcement. Case Studies in Construction Materials, 2019. 10.

100.	Bright Singh, S. and M. Madasamy, Investigation of aggregate size effects on properties of basalt and carbon fibre-reinforced pervious concrete. Road Materials and Pavement Design, 2021. 23(6): p. 1305-1328.

101.	Bright Singh, S. and M. Murugan, Performance of carbon fibre-reinforced pervious concrete (CFRPC) subjected to static, cyclic and impact loads. International Journal of Pavement Engineering, 2021. 23(9): p. 3113-3128.

102.	Lee, M.-G., et al., Mechanical Properties of High-Strength Pervious Concrete with Steel Fiber or Glass Fiber. Buildings, 2022. 12(5).

103.	Wu, J., et al., Research on the Mechanical and Physical Properties of Basalt Fiber-Reinforced Pervious Concrete. Materials (Basel), 2022. 15(19).

104.	Zhang, Y., et al., Comparative laboratory measurement of pervious concrete permeability using constant-head and falling-head permeameter methods. Construction and Building Materials, 2020. 263.

105.	Sandoval, G.F.B., et al., Comparison between the falling head and the constant head permeability tests to assess the permeability coefficient of sustainable Pervious Concretes. Case Studies in Construction Materials, 2017. 7: p. 317-328.

106.	Abdelhady, A., L. Hui, and H. Zhang, Comprehensive study to accurately predict the water permeability of pervious concrete using constant head method. Construction and Building Materials, 2021. 308.

107.	Li, L.G., et al., Pervious concrete: effects of porosity on permeability and strength. Magazine of Concrete Research, 2021. 73(2): p. 69-79.

108.	Roy, D.M. and G.R. Gouda, Porosity-Strength Relation in Cementitious Materials with Very High Strengths. Journal of the American Ceramic Society, 1973. 56(10): p. 549-550.

109.	Chindaprasirt, P., et al., Cement paste characteristics and porous concrete properties. Construction and Building Materials, 2008. 22(5): p. 894-901.

110.	Chindaprasirt, P., et al., Effects of binder strength and aggregate size on the compressive strength and void ratio of porous concrete. International Journal of Minerals, Metallurgy and Materials, 2009. 16(6): p. 714-719.

111.	Kumar, R. and B. Bhattacharjee, Porosity, pore size distribution and in situ strength of concrete. Cement and Concrete Research, 2003. 33(1): p. 155-164.

112.	Lian, C., Y. Zhuge, and S. Beecham, The relationship between porosity and strength for porous concrete. Construction and Building Materials, 2011. 25(11): p. 4294-4298.

113.	Kendall, K., et al., The relation between porosity, microstructure and strength, and the approach to advanced cement-based materials. Philosophical Transactions of the Royal Society of London. Series A, Mathematical and Physical Sciences, 1983. 310(1511): p. 139-153.

114.	Deo, O. and N. Neithalath, Compressive behavior of pervious concretes and a quantification of the influence of random pore structure features. Materials Science and Engineering: A, 2010. 528(1): p. 402-412.

115.	Zhong, R. and K. Wille, Compression response of normal and high strength pervious concrete. Construction and Building Materials, 2016. 109: p. 177-187.

116.	Shan, J., et al., Pore characteristics of pervious concrete and their influence on permeability attributes. Construction and Building Materials, 2022. 327.

117.	Cui, X., et al., Strength-permeability Model of Pervious Cement Concrete. Journal of Chongqing Jianzhu University, 2013(4): p. 114-120.

118.	Jinlong, W., et al., Study on main influencing factors of strength and permeability of new pervious concrete. New Building Materials, 2017. 44(11): p. 71-74.

119.	Barreto sandoval, G.F., et al., Correlation between Permeability and Porosity for Pervious Concrete (PC). Dyna, 2019. 86(209): p. 151-159.

120.	Sičáková, A. and M. Kováč, Relationships between Functional Properties of Pervious Concrete. Sustainability, 2020. 12(16).

121.	Feng, Z., et al., Research on the Matching Relationship Between Permeability Performance and Compressive Strength of Pervious Concrete. Construction Technology, 2020. 49(15): p. 16-21.

122.	Li, L.G., et al., Roles of mortar volume in porosity, permeability and strength of pervious concrete. Journal of Infrastructure Preservation and Resilience, 2021. 2(1).

123.	Li, L.G., et al., Effects of aggregate bulking and film thicknesses on water permeability and strength of pervious concrete. Powder Technology, 2022. 396: p. 743-753.

124.	Bian, W., et al., Improved mix design method for pervious concrete based on slurry layer thickness. Magazine of Concrete Research, 2022. 74(2): p. 81-90.

125.	Tang, C.-W., C.-K. Cheng, and L.-W. Ean, Mix Design and Engineering Properties of Fiber-Reinforced Pervious Concrete Using Lightweight Aggregates. Applied Sciences, 2022. 12(1).

126.	Wen, C., et al., Influence of fibers on the mechanical properties and durability of ultra-high-performance concrete: A review. Journal of Building Engineering, 2022. 52.

Table 1. The various types of fibers with its properties.

| Material variety | Type | Density | Tensile strength (MPa) | Modulus of elasticity (GPa) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Synthetic | Polypropylene fiber | 900-910 | 300-900 | 3.5-11 | [32] |
|  | Polypropylene thick fiber | 910 | 300-900 | 3.5-11 | [41] |
|  | Polyolefin fiber | 910 | - | - | [25] |
|  | Polyphenylene sulfide fiber (PPS) | 900 | - | 3.5 | [26] |
|  | Polyester fiber | 1380 | 11-15 | 6-18 | [28] |
|  | Ferro-green fiber | 910 | - | - | [30] |
|  | Green-net fiber | 910 | - | - | [30] |
|  | Recycled rubber fiber | 1090 | - | - | [32] |
|  | Polyvinyl Chloride fiber (PVC) | 2750 | 4840 | - | [34] |
|  | Polyvinyl Alcohol fiber (PVA) | 1300 | 1050 | 60-120 | [40] |
|  | Waste plastic fiber | 940-1100 | 101 | - | [67] |
|  | Kevlar fiber (KF) | 1480 | 1980 | - | [40] |
|  | Ultra-high molecular weight polyethylene fiber (UHMWPE) | 970 | 3000 | - | [40] |
|  | Polyacrylonitrile fiber (PANF) | 1180 | 500 | - | [44] |
|  | Waste cloth strip | - | - | - | [45] |
|  | Barchip fiber | 900 | 640 | 12 | [14] |
| Natural | Cellulose fiber | - | - | - | [20] |
|  | Hemp fiber | 1500 | 400-938 | 14.5-53 | [43] |
|  | Natural kenaf fiber | 1900 | 930 | 14.5-53 | [46] |
| Carbon based | Carbon fiber | 1600-1900 | 1800-4300 | 228-238 | [100] |
|  | Cured carbon fiber composite material | - | - | - | [31] |
| Metallic | Steel fiber | 7800-7850 | 1100-1450 | 200-250 | [14] |
|  | Copper-coated steel fiber | 7850 | - | - | [41] |
|  | Amorphous metallic fiber (AMF) | 7200 | 1400 | - | [42] |
| Inorganic | Glass fiber | 2460-2700 | 1050-3850 | 70-80 | [26] |
|  | Basalt fiber | 2650-2700 | 324-4840 | 35-115 | [92] |

Table 2. The summary of different standards for different properties of PC.

| Properties |  | UK | US | Chinese |
| --- | --- | --- | --- | --- |
| Porosity | Standard code | ISO 17785-2:2018 [51] | ASTM C1754/C1754M [55] | DB11/T 775-2021 [62] CJJ/T 253-2016 [63] |
|  | Specimens size | CY D100mm H100mm~300mm | CY D100mm H100mm~300mm | CU:150 |
| Compressive strength | Standard code | BS EN 12390-3 [52] | ASTM C39 [50] | GT/B 50081-2019 [64] |
|  | Specimens size | CU100/CU 150/ CY D160H320 | CY D150H300/ CY D100H200/ | CU 100 0.95/ CU 150/ CU 200 1.05 |
| Split tensile strength | Standard code | BS EN 12390-6 [53] | ASTM C496-17 [56] | GT/B 50081-2019 [64] |
|  | Specimens size | CY D150H300 | CY D150H300 | CU 100 0.85/ CU 150/ CU 200 |
| Flexural Strength | Standard code | BS EN 12390-5 [54] | ASTM C78 [57] ASTM C1161 | GT/B 50081-2019 [64] |
|  | Specimens size | 100*100*400 | 100*100*400/ 100*100*500 | 150*150*600/ 150*150*550/ 100*100*400 0.85 |
| Permeability | Standard code | - | ACI 522 [58] ASTM D2434 [59] ASTM C1701 [60] ASTM D5084 [61] | CJJ/T 135-2009 [65] |
|  | Specimens size | - | CY D100H150 | CY D100H50 |

* CY: cylinder samples, CU: cube samples.

Table 3. The quantification of fibers in PC.

| Addition method | In terms of | Notes |
| --- | --- | --- |
| 1 | Volume fraction in unit of (m^3/m^3) | It can be directly calculated by multiplying the specific density of fibers |
| 2 | dosage weight in unit of 1kg/m^3 | The content is directly shown |
| 3 | Weight percentage of cement (%) | Consider fiber belonging to paste |
| 4 | Volume percentage of cement | Consider fiber belonging to paste and consider the volume of fibers |
| 5 | Weight percentage of aggregates |  |
| 6 | Volume percentage of aggregates |  |

Table 4. The process type and process diagram for FPC.

Table 5.  The compaction method in FPC.

| Method number | Compacting method | Advantage | Disadvantage |
| --- | --- | --- | --- |
| 1 | Using standard hammer referred to ASTM C09.49 | Could control compacted energy | Not easy to implement |
| 2 | Rodding 25 times + Vibration 5-10s for three layers | Easy to implement | lead to over compacted then segregation |
| 3 | Vibration 5s |  | vibration would easily lead to segregation |
| 4 | Rodding 25 times |  | Cannot control consistency for each samples |
| 5 | Bar vibration | Usually in in-situ construction | Lead to over compacted |
| 6 | Hydraulic press | Could control compacted energy | Cannot control the sample thickness, which would change due to different proportions |

Table 6. The curing method in FPC.

| Method number | Curing method | Advantage | Disadvantage |
| --- | --- | --- | --- |
| 1 | water curing in 22-25℃ for 28 days | The same as conventional concrete, easy to implement | The water tank may not control temperature strictly |
| 2 | moist-cured for 28 days by a film covering | Convenient, usually for in-situ construction | Not standard |
| 3 | moist-cured for 28 days in a curing chamber (>95% RH. 20 °C) | Standard control curing condition | The space of chamber is limited |

Table 7. The prediction model of compressive strength for pervious concrete.

|  | Equations | Mathematic Law | Factor | R2 | Year/Reference |
| --- | --- | --- | --- | --- | --- |
| (1) | σ=σ0exp-bp | Exponential | porosity | - | 1973/ [108] |
| (2) | σ=KfcafefafTC(1-p)rm | Linear | In-situ, aggregate type, environment, age and temperature | - | 2003/ [111] |
| (3) | σ=152e-0.084p | Exponential | Water reducer and superplasticizer | 0.96 | 2008/ [109] |
| (4) | σ=σ0exp[-0.1962-0.0174FMp] | Exponential | Binder strength/Aggregate size | - | 2009/ [110] |
| (5) | σ=α0+α1ln⁡(dMFS)lndn+α2ϕASp-1+α0lnΓ3D | Power | Pore structure | - | 2010/ [114] |
| (6) | σ=B1-pme-np | Mixed | Young’s Modulus/ Fracture energy | 0.84 | 1983,2011/[112, 113] |
| (7) | σ=σ01-mpdd0n | Linear | Aggregate size, binder strength and Aggregate/Binder ratio | - | 2016/ [115] |
| (8) | σ=-57.4+301.8*wc-581.9*wc2lnp+83.4 | Mixed | w/c ratio | 0.951 | 2021/ [107] |

Table 8. The prediction model of permeability coefficient for pervious concrete.

|  | Equations | Mathematic Law | Factor | R2 | Year/Reference |
| --- | --- | --- | --- | --- | --- |
| (1) | k=0.00129p3-0.02769p2+0.32165p | Power | Target porosity | 0.999 | 2013/ [117] |
| (2) | k=-2.27762+0.16315p | Linear | Target porosity | 0.978 | 2017/ [118] |
| (3) | kp=1i2g(h-hf) | Linear | Based on Darcy’s and Bernoulli’s Law | 0.96 | 2019/ [119] |
| (4) | k=0.2259e0.1092p | Exponential | Void ratio and density | 0.753 | 2020/ [120] |
| (5) | k=0.004p2.036 | Power | Interconnected porosity | 0.846 | 2020/ [121] |
| (6) | k=1.373e0.080p-1.666 k=1.322e0.089p-1.526 | Mixed | Interconnected porosity/Unsubmerged or submerged | 0.987 0.993 | 2021/ [122] |
| (7) | k=e[-0.395-18.35WFT+-2.81-14.5WFTPFT] | Exponential | Water film thickness/Paste film thickness | 0.959 | 2022/ [123] |
| (8) | k=16.17-20.6PFT | Linear | Slurry layer thickness | 0.997 | 2022/ [124] |

Table 9. The optimum range on properties of PC for each type of fibers.

| Properties | Synthetic | Carbon-based | Metallic | Inorganic |
| --- | --- | --- | --- | --- |
| Compressive strength | 0-1% | 0-1.5% | 0.5-2% | 0.1-0.5% |
|  | 0-20mm | 6-12mm | 30-36mm | 10-25mm |
| Flexural strength | 0-1% | 3-5% | 0-2% | 0-0.5% |
|  | 6-12/50-60mm | 0-12mm | 0-60mm | 12-36mm |
| Splitting tensile strength | 0-0.5% | 0-5% | 0-2% | 0-0.5% |
|  | 10-16/50-60mm | 2-12mm | 6-60mm | 6-12m |
| Porosity | 0-2% | CCFCM: increasing Pure CF: decreasing | Almost increasing 0-2% | Almost decreasing 0-1% |
|  | 0-60mm | 2-12mm | 12-36mm | 6-36mm |
| Permeability - constant head method | 0.2-0.5% | Decreasing 0.2% | No significant increasing 0-0.15% | Almost decreasing 0.075-0.3% |
|  | 12-20mm | 6mm | 30mm | 6-24mm |
| Permeability - Falling head method | No significant decreasing 0-2% | Decreasing | No significant decreasing 1-2% | 0.25-0.5% |
|  | 19.1-50mm | 12mm >6mm | 30mm | 36mm |

Table 10. The summary of research for each types of fibers.

| Fiber types | E | TS | The research range based on public articles |  |  | Research Gap | Best scenario | Limit |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Volume fraction | Length | Aspect ratio |  |  |  |
| Synthetic | 3.5-18 | 101-900 | 0~5% | 0-40mm | 0-100 300-750 | - Lack transverse comparison on different length and aspect ratio - Lack of high aspect ratio | VF= 0~1% Length = 0~20mm | 1) w/c=0.27~0.33 2) Dense compaction |
| Carbon-based | 3.5-18 | 1600-1900 | 0~5% | 0-12mm | 0-100 700-800 1700-1800 | 1) Lack transverse comparison on different length and aspect ratio 2) Lack of high length of fiber | Pure CF: 1~5% CCFCM: VF = 0-1.5% Length = 6~12mm | w/c=0.24-0.27 |
| Metallic | 200-250 | 1100-1450 | 0~2% | 40-60mm | 0-150 | Lack transverse comparison on different length and aspect ratio | VF = 0.5~2% Length = 30-36mm | High strength matrix |
| Inorganic | 95-115 | 3300-4500 | 0~0.5% | 5-40mm | 0-120 600-1600 | 1) Lack transverse comparison on different length and aspect ratio 2) Lack of high volume fraction studies | VF = 0.1~0.5% Length = 10-25mm | w/c = 0.25-0.3 |
| Natural | 14.5-53 | 400-938 | 0.2% 2% | 0-10mm | 0-20 | 1) Lack comprehensive research on Natural fiber 2) Lack transverse comparison on different length and aspect ratio | N/A | N/A |

Figure 1. The research timeline of fiber addition in PC.

Figure 2. The fiber volume fraction distribution for Synthetic fibers on compressive strength a) Cylinder specimens, b) Cube specimens.

Figure 3. The fiber volume fraction distribution for Carbon-based, Metallic and inorganic fibers on compressive strength a) Cylinder specimens, b) Cube specimens.

Figure 4. The fiber volume fraction distribution on flexural strength a) Synthetic, b) Carbon-based, c) Metallic, and d) Inorganic fibers.

Figure 5. The fiber volume fraction distribution on splitting tensile strength a) Synthetic, b) Carbon-based, c) Metallic, and d) Inorganic fibers.

Figure 6. The fiber volume fraction distribution on porosity a) Synthetic, b) Carbon-based, c) Metallic, and d) Inorganic fibers.

Figure 7. The fiber volume fraction distribution on permeability for each type of fiber a) Constant head test method b) Falling head test method.

Figure 8. The relationship between porosity and compressive strength for different types of fibers a)Overall Exponential Fitting b)STF c)MF d)WPF.

Figure 9. The relationship between porosity and compressive strength for four types of fibers a) small size aggregates b) large size aggregates [97, 100, 101].

Figure 10. The relationship between porosity and compressive strength for Ali [38] and Xiao [72]’s research.

Figure 11. The Mehrabi’s research on relationship between porosity and permeability.

Figure 12. The correlation between porosity and permeability a) Wu’s research [23] b) Hesami’s research [26].

Figure 13. The correlation between permeability and a) Compressive strength b) Flexural strength [38, 72].

.

Figure 14. The correlation between permeability and compressive strength for four types of fibers [97, 100, 101].

Figure 15. The fiber length and aspect ratio distribution for research range.