APPENDIX

A1. Modal analysis data

A2. Wireline log and water saturation data

A3. Core analysis data

A4. XRD data

A5. Isotope data

APPENDIX 1 – Modal analysis data

Table A1.1: Thin section modal analysis for Singleton-1 (S), Horndean-1A (HO), Hesters Copse-1 (HE), Chilgrove-1 (C), Ashington-1 (A) and Storrington-2 (ST) wells.

| TVDSS (ft) | 4392.4 | 4383.9 | 4372.9 | 4357.6 | 4309.3 | 4308.2 | 4306.5 | 4303.1 | 4296.0 | 4284.3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 174.4 | 165.9 | 154.9 | 139.6 | 91.3 | 90.2 | 88.5 | 85.1 | 78.0 | 66.3 |
| Facies | I | I | I | I | I | IIa | I | I | I | I |
| Sample No. | S-2 | S-3 | S-4 | S-5 | S-8 | S-10 | S-12 | S-14 | S-16 | S-17 |
| Ooids | 30.8 | 33.2 | 40.4 | 31.2 | 35.2 | 5.0 | 30.4 | 39.6 | 47.6 | 42.2 |
| Bivalve shells | 8.0 | 7.4 | 5.2 | 9.0 | 6.6 | 13.8 | 6.2 | 5.6 | 6.8 | 5.8 |
| Brachiopod shells | 2.0 | 4.2 | 3.0 | 3.2 | 3.8 | 12.6 | 2.2 | 2.4 | 1.8 | 2.6 |
| Echinoderm plates | 3.2 | 2.6 | 3.4 | 2.6 | 2.8 | 3.8 | 3.4 | 3.0 | 2.4 | 2.2 |
| Intraclasts | 0.8 | 0.2 | 1.0 | 0.6 | 0.8 | 1.4 | 1.6 | 1.2 | 1.0 | 0.8 |
| Peloids | 2.8 | 1.4 | 1.6 | 1.0 | 0.6 | 2.0 | 3.6 | 2.4 | 2.8 | 3.6 |
| Micritic matrix | 2.4 | 13.4 | 1.2 | 2.4 | 0.6 | 10.0 | 1.4 | 1.2 | 1.0 | 0 |
| Syntaxial overgrowth cement | 1.4 | 0.2 | 1.0 | 0.8 | 2.2 | 2.6 | 3.2 | 3.0 | 1.4 | 1.6 |
| Isopachous calcite cement | 3.2 | 2.6 | 2.2 | 2.6 | 3.2 | 7.0 | 2.4 | 2.0 | 2.4 | 2.6 |
| Intergranular Non-Fe calcite cement | 8.4 | 7.6 | 9.6 | 15.8 | 14.8 | 16.6 | 20.4 | 13.8 | 11.4 | 11.6 |
| Intragranular Non-Fe calcite cement | 1.6 | 2.4 | 6.2 | 9.2 | 10.0 | 6.4 | 12.0 | 7.2 | 3.8 | 6.2 |
| Intergranular Fe-calcite cement | 15.6 | 10.4 | 11.0 | 8.2 | 8.6 | 4.4 | 4.0 | 5.6 | 5.0 | 8.8 |
| Intragranular Fe-calcite cement | 7.2 | 3.6 | 4.2 | 3.0 | 3.4 | 2.6 | 3.2 | 2.2 | 3.0 | 2.8 |
| Non-Fe dolomite cement | 6.6 | 0.6 | 3.6 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Coarse dolomite cement | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 2.2 | 4.4 | 1.4 | 4.8 | 2.4 | 8.6 | 3.0 | 4.8 | 4.6 | 4.8 |
| Intragranular porosity | 0.6 | 4.0 | 1.8 | 3.6 | 3.6 | 1.6 | 2.6 | 4.4 | 5.0 | 3.4 |
| Quartz | 1.8 | 1.8 | 2.0 | 0.6 | 0.2 | 0 | 0 | 0 | 0 | 0.2 |
| Clay minerals | 0 | 0 | 0 | 0 | 0 | 0.4 | 0 | 0 | 0 | 0 |
| Pyrite | 0.2 | 0 | 0.4 | 0 | 0 | 0.4 | 0 | 0 | 0 | 0 |
| Coral plates | 1.2 | 0 | 0.8 | 1.4 | 1.2 | 0.8 | 0.4 | 0 | 0 | 0.8 |

| TVDSS (ft) | 4269.6 | 4251.8 | 4241.0 | 4228.3 | 4220.6 | 4218.7 | 4431.5 | 4425.4 | 4422.9 | 4412.9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 51.6 | 33.8 | 23.0 | 10.3 | 2.6 | 0.7 | 199.5 | 193.4 | 190.9 | 180.9 |
| Facies | III | I | III | IIa | IIa | IIa | I | I | I | I |
| Sample No. | S-19 | S-20 | S-21 | S-23 | S-24 | S-25 | HO-2 | HO-4 | HO-5 | HO-7 |
| Ooids | 3.6 | 38.4 | 3.4 | 2.4 | 3.8 | 10.6 | 49.0 | 32.6 | 40.2 | 45.6 |
| Bivalve shells | 9.2 | 5.6 | 10.4 | 9.8 | 17.2 | 17.6 | 3.8 | 3.8 | 3.6 | 4.8 |
| Brachiopod shells | 6.6 | 3.0 | 5.8 | 7.4 | 12.4 | 10.8 | 1.0 | 2.4 | 2.0 | 1.8 |
| Echinoderm plates | 2.8 | 9.6 | 2.0 | 1.6 | 3.8 | 4.2 | 1.6 | 3.8 | 2.6 | 2.0 |
| Intraclasts | 0 | 1.2 | 1.8 | 2.0 | 0 | 0.4 | 0.2 | 2.4 | 0 | 0.4 |
| Peloids | 3.6 | 3.2 | 3.4 | 2.0 | 2.4 | 3.2 | 0.6 | 1.8 | 1.0 | 1.6 |
| Micritic matrix | 31.6 | 8.2 | 35.8 | 19.6 | 5.8 | 11.6 | 0.6 | 1.6 | 0.4 | 1.0 |
| Syntaxial overgrowth cement | 0.6 | 1.6 | 0.4 | 0.4 | 0.8 | 2.8 | 1.0 | 3.4 | 3.2 | 1.4 |
| Isopachous calcite cement | 2.6 | 1.2 | 1.8 | 2.8 | 4.6 | 3.6 | 3.0 | 4.6 | 4.0 | 3.6 |
| Intergranular Non-Fe calcite cement | 10.8 | 5.2 | 3.6 | 4.8 | 6.2 | 4.2 | 6.4 | 3.2 | 9.4 | 7.6 |
| Intragranular Non-Fe calcite cement | 6.0 | 3.6 | 3.4 | 3.2 | 2.2 | 1.4 | 3.6 | 2.4 | 5.8 | 4.0 |
| Intergranular Fe-calcite cement | 10.8 | 5.4 | 3.8 | 10.6 | 26.8 | 10.8 | 15.0 | 17.2 | 16.0 | 14.2 |
| Intragranular Fe-calcite cement | 1.2 | 1.6 | 1.0 | 5.0 | 4.0 | 4.8 | 4.8 | 9.4 | 5.6 | 6.0 |
| Non-Fe dolomite cement | 1.2 | 0 | 15.4 | 12.2 | 1.4 | 1.8 | 2.4 | 1.4 | 0 | 0 |
| Coarse dolomite cement | 0 | 0 | 0 | 3.8 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 3.8 | 5.4 | 3.6 | 4.2 | 2.4 | 4.4 | 2.8 | 4.4 | 1.8 | 1.8 |
| Intragranular porosity | 3.4 | 4.8 | 2.4 | 3.8 | 3.4 | 3.8 | 3.6 | 4.0 | 3.4 | 4.2 |
| Quartz | 0.8 | 1.0 | 0.8 | 1.0 | 1.0 | 1.2 | 0.6 | 1.0 | 0.4 | 0 |
| Clay minerals | 0.6 | 0 | 0.4 | 1.6 | 0 | 0 | 0 | 0.2 | 0 | 0 |
| Pyrite | 0 | 0 | 0.4 | 1.8 | 0 | 0 | 0 | 0.4 | 0 | 0 |
| Coral plates | 0.8 | 1.0 | 0.4 | 0 | 1.8 | 2.8 | 0 | 0 | 0.6 | 0 |

| TVDSS (ft) | 4406.4 | 4368.3 | 4329.4 | 4323.6 | 4317.4 | 4311.4 | 4300.9 | 4285.9 | 4280.4 | 4266.6 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 174.4 | 136.3 | 97.4 | 91.6 | 85.4 | 79.4 | 68.9 | 53.9 | 48.4 | 34.6 |
| Facies | I | IIa | I | I | IIa | IIa | I | I | IIa | III |
| Sample No. | HO-8 | HO-9 | HO-10 | HO-12 | HO-14 | HO-15 | HO-16 | HO-17 | HO-18 | HO-20 |
| Ooids | 41.2 | 21.8 | 42.4 | 52.8 | 9.8 | 21.2 | 35.4 | 24.6 | 11.0 | 0.8 |
| Bivalve shells | 5.2 | 11.8 | 4.8 | 3.6 | 19.2 | 12.8 | 5.2 | 4.0 | 6.6 | 8.8 |
| Brachiopod shells | 1.8 | 5.4 | 2.6 | 1.8 | 6.6 | 7.2 | 3.2 | 2.4 | 5.8 | 4.6 |
| Echinoderm plates | 4.8 | 3.6 | 5.2 | 2.4 | 2.6 | 11.4 | 11.8 | 4.0 | 1.4 | 1.2 |
| Intraclasts | 1.0 | 1.8 | 2.0 | 0.4 | 1.6 | 2.6 | 3.4 | 2.6 | 1.2 | 0 |
| Peloids | 0 | 2.6 | 2.8 | 0.8 | 3.6 | 4.8 | 2.4 | 3.0 | 4.2 | 3.8 |
| Micritic matrix | 0.6 | 20.6 | 5.8 | 11.6 | 24.8 | 2.2 | 3.0 | 4.0 | 2.8 | 43.2 |
| Syntaxial overgrowth cement | 2.2 | 2.4 | 4.4 | 2.8 | 0.4 | 4.4 | 5.4 | 1.6 | 0.6 | 0.2 |
| Isopachous calcite cement | 1.8 | 0.6 | 1.6 | 1.6 | 1.4 | 3.4 | 3.8 | 4.2 | 5.2 | 2.8 |
| Intergranular Non-Fe calcite cement | 6.8 | 7.4 | 6.8 | 6.2 | 6.4 | 5.8 | 7.2 | 12.6 | 15.4 | 9.4 |
| Intragranular Non-Fe calcite cement | 2.0 | 2.8 | 1.4 | 2.6 | 4.8 | 6.4 | 4.6 | 7.6 | 6.0 | 3.4 |
| Intergranular Fe-calcite cement | 12.8 | 8.4 | 2.2 | 3.8 | 6.2 | 6.6 | 3.0 | 3.2 | 12.6 | 7.2 |
| Intragranular Fe-calcite cement | 6.8 | 4.4 | 1.0 | 1.4 | 2.4 | 1.2 | 1.6 | 2.4 | 7.0 | 3.4 |
| Non-Fe dolomite cement | 0 | 2.2 | 0 | 1.0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Coarse dolomite cement | 0 | 0.6 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 6.8 | 0.8 | 8.2 | 1.8 | 4.8 | 2.6 | 3.0 | 14.2 | 10.2 | 5.2 |
| Intragranular porosity | 5.4 | 1.4 | 5.8 | 3.8 | 2.0 | 4.4 | 4.8 | 7.2 | 8.4 | 2.4 |
| Quartz | 0.4 | 1.0 | 0.8 | 0.6 | 1.0 | 0.4 | 0 | 0.6 | 0.6 | 0.8 |
| Clay minerals | 0 | 0 | 0 | 0 | 0.4 | 0 | 0 | 0 | 0 | 0.4 |
| Pyrite | 0 | 0 | 0 | 0.4 | 0.4 | 0 | 0 | 0.6 | 0 | 0.6 |
| Coral plates | 0.4 | 0.4 | 2.2 | 0.6 | 1.6 | 2.6 | 2.2 | 1.2 | 1.0 | 1.8 |

| TVDSS (ft) | 4252.7 | 4244.9 | 3699.5 | 3691.5 | 3686.0 | 3674.5 | 3672.3 | 3670.5 | 3669.0 | 3667.5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 20.7 | 12.9 | 148.5 | 140.5 | 135.0 | 123.5 | 121.5 | 119.5 | 118.0 | 116.5 |
| Facies | III | IIa | I | III | III | III | IIa | III | I | I |
| Sample No. | HO-23 | HO-25 | HE-1 | HE-2 | HE-3 | HE-5 | HE-6 | HE-7 | HE-8 | HE-9 |
| Ooids | 0.6 | 25.4 | 39.6 | 3.4 | 1.0 | 2.4 | 7.8 | 0.6 | 37.2 | 42.2 |
| Bivalve shells | 8.0 | 12.4 | 7.4 | 4.2 | 4.2 | 3.4 | 11.0 | 3.4 | 4.4 | 6.4 |
| Brachiopod shells | 4.4 | 7.4 | 1.8 | 2.0 | 1.4 | 1.6 | 5.6 | 2.2 | 2.0 | 3.0 |
| Echinoderm plates | 1.8 | 8.2 | 4.0 | 1.0 | 1.2 | 2.2 | 3.4 | 1.4 | 2.8 | 4.2 |
| Intraclasts | 0 | 3.2 | 1.0 | 0 | 0 | 0.2 | 0.8 | 0 | 1.8 | 0.6 |
| Peloids | 3.2 | 4.4 | 0.4 | 6.4 | 11.0 | 3.2 | 12.6 | 7.8 | 15.2 | 1.8 |
| Micritic matrix | 30.8 | 13.8 | 3.6 | 41.4 | 35.4 | 23.2 | 25.6 | 36.0 | 6.0 | 3.8 |
| Syntaxial overgrowth cement | 0.4 | 4.8 | 1.2 | 0 | 0 | 0 | 0.4 | 0 | 0.4 | 1.4 |
| Isopachous calcite cement | 4.6 | 3.2 | 3.2 | 0 | 0 | 0 | 0 | 0 | 1.2 | 3.0 |
| Intergranular Non-Fe calcite cement | 7.4 | 1.4 | 18.2 | 8.2 | 4.2 | 2.2 | 6.2 | 1.2 | 3.4 | 3.4 |
| Intragranular Non-Fe calcite cement | 2.8 | 0.4 | 5.4 | 2.6 | 3.8 | 0.4 | 1.2 | 0.6 | 2.0 | 7.4 |
| Intergranular Fe-calcite cement | 17.4 | 4.0 | 9.0 | 6.8 | 5.4 | 7.6 | 5.0 | 2.4 | 6.0 | 9.6 |
| Intragranular Fe-calcite cement | 7.6 | 2.4 | 1.2 | 0.8 | 3.0 | 0 | 3.8 | 0 | 2.2 | 2.0 |
| Non-Fe dolomite cement | 1.0 | 0 | 0 | 11.6 | 18.2 | 43.6 | 13.6 | 36.4 | 9.2 | 4.2 |
| Coarse dolomite cement | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 4.6 | 2.2 | 2.4 | 0.4 | 0 | 0 | 0.4 | 0 | 0.4 | 2.4 |
| Intragranular porosity | 2.2 | 2.8 | 0.2 | 0.6 | 0.8 | 0.4 | 0.4 | 0.4 | 0.4 | 1.6 |
| Quartz | 0.6 | 0.6 | 1.0 | 9.0 | 8.0 | 7.4 | 1.8 | 5.4 | 3.4 | 1.2 |
| Clay minerals | 0 | 0 | 0.4 | 0.4 | 0.8 | 0.4 | 0 | 0.6 | 0.8 | 0 |
| Pyrite | 0 | 0 | 0 | 0.8 | 1.0 | 1.2 | 0 | 1.6 | 0.4 | 0.6 |
| Coral plates | 2.6 | 3.4 | 0 | 0.4 | 0.6 | 0.6 | 0.4 | 0 | 0.8 | 1.2 |

| TVDSS (ft) | 3666.0 | 3662.9 | 3659.0 | 3651.0 | 3645.0 | 3600.0 | 3586.1 | 3557.0 | 4320.0 | 4317.5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 115.0 | 111.9 | 108.0 | 100.0 | 94.0 | 49.0 | 35.1 | 6.0 | 131.0 | 128.5 |
| Facies | I | I | I | I | I | I | I | I | IIb | IIa |
| Sample No. | HE-10 | HE-11 | HE-13 | HE-16 | HE-18 | HE-21 | HE-22 | HE-23 | C-2 | C-4 |
| Ooids | 47.4 | 46.6 | 57.0 | 35.6 | 46.2 | 24.2 | 39.2 | 30.6 | 5.4 | 5.8 |
| Bivalve shells | 7.8 | 5.8 | 1.8 | 3.2 | 2.4 | 5.8 | 9.6 | 4.4 | 5.6 | 8.2 |
| Brachiopod shells | 4.2 | 2.4 | 0.6 | 0.8 | 1.2 | 4.4 | 6.2 | 1.4 | 1.8 | 5.6 |
| Echinoderm plates | 3.6 | 3.6 | 4.4 | 3.0 | 0.8 | 3.2 | 3.4 | 9.4 | 10.2 | 5.0 |
| Intraclasts | 1.0 | 2.2 | 1.6 | 2.2 | 0.8 | 0.8 | 0.2 | 1.6 | 4.8 | 1.0 |
| Peloids | 2.4 | 1.2 | 0 | 1.0 | 0 | 20.8 | 3.4 | 0.6 | 5.6 | 2.4 |
| Micritic matrix | 2.2 | 5.4 | 0 | 2.8 | 0.6 | 4.6 | 4.0 | 0.6 | 0.8 | 1.2 |
| Syntaxial overgrowth cement | 2.8 | 1.2 | 1.4 | 2.6 | 0.2 | 0.8 | 1.6 | 3.4 | 4.8 | 8.4 |
| Isopachous calcite cement | 4.4 | 2.6 | 3.8 | 6.0 | 3.6 | 3.4 | 4.6 | 3.2 | 4.2 | 3.8 |
| Intergranular Non-Fe calcite cement | 0.8 | 3.6 | 11.0 | 12.2 | 8.8 | 4.2 | 2.0 | 14.6 | 21.4 | 20.6 |
| Intragranular Non-Fe calcite cement | 8.0 | 4.8 | 4.2 | 11.8 | 9.4 | 8.0 | 3.6 | 6.6 | 8.2 | 6.2 |
| Intergranular Fe-calcite cement | 6.8 | 7.2 | 5.0 | 8.4 | 11.4 | 9.8 | 8.4 | 6.2 | 12.6 | 17.6 |
| Intragranular Fe-calcite cement | 0 | 3.2 | 2.8 | 2.4 | 7.2 | 2.0 | 0.8 | 5.6 | 7.2 | 8.8 |
| Non-Fe dolomite cement | 2.0 | 1.8 | 0 | 0 | 0 | 3.2 | 5.6 | 1.8 | 0 | 0 |
| Coarse dolomite cement | 0.4 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 2.6 | 4.4 | 3.8 | 4.6 | 4.0 | 1.6 | 2.4 | 3.8 | 1.4 | 1.4 |
| Intragranular porosity | 1.8 | 1.8 | 1.8 | 2.2 | 2.6 | 2.2 | 3.2 | 2.0 | 2.2 | 1.6 |
| Quartz | 0.6 | 0.8 | 0.8 | 0.8 | 0.8 | 0.6 | 1.0 | 0 | 0.8 | 0 |
| Clay minerals | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.8 | 0 | 0 |
| Pyrite | 0 | 0 | 0 | 0.4 | 0 | 0 | 0 | 2.2 | 0 | 0 |
| Coral plates | 1.2 | 1.4 | 0 | 0 | 0 | 0.4 | 0.8 | 1.2 | 3.0 | 2.4 |

| TVDSS (ft) | 4316.0 | 4313.1 | 4311.0 | 4299.5 | 4289.5 | 4287.0 | 4284.0 | 4276.5 | 4272.0 | 4262.0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 127.0 | 124.1 | 122.0 | 110.5 | 100.5 | 98.0 | 95.0 | 87.5 | 83.0 | 73.0 |
| Facies | III | IIa | III | III | IIa | I | I | III | IIa | IIb |
| Sample No. | C-5 | C-6 | C-7 | C-9 | C-10 | C-11 | C-12 | C-14 | C-16 | C-17 |
| Ooids | 0.8 | 3.2 | 0.6 | 0.6 | 8.6 | 28.2 | 29.0 | 5.6 | 18.4 | 7.4 |
| Bivalve shells | 6.0 | 15.8 | 8.6 | 6.6 | 11.0 | 4.8 | 3.4 | 6.2 | 7.6 | 6.2 |
| Brachiopod shells | 8.4 | 9.2 | 7.2 | 2.4 | 7.8 | 2.8 | 4.0 | 3.0 | 4.2 | 3.2 |
| Echinoderm plates | 7.2 | 9.8 | 4.2 | 3.4 | 4.0 | 2.8 | 5.4 | 3.8 | 5.6 | 14.6 |
| Intraclasts | 1.8 | 0.8 | 0.8 | 0.6 | 0.8 | 0.8 | 1.0 | 0.8 | 1.4 | 2.2 |
| Peloids | 2.4 | 0.4 | 4.0 | 3.6 | 4.2 | 5.4 | 1.6 | 1.8 | 0.6 | 3.8 |
| Micritic matrix | 28.8 | 23.6 | 48.2 | 53.2 | 26.0 | 10.2 | 0.8 | 43.4 | 16.2 | 26.4 |
| Syntaxial overgrowth cement | 2.0 | 7.6 | 0.4 | 0.6 | 1.2 | 0.8 | 4.4 | 0.6 | 4.6 | 0.4 |
| Isopachous calcite cement | 2.4 | 3.2 | 1.6 | 1.6 | 3.2 | 2.0 | 5.2 | 2.0 | 2.6 | 2.4 |
| Intergranular Non-Fe calcite cement | 13.4 | 2.8 | 7.2 | 7.2 | 8.4 | 14.2 | 17.6 | 13.2 | 8.0 | 9.4 |
| Intragranular Non-Fe calcite cement | 5.4 | 7.4 | 3.4 | 6.0 | 6.6 | 7.0 | 12.0 | 6.4 | 10.4 | 3.4 |
| Intergranular Fe-calcite cement | 13.0 | 10.4 | 8.8 | 6.8 | 7.2 | 11.0 | 6.4 | 4.6 | 12.2 | 11.6 |
| Intragranular Fe-calcite cement | 4.2 | 0.8 | 1.4 | 4.2 | 4.6 | 5.6 | 5.0 | 2.6 | 2.6 | 4.2 |
| Non-Fe dolomite cement | 0.8 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.0 |
| Coarse dolomite cement | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 1.2 | 0.4 | 1.0 | 0.6 | 1.4 | 1.2 | 1.2 | 2.2 | 0.4 | 0.8 |
| Intragranular porosity | 0.8 | 0.6 | 0.4 | 0.2 | 2.0 | 1.8 | 1.8 | 1.0 | 1.2 | 0.6 |
| Quartz | 0.4 | 0.4 | 0.4 | 0.6 | 0.6 | 0.2 | 0 | 0 | 0 | 0.6 |
| Clay minerals | 0.2 | 0 | 0 | 0 | 0.4 | 0.2 | 0 | 0 | 0 | 0 |
| Pyrite | 0 | 0 | 0 | 0 | 0.4 | 0 | 0 | 0 | 0 | 0 |
| Coral plates | 0.8 | 3.6 | 1.8 | 1.8 | 1.6 | 1.0 | 1.2 | 2.8 | 4.0 | 1.8 |

| TVDSS (ft) | 4258.6 | 4255.8 | 4244.6 | 4229.0 | 4369.5 | 4361.1 | 4340.8 | 4328.1 | 4313.3 | 4310.5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 69.6 | 66.8 | 55.6 | 40.0 | 139.5 | 131.1 | 110.8 | 98.1 | 83.3 | 80.5 |
| Facies | III | IIa | I | IIa | IIa | IIa | IIa | I | I | I |
| Sample No. | C-18 | C-19 | C-20 | C-21 | A-2 | A-3 | A-5 | A-6 | A-8 | A-10 |
| Ooids | 2.4 | 4.2 | 30.4 | 3.4 | 4.4 | 5.6 | 6.8 | 28.4 | 41.4 | 44.2 |
| Bivalve shells | 7.6 | 18.2 | 10.2 | 17.2 | 15.2 | 17.2 | 12.0 | 6.2 | 3.0 | 2.6 |
| Brachiopod shells | 3.8 | 13.6 | 4.4 | 13.8 | 9.2 | 12.6 | 7.8 | 2.2 | 1.8 | 1.6 |
| Echinoderm plates | 3.4 | 4.0 | 3.2 | 4.4 | 4.2 | 5.8 | 2.4 | 4.8 | 2.6 | 2.6 |
| Intraclasts | 2.0 | 1.4 | 1.2 | 2.8 | 0 | 0.6 | 1.0 | 0 | 0.6 | 1.4 |
| Peloids | 6.2 | 5.6 | 1.8 | 6.8 | 0.4 | 2.4 | 4.4 | 0.8 | 1.6 | 3.8 |
| Micritic matrix | 27.8 | 8.6 | 4.2 | 15.6 | 11.4 | 3.2 | 26.2 | 8.4 | 1.4 | 1.8 |
| Syntaxial overgrowth cement | 1.6 | 1.4 | 3.4 | 2.4 | 2.4 | 2.8 | 1.0 | 2.8 | 4.8 | 3.6 |
| Isopachous calcite cement | 0.8 | 2.4 | 3.8 | 2.0 | 2.4 | 3.2 | 5.2 | 10.6 | 3.2 | 2.8 |
| Intergranular Non-Fe calcite cement | 1.6 | 9.0 | 18.4 | 9.8 | 9.0 | 12.6 | 16.6 | 12.2 | 6.8 | 10.2 |
| Intragranular Non-Fe calcite cement | 0 | 4.6 | 2.8 | 2.2 | 3.2 | 4.8 | 6.0 | 10.8 | 9.4 | 3.6 |
| Intergranular Fe-calcite cement | 2.0 | 8.4 | 9.2 | 4.6 | 5.4 | 16.4 | 4.8 | 4.2 | 17.2 | 15.4 |
| Intragranular Fe-calcite cement | 0.2 | 2.2 | 3.0 | 0.4 | 2.0 | 6.8 | 2.6 | 3.4 | 4.6 | 3.4 |
| Non-Fe dolomite cement | 33.6 | 8.6 | 0 | 6.2 | 25.2 | 0.8 | 1.0 | 0 | 0 | 1.6 |
| Coarse dolomite cement | 0 | 0 | 0 | 0 | 1.0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 1.0 | 0.8 | 0.4 | 0.4 | 0.8 | 0.6 | 0.2 | 2.2 | 0 | 0.4 |
| Intragranular porosity | 0.6 | 1.4 | 1.0 | 0.8 | 0.2 | 0.4 | 0.4 | 1.6 | 0.4 | 0.6 |
| Quartz | 2.4 | 1.6 | 0 | 2.6 | 1.8 | 0.6 | 0.8 | 0 | 0.2 | 0 |
| Clay minerals | 0.8 | 0 | 0 | 0.6 | 0 | 0 | 0 | 0.8 | 0 | 0 |
| Pyrite | 1.2 | 0.4 | 0 | 1.4 | 0.4 | 0 | 0 | 0.6 | 0 | 0 |
| Coral plates | 1.0 | 3.6 | 2.6 | 2.6 | 1.4 | 3.6 | 0.8 | 0 | 1.0 | 0.4 |

| TVDSS (ft) | 4310.0 | 4308.1 | 4303.8 | 4298.4 | 4283.9 | 4273.0 | 4269.8 | 4265.6 | 4250.3 | 4243.2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 80.0 | 78.1 | 73.8 | 68.4 | 53.9 | 43.0 | 39.8 | 35.6 | 20.3 | 13.2 |
| Facies | I | IIb | IIa | IIa | IIb | IIa | IIa | I | IIa | IIa |
| Sample No. | A-11 | A-12 | A-14 | A-16 | A-17 | A-18 | A-19 | A-21 | A-24 | A-25 |
| Ooids | 40.4 | 9.2 | 17.4 | 20.8 | 18.0 | 12.6 | 8.8 | 33.4 | 20.4 | 8.6 |
| Bivalve shells | 4.4 | 7.2 | 10.6 | 10.4 | 8.2 | 14.8 | 14.6 | 4.2 | 10.2 | 18.6 |
| Brachiopod shells | 1.8 | 5.2 | 6.6 | 7.6 | 4.6 | 10.4 | 6.8 | 3.6 | 7.6 | 6.8 |
| Echinoderm plates | 3.6 | 19.8 | 4.2 | 3.2 | 13.8 | 6.4 | 4.6 | 2.8 | 9.4 | 3.6 |
| Intraclasts | 3.0 | 3.2 | 4.4 | 3.2 | 3.6 | 3.0 | 2.8 | 0.6 | 1.4 | 1.4 |
| Peloids | 2.4 | 0.8 | 11.2 | 5.6 | 1.8 | 2.2 | 3.4 | 0.4 | 2.4 | 0 |
| Micritic matrix | 2.0 | 1.6 | 5.0 | 6.8 | 2.4 | 14.2 | 36.4 | 0.2 | 14.6 | 2.0 |
| Syntaxial overgrowth cement | 5.4 | 7.2 | 3.8 | 2.2 | 4.8 | 3.4 | 2.8 | 1.2 | 2.6 | 2.2 |
| Isopachous calcite cement | 3.2 | 7.4 | 3.0 | 1.0 | 1.6 | 4.0 | 3.2 | 4.0 | 1.2 | 10.4 |
| Intergranular Non-Fe calcite cement | 11.8 | 13.2 | 10.0 | 6.2 | 13.6 | 12.0 | 2.8 | 18.6 | 11.6 | 7.6 |
| Intragranular Non-Fe calcite cement | 5.2 | 10.8 | 4.4 | 13.0 | 6.2 | 1.8 | 3.0 | 7.6 | 1.6 | 4.2 |
| Intergranular Fe-calcite cement | 10.0 | 4.8 | 12.2 | 7.8 | 14.4 | 10.6 | 0.6 | 17.8 | 8.4 | 17.2 |
| Intragranular Fe-calcite cement | 2.4 | 4.4 | 0.6 | 4.6 | 1.0 | 1.2 | 3.6 | 2.6 | 0.8 | 12.2 |
| Non-Fe dolomite cement | 1.8 | 0 | 3.6 | 3.4 | 0 | 0 | 1.6 | 0 | 3.6 | 1.4 |
| Coarse dolomite cement | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Intergranular porosity | 0.2 | 0.6 | 0 | 0.4 | 0.2 | 0 | 0.8 | 0.4 | 0 | 0.8 |
| Intragranular porosity | 0.6 | 1.0 | 0.4 | 1.0 | 1.6 | 0.6 | 0.4 | 0.6 | 0 | 1.0 |
| Quartz | 0.4 | 0.4 | 0.4 | 1.8 | 0.4 | 0 | 1.0 | 0.4 | 1.6 | 0.8 |
| Clay minerals | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.4 | 0 | 0.4 |
| Pyrite | 0 | 2.6 | 0.6 | 0 | 0.6 | 0 | 0 | 0 | 0 | 0 |
| Coral plates | 1.4 | 0.6 | 1.6 | 1.0 | 3.2 | 2.8 | 2.8 | 1.2 | 2.6 | 0.8 |

| TVDSS (ft) | 4092.0 | 4077.5 | 4064.0 | 4054.0 | 4045.0 | 4040.0 | 4035.0 | 4031.0 | 4024.0 | 4013.0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 203.1 | 188.6 | 175.1 | 165.1 | 156.1 | 151.1 | 146.1 | 142.1 | 135.1 | 124.1 |
| Facies | IIa | I | IIa | IIa | I | IIa | I | I | I | I |
| Sample No. | ST-1 | ST-2 | ST-3 | ST-4 | ST-5 | ST-6 | ST-7 | ST-8 | ST-9 | ST-10 |
| Ooids | 14.6 | 31.8 | 23.2 | 13.0 | 39.0 | 22.0 | 41.2 | 49.0 | 50.2 | 52.8 |
| Bivalve shells | 15.8 | 6.8 | 18.6 | 14.4 | 6.6 | 12.4 | 4.8 | 2.6 | 3.8 | 1.4 |
| Brachiopod shells | 13.2 | 5.6 | 15.4 | 12.8 | 5.0 | 10.6 | 1.6 | 2.0 | 1.6 | 0.8 |
| Echinoderm plates | 4.4 | 5.8 | 7.0 | 8.0 | 4.4 | 8.8 | 6.0 | 5.8 | 3.2 | 4.6 |
| Intraclasts | 1.2 | 1.8 | 2.2 | 1.6 | 1.2 | 0.8 | 1.2 | 0.6 | 0.4 | 0.8 |
| Peloids | 3.6 | 2.4 | 1.6 | 2.4 | 0.6 | 1.4 | 0.6 | 0 | 0 | 0.2 |
| Micritic matrix | 10.6 | 7.0 | 1.4 | 26.6 | 0.4 | 6.8 | 3.4 | 2.2 | 0 | 1.2 |
| Syntaxial overgrowth cement | 0.4 | 0.8 | 2.0 | 1.2 | 1.8 | 2.2 | 2.6 | 2.0 | 0.6 | 0.4 |
| Isopachous calcite cement | 1.8 | 0.6 | 0.6 | 0.4 | 1.4 | 1.6 | 2.8 | 3.2 | 3.4 | 2.2 |
| Intergranular Non-Fe calcite cement | 5.6 | 7.0 | 5.2 | 4.0 | 12.2 | 8.4 | 10.2 | 13.6 | 16.2 | 14.8 |
| Intragranular Non-Fe calcite cement | 1.0 | 3.4 | 3.0 | 1.6 | 5.0 | 5.0 | 6.6 | 2.8 | 5.0 | 4.6 |
| Intergranular Fe-calcite cement | 15.2 | 15.2 | 11.6 | 8.4 | 14.6 | 9.6 | 7.0 | 5.2 | 4.6 | 5.0 |
| Intragranular Fe-calcite cement | 4.0 | 2.8 | 3.2 | 0.8 | 4.4 | 6.2 | 4.0 | 1.6 | 1.0 | 0.4 |
| Non-Fe dolomite cement | 4.6 | 6.4 | 0.8 | 0.4 | 0 | 0 | 0.6 | 0.6 | 0.6 | 0.4 |
| Coarse dolomite cement | 0 | 0 | 0 | 1.0 | 0 | 0 | 0.2 | 0 | 0 | 0 |
| Intergranular porosity | 1.8 | 0.6 | 0.4 | 0.6 | 0.6 | 0.6 | 2.4 | 3.0 | 3.2 | 8.0 |
| Intragranular porosity | 0.2 | 0.4 | 0.4 | 0.2 | 0.2 | 0.2 | 2.0 | 2.4 | 4.8 | 1.4 |
| Quartz | 0.6 | 0.2 | 0 | 0.2 | 0 | 0 | 0.2 | 0.4 | 0.4 | 0.4 |
| Clay minerals | 0.4 | 0 | 0 | 0.2 | 0 | 0.4 | 0 | 0.2 | 0 | 0 |
| Pyrite | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Coral plates | 1.0 | 1.4 | 3.4 | 2.2 | 2.6 | 3.0 | 2.6 | 2.8 | 1.0 | 0.6 |

| TVDSS (ft) | 4011.0 | 3992.0 | 3985.9 | 3966.0 | 3938.4 | 3927.8 | 3921.3 | 3918.0 | 3893.0 | 3891.0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Depth below top of the Gt. Oolite F. (ft) | 122.1 | 103.1 | 97.0 | 77.1 | 49.5 | 38.9 | 32.4 | 29.1 | 4.1 | 2.1 |
| Facies | I | I | I | I | IIa | I | I | I | IIa | IIa |
| Sample No. | ST-11 | ST-12 | ST-13 | ST-14 | ST-15 | ST-16 | ST-17 | ST-18 | ST-19 | ST-20 |
| Ooids | 38.8 | 49.0 | 27.8 | 34.0 | 17.2 | 38.8 | 49.6 | 46.4 | 5.8 | 9.2 |
| Bivalve shells | 3.4 | 1.0 | 7.4 | 5.2 | 15.4 | 5.0 | 3.2 | 2.1 | 18.8 | 19.6 |
| Brachiopod shells | 2.8 | 0.4 | 5.6 | 4.0 | 11.0 | 3.2 | 2.2 | 2.0 | 14.0 | 15.2 |
| Echinoderm plates | 1.4 | 5.0 | 5.2 | 2.8 | 6.8 | 5.6 | 1.8 | 6.2 | 7.8 | 6.2 |
| Intraclasts | 0.4 | 0.6 | 4.6 | 3.8 | 3.0 | 1.2 | 0.8 | 2.0 | 1.4 | 2.2 |
| Peloids | 0.4 | 0 | 5.6 | 20.6 | 2.8 | 3.8 | 0.4 | 0.4 | 4.8 | 3.6 |
| Micritic matrix | 1.6 | 0 | 2.2 | 6.6 | 5.8 | 2.0 | 0.2 | 0 | 10.4 | 6.2 |
| Syntaxial overgrowth cement | 0.8 | 0.8 | 4.0 | 0.6 | 3.2 | 1.8 | 0.6 | 1.0 | 2.2 | 2.8 |
| Isopachous calcite cement | 2.0 | 2.8 | 1.8 | 0.4 | 1.2 | 1.6 | 1.8 | 1.0 | 0.8 | 0.8 |
| Intergranular Non-Fe calcite cement | 18.4 | 12.0 | 11.2 | 5.6 | 7.2 | 8.6 | 7.4 | 7.8 | 4.0 | 5.6 |
| Intragranular Non-Fe calcite cement | 7.2 | 9.6 | 5.2 | 0.4 | 1.2 | 5.8 | 6.0 | 2.5 | 1.2 | 1.2 |
| Intergranular Fe-calcite cement | 8.0 | 10.4 | 10.0 | 5.4 | 10.4 | 11.0 | 16.2 | 15.4 | 8.8 | 11.4 |
| Intragranular Fe-calcite cement | 3.6 | 2.4 | 1.6 | 0.4 | 1.6 | 1.2 | 1.0 | 2.2 | 3.2 | 2.6 |
| Non-Fe dolomite cement | 0 | 0 | 0.6 | 1.0 | 3.2 | 0 | 0 | 2.0 | 4.4 | 3.0 |
| Coarse dolomite cement | 0 | 0 | 0 | 0 | 0.2 | 0 | 0 | 0 | 0.8 | 2.4 |
| Intergranular porosity | 9.2 | 5.2 | 4.6 | 4.6 | 5.0 | 5.8 | 6.6 | 4.0 | 4.2 | 0.8 |
| Intragranular porosity | 1.2 | 0.4 | 0.6 | 0.8 | 0.6 | 3.0 | 1.8 | 1.4 | 1.2 | 1.4 |
| Quartz | 0.2 | 0 | 0 | 0.6 | 0.2 | 0.4 | 0 | 0 | 0.8 | 0.6 |
| Clay minerals | 0 | 0 | 0 | 0.8 | 0.4 | 0 | 0 | 0 | 0.6 | 0.8 |
| Pyrite | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Coral plates | 0.6 | 0.4 | 2.0 | 2.4 | 3.6 | 1.2 | 0.4 | 3.6 | 4.8 | 4.4 |

APPENDIX 2 – Wireline log and water saturation data

Table A2.1: Neutron porosity, sonic transit time, bulk density, deep induction resistivity and gamma ray data for the Great Oolite Formation in the Singleton-1 well.

| TVDSS (ft) | N.PHI (p.u.) | SONIC T. (µsec/ft) | DENS. (g/cm3) | RESIS. (Ω.m-1) | GR (API) |
| --- | --- | --- | --- | --- | --- |
| 4218.1 | 0.17 | 66.50 | 2.58 | 13.37 | 25.56 |
| 4218.4 | 0.17 | 66.25 | 2.59 | 14.21 | 25.83 |
| 4218.7 | 0.15 | 65.38 | 2.58 | 16.19 | 24.39 |
| 4219.0 | 0.13 | 63.63 | 2.57 | 17.31 | 20.31 |
| 4219.4 | 0.11 | 63.00 | 2.57 | 17.26 | 18.30 |
| 4219.7 | 0.10 | 63.25 | 2.56 | 17.64 | 17.20 |
| 4220.0 | 0.10 | 64.38 | 2.55 | 18.96 | 14.51 |
| 4220.3 | 0.11 | 65.13 | 2.52 | 20.65 | 13.45 |
| 4220.6 | 0.11 | 65.75 | 2.51 | 22.83 | 12.59 |
| 4221.0 | 0.12 | 65.63 | 2.49 | 24.45 | 15.57 |
| 4221.3 | 0.13 | 66.00 | 2.49 | 25.52 | 14.74 |
| 4221.6 | 0.13 | 66.00 | 2.49 | 25.48 | 13.88 |
| 4221.9 | 0.13 | 66.63 | 2.50 | 24.45 | 11.73 |
| 4222.2 | 0.13 | 66.88 | 2.50 | 23.83 | 12.83 |
| 4222.5 | 0.13 | 66.75 | 2.50 | 23.05 | 13.23 |
| 4222.9 | 0.13 | 67.38 | 2.50 | 22.40 | 13.23 |
| 4223.2 | 0.13 | 66.13 | 2.51 | 21.53 | 14.48 |
| 4223.5 | 0.12 | 64.75 | 2.53 | 21.21 | 14.06 |
| 4223.8 | 0.11 | 63.88 | 2.53 | 21.54 | 15.49 |
| 4224.1 | 0.11 | 64.00 | 2.53 | 21.36 | 15.13 |
| 4224.5 | 0.12 | 65.63 | 2.52 | 20.97 | 16.00 |
| 4224.8 | 0.13 | 67.38 | 2.50 | 20.62 | 15.53 |
| 4225.1 | 0.14 | 68.63 | 2.49 | 20.04 | 13.04 |
| 4225.4 | 0.14 | 68.63 | 2.47 | 19.63 | 12.84 |
| 4225.7 | 0.14 | 67.88 | 2.48 | 19.27 | 12.59 |
| 4226.1 | 0.13 | 67.50 | 2.49 | 19.17 | 14.02 |
| 4226.4 | 0.13 | 66.75 | 2.49 | 18.52 | 13.63 |
| 4226.7 | 0.14 | 67.50 | 2.48 | 17.92 | 14.80 |
| 4227.0 | 0.14 | 67.13 | 2.48 | 17.12 | 14.15 |
| 4227.3 | 0.13 | 66.88 | 2.49 | 16.90 | 13.52 |
| 4227.6 | 0.13 | 66.50 | 2.52 | 16.67 | 12.58 |
| 4228.0 | 0.13 | 66.88 | 2.51 | 16.73 | 13.56 |
| 4228.3 | 0.14 | 67.75 | 2.51 | 16.85 | 15.30 |
| 4228.6 | 0.15 | 68.88 | 2.48 | 17.19 | 15.56 |
| 4228.9 | 0.14 | 67.75 | 2.48 | 17.60 | 15.59 |
| 4229.2 | 0.13 | 66.38 | 2.49 | 18.23 | 13.45 |
| 4229.6 | 0.12 | 66.00 | 2.53 | 18.82 | 11.63 |
| 4229.9 | 0.12 | 66.25 | 2.52 | 19.61 | 10.74 |
| 4230.2 | 0.12 | 67.00 | 2.49 | 19.78 | 11.36 |
| 4230.5 | 0.13 | 67.25 | 2.47 | 19.77 | 13.24 |
| 4230.8 | 0.12 | 66.00 | 2.47 | 20.82 | 13.75 |
| 4231.1 | 0.12 | 64.25 | 2.49 | 21.70 | 13.08 |
| 4231.5 | 0.11 | 64.13 | 2.50 | 22.35 | 12.44 |
| 4231.8 | 0.11 | 64.50 | 2.52 | 22.01 | 12.64 |
| 4232.1 | 0.12 | 66.50 | 2.54 | 21.62 | 14.22 |
| 4232.4 | 0.14 | 69.13 | 2.54 | 19.83 | 16.03 |
| 4232.7 | 0.16 | 71.63 | 2.51 | 17.90 | 17.70 |
| 4233.1 | 0.18 | 72.75 | 2.46 | 17.17 | 17.89 |
| 4233.4 | 0.18 | 72.88 | 2.43 | 16.82 | 15.98 |
| 4233.7 | 0.17 | 70.88 | 2.43 | 16.63 | 15.00 |
| 4234.0 | 0.17 | 68.50 | 2.46 | 15.97 | 13.83 |
| 4234.3 | 0.15 | 67.75 | 2.48 | 15.45 | 13.23 |
| 4234.6 | 0.14 | 66.50 | 2.51 | 15.42 | 11.55 |
| 4235.0 | 0.13 | 66.25 | 2.53 | 15.15 | 13.67 |
| 4235.3 | 0.13 | 67.00 | 2.54 | 15.34 | 14.45 |
| 4235.6 | 0.14 | 68.25 | 2.50 | 15.48 | 15.27 |
| 4235.9 | 0.14 | 68.13 | 2.48 | 15.83 | 15.09 |
| 4236.2 | 0.13 | 67.00 | 2.49 | 16.08 | 16.75 |
| 4236.6 | 0.13 | 66.38 | 2.50 | 16.02 | 15.88 |
| 4236.9 | 0.12 | 65.00 | 2.52 | 16.12 | 13.83 |
| 4237.2 | 0.12 | 64.25 | 2.51 | 16.84 | 12.24 |
| 4237.5 | 0.11 | 63.50 | 2.53 | 17.77 | 12.61 |
| 4237.8 | 0.11 | 64.13 | 2.52 | 18.25 | 13.39 |
| 4238.2 | 0.11 | 64.38 | 2.52 | 19.56 | 12.58 |
| 4238.5 | 0.11 | 64.38 | 2.51 | 19.67 | 14.59 |
| 4238.8 | 0.12 | 65.13 | 2.51 | 20.07 | 13.56 |
| 4239.1 | 0.12 | 64.50 | 2.51 | 20.57 | 13.80 |
| 4239.4 | 0.12 | 65.13 | 2.52 | 20.54 | 12.57 |
| 4239.7 | 0.12 | 65.38 | 2.51 | 20.60 | 13.41 |
| 4240.1 | 0.12 | 65.00 | 2.52 | 20.17 | 13.63 |
| 4240.4 | 0.12 | 66.25 | 2.52 | 19.62 | 12.91 |
| 4240.7 | 0.13 | 66.25 | 2.54 | 19.23 | 13.66 |
| 4241.0 | 0.13 | 67.13 | 2.55 | 18.27 | 14.52 |
| 4241.3 | 0.13 | 65.88 | 2.56 | 16.60 | 15.53 |
| 4241.7 | 0.12 | 66.63 | 2.57 | 14.85 | 15.96 |
| 4242.0 | 0.13 | 66.38 | 2.57 | 13.73 | 17.17 |
| 4242.3 | 0.13 | 66.13 | 2.57 | 12.29 | 19.39 |
| 4242.6 | 0.14 | 67.50 | 2.57 | 11.03 | 21.28 |
| 4242.9 | 0.15 | 67.75 | 2.57 | 9.92 | 23.92 |
| 4243.2 | 0.17 | 68.38 | 2.57 | 8.88 | 23.64 |
| 4243.6 | 0.17 | 68.75 | 2.57 | 8.56 | 25.56 |
| 4243.9 | 0.16 | 68.38 | 2.54 | 8.62 | 23.77 |
| 4244.2 | 0.14 | 68.13 | 2.51 | 8.76 | 22.52 |
| 4244.5 | 0.14 | 67.38 | 2.50 | 8.82 | 18.19 |
| 4244.8 | 0.14 | 66.75 | 2.51 | 9.11 | 17.03 |
| 4245.2 | 0.14 | 66.25 | 2.53 | 9.50 | 17.58 |
| 4245.5 | 0.13 | 66.13 | 2.56 | 10.22 | 19.09 |
| 4245.8 | 0.13 | 69.00 | 2.57 | 10.92 | 21.45 |
| 4246.1 | 0.14 | 69.50 | 2.57 | 11.50 | 23.92 |
| 4246.4 | 0.17 | 70.25 | 2.53 | 12.27 | 23.67 |
| 4246.7 | 0.18 | 70.63 | 2.49 | 13.01 | 21.41 |
| 4247.1 | 0.19 | 70.63 | 2.44 | 13.30 | 18.69 |
| 4247.4 | 0.18 | 69.63 | 2.43 | 13.62 | 17.59 |
| 4247.7 | 0.17 | 71.63 | 2.44 | 14.06 | 16.16 |
| 4248.0 | 0.16 | 71.00 | 2.44 | 14.95 | 15.79 |
| 4248.3 | 0.17 | 72.63 | 2.39 | 15.82 | 14.11 |
| 4248.7 | 0.19 | 73.25 | 2.35 | 16.53 | 12.48 |
| 4249.0 | 0.20 | 73.50 | 2.35 | 16.97 | 10.86 |
| 4249.3 | 0.20 | 77.75 | 2.36 | 17.07 | 10.80 |
| 4249.6 | 0.21 | 77.38 | 2.36 | 17.19 | 12.01 |
| 4249.9 | 0.22 | 78.38 | 2.34 | 17.23 | 12.02 |
| 4250.2 | 0.23 | 77.25 | 2.34 | 17.07 | 12.27 |
| 4250.6 | 0.22 | 75.88 | 2.36 | 17.03 | 12.81 |
| 4250.9 | 0.20 | 74.25 | 2.41 | 17.12 | 13.46 |
| 4251.2 | 0.18 | 72.38 | 2.44 | 17.13 | 14.48 |
| 4251.5 | 0.18 | 73.00 | 2.42 | 17.08 | 13.67 |
| 4251.8 | 0.18 | 73.00 | 2.41 | 17.14 | 12.84 |
| 4252.1 | 0.18 | 73.50 | 2.39 | 16.89 | 12.46 |
| 4252.5 | 0.19 | 72.38 | 2.38 | 16.94 | 12.38 |
| 4252.8 | 0.20 | 71.63 | 2.38 | 17.06 | 12.80 |
| 4253.1 | 0.19 | 69.88 | 2.40 | 17.18 | 12.59 |
| 4253.4 | 0.18 | 69.50 | 2.43 | 17.33 | 13.13 |
| 4253.7 | 0.16 | 69.50 | 2.45 | 17.51 | 13.20 |
| 4254.1 | 0.16 | 69.63 | 2.46 | 17.88 | 13.70 |
| 4254.4 | 0.15 | 69.25 | 2.46 | 18.05 | 14.30 |
| 4254.7 | 0.14 | 69.00 | 2.45 | 18.10 | 14.75 |
| 4255.0 | 0.15 | 68.38 | 2.46 | 18.45 | 14.96 |
| 4255.3 | 0.15 | 68.88 | 2.44 | 18.71 | 14.11 |
| 4255.6 | 0.16 | 70.13 | 2.43 | 18.79 | 14.25 |
| 4256.0 | 0.17 | 70.75 | 2.43 | 18.86 | 14.40 |
| 4256.3 | 0.17 | 70.88 | 2.44 | 18.92 | 15.04 |
| 4256.6 | 0.16 | 71.38 | 2.46 | 18.87 | 13.82 |
| 4256.9 | 0.15 | 70.13 | 2.48 | 18.91 | 12.75 |
| 4257.2 | 0.13 | 68.88 | 2.50 | 18.72 | 11.68 |
| 4257.5 | 0.13 | 66.75 | 2.50 | 18.77 | 12.55 |
| 4257.9 | 0.13 | 64.25 | 2.49 | 19.04 | 13.17 |
| 4258.2 | 0.13 | 64.00 | 2.48 | 19.30 | 15.34 |
| 4258.5 | 0.11 | 60.88 | 2.50 | 19.64 | 14.95 |
| 4258.8 | 0.10 | 61.50 | 2.52 | 20.10 | 15.76 |
| 4259.1 | 0.09 | 61.38 | 2.53 | 20.42 | 14.67 |
| 4259.4 | 0.09 | 61.00 | 2.55 | 20.38 | 16.36 |
| 4259.8 | 0.09 | 61.75 | 2.57 | 20.48 | 16.73 |
| 4260.1 | 0.09 | 63.38 | 2.59 | 20.48 | 17.80 |
| 4260.4 | 0.10 | 64.88 | 2.57 | 20.18 | 18.94 |
| 4260.7 | 0.11 | 66.38 | 2.53 | 20.39 | 17.78 |
| 4261.0 | 0.12 | 66.13 | 2.50 | 20.19 | 17.25 |
| 4261.3 | 0.13 | 65.38 | 2.50 | 19.92 | 14.70 |
| 4261.7 | 0.12 | 64.50 | 2.52 | 19.63 | 16.75 |
| 4262.0 | 0.12 | 63.13 | 2.53 | 19.43 | 16.47 |
| 4262.3 | 0.11 | 61.38 | 2.54 | 19.42 | 17.84 |
| 4262.6 | 0.10 | 60.25 | 2.55 | 19.30 | 17.86 |
| 4262.9 | 0.08 | 59.50 | 2.56 | 19.56 | 19.48 |
| 4263.2 | 0.08 | 59.25 | 2.57 | 19.88 | 18.50 |
| 4263.6 | 0.08 | 59.63 | 2.57 | 19.62 | 16.66 |
| 4263.9 | 0.07 | 59.25 | 2.58 | 19.21 | 16.75 |
| 4264.2 | 0.07 | 60.13 | 2.59 | 19.22 | 18.34 |
| 4264.5 | 0.07 | 60.13 | 2.61 | 18.86 | 19.44 |
| 4264.8 | 0.07 | 60.13 | 2.61 | 18.39 | 19.08 |
| 4265.1 | 0.08 | 60.63 | 2.63 | 17.84 | 21.70 |
| 4265.5 | 0.07 | 61.00 | 2.65 | 17.23 | 25.22 |
| 4265.8 | 0.07 | 60.75 | 2.66 | 16.42 | 26.95 |
| 4266.1 | 0.07 | 61.13 | 2.67 | 16.02 | 26.25 |
| 4266.4 | 0.08 | 62.00 | 2.65 | 15.90 | 24.31 |
| 4266.7 | 0.08 | 62.38 | 2.66 | 15.56 | 25.23 |
| 4267.0 | 0.08 | 62.88 | 2.65 | 15.11 | 26.27 |
| 4267.3 | 0.09 | 63.50 | 2.65 | 15.15 | 26.95 |
| 4267.7 | 0.09 | 62.63 | 2.63 | 15.25 | 27.34 |
| 4268.0 | 0.08 | 61.50 | 2.64 | 15.10 | 24.27 |
| 4268.3 | 0.07 | 60.00 | 2.66 | 15.05 | 25.13 |
| 4268.6 | 0.07 | 59.13 | 2.66 | 15.12 | 25.19 |
| 4268.9 | 0.07 | 58.88 | 2.67 | 15.29 | 27.50 |
| 4269.2 | 0.06 | 59.00 | 2.67 | 15.42 | 26.30 |
| 4269.6 | 0.06 | 58.13 | 2.67 | 15.75 | 24.02 |
| 4269.9 | 0.05 | 56.75 | 2.66 | 16.36 | 19.86 |
| 4270.2 | 0.05 | 57.00 | 2.66 | 17.07 | 17.47 |
| 4270.5 | 0.05 | 56.38 | 2.65 | 17.91 | 15.80 |
| 4270.8 | 0.05 | 56.75 | 2.64 | 18.46 | 15.99 |
| 4271.1 | 0.05 | 59.13 | 2.62 | 19.10 | 17.28 |
| 4271.5 | 0.06 | 60.50 | 2.62 | 20.13 | 17.48 |
| 4271.8 | 0.06 | 60.38 | 2.61 | 20.64 | 18.94 |
| 4272.1 | 0.06 | 61.38 | 2.62 | 20.85 | 20.67 |
| 4272.4 | 0.05 | 61.25 | 2.61 | 20.88 | 22.23 |
| 4272.7 | 0.06 | 60.75 | 2.61 | 20.69 | 23.58 |
| 4273.0 | 0.07 | 60.13 | 2.62 | 20.41 | 20.98 |
| 4273.3 | 0.08 | 61.00 | 2.61 | 20.00 | 20.69 |
| 4273.7 | 0.07 | 60.38 | 2.60 | 19.79 | 19.59 |
| 4274.0 | 0.07 | 60.13 | 2.59 | 19.42 | 19.38 |
| 4274.3 | 0.08 | 61.88 | 2.58 | 19.29 | 17.78 |
| 4274.6 | 0.09 | 63.00 | 2.58 | 19.55 | 17.63 |
| 4274.9 | 0.10 | 63.88 | 2.57 | 19.78 | 19.03 |
| 4275.2 | 0.11 | 64.63 | 2.56 | 20.18 | 20.53 |
| 4275.5 | 0.11 | 62.88 | 2.54 | 20.53 | 19.77 |
| 4275.9 | 0.10 | 62.75 | 2.55 | 21.22 | 19.13 |
| 4276.2 | 0.10 | 63.88 | 2.56 | 21.16 | 19.28 |
| 4276.5 | 0.10 | 64.25 | 2.56 | 21.55 | 21.14 |
| 4276.8 | 0.11 | 65.50 | 2.53 | 21.67 | 22.70 |
| 4277.1 | 0.13 | 67.88 | 2.50 | 22.33 | 22.44 |
| 4277.4 | 0.14 | 67.13 | 2.48 | 22.52 | 19.97 |
| 4277.7 | 0.14 | 64.63 | 2.47 | 22.77 | 19.00 |
| 4278.1 | 0.13 | 64.50 | 2.48 | 22.52 | 16.73 |
| 4278.4 | 0.12 | 65.00 | 2.50 | 22.71 | 16.38 |
| 4278.7 | 0.12 | 66.63 | 2.51 | 22.37 | 13.97 |
| 4279.0 | 0.13 | 67.25 | 2.49 | 22.37 | 12.46 |
| 4279.3 | 0.14 | 68.50 | 2.48 | 22.45 | 12.21 |
| 4279.6 | 0.14 | 68.50 | 2.48 | 22.77 | 13.65 |
| 4280.0 | 0.14 | 66.13 | 2.48 | 22.68 | 14.08 |
| 4280.3 | 0.14 | 65.50 | 2.47 | 22.78 | 14.28 |
| 4280.6 | 0.13 | 65.88 | 2.49 | 23.03 | 13.10 |
| 4280.9 | 0.12 | 66.75 | 2.51 | 22.79 | 13.04 |
| 4281.2 | 0.12 | 69.63 | 2.52 | 22.56 | 12.59 |
| 4281.5 | 0.14 | 70.50 | 2.48 | 22.38 | 12.18 |
| 4281.8 | 0.16 | 71.38 | 2.45 | 22.19 | 14.96 |
| 4282.1 | 0.17 | 72.63 | 2.42 | 21.89 | 17.16 |
| 4282.5 | 0.17 | 71.50 | 2.42 | 21.61 | 16.94 |
| 4282.8 | 0.18 | 71.50 | 2.43 | 21.37 | 15.32 |
| 4283.1 | 0.17 | 71.88 | 2.44 | 20.98 | 14.51 |
| 4283.4 | 0.17 | 69.63 | 2.43 | 20.05 | 15.31 |
| 4283.7 | 0.16 | 70.00 | 2.43 | 20.00 | 14.74 |
| 4284.0 | 0.17 | 70.75 | 2.43 | 19.96 | 12.92 |
| 4284.3 | 0.17 | 70.00 | 2.44 | 20.23 | 11.46 |
| 4284.7 | 0.17 | 71.13 | 2.45 | 20.46 | 10.19 |
| 4285.0 | 0.17 | 72.13 | 2.43 | 20.65 | 10.19 |
| 4285.3 | 0.18 | 73.25 | 2.42 | 21.08 | 11.34 |
| 4285.6 | 0.18 | 74.13 | 2.40 | 21.20 | 12.38 |
| 4285.9 | 0.18 | 75.00 | 2.39 | 21.61 | 13.02 |
| 4286.2 | 0.19 | 75.63 | 2.37 | 21.55 | 11.77 |
| 4286.5 | 0.19 | 77.63 | 2.39 | 21.80 | 11.31 |
| 4286.9 | 0.19 | 75.63 | 2.38 | 21.88 | 10.53 |
| 4287.2 | 0.19 | 73.38 | 2.38 | 21.71 | 10.98 |
| 4287.5 | 0.19 | 71.25 | 2.39 | 21.77 | 13.67 |
| 4287.8 | 0.16 | 69.13 | 2.43 | 21.79 | 13.65 |
| 4288.1 | 0.15 | 70.38 | 2.46 | 21.78 | 14.53 |
| 4288.4 | 0.15 | 70.75 | 2.46 | 21.40 | 14.02 |
| 4288.7 | 0.17 | 70.13 | 2.44 | 21.17 | 15.02 |
| 4289.0 | 0.18 | 70.63 | 2.42 | 21.40 | 15.68 |
| 4289.4 | 0.17 | 69.75 | 2.43 | 21.47 | 15.12 |
| 4289.7 | 0.16 | 69.00 | 2.45 | 21.32 | 15.14 |
| 4290.0 | 0.16 | 71.00 | 2.48 | 21.39 | 13.91 |
| 4290.3 | 0.16 | 72.38 | 2.46 | 20.83 | 13.54 |
| 4290.6 | 0.17 | 71.75 | 2.44 | 20.33 | 11.63 |
| 4290.9 | 0.18 | 73.00 | 2.41 | 19.94 | 11.19 |
| 4291.2 | 0.18 | 71.88 | 2.42 | 19.65 | 10.36 |
| 4291.6 | 0.17 | 70.38 | 2.41 | 19.50 | 12.38 |
| 4291.9 | 0.16 | 71.38 | 2.42 | 19.20 | 13.61 |
| 4292.2 | 0.16 | 71.00 | 2.42 | 18.63 | 14.09 |
| 4292.5 | 0.17 | 72.63 | 2.41 | 17.93 | 13.26 |
| 4292.8 | 0.17 | 73.63 | 2.41 | 17.42 | 11.56 |
| 4293.1 | 0.17 | 73.75 | 2.39 | 16.93 | 11.14 |
| 4293.4 | 0.18 | 74.63 | 2.40 | 16.31 | 10.38 |
| 4293.7 | 0.19 | 75.13 | 2.39 | 15.64 | 11.57 |
| 4294.1 | 0.19 | 75.25 | 2.40 | 15.18 | 11.34 |
| 4294.4 | 0.19 | 75.25 | 2.39 | 14.36 | 11.55 |
| 4294.7 | 0.20 | 75.13 | 2.40 | 13.72 | 11.54 |
| 4295.0 | 0.20 | 74.88 | 2.39 | 13.51 | 10.70 |
| 4295.3 | 0.20 | 76.13 | 2.39 | 13.06 | 10.77 |
| 4295.6 | 0.19 | 75.38 | 2.39 | 12.51 | 9.62 |
| 4295.9 | 0.18 | 75.50 | 2.39 | 12.15 | 10.69 |
| 4296.2 | 0.18 | 74.88 | 2.39 | 12.06 | 11.03 |
| 4296.6 | 0.19 | 74.50 | 2.40 | 11.82 | 11.33 |
| 4296.9 | 0.20 | 74.00 | 2.40 | 11.77 | 12.14 |
| 4297.2 | 0.19 | 73.50 | 2.40 | 11.73 | 12.59 |
| 4297.5 | 0.18 | 70.50 | 2.40 | 11.83 | 12.58 |
| 4297.8 | 0.16 | 69.38 | 2.42 | 12.15 | 11.21 |
| 4298.1 | 0.16 | 67.88 | 2.45 | 12.30 | 10.89 |
| 4298.4 | 0.14 | 66.63 | 2.47 | 12.56 | 11.17 |
| 4298.7 | 0.14 | 68.25 | 2.47 | 12.76 | 11.67 |
| 4299.1 | 0.14 | 68.75 | 2.46 | 13.06 | 12.29 |
| 4299.4 | 0.16 | 69.38 | 2.46 | 13.28 | 12.01 |
| 4299.7 | 0.17 | 69.38 | 2.47 | 13.46 | 12.81 |
| 4300.0 | 0.16 | 68.75 | 2.47 | 13.46 | 12.70 |
| 4300.3 | 0.15 | 68.50 | 2.48 | 13.34 | 12.98 |
| 4300.6 | 0.13 | 68.63 | 2.47 | 13.24 | 12.84 |
| 4300.9 | 0.14 | 69.50 | 2.47 | 13.03 | 13.20 |
| 4301.2 | 0.16 | 71.38 | 2.43 | 12.74 | 13.21 |
| 4301.5 | 0.17 | 73.38 | 2.40 | 12.37 | 12.87 |
| 4301.9 | 0.18 | 74.50 | 2.38 | 12.12 | 12.23 |
| 4302.2 | 0.19 | 75.13 | 2.38 | 11.70 | 12.37 |
| 4302.5 | 0.20 | 74.38 | 2.37 | 11.28 | 12.16 |
| 4302.8 | 0.19 | 73.25 | 2.38 | 11.04 | 11.69 |
| 4303.1 | 0.18 | 70.88 | 2.40 | 10.81 | 10.91 |
| 4303.4 | 0.18 | 71.00 | 2.42 | 10.56 | 11.53 |
| 4303.7 | 0.18 | 71.00 | 2.43 | 10.32 | 11.37 |
| 4304.0 | 0.18 | 72.00 | 2.42 | 10.28 | 11.72 |
| 4304.3 | 0.17 | 70.38 | 2.41 | 10.20 | 10.95 |
| 4304.7 | 0.16 | 70.63 | 2.42 | 10.14 | 10.63 |
| 4305.0 | 0.15 | 69.88 | 2.45 | 10.06 | 11.74 |
| 4305.3 | 0.14 | 70.38 | 2.47 | 9.85 | 13.32 |
| 4305.6 | 0.14 | 72.88 | 2.46 | 9.28 | 15.34 |
| 4305.9 | 0.17 | 75.75 | 2.40 | 8.74 | 16.13 |
| 4306.2 | 0.19 | 77.38 | 2.38 | 8.37 | 15.70 |
| 4306.5 | 0.21 | 77.38 | 2.37 | 8.02 | 16.44 |
| 4306.8 | 0.22 | 77.00 | 2.37 | 7.76 | 16.27 |
| 4307.1 | 0.22 | 77.00 | 2.37 | 7.56 | 16.81 |
| 4307.5 | 0.22 | 76.75 | 2.36 | 7.26 | 15.91 |
| 4307.8 | 0.21 | 75.00 | 2.35 | 7.05 | 15.41 |
| 4308.1 | 0.21 | 74.38 | 2.36 | 6.98 | 15.05 |
| 4308.4 | 0.20 | 73.88 | 2.37 | 6.96 | 14.39 |
| 4308.7 | 0.20 | 73.63 | 2.38 | 6.97 | 13.59 |
| 4309.0 | 0.20 | 74.25 | 2.38 | 7.01 | 12.19 |
| 4309.3 | 0.21 | 76.88 | 2.37 | 7.02 | 12.73 |
| 4309.6 | 0.22 | 76.88 | 2.37 | 7.12 | 13.15 |
| 4309.9 | 0.22 | 77.88 | 2.37 | 7.16 | 13.96 |
| 4310.3 | 0.21 | 78.00 | 2.36 | 7.16 | 12.44 |
| 4310.6 | 0.20 | 78.00 | 2.35 | 7.20 | 11.38 |
| 4310.9 | 0.20 | 76.38 | 2.37 | 7.22 | 11.59 |
| 4311.2 | 0.18 | 73.63 | 2.39 | 7.27 | 13.43 |
| 4311.5 | 0.17 | 71.88 | 2.43 | 7.28 | 14.72 |
| 4311.8 | 0.15 | 70.88 | 2.47 | 7.36 | 15.66 |
| 4312.1 | 0.14 | 67.50 | 2.49 | 7.39 | 16.61 |
| 4312.4 | 0.13 | 67.88 | 2.50 | 7.47 | 18.02 |
| 4312.7 | 0.13 | 68.38 | 2.50 | 7.48 | 19.88 |
| 4313.0 | 0.15 | 68.88 | 2.50 | 7.51 | 21.97 |
| 4313.4 | 0.15 | 70.25 | 2.49 | 7.57 | 23.28 |
| 4313.7 | 0.15 | 69.38 | 2.48 | 7.65 | 23.53 |
| 4314.0 | 0.15 | 69.88 | 2.47 | 7.64 | 23.56 |
| 4314.3 | 0.15 | 71.00 | 2.47 | 7.61 | 22.75 |
| 4314.6 | 0.16 | 72.88 | 2.46 | 7.53 | 22.27 |
| 4314.9 | 0.18 | 74.88 | 2.45 | 7.39 | 21.30 |
| 4315.2 | 0.20 | 78.25 | 2.41 | 7.22 | 20.44 |
| 4315.5 | 0.22 | 79.63 | 2.39 | 7.07 | 18.20 |
| 4315.8 | 0.23 | 79.50 | 2.36 | 6.91 | 16.50 |
| 4316.1 | 0.24 | 80.50 | 2.35 | 6.75 | 16.00 |
| 4316.5 | 0.23 | 80.00 | 2.33 | 6.57 | 16.03 |
| 4316.8 | 0.22 | 79.38 | 2.33 | 6.40 | 14.97 |
| 4317.1 | 0.21 | 79.25 | 2.34 | 6.23 | 13.95 |
| 4317.4 | 0.22 | 79.25 | 2.35 | 6.10 | 12.96 |
| 4317.7 | 0.22 | 78.88 | 2.36 | 6.03 | 12.13 |
| 4318.0 | 0.22 | 78.00 | 2.35 | 6.00 | 12.01 |
| 4318.3 | 0.22 | 76.38 | 2.36 | 6.02 | 12.01 |
| 4318.6 | 0.22 | 75.63 | 2.36 | 6.06 | 12.65 |
| 4318.9 | 0.21 | 74.00 | 2.38 | 6.10 | 13.09 |
| 4319.2 | 0.19 | 72.25 | 2.40 | 6.18 | 12.93 |
| 4319.5 | 0.19 | 70.88 | 2.43 | 6.25 | 12.47 |
| 4319.9 | 0.16 | 70.13 | 2.45 | 6.24 | 12.78 |
| 4320.2 | 0.15 | 71.25 | 2.47 | 6.21 | 12.72 |
| 4320.5 | 0.15 | 72.63 | 2.45 | 6.16 | 13.67 |
| 4320.8 | 0.16 | 73.88 | 2.44 | 6.01 | 13.24 |
| 4321.1 | 0.18 | 74.88 | 2.42 | 5.80 | 14.11 |
| 4321.4 | 0.18 | 75.13 | 2.42 | 5.62 | 14.70 |
| 4321.7 | 0.19 | 75.50 | 2.43 | 5.47 | 14.59 |
| 4322.0 | 0.19 | 76.25 | 2.43 | 5.29 | 15.15 |
| 4322.3 | 0.19 | 75.75 | 2.43 | 5.08 | 14.44 |
| 4322.6 | 0.19 | 74.13 | 2.44 | 4.83 | 14.30 |
| 4322.9 | 0.19 | 74.00 | 2.44 | 4.69 | 14.65 |
| 4323.3 | 0.18 | 73.38 | 2.46 | 4.63 | 15.04 |
| 4323.6 | 0.18 | 72.50 | 2.46 | 4.62 | 15.74 |
| 4323.9 | 0.17 | 72.75 | 2.46 | 4.69 | 14.45 |
| 4324.2 | 0.17 | 72.88 | 2.45 | 4.79 | 15.15 |
| 4324.5 | 0.17 | 73.38 | 2.45 | 4.89 | 15.89 |
| 4324.8 | 0.18 | 74.75 | 2.44 | 4.98 | 16.63 |
| 4325.1 | 0.19 | 75.75 | 2.43 | 5.11 | 15.08 |
| 4325.4 | 0.20 | 77.63 | 2.41 | 5.20 | 15.26 |
| 4325.7 | 0.21 | 77.88 | 2.40 | 5.31 | 15.10 |
| 4326.0 | 0.22 | 78.00 | 2.38 | 5.40 | 15.95 |
| 4326.3 | 0.21 | 77.75 | 2.38 | 5.41 | 15.49 |
| 4326.6 | 0.21 | 77.50 | 2.39 | 5.42 | 15.58 |
| 4327.0 | 0.21 | 77.63 | 2.39 | 5.40 | 15.77 |
| 4327.3 | 0.21 | 78.13 | 2.39 | 5.35 | 15.88 |
| 4327.6 | 0.21 | 78.25 | 2.40 | 5.30 | 15.51 |
| 4327.9 | 0.19 | 77.25 | 2.41 | 5.26 | 15.64 |
| 4328.2 | 0.19 | 75.38 | 2.43 | 5.25 | 15.84 |
| 4328.5 | 0.18 | 73.00 | 2.44 | 5.27 | 16.50 |
| 4328.8 | 0.18 | 71.38 | 2.46 | 5.31 | 15.37 |
| 4329.1 | 0.18 | 70.38 | 2.48 | 5.34 | 15.56 |
| 4329.4 | 0.18 | 69.13 | 2.50 | 5.40 | 17.30 |
| 4329.7 | 0.17 | 69.38 | 2.51 | 5.47 | 18.88 |
| 4330.0 | 0.16 | 69.50 | 2.50 | 5.56 | 19.53 |
| 4330.3 | 0.16 | 69.25 | 2.49 | 5.68 | 17.38 |
| 4330.6 | 0.16 | 69.13 | 2.50 | 5.80 | 17.78 |
| 4331.0 | 0.16 | 68.75 | 2.51 | 5.91 | 17.05 |
| 4331.3 | 0.17 | 71.00 | 2.52 | 6.11 | 17.61 |
| 4331.6 | 0.17 | 71.00 | 2.49 | 6.28 | 15.95 |
| 4331.9 | 0.17 | 71.63 | 2.46 | 6.44 | 15.02 |
| 4332.2 | 0.16 | 71.50 | 2.44 | 6.54 | 16.36 |
| 4332.5 | 0.16 | 70.13 | 2.47 | 6.66 | 16.33 |
| 4332.8 | 0.16 | 70.63 | 2.49 | 6.78 | 16.94 |
| 4333.1 | 0.16 | 69.88 | 2.50 | 6.93 | 15.38 |
| 4333.4 | 0.16 | 70.25 | 2.50 | 7.00 | 15.88 |
| 4333.7 | 0.16 | 71.25 | 2.50 | 7.09 | 16.00 |
| 4334.0 | 0.16 | 71.50 | 2.49 | 7.13 | 16.48 |
| 4334.3 | 0.17 | 71.50 | 2.47 | 7.17 | 17.50 |
| 4334.6 | 0.17 | 71.13 | 2.47 | 7.18 | 18.34 |
| 4334.9 | 0.17 | 71.38 | 2.46 | 7.25 | 18.00 |
| 4335.3 | 0.17 | 72.25 | 2.45 | 7.26 | 17.36 |
| 4335.6 | 0.18 | 73.00 | 2.43 | 7.23 | 16.81 |
| 4335.9 | 0.19 | 74.38 | 2.43 | 7.21 | 15.53 |
| 4336.2 | 0.19 | 74.75 | 2.42 | 7.19 | 14.25 |
| 4336.5 | 0.19 | 74.88 | 2.43 | 7.16 | 12.53 |
| 4336.8 | 0.18 | 74.25 | 2.43 | 7.19 | 12.36 |
| 4337.1 | 0.19 | 74.13 | 2.44 | 7.18 | 13.34 |
| 4337.4 | 0.18 | 73.13 | 2.45 | 7.16 | 14.48 |
| 4337.7 | 0.18 | 72.38 | 2.45 | 7.14 | 15.83 |
| 4338.0 | 0.17 | 72.88 | 2.45 | 7.08 | 15.37 |
| 4338.3 | 0.17 | 73.63 | 2.45 | 7.02 | 15.26 |
| 4338.6 | 0.18 | 74.00 | 2.45 | 6.96 | 14.46 |
| 4338.9 | 0.18 | 74.63 | 2.43 | 6.87 | 14.91 |
| 4339.2 | 0.18 | 74.00 | 2.42 | 6.75 | 14.64 |
| 4339.5 | 0.18 | 73.25 | 2.44 | 6.66 | 16.23 |
| 4339.8 | 0.19 | 74.00 | 2.44 | 6.50 | 17.13 |
| 4340.2 | 0.20 | 75.75 | 2.43 | 6.40 | 17.13 |
| 4340.5 | 0.20 | 74.75 | 2.42 | 6.28 | 16.00 |
| 4340.8 | 0.19 | 74.75 | 2.42 | 6.09 | 15.85 |
| 4341.1 | 0.18 | 74.13 | 2.42 | 6.00 | 16.69 |
| 4341.4 | 0.18 | 73.63 | 2.43 | 5.91 | 18.03 |
| 4341.7 | 0.20 | 72.88 | 2.43 | 5.84 | 16.89 |
| 4342.0 | 0.19 | 73.38 | 2.43 | 5.74 | 15.88 |
| 4342.3 | 0.19 | 72.25 | 2.42 | 5.69 | 15.15 |
| 4342.6 | 0.18 | 71.75 | 2.44 | 5.61 | 15.88 |
| 4342.9 | 0.17 | 71.50 | 2.47 | 5.51 | 16.09 |
| 4343.2 | 0.17 | 70.50 | 2.49 | 5.44 | 17.34 |
| 4343.5 | 0.17 | 70.75 | 2.50 | 5.34 | 17.05 |
| 4343.8 | 0.17 | 70.38 | 2.50 | 5.29 | 19.20 |
| 4344.1 | 0.17 | 70.38 | 2.49 | 5.26 | 18.19 |
| 4344.4 | 0.18 | 70.38 | 2.48 | 5.21 | 18.73 |
| 4344.7 | 0.18 | 70.00 | 2.49 | 5.18 | 17.66 |
| 4345.0 | 0.18 | 69.75 | 2.49 | 5.15 | 19.83 |
| 4345.4 | 0.18 | 69.63 | 2.49 | 5.15 | 20.05 |
| 4345.7 | 0.19 | 70.50 | 2.50 | 5.12 | 19.47 |
| 4346.0 | 0.18 | 70.75 | 2.50 | 5.10 | 18.08 |
| 4346.3 | 0.19 | 70.88 | 2.50 | 5.08 | 18.06 |
| 4346.6 | 0.19 | 72.00 | 2.48 | 5.07 | 20.25 |
| 4346.9 | 0.20 | 72.38 | 2.47 | 5.08 | 19.41 |
| 4347.2 | 0.19 | 72.75 | 2.44 | 5.08 | 20.70 |
| 4347.5 | 0.19 | 72.88 | 2.43 | 5.11 | 19.59 |
| 4347.8 | 0.20 | 72.00 | 2.44 | 5.15 | 20.94 |
| 4348.1 | 0.20 | 70.75 | 2.47 | 5.19 | 20.52 |
| 4348.4 | 0.21 | 69.25 | 2.49 | 5.29 | 20.34 |
| 4348.7 | 0.19 | 67.38 | 2.51 | 5.37 | 19.88 |
| 4349.0 | 0.18 | 65.63 | 2.53 | 5.53 | 18.23 |
| 4349.3 | 0.16 | 65.25 | 2.56 | 5.67 | 16.89 |
| 4349.6 | 0.16 | 66.50 | 2.56 | 5.80 | 16.05 |
| 4349.9 | 0.16 | 67.50 | 2.56 | 5.99 | 16.77 |
| 4350.2 | 0.16 | 67.38 | 2.53 | 6.19 | 17.84 |
| 4350.5 | 0.16 | 68.88 | 2.50 | 6.41 | 17.77 |
| 4350.8 | 0.17 | 68.63 | 2.48 | 6.60 | 18.08 |
| 4351.1 | 0.17 | 69.63 | 2.47 | 6.77 | 17.52 |
| 4351.4 | 0.17 | 70.75 | 2.46 | 6.87 | 15.92 |
| 4351.8 | 0.16 | 70.63 | 2.44 | 6.99 | 15.69 |
| 4352.1 | 0.16 | 70.75 | 2.43 | 7.15 | 15.79 |
| 4352.4 | 0.17 | 70.63 | 2.43 | 7.21 | 16.33 |
| 4352.7 | 0.18 | 69.75 | 2.44 | 7.30 | 14.47 |
| 4353.0 | 0.17 | 70.50 | 2.45 | 7.41 | 12.38 |
| 4353.3 | 0.17 | 70.25 | 2.46 | 7.39 | 12.51 |
| 4353.6 | 0.17 | 70.75 | 2.47 | 7.44 | 13.81 |
| 4353.9 | 0.18 | 71.88 | 2.47 | 7.50 | 14.57 |
| 4354.2 | 0.18 | 70.38 | 2.46 | 7.54 | 14.41 |
| 4354.5 | 0.17 | 70.00 | 2.45 | 7.57 | 14.45 |
| 4354.8 | 0.16 | 68.13 | 2.45 | 7.51 | 14.88 |
| 4355.1 | 0.15 | 67.63 | 2.46 | 7.51 | 14.71 |
| 4355.4 | 0.15 | 67.75 | 2.48 | 7.49 | 14.71 |
| 4355.7 | 0.15 | 68.13 | 2.49 | 7.46 | 14.29 |
| 4356.0 | 0.15 | 69.88 | 2.48 | 7.45 | 14.31 |
| 4356.3 | 0.15 | 69.88 | 2.47 | 7.37 | 14.16 |
| 4356.6 | 0.16 | 71.63 | 2.47 | 7.16 | 15.32 |
| 4356.9 | 0.16 | 72.25 | 2.46 | 6.97 | 16.70 |
| 4357.2 | 0.18 | 72.00 | 2.46 | 6.80 | 17.44 |
| 4357.5 | 0.18 | 72.75 | 2.45 | 6.65 | 17.14 |
| 4357.8 | 0.18 | 72.75 | 2.46 | 6.51 | 16.56 |
| 4358.1 | 0.17 | 73.25 | 2.46 | 6.32 | 14.79 |
| 4358.4 | 0.18 | 72.25 | 2.45 | 6.11 | 13.93 |
| 4358.7 | 0.19 | 70.88 | 2.43 | 6.02 | 13.27 |
| 4359.0 | 0.19 | 70.25 | 2.43 | 5.97 | 13.66 |
| 4359.3 | 0.18 | 69.38 | 2.44 | 5.96 | 13.95 |
| 4359.6 | 0.17 | 68.75 | 2.47 | 5.99 | 12.72 |
| 4360.0 | 0.16 | 68.00 | 2.48 | 6.06 | 11.31 |
| 4360.3 | 0.15 | 68.13 | 2.49 | 6.21 | 10.14 |
| 4360.6 | 0.14 | 68.38 | 2.49 | 6.36 | 12.36 |
| 4360.9 | 0.14 | 69.63 | 2.48 | 6.40 | 13.06 |
| 4361.2 | 0.15 | 69.75 | 2.48 | 6.43 | 15.34 |
| 4361.5 | 0.15 | 70.13 | 2.47 | 6.45 | 14.19 |
| 4361.8 | 0.15 | 70.75 | 2.47 | 6.41 | 14.63 |
| 4362.1 | 0.16 | 69.88 | 2.47 | 6.37 | 14.19 |
| 4362.4 | 0.17 | 70.63 | 2.48 | 6.31 | 14.55 |
| 4362.7 | 0.17 | 70.13 | 2.47 | 6.29 | 14.99 |
| 4363.0 | 0.17 | 69.75 | 2.46 | 6.33 | 14.84 |
| 4363.3 | 0.17 | 69.25 | 2.47 | 6.37 | 14.20 |
| 4363.6 | 0.16 | 69.25 | 2.47 | 6.42 | 14.11 |
| 4363.9 | 0.15 | 69.13 | 2.48 | 6.38 | 13.56 |
| 4364.2 | 0.15 | 69.25 | 2.48 | 6.36 | 13.43 |
| 4364.5 | 0.16 | 68.88 | 2.48 | 6.44 | 13.34 |
| 4364.8 | 0.17 | 68.38 | 2.48 | 6.49 | 13.24 |
| 4365.1 | 0.16 | 69.63 | 2.47 | 6.45 | 13.13 |
| 4365.4 | 0.16 | 70.50 | 2.48 | 6.42 | 13.20 |
| 4365.7 | 0.16 | 71.00 | 2.47 | 6.37 | 13.02 |
| 4366.0 | 0.16 | 71.13 | 2.46 | 6.27 | 13.29 |
| 4366.3 | 0.17 | 70.13 | 2.45 | 6.15 | 13.11 |
| 4366.6 | 0.17 | 69.38 | 2.45 | 6.04 | 13.54 |
| 4366.9 | 0.18 | 69.00 | 2.48 | 5.98 | 14.57 |
| 4367.2 | 0.17 | 70.00 | 2.48 | 5.82 | 16.44 |
| 4367.5 | 0.17 | 70.25 | 2.50 | 5.66 | 16.45 |
| 4367.8 | 0.17 | 70.25 | 2.50 | 5.53 | 17.05 |
| 4368.1 | 0.17 | 71.13 | 2.51 | 5.46 | 15.38 |
| 4368.4 | 0.17 | 71.00 | 2.50 | 5.35 | 14.63 |
| 4368.7 | 0.17 | 72.25 | 2.50 | 5.27 | 13.74 |
| 4369.0 | 0.17 | 72.25 | 2.48 | 5.25 | 13.33 |
| 4369.3 | 0.17 | 71.88 | 2.47 | 5.24 | 14.20 |
| 4369.6 | 0.17 | 71.50 | 2.48 | 5.24 | 14.06 |
| 4369.9 | 0.17 | 71.13 | 2.49 | 5.27 | 13.81 |
| 4370.2 | 0.17 | 70.63 | 2.49 | 5.29 | 14.16 |
| 4370.5 | 0.17 | 69.50 | 2.47 | 5.30 | 15.19 |
| 4370.9 | 0.17 | 69.13 | 2.47 | 5.30 | 17.33 |
| 4371.2 | 0.16 | 70.25 | 2.50 | 5.33 | 18.34 |
| 4371.5 | 0.17 | 71.38 | 2.51 | 5.34 | 16.98 |
| 4371.8 | 0.17 | 71.38 | 2.49 | 5.36 | 16.38 |
| 4372.1 | 0.18 | 71.75 | 2.46 | 5.34 | 16.05 |
| 4372.4 | 0.17 | 71.63 | 2.46 | 5.31 | 17.17 |
| 4372.7 | 0.17 | 70.63 | 2.47 | 5.31 | 17.56 |
| 4373.0 | 0.17 | 71.50 | 2.47 | 5.35 | 17.89 |
| 4373.3 | 0.18 | 71.13 | 2.47 | 5.41 | 18.64 |
| 4373.6 | 0.18 | 72.50 | 2.46 | 5.48 | 17.64 |
| 4373.9 | 0.18 | 72.25 | 2.47 | 5.50 | 16.89 |
| 4374.2 | 0.17 | 72.88 | 2.46 | 5.46 | 16.20 |
| 4374.5 | 0.17 | 74.38 | 2.46 | 5.43 | 16.22 |
| 4374.8 | 0.17 | 72.63 | 2.45 | 5.39 | 16.25 |
| 4375.1 | 0.18 | 73.50 | 2.44 | 5.40 | 15.91 |
| 4375.4 | 0.18 | 72.75 | 2.44 | 5.42 | 16.25 |
| 4375.7 | 0.17 | 72.25 | 2.45 | 5.43 | 15.27 |
| 4376.0 | 0.17 | 71.63 | 2.47 | 5.40 | 14.41 |
| 4376.3 | 0.17 | 71.63 | 2.47 | 5.39 | 15.09 |
| 4376.6 | 0.17 | 70.38 | 2.46 | 5.35 | 15.05 |
| 4376.9 | 0.17 | 71.38 | 2.46 | 5.33 | 15.60 |
| 4377.2 | 0.17 | 71.00 | 2.47 | 5.32 | 14.08 |
| 4377.5 | 0.18 | 71.38 | 2.48 | 5.29 | 13.93 |
| 4377.8 | 0.18 | 72.38 | 2.47 | 5.28 | 14.07 |
| 4378.1 | 0.17 | 71.63 | 2.46 | 5.25 | 15.59 |
| 4378.4 | 0.16 | 71.13 | 2.45 | 5.16 | 17.09 |
| 4378.7 | 0.17 | 71.38 | 2.46 | 5.11 | 17.22 |
| 4379.0 | 0.17 | 71.25 | 2.46 | 5.11 | 16.34 |
| 4379.3 | 0.17 | 72.00 | 2.47 | 5.11 | 16.38 |
| 4379.6 | 0.18 | 71.63 | 2.49 | 5.13 | 16.94 |
| 4379.9 | 0.17 | 70.13 | 2.48 | 5.14 | 16.33 |
| 4380.2 | 0.17 | 71.13 | 2.46 | 5.15 | 15.46 |
| 4380.5 | 0.16 | 70.75 | 2.45 | 5.14 | 13.02 |
| 4380.8 | 0.16 | 71.63 | 2.45 | 5.12 | 14.23 |
| 4381.1 | 0.17 | 71.63 | 2.45 | 5.05 | 14.59 |
| 4381.4 | 0.17 | 71.75 | 2.46 | 4.95 | 17.03 |
| 4381.7 | 0.16 | 71.50 | 2.48 | 4.89 | 16.58 |
| 4382.0 | 0.17 | 71.13 | 2.49 | 4.84 | 17.56 |
| 4382.3 | 0.17 | 71.13 | 2.49 | 4.81 | 16.53 |
| 4382.6 | 0.18 | 71.00 | 2.48 | 4.76 | 17.34 |
| 4382.9 | 0.17 | 70.25 | 2.49 | 4.69 | 16.98 |
| 4383.2 | 0.16 | 70.00 | 2.49 | 4.64 | 18.33 |
| 4383.5 | 0.16 | 70.00 | 2.50 | 4.62 | 17.77 |
| 4383.8 | 0.16 | 69.63 | 2.50 | 4.65 | 17.05 |
| 4384.1 | 0.16 | 69.50 | 2.50 | 4.69 | 16.41 |
| 4384.4 | 0.16 | 70.38 | 2.50 | 4.69 | 16.03 |
| 4384.7 | 0.16 | 70.63 | 2.50 | 4.68 | 16.75 |
| 4385.1 | 0.15 | 70.75 | 2.49 | 4.69 | 15.40 |
| 4385.4 | 0.15 | 69.50 | 2.48 | 4.73 | 15.43 |
| 4385.7 | 0.16 | 68.38 | 2.48 | 4.74 | 15.52 |
| 4386.0 | 0.16 | 69.25 | 2.47 | 4.81 | 17.09 |
| 4386.3 | 0.15 | 68.38 | 2.47 | 4.90 | 17.14 |
| 4386.6 | 0.16 | 68.75 | 2.47 | 4.95 | 16.33 |
| 4386.9 | 0.16 | 68.50 | 2.48 | 5.02 | 17.25 |
| 4387.2 | 0.16 | 67.13 | 2.47 | 5.18 | 17.77 |
| 4387.5 | 0.14 | 65.88 | 2.47 | 5.34 | 17.84 |
| 4387.8 | 0.14 | 65.50 | 2.49 | 5.46 | 15.90 |
| 4388.1 | 0.13 | 65.75 | 2.53 | 5.59 | 16.59 |
| 4388.4 | 0.13 | 66.13 | 2.54 | 5.69 | 16.42 |
| 4388.7 | 0.14 | 67.38 | 2.53 | 5.80 | 16.53 |
| 4389.0 | 0.15 | 68.00 | 2.51 | 5.88 | 15.61 |
| 4389.3 | 0.15 | 67.88 | 2.49 | 5.90 | 16.64 |
| 4389.6 | 0.15 | 67.38 | 2.50 | 5.93 | 16.98 |
| 4389.9 | 0.14 | 67.38 | 2.50 | 5.92 | 16.97 |
| 4390.2 | 0.15 | 66.88 | 2.50 | 5.99 | 15.63 |
| 4390.5 | 0.15 | 66.63 | 2.49 | 6.20 | 15.60 |
| 4390.8 | 0.15 | 65.50 | 2.50 | 6.39 | 15.27 |
| 4391.1 | 0.13 | 63.75 | 2.52 | 6.67 | 15.65 |
| 4391.4 | 0.13 | 62.63 | 2.54 | 7.02 | 15.97 |
| 4391.7 | 0.12 | 60.25 | 2.54 | 7.60 | 15.95 |
| 4392.0 | 0.11 | 59.25 | 2.56 | 8.12 | 16.08 |
| 4392.3 | 0.10 | 57.75 | 2.58 | 8.70 | 16.95 |

Table A2.2: Neutron porosity, sonic transit time, bulk density, deep induction resistivity and gamma ray data for the Great Oolite Formation in the Horndean-1A well.

| TVDSS (ft) | N.PHI (p.u.) | SONIC T. (µsec/ft) | DENS. (g/cm3) | RESIS. (Ω.m-1) | GR (API) |
| --- | --- | --- | --- | --- | --- |
| 4232.4 | 0.15 | 68.38 | 2.53 | 10.19 | 22.58 |
| 4232.9 | 0.17 | 70.38 | 2.54 | 10.42 | 20.03 |
| 4233.4 | 0.17 | 72.75 | 2.52 | 10.34 | 11.71 |
| 4233.9 | 0.17 | 73.00 | 2.49 | 10.48 | 9.82 |
| 4234.4 | 0.17 | 74.75 | 2.44 | 11.17 | 8.57 |
| 4234.9 | 0.17 | 74.00 | 2.43 | 12.51 | 10.43 |
| 4235.4 | 0.17 | 73.19 | 2.43 | 13.65 | 10.08 |
| 4235.9 | 0.18 | 72.56 | 2.45 | 14.31 | 12.91 |
| 4236.4 | 0.18 | 72.19 | 2.44 | 14.48 | 13.34 |
| 4236.9 | 0.17 | 72.00 | 2.45 | 14.44 | 13.98 |
| 4237.4 | 0.16 | 72.38 | 2.44 | 14.32 | 13.04 |
| 4237.9 | 0.16 | 71.38 | 2.45 | 14.62 | 11.05 |
| 4238.4 | 0.16 | 72.00 | 2.45 | 15.11 | 10.70 |
| 4238.9 | 0.16 | 71.19 | 2.45 | 15.41 | 10.34 |
| 4239.4 | 0.16 | 71.75 | 2.45 | 15.63 | 10.97 |
| 4239.9 | 0.16 | 71.19 | 2.47 | 16.03 | 10.69 |
| 4240.4 | 0.17 | 71.56 | 2.49 | 16.19 | 9.77 |
| 4240.9 | 0.17 | 71.56 | 2.49 | 16.05 | 10.08 |
| 4241.4 | 0.18 | 71.19 | 2.47 | 16.02 | 10.40 |
| 4241.9 | 0.18 | 71.56 | 2.47 | 16.23 | 11.43 |
| 4242.4 | 0.17 | 72.19 | 2.46 | 15.69 | 10.83 |
| 4242.9 | 0.17 | 72.19 | 2.45 | 14.09 | 10.21 |
| 4243.4 | 0.17 | 71.56 | 2.43 | 11.67 | 9.20 |
| 4243.9 | 0.16 | 71.38 | 2.45 | 9.65 | 12.34 |
| 4244.4 | 0.16 | 69.75 | 2.47 | 8.16 | 14.52 |
| 4244.9 | 0.15 | 69.38 | 2.51 | 6.90 | 15.74 |
| 4245.4 | 0.15 | 69.00 | 2.52 | 5.97 | 14.52 |
| 4245.9 | 0.15 | 69.56 | 2.52 | 5.51 | 13.58 |
| 4246.4 | 0.16 | 70.38 | 2.52 | 5.22 | 13.27 |
| 4246.9 | 0.17 | 70.56 | 2.50 | 5.06 | 13.24 |
| 4247.4 | 0.16 | 70.56 | 2.49 | 4.97 | 11.42 |
| 4247.9 | 0.17 | 70.56 | 2.47 | 5.01 | 11.14 |
| 4248.4 | 0.17 | 71.56 | 2.47 | 5.26 | 11.52 |
| 4248.9 | 0.17 | 72.00 | 2.45 | 5.72 | 14.04 |
| 4249.4 | 0.16 | 72.00 | 2.44 | 6.25 | 14.62 |
| 4249.9 | 0.15 | 71.19 | 2.44 | 6.99 | 13.27 |
| 4250.4 | 0.15 | 70.75 | 2.44 | 7.81 | 12.23 |
| 4250.9 | 0.15 | 71.00 | 2.45 | 8.53 | 11.92 |
| 4251.4 | 0.15 | 71.38 | 2.46 | 9.10 | 11.93 |
| 4251.9 | 0.15 | 73.38 | 2.46 | 9.97 | 10.68 |
| 4252.4 | 0.16 | 73.38 | 2.45 | 10.82 | 10.02 |
| 4252.9 | 0.16 | 72.00 | 2.43 | 11.94 | 9.78 |
| 4253.4 | 0.15 | 71.19 | 2.44 | 13.25 | 11.73 |
| 4253.9 | 0.13 | 71.19 | 2.46 | 14.54 | 11.80 |
| 4254.4 | 0.13 | 71.19 | 2.47 | 15.26 | 11.75 |
| 4254.9 | 0.14 | 72.38 | 2.49 | 15.09 | 10.78 |
| 4255.4 | 0.15 | 72.38 | 2.50 | 15.34 | 12.34 |
| 4255.9 | 0.14 | 70.19 | 2.52 | 16.06 | 14.90 |
| 4256.4 | 0.12 | 68.00 | 2.51 | 16.41 | 15.84 |
| 4256.9 | 0.12 | 66.19 | 2.51 | 16.52 | 15.82 |
| 4257.4 | 0.10 | 63.38 | 2.52 | 16.77 | 15.79 |
| 4257.9 | 0.08 | 60.78 | 2.56 | 16.73 | 15.73 |
| 4258.4 | 0.06 | 59.59 | 2.58 | 16.33 | 15.19 |
| 4258.9 | 0.05 | 58.38 | 2.59 | 16.05 | 15.22 |
| 4259.4 | 0.04 | 59.38 | 2.60 | 15.97 | 14.98 |
| 4259.9 | 0.05 | 60.00 | 2.58 | 15.82 | 16.73 |
| 4260.4 | 0.07 | 62.00 | 2.57 | 15.56 | 16.84 |
| 4260.9 | 0.09 | 63.00 | 2.55 | 14.28 | 18.69 |
| 4261.4 | 0.09 | 63.59 | 2.55 | 13.16 | 17.78 |
| 4261.9 | 0.09 | 64.19 | 2.55 | 12.14 | 16.38 |
| 4262.4 | 0.09 | 65.38 | 2.55 | 11.63 | 13.88 |
| 4262.9 | 0.10 | 67.56 | 2.52 | 11.27 | 13.30 |
| 4263.4 | 0.12 | 68.56 | 2.49 | 10.98 | 13.33 |
| 4263.9 | 0.13 | 69.38 | 2.45 | 10.41 | 15.93 |
| 4264.4 | 0.14 | 70.19 | 2.45 | 10.05 | 16.88 |
| 4264.9 | 0.14 | 69.75 | 2.45 | 9.91 | 16.86 |
| 4265.4 | 0.14 | 70.19 | 2.47 | 10.05 | 15.23 |
| 4265.9 | 0.14 | 69.75 | 2.47 | 10.46 | 15.19 |
| 4266.4 | 0.13 | 67.75 | 2.49 | 11.05 | 17.03 |
| 4266.9 | 0.12 | 66.19 | 2.50 | 11.55 | 17.61 |
| 4267.4 | 0.11 | 64.56 | 2.52 | 12.21 | 17.27 |
| 4267.9 | 0.10 | 63.00 | 2.51 | 12.64 | 16.31 |
| 4268.4 | 0.08 | 62.38 | 2.52 | 12.96 | 16.05 |
| 4268.9 | 0.08 | 61.38 | 2.53 | 13.13 | 16.39 |
| 4269.4 | 0.08 | 61.00 | 2.55 | 12.87 | 16.52 |
| 4269.9 | 0.08 | 60.78 | 2.55 | 12.69 | 18.95 |
| 4270.4 | 0.08 | 61.19 | 2.57 | 12.74 | 18.89 |
| 4270.9 | 0.08 | 63.00 | 2.58 | 12.90 | 20.59 |
| 4271.4 | 0.09 | 62.19 | 2.57 | 12.77 | 18.66 |
| 4271.9 | 0.10 | 61.59 | 2.56 | 12.04 | 17.95 |
| 4272.4 | 0.08 | 59.38 | 2.57 | 10.64 | 13.56 |
| 4272.9 | 0.07 | 60.00 | 2.58 | 9.36 | 11.40 |
| 4273.4 | 0.07 | 63.00 | 2.58 | 8.45 | 12.97 |
| 4273.9 | 0.09 | 67.38 | 2.52 | 7.84 | 16.06 |
| 4274.4 | 0.14 | 73.38 | 2.46 | 7.24 | 19.11 |
| 4274.9 | 0.18 | 75.38 | 2.41 | 6.66 | 17.28 |
| 4275.4 | 0.20 | 75.38 | 2.39 | 5.95 | 15.16 |
| 4275.9 | 0.18 | 73.75 | 2.40 | 5.54 | 13.73 |
| 4276.4 | 0.17 | 74.38 | 2.42 | 5.35 | 14.06 |
| 4276.9 | 0.17 | 74.19 | 2.42 | 5.43 | 14.96 |
| 4277.4 | 0.18 | 74.56 | 2.42 | 5.62 | 13.70 |
| 4277.9 | 0.19 | 73.75 | 2.42 | 5.91 | 14.02 |
| 4278.4 | 0.17 | 72.19 | 2.42 | 6.27 | 13.70 |
| 4278.9 | 0.15 | 70.56 | 2.45 | 6.57 | 13.97 |
| 4279.4 | 0.15 | 68.56 | 2.45 | 6.88 | 13.58 |
| 4279.9 | 0.15 | 69.75 | 2.48 | 7.36 | 12.90 |
| 4280.4 | 0.16 | 70.00 | 2.46 | 7.83 | 13.86 |
| 4280.9 | 0.16 | 70.00 | 2.46 | 8.29 | 12.99 |
| 4281.4 | 0.17 | 71.56 | 2.44 | 8.46 | 14.30 |
| 4281.9 | 0.18 | 71.56 | 2.46 | 8.47 | 13.34 |
| 4282.4 | 0.19 | 72.19 | 2.45 | 8.41 | 15.16 |
| 4282.9 | 0.19 | 71.75 | 2.42 | 8.52 | 13.59 |
| 4283.4 | 0.19 | 71.38 | 2.39 | 8.81 | 14.20 |
| 4283.9 | 0.17 | 71.19 | 2.40 | 9.22 | 13.59 |
| 4284.4 | 0.17 | 71.00 | 2.41 | 9.73 | 14.23 |
| 4284.9 | 0.18 | 69.38 | 2.42 | 10.13 | 13.60 |
| 4285.4 | 0.17 | 67.75 | 2.45 | 10.52 | 12.30 |
| 4285.9 | 0.15 | 66.19 | 2.47 | 10.85 | 11.41 |
| 4286.4 | 0.13 | 65.38 | 2.50 | 11.14 | 11.47 |
| 4286.9 | 0.13 | 67.19 | 2.48 | 11.40 | 11.55 |
| 4287.4 | 0.14 | 69.00 | 2.47 | 11.42 | 12.46 |
| 4287.9 | 0.17 | 68.75 | 2.45 | 11.38 | 12.42 |
| 4288.4 | 0.19 | 70.75 | 2.44 | 11.13 | 13.02 |
| 4288.9 | 0.19 | 71.00 | 2.42 | 10.95 | 12.38 |
| 4289.4 | 0.17 | 70.38 | 2.42 | 10.84 | 11.47 |
| 4289.9 | 0.16 | 71.00 | 2.45 | 10.81 | 11.16 |
| 4290.4 | 0.17 | 71.38 | 2.46 | 11.12 | 10.54 |
| 4290.9 | 0.19 | 71.56 | 2.46 | 11.56 | 10.77 |
| 4291.4 | 0.19 | 72.56 | 2.41 | 11.95 | 9.91 |
| 4291.9 | 0.19 | 71.75 | 2.40 | 12.48 | 12.17 |
| 4292.4 | 0.19 | 72.38 | 2.40 | 12.85 | 12.58 |
| 4292.9 | 0.20 | 73.38 | 2.42 | 13.07 | 13.13 |
| 4293.4 | 0.20 | 73.56 | 2.40 | 13.27 | 11.45 |
| 4293.9 | 0.20 | 73.38 | 2.40 | 13.30 | 10.49 |
| 4294.4 | 0.19 | 73.38 | 2.38 | 13.51 | 9.84 |
| 4294.9 | 0.19 | 72.75 | 2.40 | 13.72 | 9.85 |
| 4295.4 | 0.18 | 72.38 | 2.40 | 13.72 | 12.32 |
| 4295.9 | 0.18 | 72.19 | 2.42 | 13.66 | 12.63 |
| 4296.4 | 0.18 | 71.75 | 2.42 | 13.82 | 13.77 |
| 4296.9 | 0.17 | 71.75 | 2.41 | 13.88 | 12.65 |
| 4297.4 | 0.17 | 71.75 | 2.40 | 13.98 | 11.77 |
| 4297.9 | 0.17 | 71.38 | 2.40 | 14.48 | 11.91 |
| 4298.4 | 0.16 | 71.75 | 2.41 | 14.75 | 13.09 |
| 4298.9 | 0.16 | 72.00 | 2.42 | 15.34 | 13.06 |
| 4299.4 | 0.16 | 71.75 | 2.42 | 15.80 | 12.09 |
| 4299.9 | 0.15 | 72.19 | 2.41 | 16.48 | 11.45 |
| 4300.4 | 0.16 | 72.19 | 2.41 | 17.39 | 12.99 |
| 4300.9 | 0.17 | 72.00 | 2.40 | 17.86 | 13.00 |
| 4301.4 | 0.17 | 72.56 | 2.41 | 18.63 | 12.38 |
| 4301.9 | 0.17 | 71.38 | 2.40 | 19.30 | 12.93 |
| 4302.4 | 0.16 | 71.00 | 2.41 | 20.19 | 11.10 |
| 4302.9 | 0.15 | 71.75 | 2.43 | 20.56 | 11.45 |
| 4303.4 | 0.15 | 71.56 | 2.43 | 21.53 | 9.69 |
| 4303.9 | 0.16 | 72.00 | 2.43 | 22.50 | 11.21 |
| 4304.4 | 0.16 | 72.56 | 2.41 | 23.41 | 11.16 |
| 4304.9 | 0.17 | 72.38 | 2.42 | 23.72 | 10.52 |
| 4305.4 | 0.16 | 72.38 | 2.42 | 24.58 | 9.28 |
| 4305.9 | 0.15 | 72.38 | 2.43 | 23.78 | 7.74 |
| 4306.4 | 0.15 | 72.56 | 2.43 | 23.34 | 8.38 |
| 4306.9 | 0.14 | 72.19 | 2.43 | 22.36 | 8.98 |
| 4307.4 | 0.15 | 72.19 | 2.41 | 22.31 | 9.56 |
| 4307.9 | 0.16 | 71.56 | 2.41 | 21.59 | 9.25 |
| 4308.4 | 0.16 | 71.56 | 2.42 | 21.30 | 8.06 |
| 4308.9 | 0.15 | 71.19 | 2.45 | 20.97 | 9.96 |
| 4309.4 | 0.15 | 71.38 | 2.45 | 20.86 | 9.31 |
| 4309.9 | 0.15 | 71.56 | 2.44 | 20.56 | 11.74 |
| 4310.4 | 0.16 | 72.38 | 2.41 | 20.48 | 10.77 |
| 4310.9 | 0.15 | 72.00 | 2.43 | 20.38 | 12.32 |
| 4311.4 | 0.14 | 71.38 | 2.44 | 20.14 | 10.18 |
| 4311.9 | 0.14 | 71.38 | 2.45 | 19.80 | 8.65 |
| 4312.4 | 0.15 | 71.19 | 2.44 | 19.27 | 8.00 |
| 4312.9 | 0.15 | 71.56 | 2.45 | 18.98 | 7.70 |
| 4313.4 | 0.16 | 72.38 | 2.44 | 18.94 | 8.04 |
| 4313.9 | 0.16 | 72.56 | 2.43 | 19.16 | 8.10 |
| 4314.4 | 0.17 | 72.38 | 2.40 | 19.69 | 12.14 |
| 4314.9 | 0.16 | 72.75 | 2.40 | 20.50 | 11.80 |
| 4315.4 | 0.16 | 72.38 | 2.40 | 20.89 | 13.28 |
| 4315.9 | 0.16 | 72.56 | 2.40 | 21.22 | 10.48 |
| 4316.4 | 0.16 | 73.38 | 2.41 | 21.66 | 11.39 |
| 4316.9 | 0.16 | 73.19 | 2.41 | 21.70 | 9.57 |
| 4317.4 | 0.17 | 73.38 | 2.43 | 21.58 | 11.42 |
| 4317.9 | 0.17 | 73.00 | 2.40 | 21.56 | 10.17 |
| 4318.4 | 0.16 | 72.19 | 2.40 | 21.92 | 10.82 |
| 4318.9 | 0.16 | 72.19 | 2.40 | 22.33 | 8.99 |
| 4319.4 | 0.15 | 71.19 | 2.41 | 22.70 | 9.67 |
| 4319.9 | 0.15 | 71.00 | 2.44 | 23.19 | 10.31 |
| 4320.4 | 0.15 | 70.38 | 2.47 | 22.27 | 10.94 |
| 4320.9 | 0.15 | 69.75 | 2.48 | 19.81 | 10.30 |
| 4321.4 | 0.15 | 68.00 | 2.47 | 16.48 | 10.55 |
| 4321.9 | 0.12 | 66.19 | 2.49 | 12.74 | 11.13 |
| 4322.4 | 0.10 | 65.38 | 2.52 | 10.08 | 15.73 |
| 4322.9 | 0.09 | 67.00 | 2.53 | 8.55 | 20.95 |
| 4323.4 | 0.13 | 68.56 | 2.53 | 7.49 | 26.33 |
| 4323.9 | 0.16 | 69.75 | 2.51 | 6.49 | 29.25 |
| 4324.4 | 0.17 | 70.00 | 2.50 | 5.48 | 26.53 |
| 4324.9 | 0.16 | 69.00 | 2.49 | 4.74 | 22.11 |
| 4325.4 | 0.15 | 69.00 | 2.50 | 4.17 | 18.31 |
| 4325.9 | 0.15 | 69.56 | 2.50 | 3.88 | 16.72 |
| 4326.4 | 0.15 | 69.75 | 2.48 | 3.69 | 17.61 |
| 4326.9 | 0.15 | 70.19 | 2.47 | 3.47 | 17.25 |
| 4327.4 | 0.17 | 70.75 | 2.47 | 3.31 | 16.34 |
| 4327.9 | 0.18 | 71.38 | 2.48 | 3.23 | 16.06 |
| 4328.4 | 0.19 | 71.56 | 2.48 | 3.22 | 16.06 |
| 4328.9 | 0.19 | 71.75 | 2.47 | 3.30 | 17.81 |
| 4329.4 | 0.19 | 72.38 | 2.43 | 3.49 | 16.95 |
| 4329.9 | 0.20 | 72.56 | 2.43 | 3.74 | 16.38 |
| 4330.4 | 0.19 | 72.38 | 2.43 | 4.07 | 14.96 |
| 4330.9 | 0.18 | 71.00 | 2.46 | 4.45 | 16.48 |
| 4331.4 | 0.18 | 69.75 | 2.46 | 4.91 | 16.78 |
| 4331.9 | 0.17 | 69.38 | 2.43 | 5.47 | 17.38 |
| 4332.4 | 0.16 | 69.38 | 2.42 | 5.98 | 16.41 |
| 4332.9 | 0.16 | 69.00 | 2.41 | 6.43 | 15.17 |
| 4333.4 | 0.16 | 69.38 | 2.42 | 6.80 | 15.48 |
| 4333.9 | 0.16 | 69.00 | 2.45 | 7.09 | 13.31 |
| 4334.4 | 0.16 | 68.38 | 2.45 | 7.23 | 14.17 |
| 4334.9 | 0.15 | 68.38 | 2.45 | 7.30 | 14.02 |
| 4335.4 | 0.15 | 68.00 | 2.46 | 7.38 | 16.52 |
| 4335.9 | 0.14 | 67.19 | 2.47 | 7.49 | 16.59 |
| 4336.4 | 0.14 | 66.56 | 2.46 | 7.51 | 16.77 |
| 4336.9 | 0.13 | 66.75 | 2.46 | 7.45 | 14.55 |
| 4337.4 | 0.12 | 66.75 | 2.47 | 7.13 | 14.80 |
| 4337.9 | 0.13 | 66.38 | 2.49 | 6.73 | 15.37 |
| 4338.4 | 0.13 | 66.56 | 2.50 | 6.28 | 19.06 |
| 4338.9 | 0.14 | 67.00 | 2.52 | 5.97 | 20.98 |
| 4339.4 | 0.15 | 67.19 | 2.51 | 5.77 | 22.20 |
| 4339.9 | 0.15 | 67.38 | 2.50 | 5.57 | 19.39 |
| 4340.4 | 0.16 | 68.56 | 2.51 | 5.38 | 19.80 |
| 4340.9 | 0.16 | 68.00 | 2.52 | 5.21 | 18.66 |
| 4341.4 | 0.15 | 67.56 | 2.52 | 5.03 | 20.00 |
| 4341.9 | 0.16 | 68.19 | 2.50 | 4.95 | 16.80 |
| 4342.4 | 0.17 | 67.75 | 2.48 | 4.90 | 16.16 |
| 4342.9 | 0.17 | 68.75 | 2.48 | 4.74 | 16.42 |
| 4343.4 | 0.17 | 70.38 | 2.46 | 4.56 | 17.67 |
| 4343.9 | 0.17 | 70.75 | 2.48 | 4.43 | 17.64 |
| 4344.4 | 0.18 | 70.56 | 2.49 | 4.28 | 20.11 |
| 4344.9 | 0.17 | 71.00 | 2.48 | 4.04 | 22.17 |
| 4345.4 | 0.17 | 71.19 | 2.48 | 3.85 | 23.41 |
| 4345.9 | 0.17 | 71.19 | 2.46 | 3.71 | 22.00 |
| 4346.4 | 0.19 | 71.56 | 2.49 | 3.58 | 20.28 |
| 4346.9 | 0.19 | 71.75 | 2.48 | 3.53 | 20.98 |
| 4347.4 | 0.19 | 71.75 | 2.49 | 3.52 | 21.80 |
| 4347.9 | 0.19 | 70.75 | 2.50 | 3.49 | 22.95 |
| 4348.4 | 0.17 | 71.00 | 2.51 | 3.48 | 21.97 |
| 4348.9 | 0.16 | 70.75 | 2.51 | 3.50 | 19.19 |
| 4349.4 | 0.16 | 70.00 | 2.49 | 3.52 | 16.77 |
| 4349.9 | 0.17 | 70.38 | 2.48 | 3.60 | 17.06 |
| 4350.4 | 0.16 | 69.75 | 2.48 | 3.63 | 17.88 |
| 4350.9 | 0.16 | 69.00 | 2.50 | 3.61 | 18.44 |
| 4351.4 | 0.15 | 71.38 | 2.52 | 3.59 | 19.14 |
| 4351.9 | 0.16 | 71.00 | 2.54 | 3.57 | 19.59 |
| 4352.4 | 0.17 | 71.56 | 2.53 | 3.48 | 20.23 |
| 4352.9 | 0.17 | 71.38 | 2.54 | 3.32 | 20.44 |
| 4353.4 | 0.17 | 73.00 | 2.51 | 3.16 | 23.77 |
| 4353.9 | 0.19 | 74.75 | 2.49 | 3.05 | 26.55 |
| 4354.4 | 0.21 | 75.38 | 2.47 | 2.99 | 26.86 |
| 4354.9 | 0.20 | 74.75 | 2.48 | 2.96 | 22.55 |
| 4355.4 | 0.19 | 73.56 | 2.48 | 2.95 | 20.36 |
| 4355.9 | 0.18 | 72.56 | 2.51 | 2.94 | 19.34 |
| 4356.4 | 0.19 | 71.38 | 2.51 | 2.92 | 19.73 |
| 4356.9 | 0.18 | 70.38 | 2.51 | 2.93 | 17.95 |
| 4357.4 | 0.16 | 69.38 | 2.48 | 2.93 | 18.45 |
| 4357.9 | 0.17 | 69.00 | 2.47 | 2.96 | 20.61 |
| 4358.4 | 0.18 | 71.00 | 2.49 | 3.09 | 23.61 |
| 4358.9 | 0.19 | 73.00 | 2.49 | 3.28 | 22.89 |
| 4359.4 | 0.21 | 73.56 | 2.49 | 3.38 | 19.72 |
| 4359.9 | 0.21 | 73.38 | 2.49 | 3.40 | 16.03 |
| 4360.4 | 0.19 | 71.75 | 2.49 | 3.32 | 14.53 |
| 4360.9 | 0.16 | 70.00 | 2.48 | 3.17 | 13.30 |
| 4361.4 | 0.15 | 69.38 | 2.47 | 3.08 | 15.67 |
| 4361.9 | 0.16 | 70.56 | 2.48 | 3.07 | 16.38 |
| 4362.4 | 0.18 | 71.56 | 2.49 | 3.08 | 19.20 |
| 4362.9 | 0.19 | 73.00 | 2.48 | 3.05 | 18.77 |
| 4363.4 | 0.19 | 72.75 | 2.46 | 2.97 | 17.84 |
| 4363.9 | 0.18 | 72.56 | 2.44 | 2.85 | 16.88 |
| 4364.4 | 0.18 | 72.19 | 2.45 | 2.74 | 16.19 |
| 4364.9 | 0.17 | 71.38 | 2.46 | 2.70 | 17.63 |
| 4365.4 | 0.16 | 72.19 | 2.48 | 2.72 | 17.30 |
| 4365.9 | 0.16 | 72.75 | 2.50 | 2.76 | 19.13 |
| 4366.4 | 0.17 | 73.38 | 2.50 | 2.81 | 20.95 |
| 4366.9 | 0.18 | 73.00 | 2.52 | 2.87 | 22.36 |
| 4367.4 | 0.18 | 72.38 | 2.54 | 2.86 | 23.11 |
| 4367.9 | 0.17 | 70.75 | 2.54 | 2.85 | 20.41 |
| 4368.4 | 0.16 | 69.75 | 2.54 | 2.87 | 19.66 |
| 4368.9 | 0.16 | 69.00 | 2.52 | 2.91 | 18.69 |
| 4369.4 | 0.16 | 69.19 | 2.54 | 3.00 | 18.33 |
| 4369.9 | 0.16 | 70.19 | 2.52 | 3.09 | 19.19 |
| 4370.4 | 0.16 | 70.75 | 2.50 | 3.19 | 19.73 |
| 4370.9 | 0.15 | 71.75 | 2.49 | 3.30 | 23.48 |
| 4371.4 | 0.16 | 72.19 | 2.51 | 3.40 | 23.81 |
| 4371.9 | 0.18 | 72.75 | 2.54 | 3.54 | 26.25 |
| 4372.4 | 0.19 | 70.38 | 2.53 | 3.73 | 23.36 |
| 4372.9 | 0.18 | 69.56 | 2.54 | 3.91 | 22.22 |
| 4373.4 | 0.16 | 68.19 | 2.54 | 4.14 | 21.06 |
| 4373.9 | 0.14 | 68.00 | 2.58 | 4.49 | 22.13 |
| 4374.4 | 0.14 | 70.00 | 2.60 | 4.93 | 24.28 |
| 4374.9 | 0.15 | 69.38 | 2.63 | 5.47 | 20.86 |
| 4375.4 | 0.15 | 67.19 | 2.61 | 6.04 | 19.59 |
| 4375.9 | 0.13 | 65.38 | 2.61 | 6.29 | 17.64 |
| 4376.4 | 0.10 | 65.75 | 2.62 | 6.41 | 21.06 |
| 4376.9 | 0.10 | 67.75 | 2.63 | 6.56 | 24.48 |
| 4377.4 | 0.12 | 69.38 | 2.64 | 6.68 | 28.45 |
| 4377.9 | 0.14 | 69.38 | 2.63 | 6.82 | 29.05 |
| 4378.4 | 0.13 | 68.19 | 2.63 | 6.73 | 27.00 |
| 4378.9 | 0.12 | 68.19 | 2.59 | 6.45 | 24.61 |
| 4379.4 | 0.12 | 68.56 | 2.57 | 6.25 | 27.16 |
| 4379.9 | 0.13 | 69.75 | 2.55 | 6.04 | 29.52 |
| 4380.4 | 0.13 | 69.19 | 2.55 | 5.68 | 29.47 |
| 4380.9 | 0.13 | 71.75 | 2.57 | 5.37 | 28.77 |
| 4381.4 | 0.14 | 71.75 | 2.58 | 4.99 | 29.59 |
| 4381.9 | 0.17 | 71.75 | 2.57 | 4.53 | 31.75 |
| 4382.4 | 0.19 | 72.38 | 2.57 | 4.24 | 28.64 |
| 4382.9 | 0.18 | 70.00 | 2.57 | 3.94 | 26.19 |
| 4383.4 | 0.17 | 71.00 | 2.57 | 3.59 | 26.13 |
| 4383.9 | 0.19 | 74.38 | 2.52 | 3.30 | 25.64 |
| 4384.4 | 0.22 | 76.38 | 2.48 | 3.06 | 26.09 |
| 4384.9 | 0.23 | 77.56 | 2.45 | 2.77 | 24.09 |
| 4385.4 | 0.22 | 79.00 | 2.43 | 2.52 | 22.78 |
| 4385.9 | 0.21 | 79.00 | 2.39 | 2.32 | 19.63 |
| 4386.4 | 0.20 | 78.56 | 2.35 | 2.15 | 17.05 |
| 4386.9 | 0.21 | 79.56 | 2.35 | 2.02 | 17.30 |
| 4387.4 | 0.21 | 79.56 | 2.38 | 1.92 | 16.67 |
| 4387.9 | 0.22 | 80.00 | 2.38 | 1.88 | 17.30 |
| 4388.4 | 0.23 | 80.56 | 2.37 | 1.85 | 14.78 |
| 4388.9 | 0.22 | 80.00 | 2.35 | 1.84 | 13.89 |
| 4389.4 | 0.21 | 78.38 | 2.38 | 1.85 | 13.65 |
| 4389.9 | 0.20 | 77.19 | 2.43 | 1.88 | 13.45 |
| 4390.4 | 0.19 | 76.00 | 2.45 | 1.91 | 14.70 |
| 4390.9 | 0.19 | 75.56 | 2.44 | 1.95 | 14.02 |
| 4391.4 | 0.20 | 76.75 | 2.43 | 1.97 | 14.60 |
| 4391.9 | 0.21 | 77.75 | 2.42 | 1.98 | 14.30 |
| 4392.4 | 0.22 | 78.56 | 2.40 | 1.96 | 13.36 |
| 4392.9 | 0.23 | 79.19 | 2.37 | 1.94 | 14.27 |
| 4393.4 | 0.23 | 79.00 | 2.37 | 1.91 | 16.67 |
| 4393.9 | 0.23 | 78.00 | 2.35 | 1.91 | 18.14 |
| 4394.4 | 0.22 | 77.56 | 2.38 | 1.92 | 18.17 |
| 4394.9 | 0.22 | 77.19 | 2.39 | 1.94 | 16.38 |
| 4395.4 | 0.22 | 77.38 | 2.43 | 1.97 | 17.41 |
| 4395.9 | 0.22 | 78.19 | 2.42 | 2.00 | 17.70 |
| 4396.4 | 0.22 | 78.38 | 2.40 | 2.05 | 18.27 |
| 4396.9 | 0.23 | 79.19 | 2.37 | 2.10 | 17.33 |
| 4397.4 | 0.24 | 79.38 | 2.37 | 2.14 | 15.77 |
| 4397.9 | 0.23 | 80.00 | 2.35 | 2.15 | 15.78 |
| 4398.4 | 0.23 | 81.19 | 2.34 | 2.14 | 16.09 |
| 4398.9 | 0.22 | 81.00 | 2.32 | 2.14 | 19.48 |
| 4399.4 | 0.22 | 80.38 | 2.33 | 2.15 | 19.09 |
| 4399.9 | 0.23 | 80.19 | 2.34 | 2.18 | 18.53 |
| 4400.4 | 0.23 | 78.75 | 2.34 | 2.24 | 17.69 |
| 4400.9 | 0.23 | 78.00 | 2.36 | 2.29 | 20.00 |
| 4401.4 | 0.24 | 78.38 | 2.36 | 2.38 | 22.14 |
| 4401.9 | 0.24 | 78.56 | 2.35 | 2.50 | 20.50 |
| 4402.4 | 0.24 | 80.00 | 2.34 | 2.66 | 18.89 |
| 4402.9 | 0.23 | 81.00 | 2.32 | 2.84 | 16.66 |
| 4403.4 | 0.23 | 81.00 | 2.35 | 3.01 | 15.77 |
| 4403.9 | 0.23 | 80.56 | 2.36 | 3.16 | 14.23 |
| 4404.4 | 0.23 | 80.00 | 2.37 | 3.25 | 14.86 |
| 4404.9 | 0.22 | 79.56 | 2.37 | 3.26 | 16.02 |
| 4405.4 | 0.23 | 79.19 | 2.34 | 3.22 | 17.67 |
| 4405.9 | 0.24 | 80.56 | 2.37 | 3.12 | 17.72 |
| 4406.4 | 0.25 | 81.19 | 2.35 | 3.05 | 17.91 |
| 4406.9 | 0.24 | 81.19 | 2.34 | 2.96 | 15.97 |
| 4407.4 | 0.25 | 82.56 | 2.32 | 2.91 | 15.90 |
| 4407.9 | 0.26 | 82.75 | 2.31 | 2.89 | 16.39 |
| 4408.4 | 0.26 | 82.75 | 2.32 | 2.91 | 18.84 |
| 4408.9 | 0.25 | 83.38 | 2.32 | 2.98 | 18.84 |
| 4409.4 | 0.23 | 83.38 | 2.34 | 3.07 | 18.84 |
| 4409.9 | 0.23 | 82.56 | 2.33 | 3.18 | 18.17 |
| 4410.4 | 0.23 | 79.19 | 2.32 | 3.30 | 17.45 |
| 4410.9 | 0.23 | 78.75 | 2.36 | 3.46 | 17.59 |
| 4411.4 | 0.21 | 77.56 | 2.37 | 3.59 | 17.06 |
| 4411.9 | 0.20 | 75.38 | 2.39 | 3.71 | 17.52 |
| 4412.4 | 0.22 | 76.38 | 2.34 | 3.80 | 16.20 |
| 4412.9 | 0.19 | 76.56 | 2.36 | 3.83 | 16.16 |
| 4413.4 | 0.19 | 75.00 | 2.38 | 3.84 | 16.09 |
| 4413.9 | 0.20 | 75.00 | 2.42 | 3.87 | 16.38 |
| 4414.4 | 0.19 | 74.38 | 2.41 | 3.88 | 14.84 |
| 4414.9 | 0.19 | 73.75 | 2.40 | 3.93 | 15.16 |
| 4415.4 | 0.19 | 73.75 | 2.40 | 3.97 | 16.06 |
| 4415.9 | 0.19 | 74.00 | 2.40 | 4.02 | 16.92 |
| 4416.4 | 0.19 | 74.00 | 2.42 | 4.08 | 16.70 |
| 4416.9 | 0.19 | 74.00 | 2.43 | 4.12 | 16.77 |
| 4417.4 | 0.20 | 73.56 | 2.43 | 4.13 | 17.81 |
| 4417.9 | 0.20 | 72.75 | 2.41 | 4.18 | 16.83 |
| 4418.4 | 0.19 | 73.75 | 2.45 | 4.20 | 17.14 |
| 4418.9 | 0.19 | 73.00 | 2.46 | 4.22 | 15.54 |
| 4419.4 | 0.19 | 72.19 | 2.49 | 4.20 | 13.96 |
| 4419.9 | 0.19 | 71.19 | 2.46 | 4.20 | 11.16 |
| 4420.4 | 0.18 | 70.75 | 2.44 | 4.16 | 10.88 |
| 4420.9 | 0.18 | 72.00 | 2.42 | 4.13 | 12.72 |
| 4421.4 | 0.17 | 72.00 | 2.41 | 4.05 | 14.23 |
| 4421.9 | 0.17 | 71.75 | 2.43 | 3.95 | 16.81 |
| 4422.4 | 0.16 | 70.75 | 2.43 | 3.80 | 16.86 |
| 4422.9 | 0.17 | 71.00 | 2.46 | 3.63 | 15.95 |
| 4423.4 | 0.18 | 72.00 | 2.45 | 3.47 | 13.04 |
| 4423.9 | 0.20 | 73.00 | 2.44 | 3.33 | 12.98 |
| 4424.4 | 0.19 | 73.19 | 2.42 | 3.25 | 13.23 |
| 4424.9 | 0.18 | 74.19 | 2.43 | 3.19 | 14.14 |
| 4425.4 | 0.18 | 74.75 | 2.41 | 3.17 | 13.87 |
| 4425.9 | 0.19 | 75.56 | 2.40 | 3.18 | 13.90 |
| 4426.4 | 0.20 | 75.19 | 2.43 | 3.20 | 13.00 |
| 4426.9 | 0.19 | 73.19 | 2.42 | 3.22 | 12.67 |
| 4427.4 | 0.18 | 72.75 | 2.45 | 3.23 | 13.38 |
| 4427.9 | 0.18 | 72.00 | 2.42 | 3.24 | 14.01 |
| 4428.4 | 0.18 | 70.56 | 2.43 | 3.25 | 13.13 |
| 4428.9 | 0.17 | 72.00 | 2.43 | 3.28 | 13.38 |
| 4429.4 | 0.17 | 73.38 | 2.41 | 3.32 | 16.45 |
| 4429.9 | 0.17 | 74.00 | 2.40 | 3.33 | 17.66 |
| 4430.4 | 0.19 | 74.56 | 2.39 | 3.31 | 18.22 |
| 4430.9 | 0.18 | 73.00 | 2.42 | 3.25 | 14.84 |
| 4431.4 | 0.17 | 71.75 | 2.44 | 3.15 | 14.85 |
| 4431.9 | 0.17 | 70.38 | 2.45 | 3.02 | 13.59 |
| 4432.4 | 0.16 | 70.19 | 2.47 | 2.93 | 19.20 |
| 4432.9 | 0.21 | 76.38 | 2.48 | 2.95 | 22.73 |
| 4433.4 | 0.24 | 75.56 | 2.48 | 2.95 | 23.16 |
| 4433.9 | 0.25 | 76.38 | 2.43 | 2.98 | 18.78 |
| 4434.4 | 0.22 | 73.75 | 2.45 | 3.01 | 16.83 |
| 4434.9 | 0.20 | 70.75 | 2.46 | 3.01 | 15.57 |
| 4435.4 | 0.17 | 70.19 | 2.49 | 3.09 | 16.45 |
| 4435.9 | 0.16 | 70.00 | 2.50 | 3.34 | 13.95 |
| 4436.4 | 0.15 | 69.75 | 2.49 | 3.60 | 15.14 |
| 4436.9 | 0.16 | 69.56 | 2.48 | 3.93 | 15.13 |
| 4437.4 | 0.16 | 68.56 | 2.48 | 4.29 | 17.55 |
| 4437.9 | 0.15 | 67.56 | 2.51 | 4.54 | 17.58 |
| 4438.4 | 0.14 | 66.75 | 2.52 | 4.61 | 17.30 |
| 4438.9 | 0.13 | 66.56 | 2.51 | 4.74 | 16.13 |
| 4439.4 | 0.14 | 67.00 | 2.50 | 4.98 | 16.77 |
| 4439.9 | 0.15 | 67.00 | 2.51 | 5.27 | 17.36 |
| 4440.4 | 0.15 | 65.19 | 2.54 | 5.43 | 17.97 |
| 4440.9 | 0.13 | 65.00 | 2.58 | 5.52 | 19.19 |
| 4441.4 | 0.13 | 64.56 | 2.61 | 5.59 | 20.13 |
| 4441.9 | 0.13 | 64.00 | 2.62 | 5.75 | 22.92 |
| 4442.4 | 0.14 | 67.19 | 2.61 | 5.95 | 23.23 |
| 4442.9 | 0.15 | 67.38 | 2.59 | 6.14 | 25.27 |
| 4443.4 | 0.16 | 68.56 | 2.59 | 6.30 | 26.02 |
| 4443.9 | 0.16 | 68.19 | 2.58 | 6.43 | 24.81 |
| 4444.4 | 0.13 | 65.75 | 2.59 | 6.41 | 24.08 |
| 4444.9 | 0.12 | 68.75 | 2.59 | 6.45 | 24.63 |
| 4445.4 | 0.15 | 70.00 | 2.59 | 6.91 | 28.88 |

Table A2.3: Neutron porosity, sonic transit time, bulk density, deep induction resistivity and gamma ray data for the Great Oolite Formation in the Storrington-2 well.

| TVDSS (ft) | N.PHI (p.u.) | SONIC T. (µsec/ft) | DENS. (g/cm3) | RESIS. (Ω.m-1) | GR (API) |
| --- | --- | --- | --- | --- | --- |
| 3889.1 | 0.09 | 63.13 | 2.56 | 9.78 | 11.56 |
| 3889.6 | 0.09 | 64.00 | 2.56 | 9.85 | 14.13 |
| 3890.1 | 0.08 | 63.25 | 2.56 | 9.77 | 15.49 |
| 3890.6 | 0.09 | 64.00 | 2.56 | 9.45 | 14.46 |
| 3891.1 | 0.10 | 63.38 | 2.56 | 8.99 | 11.85 |
| 3891.6 | 0.11 | 63.88 | 2.55 | 8.61 | 10.44 |
| 3892.1 | 0.11 | 64.75 | 2.53 | 8.41 | 10.70 |
| 3892.5 | 0.11 | 65.50 | 2.53 | 8.31 | 9.96 |
| 3893.0 | 0.11 | 66.13 | 2.54 | 8.22 | 10.24 |
| 3893.5 | 0.10 | 65.63 | 2.55 | 8.16 | 10.23 |
| 3894.0 | 0.09 | 65.50 | 2.56 | 8.11 | 12.42 |
| 3894.5 | 0.08 | 64.38 | 2.57 | 7.97 | 11.92 |
| 3895.0 | 0.10 | 63.88 | 2.55 | 7.78 | 12.40 |
| 3895.5 | 0.12 | 63.50 | 2.54 | 7.65 | 12.13 |
| 3895.9 | 0.13 | 64.00 | 2.52 | 7.62 | 13.32 |
| 3896.4 | 0.13 | 66.75 | 2.53 | 7.67 | 12.62 |
| 3896.9 | 0.12 | 67.00 | 2.53 | 7.78 | 12.07 |
| 3897.4 | 0.11 | 67.88 | 2.55 | 7.95 | 12.14 |
| 3897.9 | 0.09 | 67.13 | 2.56 | 8.21 | 11.69 |
| 3898.4 | 0.08 | 66.25 | 2.57 | 8.70 | 10.84 |
| 3898.9 | 0.06 | 65.13 | 2.57 | 9.48 | 10.05 |
| 3899.3 | 0.05 | 63.63 | 2.59 | 10.63 | 11.90 |
| 3899.8 | 0.05 | 62.63 | 2.61 | 11.81 | 12.80 |
| 3900.3 | 0.05 | 61.38 | 2.65 | 12.27 | 12.78 |
| 3900.8 | 0.08 | 58.75 | 2.67 | 12.13 | 13.77 |
| 3901.3 | 0.12 | 58.50 | 2.68 | 11.58 | 17.83 |
| 3901.8 | 0.16 | 60.75 | 2.50 | 10.64 | 16.05 |
| 3902.3 | 0.18 | 65.00 | 2.50 | 9.80 | 20.03 |
| 3902.7 | 0.18 | 68.38 | 2.48 | 9.37 | 18.88 |
| 3903.2 | 0.10 | 53.70 | 2.68 | 9.27 | 19.53 |
| 3903.7 | 0.11 | 52.10 | 2.69 | 9.32 | 18.38 |
| 3904.2 | 0.06 | 68.25 | 2.51 | 9.47 | 18.09 |
| 3904.7 | 0.03 | 57.30 | 2.70 | 9.89 | 20.91 |
| 3905.2 | 0.03 | 61.00 | 2.70 | 10.66 | 18.30 |
| 3905.7 | 0.04 | 57.63 | 2.68 | 11.84 | 16.02 |
| 3906.2 | 0.05 | 55.50 | 2.68 | 13.53 | 16.13 |
| 3906.6 | 0.06 | 57.13 | 2.67 | 15.52 | 15.98 |
| 3907.1 | 0.05 | 57.38 | 2.68 | 16.95 | 13.30 |
| 3907.6 | 0.04 | 58.63 | 2.67 | 17.41 | 15.59 |
| 3908.1 | 0.04 | 59.00 | 2.68 | 16.94 | 16.39 |
| 3908.6 | 0.05 | 57.50 | 2.67 | 15.48 | 15.66 |
| 3909.1 | 0.07 | 57.50 | 2.68 | 13.60 | 14.96 |
| 3909.6 | 0.10 | 58.50 | 2.68 | 11.90 | 17.28 |
| 3910.0 | 0.13 | 59.88 | 2.67 | 10.57 | 18.22 |
| 3910.5 | 0.15 | 63.25 | 2.52 | 9.54 | 18.19 |
| 3911.0 | 0.10 | 51.10 | 2.67 | 8.71 | 18.41 |
| 3911.5 | 0.16 | 66.63 | 2.46 | 8.12 | 19.55 |
| 3912.0 | 0.14 | 53.50 | 2.61 | 7.74 | 19.11 |
| 3912.5 | 0.12 | 55.50 | 2.65 | 7.47 | 18.84 |
| 3913.0 | 0.11 | 67.00 | 2.58 | 7.29 | 17.84 |
| 3913.4 | 0.11 | 66.00 | 2.57 | 7.24 | 15.88 |
| 3913.9 | 0.12 | 65.88 | 2.54 | 7.27 | 13.11 |
| 3914.4 | 0.13 | 65.50 | 2.53 | 7.42 | 13.09 |
| 3914.9 | 0.13 | 66.13 | 2.55 | 7.68 | 12.38 |
| 3915.4 | 0.13 | 66.38 | 2.56 | 7.93 | 12.77 |
| 3915.9 | 0.13 | 66.38 | 2.57 | 8.14 | 13.81 |
| 3916.4 | 0.12 | 65.63 | 2.55 | 8.37 | 13.86 |
| 3916.8 | 0.11 | 65.38 | 2.54 | 8.61 | 13.98 |
| 3917.3 | 0.09 | 65.25 | 2.54 | 8.92 | 10.56 |
| 3917.8 | 0.09 | 64.75 | 2.56 | 9.26 | 8.83 |
| 3918.3 | 0.10 | 64.00 | 2.57 | 9.54 | 7.35 |
| 3918.8 | 0.11 | 63.13 | 2.57 | 9.71 | 7.34 |
| 3919.3 | 0.12 | 63.13 | 2.55 | 9.80 | 8.76 |
| 3919.8 | 0.13 | 64.00 | 2.53 | 9.83 | 8.77 |
| 3920.3 | 0.12 | 65.38 | 2.52 | 9.84 | 8.30 |
| 3920.7 | 0.11 | 66.50 | 2.52 | 9.82 | 6.88 |
| 3921.2 | 0.10 | 66.00 | 2.54 | 9.80 | 8.34 |
| 3921.7 | 0.08 | 65.63 | 2.55 | 9.77 | 9.30 |
| 3922.2 | 0.07 | 64.50 | 2.57 | 9.84 | 9.31 |
| 3922.7 | 0.06 | 63.38 | 2.59 | 10.22 | 8.33 |
| 3923.2 | 0.04 | 62.13 | 2.61 | 11.08 | 9.77 |
| 3923.7 | 0.02 | 60.50 | 2.63 | 12.40 | 13.56 |
| 3924.1 | 0.01 | 57.88 | 2.66 | 14.12 | 16.19 |
| 3924.6 | 0.01 | 55.88 | 2.68 | 16.13 | 16.34 |
| 3925.1 | 0.01 | 53.88 | 2.70 | 18.28 | 12.79 |
| 3925.6 | 0.01 | 51.63 | 2.71 | 20.59 | 10.69 |
| 3926.1 | 0.01 | 51.38 | 2.70 | 21.45 | 8.64 |
| 3926.6 | 0.01 | 50.63 | 2.71 | 21.95 | 10.31 |
| 3927.1 | 0.01 | 50.13 | 2.70 | 23.66 | 10.95 |
| 3927.5 | 0.01 | 51.63 | 2.70 | 23.66 | 11.17 |
| 3928.0 | 0.01 | 54.13 | 2.68 | 23.84 | 10.17 |
| 3928.5 | 0.01 | 52.50 | 2.69 | 25.50 | 9.94 |
| 3929.0 | 0.01 | 51.63 | 2.68 | 25.75 | 10.42 |
| 3929.5 | 0.01 | 50.88 | 2.69 | 26.75 | 9.01 |
| 3930.0 | 0.01 | 53.38 | 2.67 | 26.06 | 9.27 |
| 3930.5 | 0.01 | 54.63 | 2.68 | 27.19 | 8.33 |
| 3930.9 | 0.01 | 53.75 | 2.68 | 27.47 | 10.00 |
| 3931.4 | 0.02 | 54.25 | 2.70 | 27.34 | 8.59 |
| 3931.9 | 0.02 | 51.00 | 2.70 | 25.72 | 9.77 |
| 3932.4 | 0.03 | 51.88 | 2.67 | 23.91 | 9.77 |
| 3932.9 | 0.04 | 62.50 | 2.65 | 23.13 | 12.13 |
| 3933.4 | 0.06 | 56.20 | 2.64 | 22.52 | 11.91 |
| 3933.9 | 0.08 | 59.40 | 2.63 | 20.61 | 14.68 |
| 3934.3 | 0.12 | 57.50 | 2.63 | 16.25 | 18.09 |
| 3934.8 | 0.14 | 58.10 | 2.60 | 13.75 | 20.95 |
| 3935.3 | 0.16 | 68.50 | 2.55 | 12.23 | 19.94 |
| 3935.8 | 0.18 | 75.25 | 2.37 | 11.15 | 19.02 |
| 3936.3 | 0.18 | 76.50 | 2.32 | 10.27 | 19.67 |
| 3936.8 | 0.19 | 77.63 | 2.28 | 9.59 | 18.09 |
| 3937.3 | 0.19 | 79.75 | 2.32 | 9.09 | 17.31 |
| 3937.8 | 0.19 | 79.13 | 2.24 | 8.78 | 13.97 |
| 3938.2 | 0.23 | 79.38 | 2.18 | 8.59 | 14.45 |
| 3938.7 | 0.16 | 80.38 | 2.20 | 8.45 | 14.51 |
| 3939.2 | 0.21 | 80.06 | 2.25 | 8.34 | 16.59 |
| 3939.7 | 0.16 | 74.94 | 2.40 | 8.17 | 16.88 |
| 3940.2 | 0.13 | 64.88 | 2.49 | 7.70 | 17.83 |
| 3940.7 | 0.20 | 73.38 | 2.45 | 7.20 | 16.73 |
| 3941.2 | 0.23 | 71.25 | 2.41 | 7.04 | 15.52 |
| 3941.6 | 0.23 | 75.13 | 2.31 | 7.12 | 14.31 |
| 3942.1 | 0.21 | 81.00 | 2.30 | 7.36 | 13.80 |
| 3942.6 | 0.21 | 79.25 | 2.21 | 7.66 | 14.77 |
| 3943.1 | 0.22 | 76.63 | 2.18 | 7.82 | 14.27 |
| 3943.6 | 0.19 | 79.25 | 2.17 | 7.88 | 14.70 |
| 3944.1 | 0.20 | 80.38 | 2.23 | 8.06 | 14.77 |
| 3944.6 | 0.10 | 57.38 | 2.53 | 8.59 | 13.88 |
| 3945.0 | 0.11 | 60.50 | 2.46 | 9.59 | 12.28 |
| 3945.5 | 0.09 | 60.00 | 2.52 | 11.07 | 10.08 |
| 3946.0 | 0.08 | 61.50 | 2.53 | 12.53 | 10.73 |
| 3946.5 | 0.09 | 58.10 | 2.58 | 13.17 | 12.82 |
| 3947.0 | 0.10 | 62.88 | 2.61 | 13.24 | 16.56 |
| 3947.5 | 0.10 | 62.13 | 2.65 | 13.17 | 22.08 |
| 3948.0 | 0.08 | 64.25 | 2.58 | 13.07 | 22.80 |
| 3948.4 | 0.08 | 63.13 | 2.67 | 13.02 | 22.81 |
| 3948.9 | 0.08 | 62.13 | 2.67 | 13.13 | 18.80 |
| 3949.4 | 0.07 | 60.88 | 2.67 | 13.65 | 18.58 |
| 3949.9 | 0.05 | 60.00 | 2.69 | 14.77 | 18.44 |
| 3950.4 | 0.03 | 59.00 | 2.65 | 16.50 | 18.63 |
| 3950.9 | 0.02 | 57.25 | 2.67 | 18.70 | 16.23 |
| 3951.4 | 0.02 | 56.50 | 2.67 | 21.45 | 13.09 |
| 3951.9 | 0.02 | 55.75 | 2.69 | 21.08 | 10.95 |
| 3952.3 | 0.02 | 55.00 | 2.69 | 22.64 | 10.70 |
| 3952.8 | 0.02 | 54.63 | 2.68 | 23.63 | 13.52 |
| 3953.3 | 0.02 | 54.38 | 2.69 | 23.22 | 15.70 |
| 3953.8 | 0.02 | 55.25 | 2.69 | 24.25 | 16.94 |
| 3954.3 | 0.02 | 55.25 | 2.70 | 24.38 | 17.05 |
| 3954.8 | 0.02 | 54.75 | 2.71 | 24.41 | 16.77 |
| 3955.3 | 0.02 | 53.63 | 2.70 | 25.16 | 16.00 |
| 3955.7 | 0.02 | 53.50 | 2.70 | 24.94 | 14.97 |
| 3956.2 | 0.03 | 53.25 | 2.69 | 24.38 | 14.09 |
| 3956.7 | 0.03 | 54.50 | 2.70 | 25.13 | 13.17 |
| 3957.2 | 0.02 | 54.50 | 2.70 | 24.81 | 12.63 |
| 3957.7 | 0.01 | 54.50 | 2.73 | 24.88 | 12.42 |
| 3958.2 | 0.01 | 53.88 | 2.74 | 25.53 | 12.86 |
| 3958.7 | 0.01 | 51.75 | 2.75 | 25.94 | 13.56 |
| 3959.1 | 0.02 | 50.75 | 2.70 | 25.16 | 12.08 |
| 3959.6 | 0.03 | 50.75 | 2.69 | 24.19 | 13.25 |
| 3960.1 | 0.04 | 52.13 | 2.68 | 24.19 | 12.80 |
| 3960.6 | 0.04 | 54.13 | 2.72 | 24.31 | 12.86 |
| 3961.1 | 0.04 | 56.13 | 2.71 | 23.69 | 12.27 |
| 3961.6 | 0.04 | 56.25 | 2.70 | 24.00 | 11.59 |
| 3962.1 | 0.04 | 56.63 | 2.68 | 23.83 | 10.64 |
| 3962.5 | 0.04 | 56.63 | 2.68 | 22.72 | 10.52 |
| 3963.0 | 0.03 | 56.00 | 2.69 | 23.17 | 12.94 |
| 3963.5 | 0.03 | 55.75 | 2.69 | 24.03 | 12.38 |
| 3964.0 | 0.04 | 55.38 | 2.65 | 22.06 | 13.63 |
| 3964.5 | 0.06 | 54.75 | 2.59 | 19.05 | 14.44 |
| 3965.0 | 0.08 | 53.75 | 2.65 | 16.50 | 13.09 |
| 3965.5 | 0.09 | 54.63 | 2.56 | 14.63 | 13.73 |
| 3966.0 | 0.09 | 56.25 | 2.53 | 13.27 | 13.53 |
| 3966.4 | 0.10 | 58.63 | 2.53 | 12.27 | 13.44 |
| 3966.9 | 0.10 | 59.75 | 2.54 | 11.59 | 12.10 |
| 3967.4 | 0.09 | 59.88 | 2.55 | 11.17 | 12.11 |
| 3967.9 | 0.09 | 60.25 | 2.55 | 10.88 | 12.38 |
| 3968.4 | 0.09 | 60.13 | 2.55 | 10.63 | 12.40 |
| 3968.9 | 0.09 | 60.38 | 2.55 | 10.45 | 10.99 |
| 3969.4 | 0.09 | 60.13 | 2.56 | 10.34 | 9.53 |
| 3969.8 | 0.09 | 59.63 | 2.55 | 10.35 | 8.11 |
| 3970.3 | 0.08 | 60.13 | 2.57 | 10.38 | 8.57 |
| 3970.8 | 0.07 | 59.88 | 2.58 | 10.17 | 9.54 |
| 3971.3 | 0.08 | 59.38 | 2.60 | 9.64 | 10.66 |
| 3971.8 | 0.09 | 59.25 | 2.58 | 8.84 | 9.98 |
| 3972.3 | 0.11 | 58.88 | 2.54 | 8.00 | 9.77 |
| 3972.8 | 0.12 | 59.75 | 2.49 | 7.30 | 9.86 |
| 3973.2 | 0.13 | 61.38 | 2.48 | 6.81 | 10.09 |
| 3973.7 | 0.14 | 62.75 | 2.47 | 6.45 | 10.27 |
| 3974.2 | 0.15 | 64.00 | 2.45 | 6.12 | 10.00 |
| 3974.7 | 0.16 | 65.25 | 2.42 | 5.86 | 9.01 |
| 3975.2 | 0.16 | 65.88 | 2.42 | 5.69 | 9.48 |
| 3975.7 | 0.15 | 67.38 | 2.43 | 5.57 | 8.78 |
| 3976.2 | 0.14 | 68.00 | 2.44 | 5.37 | 10.70 |
| 3976.6 | 0.15 | 68.13 | 2.45 | 5.01 | 9.98 |
| 3977.1 | 0.16 | 67.00 | 2.43 | 4.53 | 9.05 |
| 3977.6 | 0.16 | 66.50 | 2.42 | 4.01 | 7.39 |
| 3978.1 | 0.17 | 67.25 | 2.40 | 3.57 | 8.14 |
| 3978.6 | 0.17 | 68.38 | 2.40 | 3.27 | 10.27 |
| 3979.1 | 0.16 | 69.63 | 2.41 | 3.08 | 10.27 |
| 3979.6 | 0.15 | 70.50 | 2.43 | 2.91 | 10.95 |
| 3980.1 | 0.15 | 70.50 | 2.44 | 2.79 | 11.43 |
| 3980.5 | 0.15 | 69.38 | 2.44 | 2.75 | 12.58 |
| 3981.0 | 0.15 | 68.50 | 2.45 | 2.75 | 10.45 |
| 3981.5 | 0.15 | 68.88 | 2.44 | 2.79 | 10.98 |
| 3982.0 | 0.16 | 68.50 | 2.42 | 2.90 | 11.53 |
| 3982.5 | 0.16 | 68.63 | 2.40 | 2.98 | 12.72 |
| 3983.0 | 0.16 | 69.50 | 2.41 | 3.01 | 10.27 |
| 3983.5 | 0.15 | 70.00 | 2.41 | 3.01 | 8.32 |
| 3983.9 | 0.15 | 70.38 | 2.43 | 3.01 | 7.82 |
| 3984.4 | 0.14 | 70.63 | 2.44 | 3.00 | 8.31 |
| 3984.9 | 0.14 | 69.88 | 2.44 | 3.01 | 7.84 |
| 3985.4 | 0.14 | 69.50 | 2.44 | 3.01 | 7.61 |
| 3985.9 | 0.13 | 69.00 | 2.45 | 3.02 | 8.06 |
| 3986.4 | 0.13 | 67.63 | 2.47 | 3.03 | 9.52 |
| 3986.9 | 0.13 | 67.00 | 2.49 | 3.01 | 10.73 |
| 3987.3 | 0.13 | 66.38 | 2.50 | 2.97 | 10.54 |
| 3987.8 | 0.13 | 65.13 | 2.48 | 2.89 | 10.98 |
| 3988.3 | 0.14 | 64.50 | 2.48 | 2.78 | 11.44 |
| 3988.8 | 0.15 | 65.25 | 2.46 | 2.67 | 10.94 |
| 3989.3 | 0.16 | 65.63 | 2.45 | 2.58 | 12.16 |
| 3989.8 | 0.16 | 67.00 | 2.43 | 2.50 | 11.39 |
| 3990.3 | 0.16 | 68.50 | 2.43 | 2.43 | 11.16 |
| 3990.7 | 0.15 | 69.38 | 2.41 | 2.38 | 10.00 |
| 3991.2 | 0.16 | 69.75 | 2.41 | 2.34 | 7.93 |
| 3991.7 | 0.16 | 70.63 | 2.41 | 2.32 | 9.13 |
| 3992.2 | 0.16 | 70.75 | 2.42 | 2.29 | 7.89 |
| 3992.7 | 0.16 | 70.63 | 2.43 | 2.26 | 8.34 |
| 3993.2 | 0.16 | 70.13 | 2.43 | 2.20 | 7.35 |
| 3993.7 | 0.17 | 70.63 | 2.43 | 2.13 | 8.53 |
| 3994.2 | 0.17 | 70.13 | 2.41 | 2.06 | 9.02 |
| 3994.6 | 0.17 | 70.88 | 2.41 | 2.01 | 9.27 |
| 3995.1 | 0.17 | 71.50 | 2.42 | 1.98 | 8.06 |
| 3995.6 | 0.16 | 72.00 | 2.43 | 1.95 | 7.13 |
| 3996.1 | 0.16 | 71.75 | 2.43 | 1.92 | 6.89 |
| 3996.6 | 0.16 | 71.25 | 2.43 | 1.92 | 7.65 |
| 3997.1 | 0.16 | 71.13 | 2.42 | 1.92 | 8.35 |
| 3997.6 | 0.16 | 71.00 | 2.41 | 1.94 | 9.07 |
| 3998.0 | 0.16 | 71.38 | 2.42 | 1.99 | 8.10 |
| 3998.5 | 0.15 | 72.50 | 2.42 | 2.02 | 8.83 |
| 3999.0 | 0.15 | 72.25 | 2.44 | 2.03 | 8.56 |
| 3999.5 | 0.15 | 72.00 | 2.45 | 2.01 | 9.02 |
| 4000.0 | 0.17 | 71.25 | 2.45 | 1.97 | 9.31 |
| 4000.5 | 0.18 | 71.13 | 2.42 | 1.93 | 9.59 |
| 4001.0 | 0.18 | 71.38 | 2.42 | 1.88 | 10.33 |
| 4001.4 | 0.17 | 72.88 | 2.41 | 1.81 | 9.56 |
| 4001.9 | 0.18 | 73.50 | 2.41 | 1.71 | 9.52 |
| 4002.4 | 0.20 | 73.63 | 2.37 | 1.60 | 9.25 |
| 4002.9 | 0.20 | 74.13 | 2.34 | 1.50 | 8.77 |
| 4003.4 | 0.20 | 75.13 | 2.34 | 1.44 | 8.52 |
| 4003.9 | 0.19 | 76.00 | 2.35 | 1.40 | 7.83 |
| 4004.4 | 0.18 | 77.00 | 2.36 | 1.38 | 9.00 |
| 4004.8 | 0.18 | 76.88 | 2.37 | 1.37 | 9.02 |
| 4005.3 | 0.18 | 75.75 | 2.39 | 1.36 | 9.49 |
| 4005.8 | 0.19 | 75.13 | 2.40 | 1.36 | 9.08 |
| 4006.3 | 0.19 | 74.38 | 2.40 | 1.37 | 9.07 |
| 4006.8 | 0.19 | 74.13 | 2.39 | 1.40 | 9.31 |
| 4007.3 | 0.19 | 74.13 | 2.40 | 1.44 | 8.08 |
| 4007.8 | 0.19 | 73.75 | 2.40 | 1.47 | 8.07 |
| 4008.2 | 0.17 | 73.88 | 2.40 | 1.48 | 8.31 |
| 4008.7 | 0.18 | 73.75 | 2.41 | 1.47 | 8.54 |
| 4009.2 | 0.18 | 73.63 | 2.40 | 1.46 | 7.86 |
| 4009.7 | 0.18 | 73.25 | 2.40 | 1.45 | 6.45 |
| 4010.2 | 0.17 | 72.50 | 2.40 | 1.44 | 6.96 |
| 4010.7 | 0.17 | 72.25 | 2.43 | 1.41 | 7.40 |
| 4011.2 | 0.19 | 71.38 | 2.43 | 1.36 | 8.57 |
| 4011.7 | 0.20 | 71.38 | 2.41 | 1.31 | 9.72 |
| 4012.1 | 0.21 | 72.50 | 2.39 | 1.26 | 10.41 |
| 4012.6 | 0.22 | 73.38 | 2.37 | 1.22 | 10.65 |
| 4013.1 | 0.21 | 74.88 | 2.37 | 1.19 | 9.24 |
| 4013.6 | 0.20 | 76.13 | 2.37 | 1.17 | 9.95 |
| 4014.1 | 0.19 | 76.38 | 2.38 | 1.17 | 9.00 |
| 4014.6 | 0.19 | 76.38 | 2.39 | 1.18 | 10.21 |
| 4015.1 | 0.18 | 75.25 | 2.40 | 1.23 | 8.84 |
| 4015.5 | 0.17 | 73.88 | 2.42 | 1.31 | 9.09 |
| 4016.0 | 0.15 | 73.38 | 2.45 | 1.40 | 8.59 |
| 4016.5 | 0.15 | 72.38 | 2.46 | 1.50 | 10.23 |
| 4017.0 | 0.14 | 70.75 | 2.46 | 1.59 | 9.98 |
| 4017.5 | 0.15 | 69.75 | 2.45 | 1.65 | 9.49 |
| 4018.0 | 0.16 | 68.75 | 2.44 | 1.67 | 8.06 |
| 4018.5 | 0.17 | 68.50 | 2.43 | 1.67 | 8.81 |
| 4018.9 | 0.18 | 70.13 | 2.43 | 1.67 | 9.55 |
| 4019.4 | 0.17 | 70.88 | 2.42 | 1.67 | 10.54 |
| 4019.9 | 0.15 | 71.75 | 2.43 | 1.70 | 11.69 |
| 4020.4 | 0.12 | 72.50 | 2.45 | 1.75 | 11.66 |
| 4020.9 | 0.12 | 69.75 | 2.49 | 1.83 | 9.97 |
| 4021.4 | 0.12 | 67.38 | 2.51 | 1.93 | 10.90 |
| 4021.9 | 0.13 | 66.13 | 2.50 | 2.08 | 13.25 |
| 4022.3 | 0.13 | 64.88 | 2.49 | 2.33 | 17.53 |
| 4022.8 | 0.14 | 65.25 | 2.48 | 2.69 | 17.55 |
| 4023.3 | 0.14 | 66.25 | 2.48 | 3.06 | 16.84 |
| 4023.8 | 0.15 | 66.25 | 2.48 | 3.35 | 15.68 |
| 4024.3 | 0.14 | 66.25 | 2.49 | 3.55 | 15.02 |
| 4024.8 | 0.13 | 66.75 | 2.49 | 3.67 | 13.85 |
| 4025.3 | 0.12 | 66.75 | 2.49 | 3.74 | 11.70 |
| 4025.7 | 0.13 | 66.38 | 2.50 | 3.77 | 10.48 |
| 4026.2 | 0.14 | 66.38 | 2.51 | 3.76 | 9.27 |
| 4026.7 | 0.15 | 66.13 | 2.49 | 3.74 | 9.73 |
| 4027.2 | 0.15 | 66.50 | 2.48 | 3.71 | 9.46 |
| 4027.7 | 0.15 | 66.63 | 2.48 | 3.67 | 10.45 |
| 4028.2 | 0.14 | 67.50 | 2.48 | 3.61 | 10.04 |
| 4028.7 | 0.14 | 68.13 | 2.48 | 3.52 | 11.28 |
| 4029.2 | 0.13 | 68.25 | 2.49 | 3.44 | 10.79 |
| 4029.6 | 0.13 | 68.38 | 2.51 | 3.39 | 10.02 |
| 4030.1 | 0.13 | 68.13 | 2.51 | 3.37 | 9.27 |
| 4030.6 | 0.13 | 67.38 | 2.52 | 3.39 | 9.72 |
| 4031.1 | 0.13 | 66.88 | 2.53 | 3.46 | 11.38 |
| 4031.6 | 0.12 | 67.00 | 2.52 | 3.58 | 11.63 |
| 4032.1 | 0.12 | 67.00 | 2.51 | 3.74 | 12.60 |
| 4032.6 | 0.11 | 67.13 | 2.50 | 3.94 | 12.10 |
| 4033.0 | 0.10 | 66.25 | 2.53 | 4.13 | 11.90 |
| 4033.5 | 0.10 | 65.88 | 2.55 | 4.33 | 10.95 |
| 4034.0 | 0.11 | 64.75 | 2.57 | 4.56 | 10.79 |
| 4034.5 | 0.12 | 64.50 | 2.56 | 4.80 | 13.57 |
| 4035.0 | 0.12 | 64.75 | 2.54 | 4.98 | 14.77 |
| 4035.5 | 0.12 | 65.38 | 2.52 | 5.08 | 16.16 |
| 4036.0 | 0.12 | 66.25 | 2.51 | 5.10 | 15.51 |
| 4036.4 | 0.12 | 66.50 | 2.52 | 5.06 | 16.13 |
| 4036.9 | 0.13 | 66.00 | 2.50 | 4.96 | 16.91 |
| 4037.4 | 0.13 | 66.88 | 2.50 | 4.87 | 14.55 |
| 4037.9 | 0.14 | 66.88 | 2.50 | 4.80 | 14.88 |
| 4038.4 | 0.14 | 67.50 | 2.50 | 4.73 | 12.69 |
| 4038.9 | 0.14 | 68.13 | 2.49 | 4.67 | 13.81 |
| 4039.4 | 0.14 | 67.75 | 2.49 | 4.63 | 12.12 |
| 4039.8 | 0.14 | 67.88 | 2.51 | 4.61 | 12.32 |
| 4040.3 | 0.13 | 67.88 | 2.54 | 4.62 | 12.34 |
| 4040.8 | 0.12 | 67.00 | 2.54 | 4.68 | 12.13 |
| 4041.3 | 0.11 | 66.75 | 2.55 | 4.79 | 12.59 |
| 4041.8 | 0.12 | 66.38 | 2.54 | 4.91 | 12.81 |
| 4042.3 | 0.12 | 65.50 | 2.54 | 5.03 | 12.83 |
| 4042.8 | 0.13 | 65.50 | 2.54 | 5.13 | 11.90 |
| 4043.2 | 0.13 | 65.88 | 2.52 | 5.19 | 11.01 |
| 4043.7 | 0.13 | 65.75 | 2.51 | 5.21 | 12.66 |
| 4044.2 | 0.13 | 66.50 | 2.51 | 5.20 | 13.60 |
| 4044.7 | 0.14 | 66.75 | 2.51 | 5.20 | 14.53 |
| 4045.2 | 0.13 | 67.13 | 2.51 | 5.22 | 14.08 |
| 4045.7 | 0.12 | 67.38 | 2.51 | 5.30 | 14.95 |
| 4046.2 | 0.11 | 66.25 | 2.54 | 5.45 | 13.56 |
| 4046.6 | 0.10 | 65.38 | 2.57 | 5.66 | 13.09 |
| 4047.1 | 0.09 | 63.88 | 2.58 | 5.94 | 11.05 |
| 4047.6 | 0.08 | 62.63 | 2.58 | 6.29 | 12.47 |
| 4048.1 | 0.08 | 62.13 | 2.58 | 6.74 | 12.42 |
| 4048.6 | 0.07 | 61.50 | 2.58 | 7.30 | 13.35 |
| 4049.1 | 0.07 | 61.38 | 2.59 | 7.93 | 13.29 |
| 4049.6 | 0.08 | 60.75 | 2.60 | 8.51 | 12.81 |
| 4050.1 | 0.08 | 60.00 | 2.60 | 8.91 | 12.81 |
| 4050.5 | 0.10 | 59.75 | 2.61 | 9.09 | 11.63 |
| 4051.0 | 0.11 | 59.75 | 2.61 | 9.12 | 13.74 |
| 4051.5 | 0.11 | 60.00 | 2.61 | 9.07 | 15.18 |
| 4052.0 | 0.11 | 60.63 | 2.60 | 8.88 | 16.91 |
| 4052.5 | 0.10 | 60.88 | 2.57 | 8.56 | 15.80 |
| 4053.0 | 0.10 | 61.38 | 2.57 | 8.29 | 13.16 |
| 4053.5 | 0.09 | 61.75 | 2.57 | 8.20 | 11.68 |
| 4053.9 | 0.09 | 61.50 | 2.57 | 8.19 | 10.97 |
| 4054.4 | 0.09 | 61.50 | 2.58 | 8.24 | 13.12 |
| 4054.9 | 0.09 | 61.13 | 2.59 | 8.42 | 15.42 |
| 4055.4 | 0.08 | 60.88 | 2.61 | 8.63 | 15.66 |
| 4055.9 | 0.09 | 60.63 | 2.62 | 8.76 | 15.25 |
| 4056.4 | 0.09 | 60.00 | 2.62 | 8.83 | 14.16 |
| 4056.9 | 0.09 | 59.50 | 2.62 | 8.85 | 12.98 |
| 4057.3 | 0.09 | 59.75 | 2.62 | 8.79 | 13.61 |
| 4057.8 | 0.10 | 60.00 | 2.60 | 8.58 | 13.57 |
| 4058.3 | 0.11 | 60.75 | 2.58 | 8.27 | 13.77 |
| 4058.8 | 0.11 | 61.25 | 2.56 | 7.96 | 10.66 |
| 4059.3 | 0.11 | 62.25 | 2.55 | 7.69 | 10.22 |
| 4059.8 | 0.11 | 63.38 | 2.54 | 7.44 | 10.96 |
| 4060.3 | 0.10 | 63.88 | 2.54 | 7.20 | 12.83 |
| 4060.7 | 0.10 | 64.25 | 2.54 | 6.97 | 12.36 |
| 4061.2 | 0.10 | 63.63 | 2.56 | 6.75 | 11.91 |
| 4061.7 | 0.11 | 63.63 | 2.57 | 6.55 | 11.24 |
| 4062.2 | 0.12 | 63.00 | 2.57 | 6.36 | 10.05 |
| 4062.7 | 0.12 | 63.50 | 2.55 | 6.20 | 10.73 |
| 4063.2 | 0.12 | 64.50 | 2.52 | 6.06 | 12.59 |
| 4063.7 | 0.12 | 65.38 | 2.53 | 5.91 | 13.31 |
| 4064.1 | 0.12 | 66.00 | 2.53 | 5.75 | 12.33 |
| 4064.6 | 0.12 | 65.38 | 2.55 | 5.65 | 10.93 |
| 4065.1 | 0.12 | 65.63 | 2.55 | 5.62 | 12.66 |
| 4065.6 | 0.12 | 64.88 | 2.54 | 5.63 | 14.13 |
| 4066.1 | 0.11 | 64.63 | 2.56 | 5.68 | 13.20 |
| 4066.6 | 0.12 | 64.00 | 2.56 | 5.79 | 11.70 |
| 4067.1 | 0.12 | 63.88 | 2.55 | 5.91 | 10.23 |
| 4067.5 | 0.12 | 63.88 | 2.55 | 6.04 | 11.15 |
| 4068.0 | 0.12 | 63.88 | 2.54 | 6.16 | 10.91 |
| 4068.5 | 0.11 | 64.00 | 2.54 | 6.29 | 10.69 |
| 4069.0 | 0.11 | 64.25 | 2.54 | 6.41 | 9.98 |
| 4069.5 | 0.11 | 64.00 | 2.54 | 6.51 | 10.69 |
| 4070.0 | 0.12 | 64.50 | 2.55 | 6.58 | 10.91 |
| 4070.5 | 0.13 | 64.25 | 2.55 | 6.61 | 10.95 |
| 4071.0 | 0.12 | 64.50 | 2.55 | 6.62 | 9.31 |
| 4071.4 | 0.11 | 64.75 | 2.55 | 6.63 | 9.10 |
| 4071.9 | 0.11 | 65.13 | 2.55 | 6.67 | 9.78 |
| 4072.4 | 0.11 | 65.00 | 2.55 | 6.73 | 10.71 |
| 4072.9 | 0.11 | 64.63 | 2.56 | 6.78 | 12.63 |
| 4073.4 | 0.11 | 64.13 | 2.57 | 6.81 | 12.86 |
| 4073.9 | 0.12 | 63.63 | 2.58 | 6.85 | 13.33 |
| 4074.4 | 0.11 | 63.50 | 2.57 | 6.90 | 11.68 |
| 4074.8 | 0.11 | 63.63 | 2.57 | 6.96 | 12.20 |
| 4075.3 | 0.11 | 63.50 | 2.56 | 7.06 | 11.54 |
| 4075.8 | 0.10 | 63.38 | 2.57 | 7.19 | 11.73 |
| 4076.3 | 0.10 | 63.13 | 2.57 | 7.34 | 10.97 |
| 4076.8 | 0.10 | 62.63 | 2.59 | 7.52 | 11.16 |
| 4077.3 | 0.10 | 62.63 | 2.59 | 7.78 | 12.77 |
| 4077.8 | 0.09 | 62.00 | 2.59 | 8.12 | 13.01 |
| 4078.2 | 0.09 | 62.00 | 2.59 | 8.54 | 13.03 |
| 4078.7 | 0.08 | 62.00 | 2.59 | 9.05 | 12.34 |
| 4079.2 | 0.08 | 61.75 | 2.61 | 9.59 | 13.05 |
| 4079.7 | 0.08 | 60.88 | 2.60 | 8.16 | 15.26 |
| 4080.2 | 0.08 | 60.88 | 2.59 | 9.82 | 15.54 |
| 4080.7 | 0.08 | 60.38 | 2.60 | 8.55 | 15.13 |
| 4081.2 | 0.07 | 60.13 | 2.61 | 8.31 | 13.88 |
| 4081.6 | 0.06 | 59.38 | 2.63 | 9.22 | 14.10 |
| 4082.1 | 0.05 | 58.63 | 2.63 | 9.34 | 13.83 |
| 4082.6 | 0.04 | 58.25 | 2.65 | 10.56 | 14.05 |
| 4083.1 | 0.04 | 57.63 | 2.66 | 10.98 | 14.72 |
| 4083.6 | 0.03 | 57.13 | 2.67 | 13.94 | 15.74 |
| 4084.1 | 0.02 | 56.50 | 2.66 | 12.42 | 14.09 |
| 4084.6 | 0.02 | 55.50 | 2.67 | 11.39 | 14.91 |
| 4085.0 | 0.01 | 54.75 | 2.69 | 11.92 | 13.90 |
| 4085.5 | 0.01 | 53.38 | 2.73 | 12.04 | 16.47 |
| 4086.0 | 0.01 | 52.50 | 2.73 | 10.22 | 14.75 |
| 4086.5 | 0.01 | 51.63 | 2.71 | 10.00 | 15.90 |
| 4087.0 | 0.01 | 51.38 | 2.70 | 10.81 | 15.91 |
| 4087.5 | 0.01 | 51.50 | 2.69 | 10.34 | 15.95 |
| 4088.0 | 0.01 | 51.88 | 2.69 | 10.31 | 19.23 |
| 4088.5 | 0.01 | 51.88 | 2.69 | 10.22 | 18.73 |
| 4088.9 | 0.01 | 52.13 | 2.71 | 10.63 | 19.45 |
| 4089.4 | 0.02 | 52.00 | 2.72 | 11.69 | 16.94 |
| 4089.9 | 0.02 | 52.00 | 2.72 | 11.72 | 15.20 |
| 4090.4 | 0.02 | 51.88 | 2.71 | 9.88 | 16.31 |
| 4090.9 | 0.04 | 51.75 | 2.72 | 9.72 | 17.00 |
| 4091.4 | 0.06 | 53.38 | 2.73 | 9.03 | 16.09 |
| 4091.9 | 0.08 | 56.38 | 2.71 | 10.09 | 16.44 |
| 4092.3 | 0.09 | 58.63 | 2.70 | 10.34 | 17.50 |
| 4092.8 | 0.08 | 60.13 | 2.69 | 10.58 | 16.50 |
| 4093.3 | 0.07 | 60.63 | 2.69 | 11.53 | 16.88 |
| 4093.8 | 0.07 | 59.75 | 2.68 | 11.31 | 16.47 |
| 4094.3 | 0.09 | 58.88 | 2.68 | 11.44 | 17.31 |
| 4094.8 | 0.11 | 59.25 | 2.67 | 11.22 | 17.59 |
| 4095.3 | 0.12 | 60.88 | 2.67 | 11.53 | 17.91 |
| 4095.7 | 0.12 | 62.63 | 2.66 | 12.13 | 17.09 |

Table A2.4: Neutron porosity, sonic transit time, bulk density, deep induction resistivity and gamma ray data for the Great Oolite Formation in the Hesters Copse-1 well.

| TVDSS (ft) | N.PHI (p.u.) | SONIC T. (µsec/ft) | DENS. (g/cm3) | RESIS. (Ω.m-1) | GR (API) |
| --- | --- | --- | --- | --- | --- |
| 3551.0 | 0.23 | 73.38 | 2.43 | 5.66 | 25.75 |
| 3551.5 | 0.16 | 68.75 | 2.56 | 6.64 | 18.95 |
| 3552.0 | 0.12 | 58.78 | 2.55 | 7.41 | 17.03 |
| 3552.5 | 0.14 | 62.78 | 2.54 | 8.14 | 17.81 |
| 3553.0 | 0.15 | 64.75 | 2.53 | 10.06 | 17.05 |
| 3553.5 | 0.15 | 65.19 | 2.53 | 10.89 | 14.88 |
| 3554.0 | 0.15 | 64.38 | 2.53 | 10.72 | 14.03 |
| 3554.5 | 0.16 | 65.00 | 2.54 | 10.01 | 13.39 |
| 3555.0 | 0.16 | 65.56 | 2.52 | 9.26 | 14.55 |
| 3555.5 | 0.17 | 66.19 | 2.51 | 8.36 | 15.94 |
| 3556.0 | 0.16 | 67.19 | 2.50 | 8.09 | 17.83 |
| 3556.5 | 0.17 | 67.75 | 2.52 | 8.29 | 16.70 |
| 3557.0 | 0.16 | 66.00 | 2.54 | 8.38 | 16.92 |
| 3557.5 | 0.15 | 65.00 | 2.56 | 8.45 | 16.63 |
| 3558.0 | 0.13 | 63.19 | 2.56 | 8.38 | 18.00 |
| 3558.5 | 0.13 | 62.19 | 2.56 | 8.42 | 18.00 |
| 3559.0 | 0.13 | 62.78 | 2.55 | 8.66 | 19.13 |
| 3559.5 | 0.14 | 63.59 | 2.54 | 8.91 | 19.67 |
| 3560.0 | 0.14 | 64.38 | 2.54 | 9.20 | 18.97 |
| 3560.5 | 0.14 | 65.00 | 2.53 | 9.24 | 16.34 |
| 3561.0 | 0.14 | 66.56 | 2.53 | 9.19 | 17.02 |
| 3561.5 | 0.14 | 66.38 | 2.51 | 9.15 | 17.53 |
| 3562.0 | 0.14 | 66.38 | 2.51 | 9.40 | 14.41 |
| 3562.5 | 0.14 | 66.56 | 2.51 | 9.52 | 15.76 |
| 3563.0 | 0.14 | 66.56 | 2.51 | 9.72 | 15.16 |
| 3563.5 | 0.14 | 66.56 | 2.52 | 9.89 | 15.99 |
| 3564.0 | 0.14 | 66.19 | 2.52 | 9.88 | 14.30 |
| 3564.5 | 0.15 | 66.56 | 2.51 | 9.91 | 15.39 |
| 3565.0 | 0.15 | 67.38 | 2.52 | 9.90 | 15.17 |
| 3565.5 | 0.15 | 67.75 | 2.50 | 9.84 | 16.34 |
| 3566.0 | 0.15 | 68.38 | 2.51 | 9.88 | 17.27 |
| 3566.5 | 0.15 | 68.19 | 2.51 | 10.01 | 17.81 |
| 3567.0 | 0.16 | 68.19 | 2.51 | 10.12 | 16.67 |
| 3567.5 | 0.15 | 67.75 | 2.51 | 10.21 | 15.81 |
| 3568.0 | 0.15 | 67.75 | 2.52 | 10.45 | 14.38 |
| 3568.5 | 0.14 | 67.75 | 2.54 | 10.66 | 14.34 |
| 3569.0 | 0.14 | 67.38 | 2.54 | 11.06 | 13.52 |
| 3569.5 | 0.14 | 66.75 | 2.53 | 11.49 | 17.41 |
| 3570.0 | 0.14 | 67.00 | 2.52 | 11.68 | 17.97 |
| 3570.5 | 0.15 | 67.00 | 2.53 | 11.71 | 17.91 |
| 3571.0 | 0.14 | 67.00 | 2.53 | 11.52 | 16.58 |
| 3571.5 | 0.15 | 67.00 | 2.54 | 11.59 | 17.70 |
| 3572.0 | 0.14 | 66.75 | 2.54 | 11.50 | 18.94 |
| 3572.5 | 0.15 | 67.00 | 2.53 | 11.86 | 18.34 |
| 3573.0 | 0.14 | 66.75 | 2.52 | 12.72 | 18.70 |
| 3573.5 | 0.14 | 67.75 | 2.51 | 13.30 | 17.52 |
| 3574.0 | 0.13 | 68.56 | 2.52 | 13.60 | 15.79 |
| 3574.5 | 0.14 | 67.75 | 2.55 | 13.82 | 13.77 |
| 3575.0 | 0.13 | 65.56 | 2.58 | 13.82 | 16.56 |
| 3575.5 | 0.12 | 63.59 | 2.59 | 14.02 | 21.28 |
| 3576.0 | 0.11 | 61.78 | 2.58 | 14.66 | 21.86 |
| 3576.5 | 0.12 | 61.59 | 2.57 | 14.91 | 20.23 |
| 3577.0 | 0.11 | 61.19 | 2.59 | 15.08 | 16.39 |
| 3577.5 | 0.10 | 61.00 | 2.63 | 14.76 | 17.52 |
| 3578.0 | 0.10 | 60.38 | 2.60 | 14.77 | 17.75 |
| 3578.5 | 0.11 | 59.59 | 2.61 | 14.48 | 20.23 |
| 3579.0 | 0.11 | 60.78 | 2.55 | 14.56 | 19.08 |
| 3579.5 | 0.11 | 60.78 | 2.54 | 14.49 | 19.66 |
| 3580.0 | 0.11 | 60.59 | 2.56 | 14.56 | 19.67 |
| 3580.5 | 0.11 | 61.19 | 2.61 | 14.25 | 20.80 |
| 3581.0 | 0.11 | 60.59 | 2.65 | 14.22 | 21.64 |
| 3581.5 | 0.10 | 60.00 | 2.64 | 13.66 | 20.22 |
| 3582.0 | 0.10 | 60.19 | 2.64 | 13.16 | 18.92 |
| 3582.5 | 0.10 | 60.19 | 2.65 | 12.93 | 20.66 |
| 3583.0 | 0.11 | 62.19 | 2.65 | 12.57 | 21.59 |
| 3583.5 | 0.12 | 62.59 | 2.65 | 12.09 | 22.89 |
| 3584.0 | 0.11 | 62.00 | 2.64 | 11.25 | 21.44 |
| 3584.5 | 0.10 | 61.78 | 2.63 | 10.23 | 21.91 |
| 3585.0 | 0.09 | 60.59 | 2.57 | 9.06 | 24.39 |
| 3585.5 | 0.12 | 66.19 | 2.55 | 8.63 | 29.67 |
| 3586.0 | 0.17 | 71.75 | 2.50 | 8.73 | 33.53 |
| 3586.5 | 0.26 | 71.75 | 2.52 | 8.79 | 31.00 |
| 3587.0 | 0.26 | 72.75 | 2.49 | 8.68 | 24.39 |
| 3587.5 | 0.25 | 68.75 | 2.48 | 8.52 | 17.48 |
| 3588.0 | 0.16 | 67.19 | 2.46 | 8.14 | 16.72 |
| 3588.5 | 0.17 | 69.56 | 2.45 | 8.41 | 15.28 |
| 3589.0 | 0.18 | 70.00 | 2.47 | 9.03 | 14.13 |
| 3589.5 | 0.16 | 69.38 | 2.51 | 9.25 | 14.92 |
| 3590.0 | 0.16 | 68.19 | 2.53 | 9.29 | 15.72 |
| 3590.5 | 0.15 | 65.56 | 2.55 | 9.02 | 17.13 |
| 3591.0 | 0.16 | 66.00 | 2.55 | 8.59 | 16.02 |
| 3591.5 | 0.15 | 65.38 | 2.54 | 8.16 | 15.45 |
| 3592.0 | 0.15 | 64.19 | 2.51 | 7.83 | 15.42 |
| 3592.5 | 0.15 | 64.56 | 2.49 | 7.52 | 15.13 |
| 3593.0 | 0.15 | 64.56 | 2.49 | 7.30 | 15.23 |
| 3593.5 | 0.15 | 64.38 | 2.53 | 7.18 | 15.27 |
| 3594.0 | 0.15 | 64.56 | 2.53 | 7.13 | 15.38 |
| 3594.5 | 0.15 | 64.75 | 2.55 | 7.12 | 15.32 |
| 3595.0 | 0.15 | 63.78 | 2.51 | 7.03 | 14.45 |
| 3595.5 | 0.15 | 64.00 | 2.52 | 6.84 | 13.82 |
| 3596.0 | 0.15 | 64.75 | 2.50 | 6.79 | 13.84 |
| 3596.5 | 0.15 | 64.75 | 2.50 | 6.68 | 16.38 |
| 3597.0 | 0.15 | 65.75 | 2.51 | 6.64 | 18.59 |
| 3597.5 | 0.15 | 65.38 | 2.54 | 6.70 | 22.70 |
| 3598.0 | 0.14 | 64.00 | 2.57 | 6.80 | 23.06 |
| 3598.5 | 0.13 | 63.19 | 2.58 | 6.90 | 21.41 |
| 3599.0 | 0.13 | 62.78 | 2.57 | 7.07 | 20.95 |
| 3599.5 | 0.13 | 63.78 | 2.55 | 7.13 | 22.58 |
| 3600.0 | 0.14 | 63.78 | 2.55 | 7.27 | 26.47 |
| 3600.5 | 0.14 | 64.00 | 2.55 | 7.46 | 22.17 |
| 3601.0 | 0.14 | 64.19 | 2.56 | 7.65 | 17.64 |
| 3601.5 | 0.14 | 64.00 | 2.56 | 7.83 | 13.46 |
| 3602.0 | 0.13 | 63.78 | 2.57 | 7.98 | 16.28 |
| 3602.5 | 0.12 | 63.38 | 2.60 | 8.05 | 18.55 |
| 3603.0 | 0.13 | 63.19 | 2.60 | 8.02 | 21.28 |
| 3603.5 | 0.12 | 62.78 | 2.59 | 8.08 | 21.06 |
| 3604.0 | 0.12 | 62.59 | 2.58 | 8.05 | 19.98 |
| 3604.5 | 0.12 | 62.59 | 2.57 | 8.04 | 17.83 |
| 3605.0 | 0.12 | 62.59 | 2.57 | 8.10 | 15.33 |
| 3605.5 | 0.11 | 62.19 | 2.58 | 8.13 | 16.13 |
| 3606.0 | 0.11 | 62.00 | 2.58 | 8.13 | 16.95 |
| 3606.5 | 0.12 | 61.38 | 2.59 | 8.28 | 18.55 |
| 3607.0 | 0.11 | 61.00 | 2.58 | 8.46 | 17.70 |
| 3607.5 | 0.11 | 60.59 | 2.59 | 8.95 | 17.42 |
| 3608.0 | 0.10 | 60.78 | 2.60 | 9.45 | 16.33 |
| 3608.5 | 0.09 | 60.59 | 2.62 | 9.95 | 16.00 |
| 3609.0 | 0.08 | 59.59 | 2.64 | 10.27 | 15.23 |
| 3609.5 | 0.07 | 59.19 | 2.65 | 10.38 | 16.67 |
| 3610.0 | 0.07 | 59.00 | 2.66 | 10.54 | 21.14 |
| 3610.5 | 0.07 | 61.59 | 2.66 | 10.83 | 26.30 |
| 3611.0 | 0.09 | 65.56 | 2.67 | 11.61 | 31.58 |
| 3611.5 | 0.11 | 65.38 | 2.66 | 12.15 | 31.58 |
| 3612.0 | 0.11 | 65.38 | 2.65 | 12.15 | 28.59 |
| 3612.5 | 0.08 | 62.00 | 2.65 | 11.80 | 24.38 |
| 3613.0 | 0.07 | 59.78 | 2.65 | 10.88 | 26.92 |
| 3613.5 | 0.08 | 61.38 | 2.64 | 10.65 | 29.47 |
| 3614.0 | 0.10 | 62.78 | 2.62 | 10.91 | 29.11 |
| 3614.5 | 0.13 | 63.19 | 2.57 | 10.79 | 22.73 |
| 3615.0 | 0.14 | 64.56 | 2.54 | 10.34 | 18.83 |
| 3615.5 | 0.15 | 63.59 | 2.52 | 9.76 | 17.28 |
| 3616.0 | 0.15 | 64.38 | 2.51 | 8.90 | 17.86 |
| 3616.5 | 0.16 | 65.19 | 2.50 | 8.29 | 18.67 |
| 3617.0 | 0.16 | 66.56 | 2.49 | 7.76 | 17.25 |
| 3617.5 | 0.17 | 68.19 | 2.47 | 7.23 | 16.31 |
| 3618.0 | 0.17 | 70.00 | 2.43 | 6.83 | 15.18 |
| 3618.5 | 0.18 | 71.00 | 2.41 | 6.48 | 16.56 |
| 3619.0 | 0.20 | 72.19 | 2.40 | 6.28 | 16.84 |
| 3619.5 | 0.20 | 73.00 | 2.41 | 6.16 | 17.41 |
| 3620.0 | 0.20 | 73.56 | 2.41 | 5.97 | 16.02 |
| 3620.5 | 0.20 | 74.00 | 2.41 | 5.82 | 14.95 |
| 3621.0 | 0.20 | 74.00 | 2.42 | 5.77 | 14.72 |
| 3621.5 | 0.21 | 73.56 | 2.44 | 5.80 | 15.60 |
| 3622.0 | 0.21 | 72.56 | 2.45 | 5.88 | 17.25 |
| 3622.5 | 0.21 | 72.19 | 2.44 | 6.03 | 18.58 |
| 3623.0 | 0.21 | 71.38 | 2.45 | 6.10 | 18.25 |
| 3623.5 | 0.20 | 69.75 | 2.47 | 6.16 | 18.55 |
| 3624.0 | 0.20 | 69.38 | 2.48 | 6.23 | 19.14 |
| 3624.5 | 0.20 | 68.56 | 2.47 | 6.31 | 22.28 |
| 3625.0 | 0.18 | 68.38 | 2.45 | 6.49 | 21.69 |
| 3625.5 | 0.17 | 69.38 | 2.47 | 6.87 | 18.63 |
| 3626.0 | 0.16 | 68.56 | 2.48 | 7.17 | 15.80 |
| 3626.5 | 0.16 | 68.38 | 2.49 | 7.35 | 14.72 |
| 3627.0 | 0.16 | 68.19 | 2.49 | 7.55 | 16.69 |
| 3627.5 | 0.16 | 68.00 | 2.48 | 7.73 | 14.98 |
| 3628.0 | 0.16 | 68.00 | 2.49 | 8.04 | 16.59 |
| 3628.5 | 0.15 | 67.75 | 2.50 | 8.39 | 14.84 |
| 3629.0 | 0.15 | 67.19 | 2.51 | 8.62 | 16.80 |
| 3629.5 | 0.14 | 66.56 | 2.51 | 8.71 | 13.73 |
| 3630.0 | 0.14 | 65.75 | 2.52 | 8.81 | 13.73 |
| 3630.5 | 0.14 | 65.56 | 2.53 | 8.94 | 11.79 |
| 3631.0 | 0.14 | 65.56 | 2.54 | 9.08 | 13.48 |
| 3631.5 | 0.14 | 65.19 | 2.55 | 9.31 | 13.88 |
| 3632.0 | 0.13 | 64.75 | 2.55 | 9.70 | 15.91 |
| 3632.5 | 0.12 | 63.78 | 2.56 | 10.09 | 15.93 |
| 3633.0 | 0.12 | 63.38 | 2.57 | 10.39 | 16.09 |
| 3633.5 | 0.12 | 63.00 | 2.58 | 10.98 | 17.13 |
| 3634.0 | 0.11 | 62.38 | 2.60 | 11.45 | 18.53 |
| 3634.5 | 0.11 | 61.78 | 2.60 | 11.70 | 19.09 |
| 3635.0 | 0.11 | 61.78 | 2.60 | 11.73 | 21.05 |
| 3635.5 | 0.12 | 62.19 | 2.57 | 11.50 | 20.50 |
| 3636.0 | 0.14 | 63.38 | 2.53 | 10.97 | 20.47 |
| 3636.5 | 0.17 | 64.38 | 2.50 | 10.20 | 16.91 |
| 3637.0 | 0.17 | 65.38 | 2.49 | 9.41 | 16.08 |
| 3637.5 | 0.17 | 66.19 | 2.48 | 8.59 | 15.34 |
| 3638.0 | 0.17 | 68.19 | 2.45 | 7.72 | 17.63 |
| 3638.5 | 0.18 | 70.00 | 2.42 | 6.97 | 18.70 |
| 3639.0 | 0.19 | 72.19 | 2.40 | 6.29 | 17.84 |
| 3639.5 | 0.20 | 74.19 | 2.40 | 5.90 | 15.80 |
| 3640.0 | 0.21 | 76.19 | 2.39 | 5.52 | 13.55 |
| 3640.5 | 0.22 | 76.75 | 2.39 | 5.30 | 15.17 |
| 3641.0 | 0.22 | 76.19 | 2.39 | 5.09 | 15.66 |
| 3641.5 | 0.21 | 75.38 | 2.40 | 5.00 | 17.95 |
| 3642.0 | 0.22 | 74.75 | 2.40 | 4.92 | 17.69 |
| 3642.5 | 0.21 | 75.00 | 2.39 | 4.87 | 16.94 |
| 3643.0 | 0.22 | 75.75 | 2.38 | 4.85 | 14.72 |
| 3643.5 | 0.22 | 76.00 | 2.38 | 4.85 | 13.31 |
| 3644.0 | 0.22 | 75.75 | 2.39 | 4.92 | 13.52 |
| 3644.5 | 0.22 | 74.75 | 2.41 | 5.00 | 14.04 |
| 3645.0 | 0.23 | 74.38 | 2.41 | 5.13 | 15.45 |
| 3645.5 | 0.21 | 73.75 | 2.41 | 5.30 | 15.48 |
| 3646.0 | 0.21 | 73.75 | 2.41 | 5.52 | 15.76 |
| 3646.5 | 0.22 | 74.00 | 2.42 | 5.84 | 15.20 |
| 3647.0 | 0.22 | 73.38 | 2.42 | 6.18 | 15.73 |
| 3647.5 | 0.20 | 73.75 | 2.43 | 6.63 | 16.64 |
| 3648.0 | 0.19 | 73.19 | 2.44 | 7.14 | 16.67 |
| 3648.5 | 0.18 | 71.19 | 2.47 | 7.70 | 16.45 |
| 3649.0 | 0.17 | 70.00 | 2.48 | 8.34 | 15.86 |
| 3649.5 | 0.17 | 68.38 | 2.48 | 8.86 | 17.20 |
| 3650.0 | 0.17 | 68.00 | 2.46 | 9.40 | 16.34 |
| 3650.5 | 0.18 | 69.19 | 2.45 | 9.57 | 17.72 |
| 3651.0 | 0.19 | 69.38 | 2.45 | 9.58 | 14.95 |
| 3651.5 | 0.20 | 69.56 | 2.46 | 9.41 | 14.91 |
| 3652.0 | 0.19 | 69.75 | 2.46 | 9.06 | 13.24 |
| 3652.5 | 0.19 | 69.56 | 2.45 | 8.60 | 12.98 |
| 3653.0 | 0.18 | 70.00 | 2.44 | 8.24 | 12.47 |
| 3653.5 | 0.19 | 71.38 | 2.44 | 7.75 | 12.27 |
| 3654.0 | 0.19 | 72.00 | 2.43 | 7.23 | 13.97 |
| 3654.5 | 0.19 | 73.00 | 2.42 | 6.80 | 14.20 |
| 3655.0 | 0.18 | 73.75 | 2.42 | 6.45 | 14.92 |
| 3655.5 | 0.18 | 73.56 | 2.42 | 6.19 | 14.01 |
| 3656.0 | 0.19 | 74.19 | 2.42 | 6.06 | 16.02 |
| 3656.5 | 0.20 | 74.38 | 2.41 | 5.89 | 18.00 |
| 3657.0 | 0.21 | 73.75 | 2.41 | 5.88 | 19.69 |
| 3657.5 | 0.21 | 73.75 | 2.43 | 5.86 | 17.11 |
| 3658.0 | 0.21 | 73.56 | 2.43 | 5.94 | 14.28 |
| 3658.5 | 0.21 | 73.00 | 2.44 | 6.11 | 12.12 |
| 3659.0 | 0.21 | 72.38 | 2.44 | 6.31 | 14.38 |
| 3659.5 | 0.20 | 72.56 | 2.43 | 6.50 | 15.90 |
| 3660.0 | 0.20 | 72.56 | 2.43 | 6.66 | 17.84 |
| 3660.5 | 0.20 | 72.00 | 2.43 | 6.86 | 17.00 |
| 3661.0 | 0.21 | 71.38 | 2.44 | 7.06 | 16.64 |
| 3661.5 | 0.19 | 71.19 | 2.44 | 7.27 | 15.19 |
| 3662.0 | 0.20 | 71.19 | 2.44 | 7.53 | 14.64 |
| 3662.5 | 0.20 | 70.56 | 2.45 | 7.81 | 14.34 |
| 3663.0 | 0.19 | 70.38 | 2.46 | 8.01 | 14.31 |
| 3663.5 | 0.18 | 69.00 | 2.47 | 8.52 | 16.03 |
| 3664.0 | 0.17 | 67.56 | 2.47 | 8.95 | 15.23 |
| 3664.5 | 0.16 | 67.75 | 2.47 | 9.53 | 15.91 |
| 3665.0 | 0.18 | 67.19 | 2.48 | 10.22 | 15.07 |
| 3665.5 | 0.19 | 67.00 | 2.49 | 10.81 | 16.16 |
| 3666.0 | 0.18 | 67.19 | 2.49 | 11.53 | 15.23 |
| 3666.5 | 0.17 | 66.00 | 2.49 | 12.11 | 14.63 |
| 3667.0 | 0.15 | 65.19 | 2.51 | 12.73 | 15.20 |
| 3667.5 | 0.13 | 64.19 | 2.54 | 13.41 | 16.09 |
| 3668.0 | 0.10 | 63.19 | 2.59 | 14.20 | 19.19 |
| 3668.5 | 0.09 | 61.78 | 2.64 | 15.54 | 18.58 |
| 3669.0 | 0.07 | 60.38 | 2.69 | 17.42 | 19.64 |

Table A2.5: Neutron porosity, sonic transit time, bulk density, deep induction resistivity and gamma ray data for the Great Oolite Formation in the Chilgrove-1 well.

| TVDSS (ft) | N.PHI (p.u.) | SONIC T. (µsec/ft) | DENS. (g/cm3) | RESIS. (Ω.m-1) | GR (API) |
| --- | --- | --- | --- | --- | --- |
| 4189.0 | 0.14 | 61.88 | 2.58 | 16.49 | 51.13 |
| 4189.5 | 0.14 | 64.38 | 2.57 | 13.24 | 52.88 |
| 4190.0 | 0.13 | 65.00 | 2.57 | 11.26 | 50.50 |
| 4190.5 | 0.14 | 64.38 | 2.58 | 10.97 | 39.75 |
| 4191.0 | 0.14 | 65.38 | 2.57 | 13.55 | 33.56 |
| 4191.5 | 0.14 | 66.38 | 2.55 | 12.33 | 29.39 |
| 4192.0 | 0.12 | 65.75 | 2.54 | 12.01 | 28.66 |
| 4192.5 | 0.12 | 65.25 | 2.54 | 11.78 | 27.67 |
| 4193.0 | 0.11 | 64.75 | 2.56 | 11.13 | 24.20 |
| 4193.5 | 0.12 | 64.50 | 2.56 | 10.47 | 24.45 |
| 4194.0 | 0.12 | 64.50 | 2.56 | 10.76 | 24.34 |
| 4194.5 | 0.11 | 64.63 | 2.51 | 10.56 | 27.19 |
| 4195.0 | 0.12 | 64.25 | 2.49 | 10.46 | 26.55 |
| 4195.5 | 0.13 | 66.38 | 2.47 | 9.92 | 27.55 |
| 4196.0 | 0.13 | 63.50 | 2.52 | 10.16 | 25.20 |
| 4196.5 | 0.15 | 65.00 | 2.53 | 10.27 | 23.61 |
| 4197.0 | 0.16 | 66.25 | 2.54 | 9.34 | 22.50 |
| 4197.5 | 0.15 | 66.63 | 2.54 | 9.15 | 22.75 |
| 4198.0 | 0.13 | 66.63 | 2.56 | 9.22 | 20.14 |
| 4198.5 | 0.13 | 66.38 | 2.57 | 10.92 | 18.66 |
| 4199.0 | 0.14 | 66.38 | 2.57 | 12.71 | 16.27 |
| 4199.5 | 0.15 | 66.25 | 2.57 | 12.76 | 16.92 |
| 4200.0 | 0.14 | 66.88 | 2.58 | 11.58 | 16.66 |
| 4200.5 | 0.13 | 65.38 | 2.61 | 12.42 | 17.67 |
| 4201.0 | 0.12 | 64.50 | 2.60 | 16.48 | 17.86 |
| 4201.5 | 0.11 | 64.13 | 2.59 | 17.21 | 17.44 |
| 4202.0 | 0.11 | 63.88 | 2.57 | 17.58 | 18.31 |
| 4202.5 | 0.11 | 63.75 | 2.59 | 17.60 | 19.58 |
| 4203.0 | 0.11 | 64.25 | 2.62 | 22.47 | 19.89 |
| 4203.5 | 0.11 | 63.75 | 2.64 | 17.96 | 19.38 |
| 4204.0 | 0.11 | 64.63 | 2.66 | 15.35 | 18.36 |
| 4204.5 | 0.11 | 64.25 | 2.67 | 15.10 | 18.98 |
| 4205.0 | 0.10 | 63.00 | 2.68 | 15.40 | 17.20 |
| 4205.5 | 0.09 | 61.38 | 2.66 | 16.09 | 17.48 |
| 4206.0 | 0.08 | 59.63 | 2.63 | 16.74 | 16.63 |
| 4206.5 | 0.08 | 58.63 | 2.61 | 18.19 | 17.17 |
| 4207.0 | 0.08 | 58.63 | 2.60 | 19.75 | 18.27 |
| 4207.5 | 0.10 | 59.75 | 2.57 | 18.71 | 20.23 |
| 4208.0 | 0.11 | 63.00 | 2.55 | 11.30 | 21.70 |
| 4208.5 | 0.12 | 65.50 | 2.51 | 10.22 | 20.08 |
| 4209.0 | 0.13 | 67.00 | 2.50 | 10.16 | 18.00 |
| 4209.5 | 0.12 | 66.25 | 2.50 | 9.70 | 18.38 |
| 4210.0 | 0.12 | 64.13 | 2.52 | 9.01 | 19.75 |
| 4210.5 | 0.11 | 63.63 | 2.53 | 9.49 | 23.31 |
| 4211.0 | 0.12 | 63.13 | 2.55 | 10.54 | 23.94 |
| 4211.5 | 0.12 | 63.00 | 2.56 | 12.34 | 23.58 |
| 4212.0 | 0.12 | 63.00 | 2.59 | 13.55 | 21.72 |
| 4212.5 | 0.12 | 63.75 | 2.59 | 14.48 | 20.23 |
| 4213.0 | 0.11 | 64.38 | 2.58 | 15.28 | 20.34 |
| 4213.5 | 0.11 | 64.13 | 2.55 | 16.05 | 18.86 |
| 4214.0 | 0.10 | 64.63 | 2.56 | 16.88 | 18.84 |
| 4214.5 | 0.09 | 63.38 | 2.57 | 16.64 | 17.22 |
| 4215.0 | 0.08 | 61.13 | 2.60 | 17.22 | 17.56 |
| 4215.5 | 0.08 | 61.00 | 2.65 | 18.92 | 16.36 |
| 4216.0 | 0.09 | 61.13 | 2.66 | 21.10 | 17.00 |
| 4216.5 | 0.09 | 61.88 | 2.64 | 21.38 | 17.77 |
| 4217.0 | 0.10 | 64.38 | 2.60 | 19.79 | 18.83 |
| 4217.5 | 0.11 | 65.00 | 2.59 | 16.04 | 17.86 |
| 4218.0 | 0.12 | 65.38 | 2.59 | 12.49 | 16.27 |
| 4218.5 | 0.13 | 66.38 | 2.58 | 11.37 | 17.13 |
| 4219.0 | 0.13 | 66.88 | 2.56 | 10.75 | 18.11 |
| 4219.5 | 0.13 | 66.75 | 2.56 | 10.39 | 20.58 |
| 4220.0 | 0.12 | 66.38 | 2.54 | 9.88 | 20.94 |
| 4220.5 | 0.12 | 66.63 | 2.53 | 8.51 | 23.17 |
| 4221.0 | 0.11 | 66.63 | 2.53 | 7.18 | 24.66 |
| 4221.5 | 0.11 | 66.13 | 2.55 | 7.19 | 24.91 |
| 4222.0 | 0.11 | 65.63 | 2.56 | 6.84 | 24.66 |
| 4222.5 | 0.11 | 65.00 | 2.56 | 7.08 | 23.67 |
| 4223.0 | 0.10 | 64.13 | 2.56 | 6.88 | 24.05 |
| 4223.5 | 0.10 | 63.13 | 2.57 | 7.49 | 23.67 |
| 4224.0 | 0.09 | 62.38 | 2.59 | 8.27 | 22.94 |
| 4224.5 | 0.09 | 62.50 | 2.61 | 8.67 | 23.80 |
| 4225.0 | 0.09 | 62.38 | 2.62 | 9.42 | 24.05 |
| 4225.5 | 0.08 | 61.88 | 2.64 | 10.01 | 24.91 |
| 4226.0 | 0.08 | 61.25 | 2.64 | 10.45 | 23.06 |
| 4226.5 | 0.07 | 61.25 | 2.64 | 11.37 | 21.83 |
| 4227.0 | 0.08 | 62.88 | 2.63 | 12.97 | 22.94 |
| 4227.5 | 0.09 | 61.25 | 2.64 | 13.30 | 27.08 |
| 4228.0 | 0.09 | 61.38 | 2.65 | 12.59 | 29.42 |
| 4228.5 | 0.09 | 60.75 | 2.68 | 12.41 | 27.20 |
| 4229.0 | 0.08 | 60.13 | 2.67 | 12.19 | 22.59 |
| 4229.5 | 0.08 | 60.63 | 2.65 | 12.16 | 22.11 |
| 4230.0 | 0.09 | 61.50 | 2.63 | 13.97 | 22.48 |
| 4230.5 | 0.10 | 62.50 | 2.64 | 14.05 | 23.34 |
| 4231.0 | 0.11 | 63.88 | 2.64 | 12.55 | 25.86 |
| 4231.5 | 0.10 | 63.13 | 2.64 | 11.82 | 27.08 |
| 4232.0 | 0.08 | 62.38 | 2.64 | 10.95 | 26.58 |
| 4232.5 | 0.07 | 60.50 | 2.64 | 11.90 | 22.31 |
| 4233.0 | 0.07 | 61.75 | 2.66 | 13.51 | 23.22 |
| 4233.5 | 0.08 | 63.88 | 2.65 | 15.33 | 24.56 |
| 4234.0 | 0.09 | 65.25 | 2.67 | 16.41 | 27.78 |
| 4234.5 | 0.10 | 65.38 | 2.67 | 16.51 | 29.47 |
| 4235.0 | 0.12 | 65.50 | 2.68 | 13.58 | 34.91 |
| 4235.5 | 0.14 | 65.75 | 2.65 | 12.08 | 44.16 |
| 4236.0 | 0.18 | 70.88 | 2.65 | 8.77 | 56.06 |
| 4236.5 | 0.22 | 66.00 | 2.64 | 7.07 | 69.38 |
| 4237.0 | 0.22 | 70.13 | 2.64 | 6.31 | 74.50 |
| 4237.5 | 0.23 | 69.63 | 2.64 | 5.42 | 74.56 |
| 4238.0 | 0.25 | 70.13 | 2.62 | 4.63 | 68.63 |
| 4238.5 | 0.22 | 70.00 | 2.63 | 4.18 | 66.31 |
| 4239.0 | 0.19 | 67.50 | 2.63 | 4.07 | 58.09 |
| 4239.5 | 0.14 | 64.50 | 2.62 | 4.48 | 43.63 |
| 4240.0 | 0.10 | 61.75 | 2.59 | 5.31 | 28.61 |
| 4240.5 | 0.10 | 61.38 | 2.59 | 6.95 | 19.98 |
| 4241.0 | 0.11 | 62.25 | 2.60 | 9.40 | 20.36 |
| 4241.5 | 0.12 | 62.88 | 2.62 | 10.69 | 18.75 |
| 4242.0 | 0.11 | 63.13 | 2.61 | 10.33 | 17.75 |
| 4242.5 | 0.11 | 61.88 | 2.60 | 10.65 | 16.89 |
| 4243.0 | 0.11 | 61.13 | 2.57 | 10.85 | 16.47 |
| 4243.5 | 0.10 | 61.25 | 2.56 | 11.34 | 17.70 |
| 4244.0 | 0.09 | 61.63 | 2.56 | 11.77 | 18.56 |
| 4244.5 | 0.10 | 61.13 | 2.58 | 11.40 | 20.09 |
| 4245.0 | 0.10 | 61.38 | 2.59 | 11.03 | 18.64 |
| 4245.5 | 0.12 | 63.63 | 2.60 | 12.16 | 18.77 |
| 4246.0 | 0.13 | 64.50 | 2.57 | 10.37 | 19.88 |
| 4246.5 | 0.13 | 65.88 | 2.54 | 8.75 | 20.31 |
| 4247.0 | 0.12 | 66.00 | 2.53 | 8.16 | 20.08 |
| 4247.5 | 0.12 | 66.00 | 2.52 | 7.75 | 19.06 |
| 4248.0 | 0.12 | 66.38 | 2.53 | 7.58 | 20.08 |
| 4248.5 | 0.12 | 65.88 | 2.53 | 7.79 | 17.84 |
| 4249.0 | 0.12 | 65.13 | 2.54 | 8.07 | 17.61 |
| 4249.5 | 0.11 | 64.88 | 2.55 | 8.16 | 17.22 |
| 4250.0 | 0.11 | 64.25 | 2.55 | 8.37 | 20.08 |
| 4250.5 | 0.11 | 64.25 | 2.55 | 9.35 | 21.81 |
| 4251.0 | 0.11 | 64.50 | 2.57 | 9.82 | 22.55 |
| 4251.5 | 0.11 | 64.13 | 2.58 | 9.27 | 21.42 |
| 4252.0 | 0.11 | 64.38 | 2.59 | 8.94 | 21.31 |
| 4252.5 | 0.11 | 64.75 | 2.58 | 8.82 | 19.94 |
| 4253.0 | 0.11 | 64.13 | 2.57 | 8.67 | 20.56 |
| 4253.5 | 0.12 | 65.13 | 2.57 | 8.09 | 20.31 |
| 4254.0 | 0.12 | 65.00 | 2.57 | 7.89 | 19.86 |
| 4254.5 | 0.12 | 65.50 | 2.57 | 7.56 | 20.47 |
| 4255.0 | 0.12 | 65.25 | 2.55 | 7.22 | 19.22 |
| 4255.5 | 0.11 | 64.50 | 2.55 | 6.89 | 20.94 |
| 4256.0 | 0.10 | 63.88 | 2.56 | 6.90 | 19.22 |
| 4256.5 | 0.10 | 63.63 | 2.57 | 7.20 | 18.50 |
| 4257.0 | 0.10 | 63.75 | 2.58 | 8.18 | 17.36 |
| 4257.5 | 0.11 | 64.38 | 2.58 | 9.30 | 18.34 |
| 4258.0 | 0.13 | 65.63 | 2.58 | 9.26 | 19.19 |
| 4258.5 | 0.13 | 66.50 | 2.57 | 8.44 | 20.80 |
| 4259.0 | 0.14 | 67.63 | 2.55 | 7.00 | 23.81 |
| 4259.5 | 0.16 | 68.38 | 2.56 | 5.95 | 27.52 |
| 4260.0 | 0.18 | 71.75 | 2.58 | 5.56 | 30.25 |
| 4260.5 | 0.19 | 71.50 | 2.58 | 5.40 | 28.47 |
| 4261.0 | 0.18 | 71.75 | 2.52 | 5.34 | 26.39 |
| 4261.5 | 0.18 | 71.63 | 2.47 | 5.10 | 23.42 |
| 4262.0 | 0.17 | 70.63 | 2.46 | 4.91 | 21.58 |
| 4262.5 | 0.17 | 70.25 | 2.47 | 5.13 | 20.56 |
| 4263.0 | 0.16 | 70.13 | 2.48 | 5.51 | 17.61 |
| 4263.5 | 0.16 | 70.00 | 2.48 | 6.20 | 17.36 |
| 4264.0 | 0.16 | 69.63 | 2.48 | 6.80 | 15.64 |
| 4264.5 | 0.15 | 69.38 | 2.47 | 7.12 | 17.00 |
| 4265.0 | 0.14 | 68.88 | 2.48 | 6.75 | 16.50 |
| 4265.5 | 0.14 | 67.13 | 2.49 | 6.80 | 18.36 |
| 4266.0 | 0.13 | 66.75 | 2.51 | 6.77 | 19.34 |
| 4266.5 | 0.13 | 65.75 | 2.52 | 6.83 | 20.56 |
| 4267.0 | 0.14 | 68.25 | 2.53 | 7.59 | 21.92 |
| 4267.5 | 0.15 | 70.25 | 2.51 | 8.07 | 22.92 |
| 4268.0 | 0.16 | 70.75 | 2.52 | 7.46 | 23.44 |
| 4268.5 | 0.17 | 71.38 | 2.52 | 6.82 | 21.08 |
| 4269.0 | 0.16 | 71.25 | 2.51 | 6.11 | 20.47 |
| 4269.5 | 0.16 | 68.88 | 2.50 | 5.60 | 18.73 |
| 4270.0 | 0.16 | 70.38 | 2.49 | 5.93 | 17.52 |
| 4270.5 | 0.16 | 70.38 | 2.48 | 6.15 | 15.54 |
| 4271.0 | 0.16 | 70.38 | 2.47 | 5.87 | 17.02 |
| 4271.5 | 0.17 | 70.13 | 2.47 | 5.75 | 18.59 |
| 4272.0 | 0.17 | 70.38 | 2.47 | 5.50 | 21.06 |
| 4272.5 | 0.17 | 70.38 | 2.47 | 5.24 | 20.56 |
| 4273.0 | 0.17 | 70.38 | 2.47 | 5.23 | 19.70 |
| 4273.5 | 0.17 | 70.88 | 2.47 | 5.55 | 17.86 |
| 4274.0 | 0.17 | 72.00 | 2.47 | 5.58 | 19.11 |
| 4274.5 | 0.17 | 72.13 | 2.46 | 5.71 | 19.47 |
| 4275.0 | 0.16 | 71.13 | 2.47 | 5.69 | 21.70 |
| 4275.5 | 0.16 | 70.00 | 2.46 | 5.81 | 18.91 |
| 4276.0 | 0.15 | 68.38 | 2.46 | 6.13 | 19.41 |
| 4276.5 | 0.15 | 67.50 | 2.47 | 6.18 | 16.91 |
| 4277.0 | 0.14 | 67.00 | 2.49 | 6.53 | 18.97 |
| 4277.5 | 0.14 | 66.25 | 2.52 | 6.87 | 19.94 |
| 4278.0 | 0.14 | 66.25 | 2.52 | 7.20 | 21.44 |
| 4278.5 | 0.13 | 66.00 | 2.51 | 7.29 | 21.45 |
| 4279.0 | 0.12 | 64.75 | 2.52 | 7.54 | 21.08 |
| 4279.5 | 0.12 | 70.38 | 2.56 | 7.56 | 21.47 |
| 4280.0 | 0.12 | 70.00 | 2.56 | 7.80 | 22.95 |
| 4280.5 | 0.13 | 69.88 | 2.56 | 7.96 | 23.81 |
| 4281.0 | 0.14 | 70.13 | 2.52 | 7.43 | 25.94 |
| 4281.5 | 0.15 | 70.13 | 2.49 | 5.73 | 26.20 |
| 4282.0 | 0.16 | 70.13 | 2.48 | 5.29 | 25.22 |
| 4282.5 | 0.17 | 70.25 | 2.48 | 5.22 | 24.06 |
| 4283.0 | 0.18 | 70.88 | 2.48 | 5.23 | 21.81 |
| 4283.5 | 0.19 | 72.38 | 2.46 | 5.25 | 22.69 |
| 4284.0 | 0.19 | 72.13 | 2.45 | 5.29 | 20.59 |
| 4284.5 | 0.19 | 72.75 | 2.43 | 4.78 | 20.84 |
| 4285.0 | 0.18 | 73.25 | 2.46 | 4.57 | 18.20 |
| 4285.5 | 0.18 | 69.38 | 2.45 | 5.12 | 17.58 |
| 4286.0 | 0.17 | 69.25 | 2.47 | 5.16 | 17.58 |
| 4286.5 | 0.17 | 69.63 | 2.45 | 5.18 | 17.08 |
| 4287.0 | 0.17 | 69.38 | 2.46 | 5.21 | 19.55 |
| 4287.5 | 0.17 | 69.75 | 2.45 | 5.05 | 20.55 |
| 4288.0 | 0.17 | 69.50 | 2.45 | 5.13 | 21.95 |
| 4288.5 | 0.18 | 69.13 | 2.43 | 5.11 | 19.61 |
| 4289.0 | 0.18 | 69.38 | 2.44 | 4.71 | 19.72 |
| 4289.5 | 0.16 | 69.13 | 2.44 | 4.45 | 20.83 |
| 4290.0 | 0.15 | 68.50 | 2.48 | 4.34 | 22.42 |
| 4290.5 | 0.13 | 66.38 | 2.51 | 5.85 | 21.06 |
| 4291.0 | 0.13 | 66.88 | 2.54 | 7.55 | 21.19 |
| 4291.5 | 0.13 | 66.38 | 2.53 | 7.61 | 21.19 |
| 4292.0 | 0.14 | 66.75 | 2.52 | 7.48 | 22.05 |
| 4292.5 | 0.13 | 66.75 | 2.51 | 7.56 | 23.19 |
| 4293.0 | 0.12 | 66.88 | 2.53 | 7.09 | 23.31 |
| 4293.5 | 0.12 | 63.88 | 2.52 | 7.06 | 23.06 |
| 4294.0 | 0.12 | 63.63 | 2.55 | 7.59 | 21.19 |
| 4294.5 | 0.11 | 62.88 | 2.55 | 7.70 | 22.52 |
| 4295.0 | 0.10 | 62.50 | 2.57 | 7.96 | 24.64 |
| 4295.5 | 0.10 | 61.75 | 2.57 | 8.02 | 29.08 |
| 4296.0 | 0.09 | 61.00 | 2.57 | 8.27 | 33.66 |
| 4296.5 | 0.09 | 60.38 | 2.56 | 8.80 | 35.22 |
| 4297.0 | 0.09 | 60.75 | 2.56 | 8.54 | 35.72 |
| 4297.5 | 0.09 | 60.50 | 2.57 | 8.14 | 32.53 |
| 4298.0 | 0.08 | 60.13 | 2.58 | 8.41 | 30.59 |
| 4298.5 | 0.08 | 60.38 | 2.59 | 8.73 | 29.23 |
| 4299.0 | 0.08 | 58.88 | 2.61 | 9.02 | 29.36 |
| 4299.5 | 0.08 | 58.75 | 2.62 | 9.37 | 29.81 |
| 4300.0 | 0.07 | 57.63 | 2.61 | 9.82 | 30.23 |
| 4300.5 | 0.07 | 58.13 | 2.61 | 10.53 | 30.13 |
| 4301.0 | 0.06 | 58.00 | 2.61 | 11.17 | 32.03 |
| 4301.5 | 0.06 | 58.13 | 2.61 | 12.25 | 32.16 |
| 4302.0 | 0.06 | 58.00 | 2.61 | 13.76 | 32.28 |
| 4302.5 | 0.06 | 57.63 | 2.62 | 15.40 | 32.28 |
| 4303.0 | 0.06 | 57.75 | 2.62 | 16.78 | 34.19 |
| 4303.5 | 0.06 | 59.13 | 2.64 | 16.79 | 33.13 |
| 4304.0 | 0.07 | 60.38 | 2.65 | 16.21 | 32.06 |
| 4304.5 | 0.07 | 60.63 | 2.65 | 14.82 | 30.34 |
| 4305.0 | 0.07 | 60.88 | 2.65 | 13.35 | 33.09 |
| 4305.5 | 0.07 | 60.63 | 2.65 | 12.11 | 31.89 |
| 4306.0 | 0.06 | 60.13 | 2.67 | 11.77 | 29.58 |
| 4306.5 | 0.06 | 59.38 | 2.67 | 12.95 | 26.42 |
| 4307.0 | 0.05 | 58.13 | 2.68 | 14.14 | 26.53 |
| 4307.5 | 0.05 | 57.00 | 2.67 | 16.68 | 26.28 |
| 4308.0 | 0.05 | 56.88 | 2.68 | 20.92 | 24.91 |
| 4308.5 | 0.05 | 56.88 | 2.67 | 23.37 | 24.05 |
| 4309.0 | 0.05 | 57.88 | 2.67 | 24.32 | 24.77 |
| 4309.5 | 0.05 | 57.88 | 2.66 | 23.31 | 24.27 |
| 4310.0 | 0.05 | 58.25 | 2.65 | 22.12 | 25.52 |
| 4310.5 | 0.06 | 58.63 | 2.65 | 21.50 | 25.03 |
| 4311.0 | 0.06 | 59.63 | 2.65 | 20.23 | 27.02 |
| 4311.5 | 0.06 | 59.50 | 2.65 | 19.02 | 26.27 |
| 4312.0 | 0.06 | 59.75 | 2.65 | 18.80 | 28.53 |
| 4312.5 | 0.06 | 59.50 | 2.65 | 17.57 | 29.89 |
| 4313.0 | 0.06 | 58.63 | 2.66 | 16.90 | 28.39 |
| 4313.5 | 0.05 | 56.63 | 2.67 | 17.36 | 24.03 |
| 4314.0 | 0.04 | 55.88 | 2.68 | 20.25 | 20.45 |
| 4314.5 | 0.05 | 54.50 | 2.67 | 22.50 | 19.47 |
| 4315.0 | 0.05 | 55.75 | 2.65 | 25.59 | 18.97 |
| 4315.5 | 0.06 | 55.63 | 2.64 | 28.08 | 17.61 |
| 4316.0 | 0.06 | 57.00 | 2.62 | 26.68 | 16.09 |
| 4316.5 | 0.06 | 56.75 | 2.62 | 24.95 | 16.47 |
| 4317.0 | 0.06 | 57.38 | 2.61 | 20.01 | 17.08 |
| 4317.5 | 0.07 | 57.63 | 2.60 | 16.45 | 18.58 |
| 4318.0 | 0.07 | 58.00 | 2.60 | 11.60 | 19.56 |
| 4318.5 | 0.08 | 58.50 | 2.60 | 10.95 | 20.44 |
| 4319.0 | 0.08 | 57.00 | 2.59 | 10.83 | 20.20 |
| 4319.5 | 0.10 | 59.38 | 2.57 | 10.93 | 19.97 |
| 4320.0 | 0.12 | 61.00 | 2.55 | 10.89 | 20.20 |
| 4320.5 | 0.13 | 63.50 | 2.53 | 10.52 | 19.09 |
| 4321.0 | 0.13 | 64.25 | 2.53 | 9.59 | 18.36 |
| 4321.5 | 0.13 | 65.13 | 2.53 | 9.55 | 17.48 |
| 4322.0 | 0.15 | 65.38 | 2.51 | 8.76 | 19.45 |
| 4322.5 | 0.17 | 67.88 | 2.50 | 7.47 | 20.19 |
| 4323.0 | 0.17 | 68.63 | 2.47 | 6.73 | 21.17 |
| 4323.5 | 0.17 | 70.38 | 2.45 | 5.85 | 21.30 |
| 4324.0 | 0.16 | 70.13 | 2.45 | 5.49 | 22.30 |
| 4324.5 | 0.17 | 70.38 | 2.45 | 5.86 | 23.55 |
| 4325.0 | 0.16 | 70.75 | 2.46 | 5.94 | 22.81 |
| 4325.5 | 0.16 | 70.00 | 2.48 | 5.43 | 20.47 |
| 4326.0 | 0.15 | 69.38 | 2.49 | 5.28 | 18.08 |
| 4326.5 | 0.15 | 68.75 | 2.48 | 5.05 | 18.83 |
| 4327.0 | 0.15 | 68.25 | 2.49 | 4.86 | 19.45 |
| 4327.5 | 0.15 | 67.25 | 2.50 | 5.23 | 18.88 |
| 4328.0 | 0.15 | 67.38 | 2.50 | 5.67 | 17.77 |
| 4328.5 | 0.14 | 67.25 | 2.48 | 5.47 | 15.66 |
| 4329.0 | 0.15 | 67.13 | 2.49 | 5.53 | 15.25 |
| 4329.5 | 0.15 | 68.13 | 2.49 | 5.50 | 16.36 |
| 4330.0 | 0.16 | 68.38 | 2.50 | 5.52 | 17.72 |
| 4330.5 | 0.16 | 69.75 | 2.48 | 5.53 | 19.97 |
| 4331.0 | 0.17 | 72.50 | 2.47 | 5.49 | 20.08 |
| 4331.5 | 0.18 | 73.63 | 2.45 | 5.66 | 18.94 |
| 4332.0 | 0.19 | 75.50 | 2.44 | 5.46 | 19.80 |
| 4332.5 | 0.18 | 74.63 | 2.42 | 5.10 | 18.17 |
| 4333.0 | 0.18 | 73.88 | 2.41 | 3.37 | 20.92 |
| 4333.5 | 0.18 | 73.63 | 2.41 | 3.40 | 19.56 |
| 4334.0 | 0.18 | 72.75 | 2.42 | 3.41 | 20.19 |
| 4334.5 | 0.17 | 72.50 | 2.44 | 3.40 | 19.44 |
| 4335.0 | 0.16 | 72.25 | 2.45 | 3.45 | 19.06 |
| 4335.5 | 0.16 | 72.63 | 2.45 | 3.45 | 20.44 |
| 4336.0 | 0.16 | 72.00 | 2.46 | 3.41 | 20.94 |
| 4336.5 | 0.17 | 71.75 | 2.45 | 3.52 | 20.20 |
| 4337.0 | 0.17 | 71.25 | 2.47 | 3.45 | 19.47 |
| 4337.5 | 0.17 | 71.00 | 2.49 | 3.47 | 18.47 |
| 4338.0 | 0.16 | 71.13 | 2.49 | 3.40 | 21.31 |
| 4338.5 | 0.16 | 70.13 | 2.48 | 3.44 | 21.20 |
| 4339.0 | 0.17 | 70.63 | 2.46 | 3.50 | 22.44 |
| 4339.5 | 0.18 | 69.63 | 2.45 | 3.41 | 19.97 |
| 4340.0 | 0.17 | 69.63 | 2.44 | 3.54 | 21.84 |
| 4340.5 | 0.16 | 69.75 | 2.45 | 3.25 | 23.94 |
| 4341.0 | 0.15 | 67.75 | 2.47 | 3.04 | 23.94 |
| 4341.5 | 0.14 | 67.38 | 2.48 | 2.68 | 21.17 |
| 4342.0 | 0.13 | 66.13 | 2.49 | 3.24 | 19.09 |
| 4342.5 | 0.13 | 64.88 | 2.53 | 3.49 | 21.17 |
| 4343.0 | 0.12 | 64.50 | 2.56 | 4.15 | 22.92 |
| 4343.5 | 0.11 | 62.88 | 2.58 | 5.34 | 25.13 |
| 4344.0 | 0.11 | 62.63 | 2.58 | 6.97 | 26.98 |
| 4344.5 | 0.12 | 62.63 | 2.56 | 7.02 | 33.50 |
| 4345.0 | 0.13 | 63.88 | 2.54 | 6.58 | 37.31 |
| 4345.5 | 0.14 | 64.75 | 2.51 | 6.30 | 42.63 |
| 4346.0 | 0.15 | 67.25 | 2.49 | 5.50 | 43.34 |
| 4346.5 | 0.15 | 68.38 | 2.48 | 5.05 | 44.47 |
| 4347.0 | 0.16 | 69.13 | 2.47 | 4.20 | 41.91 |
| 4347.5 | 0.17 | 70.13 | 2.48 | 4.02 | 36.41 |
| 4348.0 | 0.18 | 70.75 | 2.48 | 3.62 | 30.13 |
| 4348.5 | 0.18 | 71.63 | 2.47 | 3.59 | 25.67 |
| 4349.0 | 0.18 | 71.50 | 2.45 | 3.42 | 23.91 |
| 4349.5 | 0.17 | 71.75 | 2.45 | 3.43 | 23.30 |
| 4350.0 | 0.18 | 72.00 | 2.45 | 3.37 | 22.19 |
| 4350.5 | 0.18 | 71.75 | 2.46 | 3.39 | 23.44 |
| 4351.0 | 0.17 | 72.00 | 2.46 | 3.46 | 22.20 |
| 4351.5 | 0.17 | 70.63 | 2.47 | 3.45 | 21.48 |
| 4352.0 | 0.17 | 70.50 | 2.47 | 3.47 | 21.33 |
| 4352.5 | 0.17 | 70.25 | 2.47 | 3.56 | 22.44 |
| 4353.0 | 0.16 | 70.00 | 2.46 | 3.46 | 21.81 |
| 4353.5 | 0.16 | 70.25 | 2.46 | 3.38 | 19.95 |
| 4354.0 | 0.15 | 69.13 | 2.46 | 3.38 | 18.59 |
| 4354.5 | 0.15 | 69.00 | 2.47 | 3.36 | 20.22 |
| 4355.0 | 0.15 | 69.13 | 2.48 | 3.53 | 19.36 |
| 4355.5 | 0.15 | 68.88 | 2.49 | 3.74 | 18.00 |
| 4356.0 | 0.14 | 68.38 | 2.49 | 3.88 | 16.52 |
| 4356.5 | 0.14 | 68.00 | 2.49 | 4.11 | 16.63 |
| 4357.0 | 0.13 | 67.38 | 2.51 | 4.23 | 19.95 |
| 4357.5 | 0.13 | 66.63 | 2.52 | 4.19 | 20.19 |
| 4358.0 | 0.12 | 65.50 | 2.53 | 4.28 | 20.69 |
| 4358.5 | 0.12 | 64.88 | 2.54 | 4.53 | 20.58 |
| 4359.0 | 0.13 | 64.25 | 2.53 | 4.83 | 22.44 |
| 4359.5 | 0.12 | 64.50 | 2.53 | 4.82 | 22.55 |
| 4360.0 | 0.12 | 64.25 | 2.53 | 5.31 | 21.30 |
| 4360.5 | 0.11 | 64.88 | 2.54 | 5.41 | 20.31 |
| 4361.0 | 0.11 | 65.50 | 2.54 | 5.40 | 18.47 |
| 4361.5 | 0.11 | 65.63 | 2.54 | 5.98 | 20.22 |
| 4362.0 | 0.12 | 65.50 | 2.53 | 5.95 | 20.84 |
| 4362.5 | 0.13 | 65.25 | 2.54 | 5.92 | 24.17 |
| 4363.0 | 0.13 | 65.88 | 2.54 | 5.66 | 20.50 |
| 4363.5 | 0.13 | 65.63 | 2.55 | 5.46 | 20.13 |
| 4364.0 | 0.13 | 65.50 | 2.56 | 5.27 | 16.95 |
| 4364.5 | 0.13 | 65.38 | 2.56 | 5.02 | 19.39 |
| 4365.0 | 0.13 | 65.88 | 2.55 | 5.03 | 18.30 |
| 4365.5 | 0.13 | 65.38 | 2.53 | 5.11 | 18.88 |
| 4366.0 | 0.12 | 65.63 | 2.53 | 4.99 | 18.14 |
| 4366.5 | 0.13 | 65.75 | 2.52 | 4.90 | 19.23 |
| 4367.0 | 0.13 | 65.63 | 2.51 | 5.16 | 20.58 |
| 4367.5 | 0.14 | 66.00 | 2.51 | 5.14 | 19.47 |
| 4368.0 | 0.14 | 66.63 | 2.51 | 5.02 | 19.97 |
| 4368.5 | 0.14 | 66.38 | 2.53 | 4.73 | 20.22 |
| 4369.0 | 0.14 | 67.00 | 2.53 | 4.22 | 21.81 |
| 4369.5 | 0.14 | 67.00 | 2.52 | 4.16 | 19.19 |
| 4370.0 | 0.14 | 66.75 | 2.51 | 4.38 | 18.94 |
| 4370.5 | 0.14 | 66.50 | 2.50 | 4.09 | 18.69 |
| 4371.0 | 0.13 | 66.63 | 2.49 | 4.33 | 19.09 |
| 4371.5 | 0.12 | 66.38 | 2.49 | 3.90 | 19.09 |
| 4372.0 | 0.12 | 66.50 | 2.49 | 3.68 | 18.48 |
| 4372.5 | 0.12 | 66.63 | 2.49 | 3.89 | 20.20 |
| 4373.0 | 0.12 | 66.25 | 2.51 | 4.19 | 20.20 |
| 4373.5 | 0.12 | 65.88 | 2.52 | 4.56 | 20.95 |
| 4374.0 | 0.12 | 64.75 | 2.52 | 4.68 | 21.45 |
| 4374.5 | 0.12 | 64.25 | 2.51 | 4.84 | 22.20 |
| 4375.0 | 0.12 | 63.88 | 2.51 | 4.84 | 24.03 |
| 4375.5 | 0.12 | 63.00 | 2.51 | 4.89 | 22.53 |
| 4376.0 | 0.11 | 63.13 | 2.52 | 4.76 | 20.67 |
| 4376.5 | 0.11 | 62.38 | 2.52 | 4.92 | 18.08 |
| 4377.0 | 0.10 | 61.63 | 2.56 | 5.22 | 17.97 |
| 4377.5 | 0.10 | 61.38 | 2.58 | 5.39 | 20.81 |
| 4378.0 | 0.10 | 61.00 | 2.60 | 6.30 | 22.94 |
| 4378.5 | 0.09 | 60.75 | 2.60 | 6.64 | 25.55 |
| 4379.0 | 0.09 | 61.25 | 2.61 | 7.02 | 26.58 |
| 4379.5 | 0.09 | 63.13 | 2.61 | 7.21 | 25.56 |
| 4380.0 | 0.09 | 62.88 | 2.60 | 7.17 | 25.08 |
| 4380.5 | 0.09 | 63.13 | 2.59 | 7.42 | 25.95 |
| 4381.0 | 0.08 | 62.75 | 2.60 | 7.43 | 29.78 |
| 4381.5 | 0.09 | 62.88 | 2.60 | 8.17 | 33.81 |
| 4382.0 | 0.09 | 63.00 | 2.62 | 8.68 | 36.47 |
| 4382.5 | 0.09 | 62.75 | 2.62 | 9.23 | 36.59 |
| 4383.0 | 0.10 | 62.88 | 2.62 | 9.69 | 37.44 |
| 4383.5 | 0.10 | 63.25 | 2.59 | 9.59 | 40.69 |
| 4384.0 | 0.10 | 63.13 | 2.57 | 8.54 | 44.03 |
| 4384.5 | 0.10 | 62.75 | 2.56 | 7.64 | 42.41 |
| 4385.0 | 0.10 | 62.50 | 2.56 | 6.92 | 33.72 |
| 4385.5 | 0.11 | 61.88 | 2.57 | 6.38 | 27.33 |
| 4386.0 | 0.11 | 62.38 | 2.57 | 6.42 | 24.17 |
| 4386.5 | 0.11 | 62.63 | 2.56 | 6.84 | 24.81 |
| 4387.0 | 0.12 | 64.38 | 2.53 | 7.65 | 25.17 |
| 4387.5 | 0.12 | 65.88 | 2.52 | 7.67 | 25.19 |
| 4388.0 | 0.13 | 66.75 | 2.52 | 6.23 | 25.91 |
| 4388.5 | 0.13 | 67.00 | 2.52 | 5.22 | 23.66 |
| 4389.0 | 0.13 | 67.63 | 2.52 | 4.64 | 22.28 |
| 4389.5 | 0.13 | 66.63 | 2.51 | 4.90 | 21.56 |
| 4390.0 | 0.14 | 66.63 | 2.48 | 5.51 | 23.44 |
| 4390.5 | 0.14 | 66.13 | 2.49 | 5.75 | 22.56 |
| 4391.0 | 0.14 | 66.00 | 2.50 | 6.52 | 20.70 |
| 4391.5 | 0.13 | 66.50 | 2.55 | 6.64 | 18.97 |
| 4392.0 | 0.13 | 66.75 | 2.55 | 6.97 | 21.58 |
| 4392.5 | 0.14 | 66.88 | 2.55 | 6.45 | 21.31 |
| 4393.0 | 0.14 | 66.63 | 2.52 | 6.07 | 23.77 |
| 4393.5 | 0.13 | 66.00 | 2.52 | 5.65 | 20.56 |
| 4394.0 | 0.12 | 65.00 | 2.52 | 5.29 | 21.81 |
| 4394.5 | 0.12 | 64.88 | 2.53 | 5.42 | 19.11 |
| 4395.0 | 0.12 | 64.63 | 2.53 | 5.16 | 19.83 |
| 4395.5 | 0.12 | 64.50 | 2.55 | 5.38 | 20.08 |
| 4396.0 | 0.12 | 64.00 | 2.55 | 5.46 | 21.69 |
| 4396.5 | 0.11 | 63.38 | 2.56 | 5.61 | 22.80 |
| 4397.0 | 0.11 | 63.25 | 2.57 | 5.72 | 22.67 |
| 4397.5 | 0.11 | 62.88 | 2.58 | 5.72 | 22.06 |
| 4398.0 | 0.10 | 62.13 | 2.59 | 5.90 | 22.19 |
| 4398.5 | 0.10 | 62.00 | 2.59 | 6.25 | 21.81 |
| 4399.0 | 0.10 | 61.63 | 2.62 | 6.49 | 25.95 |
| 4399.5 | 0.10 | 61.38 | 2.61 | 6.80 | 28.05 |
| 4400.0 | 0.10 | 61.63 | 2.61 | 6.90 | 31.42 |
| 4400.5 | 0.09 | 61.38 | 2.60 | 7.26 | 27.66 |
| 4401.0 | 0.08 | 61.13 | 2.57 | 7.34 | 25.92 |
| 4401.5 | 0.08 | 61.38 | 2.57 | 7.00 | 24.28 |
| 4402.0 | 0.08 | 61.25 | 2.59 | 7.33 | 24.89 |
| 4402.5 | 0.08 | 61.63 | 2.62 | 7.48 | 29.47 |
| 4403.0 | 0.08 | 61.13 | 2.65 | 8.03 | 29.95 |
| 4403.5 | 0.08 | 61.13 | 2.64 | 8.47 | 32.31 |
| 4404.0 | 0.08 | 60.88 | 2.64 | 9.04 | 27.86 |
| 4404.5 | 0.07 | 61.13 | 2.62 | 9.65 | 23.92 |
| 4405.0 | 0.06 | 59.88 | 2.62 | 10.00 | 21.09 |
| 4405.5 | 0.06 | 60.25 | 2.63 | 10.71 | 20.63 |
| 4406.0 | 0.06 | 60.00 | 2.64 | 11.46 | 23.73 |
| 4406.5 | 0.07 | 61.13 | 2.64 | 11.23 | 25.05 |
| 4407.0 | 0.07 | 61.00 | 2.66 | 11.22 | 25.67 |
| 4407.5 | 0.07 | 59.38 | 2.65 | 10.94 | 26.38 |
| 4408.0 | 0.06 | 59.13 | 2.65 | 11.45 | 25.91 |
| 4408.5 | 0.06 | 60.13 | 2.64 | 11.63 | 27.05 |
| 4409.0 | 0.06 | 60.25 | 2.64 | 13.38 | 24.70 |
| 4409.5 | 0.06 | 60.25 | 2.65 | 15.24 | 24.47 |
| 4410.0 | 0.07 | 60.50 | 2.65 | 15.32 | 24.80 |
| 4410.5 | 0.07 | 60.75 | 2.65 | 14.85 | 27.89 |
| 4411.0 | 0.08 | 60.75 | 2.64 | 14.01 | 29.70 |
| 4411.5 | 0.07 | 59.88 | 2.65 | 13.32 | 26.86 |
| 4412.0 | 0.06 | 58.63 | 2.67 | 12.59 | 24.63 |
| 4412.5 | 0.05 | 58.88 | 2.67 | 13.02 | 22.42 |
| 4413.0 | 0.06 | 60.63 | 2.67 | 14.32 | 24.77 |
| 4413.5 | 0.07 | 62.13 | 2.66 | 17.46 | 28.91 |
| 4414.0 | 0.09 | 64.63 | 2.67 | 18.87 | 33.09 |
| 4414.5 | 0.11 | 66.38 | 2.61 | 14.90 | 37.50 |
| 4415.0 | 0.11 | 67.25 | 2.60 | 11.90 | 35.78 |
| 4415.5 | 0.12 | 69.13 | 2.65 | 10.12 | 39.00 |
| 4416.0 | 0.14 | 70.63 | 2.66 | 8.49 | 41.53 |
| 4416.5 | 0.16 | 71.50 | 2.65 | 7.43 | 47.88 |
| 4417.0 | 0.15 | 70.25 | 2.63 | 7.35 | 47.13 |

Table A2.6: Water saturation data (calculated using Archie formula, Archie 1942) for the Great Oolite Formation in the Singleton-1 well.

| TVDSS (ft) | Sw (%) |
| --- | --- |
| 4218.1 | 37.36 |
| 4218.4 | 36.68 |
| 4218.7 | 39.59 |
| 4219.0 | 43.87 |
| 4219.4 | 50.14 |
| 4219.7 | 53.20 |
| 4220.0 | 53.34 |
| 4220.3 | 47.22 |
| 4220.6 | 42.46 |
| 4221.0 | 37.48 |
| 4221.3 | 35.69 |
| 4221.6 | 35.21 |
| 4221.9 | 35.42 |
| 4222.2 | 36.61 |
| 4222.5 | 36.94 |
| 4222.9 | 38.52 |
| 4223.2 | 39.53 |
| 4223.5 | 42.94 |
| 4223.8 | 45.49 |
| 4224.1 | 45.29 |
| 4224.5 | 41.86 |
| 4224.8 | 38.68 |
| 4225.1 | 36.92 |
| 4225.4 | 37.77 |
| 4225.7 | 38.88 |
| 4226.1 | 39.78 |
| 4226.4 | 40.16 |
| 4226.7 | 39.98 |
| 4227.0 | 40.85 |
| 4227.3 | 42.52 |
| 4227.6 | 43.10 |
| 4228.0 | 43.02 |
| 4228.3 | 40.36 |
| 4228.6 | 38.00 |
| 4228.9 | 39.03 |
| 4229.2 | 40.18 |
| 4229.6 | 45.10 |
| 4229.9 | 43.55 |
| 4230.2 | 42.71 |
| 4230.5 | 40.58 |
| 4230.8 | 41.37 |
| 4231.1 | 41.82 |
| 4231.5 | 42.90 |
| 4231.8 | 42.86 |
| 4232.1 | 41.89 |
| 4232.4 | 37.59 |
| 4232.7 | 34.53 |
| 4233.1 | 32.48 |
| 4233.4 | 32.63 |
| 4233.7 | 33.32 |
| 4234.0 | 35.07 |
| 4234.3 | 39.26 |
| 4234.6 | 42.38 |
| 4235.0 | 44.80 |
| 4235.3 | 43.63 |
| 4235.6 | 42.86 |
| 4235.9 | 42.13 |
| 4236.2 | 42.96 |
| 4236.6 | 43.92 |
| 4236.9 | 45.71 |
| 4237.2 | 45.77 |
| 4237.5 | 48.23 |
| 4237.8 | 50.08 |
| 4238.2 | 47.63 |
| 4238.5 | 47.11 |
| 4238.8 | 44.09 |
| 4239.1 | 42.90 |
| 4239.4 | 42.28 |
| 4239.7 | 41.58 |
| 4240.1 | 42.32 |
| 4240.4 | 41.94 |
| 4240.7 | 41.42 |
| 4241.0 | 42.75 |
| 4241.3 | 44.43 |
| 4241.7 | 47.52 |
| 4242.0 | 48.28 |
| 4242.3 | 51.64 |
| 4242.6 | 50.04 |
| 4242.9 | 48.20 |
| 4243.2 | 46.88 |
| 4243.6 | 47.73 |
| 4243.9 | 49.47 |
| 4244.2 | 53.38 |
| 4244.5 | 56.03 |
| 4244.8 | 54.81 |
| 4245.2 | 54.44 |
| 4245.5 | 54.42 |
| 4245.8 | 54.24 |
| 4246.1 | 48.10 |
| 4246.4 | 39.98 |
| 4246.7 | 35.77 |
| 4247.1 | 34.37 |
| 4247.4 | 36.27 |
| 4247.7 | 37.67 |
| 4248.0 | 38.06 |
| 4248.3 | 35.43 |
| 4248.7 | 31.45 |
| 4249.0 | 29.34 |
| 4249.3 | 29.26 |
| 4249.6 | 27.76 |
| 4249.9 | 26.80 |
| 4250.2 | 25.84 |
| 4250.6 | 27.06 |
| 4250.9 | 29.49 |
| 4251.2 | 31.07 |
| 4251.5 | 32.40 |
| 4251.8 | 32.01 |
| 4252.1 | 31.28 |
| 4252.5 | 30.93 |
| 4252.8 | 29.54 |
| 4253.1 | 30.88 |
| 4253.4 | 31.52 |
| 4253.7 | 34.12 |
| 4254.1 | 34.95 |
| 4254.4 | 36.68 |
| 4254.7 | 38.02 |
| 4255.0 | 37.21 |
| 4255.3 | 36.50 |
| 4255.6 | 33.55 |
| 4256.0 | 32.75 |
| 4256.3 | 32.00 |
| 4256.6 | 33.11 |
| 4256.9 | 36.32 |
| 4257.2 | 39.95 |
| 4257.5 | 42.21 |
| 4257.9 | 40.74 |
| 4258.2 | 40.76 |
| 4258.5 | 44.90 |
| 4258.8 | 49.10 |
| 4259.1 | 52.98 |
| 4259.4 | 52.53 |
| 4259.8 | 54.50 |
| 4260.1 | 53.43 |
| 4260.4 | 51.29 |
| 4260.7 | 45.18 |
| 4261.0 | 41.67 |
| 4261.3 | 41.02 |
| 4261.7 | 42.24 |
| 4262.0 | 42.44 |
| 4262.3 | 46.24 |
| 4262.6 | 52.39 |
| 4262.9 | 60.60 |
| 4263.2 | 62.19 |
| 4263.6 | 64.82 |
| 4263.9 | 70.53 |
| 4264.2 | 71.45 |
| 4264.5 | 70.24 |
| 4264.8 | 69.34 |
| 4265.1 | 68.63 |
| 4265.5 | 71.53 |
| 4265.8 | 72.27 |
| 4266.1 | 74.04 |
| 4266.4 | 71.64 |
| 4266.7 | 69.11 |
| 4267.0 | 67.04 |
| 4267.3 | 65.55 |
| 4267.7 | 66.05 |
| 4268.0 | 70.10 |
| 4268.3 | 75.34 |
| 4268.6 | 79.06 |
| 4268.9 | 84.09 |
| 4269.2 | 87.40 |
| 4269.6 | 96.44 |
| 4269.9 | 97.93 |
| 4270.2 | 95.80 |
| 4270.5 | 95.00 |
| 4270.8 | 107.20 |
| 4271.1 | 92.56 |
| 4271.5 | 81.77 |
| 4271.8 | 79.56 |
| 4272.1 | 84.38 |
| 4272.4 | 85.72 |
| 4272.7 | 74.90 |
| 4273.0 | 67.65 |
| 4273.3 | 65.01 |
| 4273.7 | 70.45 |
| 4274.0 | 69.27 |
| 4274.3 | 65.34 |
| 4274.6 | 56.29 |
| 4274.9 | 51.31 |
| 4275.2 | 46.93 |
| 4275.5 | 45.03 |
| 4275.9 | 47.85 |
| 4276.2 | 50.62 |
| 4276.5 | 49.71 |
| 4276.8 | 43.18 |
| 4277.1 | 36.99 |
| 4277.4 | 34.26 |
| 4277.7 | 33.87 |
| 4278.1 | 38.15 |
| 4278.4 | 41.24 |
| 4278.7 | 40.59 |
| 4279.0 | 37.47 |
| 4279.3 | 34.98 |
| 4279.6 | 33.87 |
| 4280.0 | 33.94 |
| 4280.3 | 35.19 |
| 4280.6 | 38.29 |
| 4280.9 | 40.86 |
| 4281.2 | 39.23 |
| 4281.5 | 34.80 |
| 4281.8 | 31.71 |
| 4282.1 | 30.52 |
| 4282.5 | 29.72 |
| 4282.8 | 28.97 |
| 4283.1 | 29.83 |
| 4283.4 | 31.13 |
| 4283.7 | 32.21 |
| 4284.0 | 31.04 |
| 4284.3 | 31.33 |
| 4284.7 | 30.03 |
| 4285.0 | 30.54 |
| 4285.3 | 28.86 |
| 4285.6 | 29.38 |
| 4285.9 | 28.10 |
| 4286.2 | 27.72 |
| 4286.5 | 27.30 |
| 4286.9 | 26.48 |
| 4287.2 | 27.22 |
| 4287.5 | 27.32 |
| 4287.8 | 31.27 |
| 4288.1 | 33.34 |
| 4288.4 | 33.22 |
| 4288.7 | 30.66 |
| 4289.0 | 28.95 |
| 4289.4 | 29.50 |
| 4289.7 | 31.07 |
| 4290.0 | 31.90 |
| 4290.3 | 32.31 |
| 4290.6 | 30.28 |
| 4290.9 | 29.34 |
| 4291.2 | 30.15 |
| 4291.6 | 31.72 |
| 4291.9 | 33.20 |
| 4292.2 | 33.69 |
| 4292.5 | 33.56 |
| 4292.8 | 33.83 |
| 4293.1 | 33.74 |
| 4293.4 | 32.44 |
| 4293.7 | 32.29 |
| 4294.1 | 31.66 |
| 4294.4 | 33.14 |
| 4294.7 | 32.31 |
| 4295.0 | 32.56 |
| 4295.3 | 33.40 |
| 4295.6 | 35.06 |
| 4295.9 | 36.77 |
| 4296.2 | 36.91 |
| 4296.6 | 36.19 |
| 4296.9 | 35.08 |
| 4297.2 | 35.63 |
| 4297.5 | 37.81 |
| 4297.8 | 40.61 |
| 4298.1 | 42.00 |
| 4298.4 | 45.25 |
| 4298.7 | 45.78 |
| 4299.1 | 46.17 |
| 4299.4 | 40.27 |
| 4299.7 | 37.64 |
| 4300.0 | 38.88 |
| 4300.3 | 42.63 |
| 4300.6 | 47.12 |
| 4300.9 | 44.46 |
| 4301.2 | 41.30 |
| 4301.5 | 38.36 |
| 4301.9 | 36.64 |
| 4302.2 | 36.19 |
| 4302.5 | 35.81 |
| 4302.8 | 36.85 |
| 4303.1 | 38.69 |
| 4303.4 | 39.71 |
| 4303.7 | 40.15 |
| 4304.0 | 41.47 |
| 4304.3 | 43.42 |
| 4304.7 | 44.75 |
| 4305.0 | 47.30 |
| 4305.3 | 50.49 |
| 4305.6 | 51.94 |
| 4305.9 | 47.00 |
| 4306.2 | 41.66 |
| 4306.5 | 39.24 |
| 4306.8 | 39.19 |
| 4307.1 | 39.03 |
| 4307.5 | 39.46 |
| 4307.8 | 41.37 |
| 4308.1 | 43.02 |
| 4308.4 | 44.64 |
| 4308.7 | 44.81 |
| 4309.0 | 43.70 |
| 4309.3 | 42.15 |
| 4309.6 | 40.31 |
| 4309.9 | 40.89 |
| 4310.3 | 41.77 |
| 4310.6 | 43.15 |
| 4310.9 | 44.08 |
| 4311.2 | 46.74 |
| 4311.5 | 49.90 |
| 4311.8 | 55.57 |
| 4312.1 | 59.78 |
| 4312.4 | 62.31 |
| 4312.7 | 61.41 |
| 4313.0 | 56.37 |
| 4313.4 | 55.16 |
| 4313.7 | 54.22 |
| 4314.0 | 55.23 |
| 4314.3 | 54.03 |
| 4314.6 | 52.43 |
| 4314.9 | 47.78 |
| 4315.2 | 43.49 |
| 4315.5 | 39.95 |
| 4315.8 | 38.97 |
| 4316.1 | 37.91 |
| 4316.5 | 39.77 |
| 4316.8 | 42.25 |
| 4317.1 | 44.83 |
| 4317.4 | 43.40 |
| 4317.7 | 44.18 |
| 4318.0 | 43.03 |
| 4318.3 | 43.15 |
| 4318.6 | 43.91 |
| 4318.9 | 45.27 |
| 4319.2 | 48.12 |
| 4319.5 | 49.98 |
| 4319.9 | 56.06 |
| 4320.2 | 60.60 |
| 4320.5 | 59.75 |
| 4320.8 | 57.12 |
| 4321.1 | 53.09 |
| 4321.4 | 53.10 |
| 4321.7 | 52.25 |
| 4322.0 | 52.84 |
| 4322.3 | 53.32 |
| 4322.6 | 54.66 |
| 4322.9 | 57.03 |
| 4323.3 | 58.54 |
| 4323.6 | 59.76 |
| 4323.9 | 61.87 |
| 4324.2 | 62.24 |
| 4324.5 | 61.27 |
| 4324.8 | 57.36 |
| 4325.1 | 54.23 |
| 4325.4 | 50.37 |
| 4325.7 | 48.14 |
| 4326.0 | 46.79 |
| 4326.3 | 47.71 |
| 4326.6 | 48.33 |
| 4327.0 | 47.57 |
| 4327.3 | 48.41 |
| 4327.6 | 49.26 |
| 4327.9 | 52.20 |
| 4328.2 | 54.02 |
| 4328.5 | 56.72 |
| 4328.8 | 55.66 |
| 4329.1 | 54.39 |
| 4329.4 | 55.75 |
| 4329.7 | 58.11 |
| 4330.0 | 61.99 |
| 4330.3 | 60.70 |
| 4330.6 | 60.41 |
| 4331.0 | 57.89 |
| 4331.3 | 56.01 |
| 4331.6 | 54.10 |
| 4331.9 | 54.05 |
| 4332.2 | 54.83 |
| 4332.5 | 54.37 |
| 4332.8 | 54.22 |
| 4333.1 | 54.26 |
| 4333.4 | 55.26 |
| 4333.7 | 53.07 |
| 4334.0 | 52.33 |
| 4334.3 | 51.36 |
| 4334.6 | 50.76 |
| 4334.9 | 50.00 |
| 4335.3 | 49.46 |
| 4335.6 | 48.03 |
| 4335.9 | 45.58 |
| 4336.2 | 45.22 |
| 4336.5 | 45.29 |
| 4336.8 | 47.46 |
| 4337.1 | 46.10 |
| 4337.4 | 48.52 |
| 4337.7 | 48.07 |
| 4338.0 | 51.12 |
| 4338.3 | 50.25 |
| 4338.6 | 49.67 |
| 4338.9 | 48.49 |
| 4339.2 | 50.13 |
| 4339.5 | 50.72 |
| 4339.8 | 49.03 |
| 4340.2 | 46.48 |
| 4340.5 | 46.27 |
| 4340.8 | 49.63 |
| 4341.1 | 51.70 |
| 4341.4 | 52.11 |
| 4341.7 | 48.98 |
| 4342.0 | 50.08 |
| 4342.3 | 51.25 |
| 4342.6 | 55.06 |
| 4342.9 | 56.67 |
| 4343.2 | 57.04 |
| 4343.5 | 58.44 |
| 4343.8 | 59.38 |
| 4344.1 | 59.54 |
| 4344.4 | 57.00 |
| 4344.7 | 55.46 |
| 4345.0 | 55.05 |
| 4345.4 | 55.36 |
| 4345.7 | 54.69 |
| 4346.0 | 56.46 |
| 4346.3 | 55.18 |
| 4346.6 | 54.41 |
| 4346.9 | 51.17 |
| 4347.2 | 53.58 |
| 4347.5 | 53.72 |
| 4347.8 | 52.27 |
| 4348.1 | 50.18 |
| 4348.4 | 49.11 |
| 4348.7 | 53.44 |
| 4349.0 | 55.13 |
| 4349.3 | 60.73 |
| 4349.6 | 60.06 |
| 4349.9 | 58.46 |
| 4350.2 | 58.58 |
| 4350.5 | 55.07 |
| 4350.8 | 53.41 |
| 4351.1 | 51.92 |
| 4351.4 | 52.71 |
| 4351.8 | 54.03 |
| 4352.1 | 53.76 |
| 4352.4 | 51.21 |
| 4352.7 | 48.81 |
| 4353.0 | 50.29 |
| 4353.3 | 49.80 |
| 4353.6 | 48.86 |
| 4353.9 | 47.68 |
| 4354.2 | 47.57 |
| 4354.5 | 50.06 |
| 4354.8 | 51.34 |
| 4355.1 | 54.06 |
| 4355.4 | 54.44 |
| 4355.7 | 55.86 |
| 4356.0 | 54.58 |
| 4356.3 | 55.51 |
| 4356.6 | 54.02 |
| 4356.9 | 53.80 |
| 4357.2 | 49.95 |
| 4357.5 | 48.76 |
| 4357.8 | 49.74 |
| 4358.1 | 53.10 |
| 4358.4 | 52.87 |
| 4358.7 | 50.62 |
| 4359.0 | 49.85 |
| 4359.3 | 51.89 |
| 4359.6 | 54.77 |
| 4360.0 | 56.88 |
| 4360.3 | 61.73 |
| 4360.6 | 64.17 |
| 4360.9 | 63.99 |
| 4361.2 | 59.95 |
| 4361.5 | 58.13 |
| 4361.8 | 58.28 |
| 4362.1 | 57.46 |
| 4362.4 | 55.18 |
| 4362.7 | 54.38 |
| 4363.0 | 54.21 |
| 4363.3 | 54.94 |
| 4363.6 | 55.66 |
| 4363.9 | 59.46 |
| 4364.2 | 61.02 |
| 4364.5 | 57.82 |
| 4364.8 | 54.45 |
| 4365.1 | 55.19 |
| 4365.4 | 57.25 |
| 4365.7 | 57.78 |
| 4366.0 | 56.59 |
| 4366.3 | 54.07 |
| 4366.6 | 53.67 |
| 4366.9 | 53.68 |
| 4367.2 | 57.04 |
| 4367.5 | 57.48 |
| 4367.8 | 57.49 |
| 4368.1 | 56.34 |
| 4368.4 | 58.39 |
| 4368.7 | 57.58 |
| 4369.0 | 57.99 |
| 4369.3 | 58.38 |
| 4369.6 | 59.01 |
| 4369.9 | 59.48 |
| 4370.2 | 58.12 |
| 4370.5 | 59.65 |
| 4370.9 | 59.63 |
| 4371.2 | 61.50 |
| 4371.5 | 59.74 |
| 4371.8 | 59.66 |
| 4372.1 | 56.34 |
| 4372.4 | 58.94 |
| 4372.7 | 58.01 |
| 4373.0 | 59.05 |
| 4373.3 | 56.30 |
| 4373.6 | 54.81 |
| 4373.9 | 55.26 |
| 4374.2 | 56.34 |
| 4374.5 | 58.31 |
| 4374.8 | 58.19 |
| 4375.1 | 55.48 |
| 4375.4 | 55.39 |
| 4375.7 | 57.09 |
| 4376.0 | 57.21 |
| 4376.3 | 58.21 |
| 4376.6 | 56.86 |
| 4376.9 | 59.47 |
| 4377.2 | 57.94 |
| 4377.5 | 56.59 |
| 4377.8 | 55.24 |
| 4378.1 | 57.42 |
| 4378.4 | 61.42 |
| 4378.7 | 60.69 |
| 4379.0 | 59.72 |
| 4379.3 | 58.16 |
| 4379.6 | 56.86 |
| 4379.9 | 59.84 |
| 4380.2 | 60.14 |
| 4380.5 | 63.62 |
| 4380.8 | 61.26 |
| 4381.1 | 60.34 |
| 4381.4 | 61.96 |
| 4381.7 | 62.67 |
| 4382.0 | 61.29 |
| 4382.3 | 60.79 |
| 4382.6 | 58.93 |
| 4382.9 | 63.53 |
| 4383.2 | 64.23 |
| 4383.5 | 66.19 |
| 4383.8 | 65.27 |
| 4384.1 | 64.63 |
| 4384.4 | 64.60 |
| 4384.7 | 66.55 |
| 4385.1 | 67.65 |
| 4385.4 | 67.77 |
| 4385.7 | 65.74 |
| 4386.0 | 65.67 |
| 4386.3 | 68.28 |
| 4386.6 | 65.52 |
| 4386.9 | 65.08 |
| 4387.2 | 63.76 |
| 4387.5 | 67.58 |
| 4387.8 | 70.89 |
| 4388.1 | 74.07 |
| 4388.4 | 72.90 |
| 4388.7 | 67.93 |
| 4389.0 | 62.97 |
| 4389.3 | 61.70 |
| 4389.6 | 63.49 |
| 4389.9 | 65.14 |
| 4390.2 | 63.57 |
| 4390.5 | 61.75 |
| 4390.8 | 61.62 |
| 4391.1 | 64.87 |
| 4391.4 | 65.06 |
| 4391.7 | 65.87 |
| 4392.0 | 70.06 |
| 4392.3 | 78.03 |
| 4392.6 | 86.31 |

Table A2.7: Water saturation data (calculated using Archie formula, Archie 1942) for the Great Oolite Formation in the Horndean-1A well.

| TVDSS (ft) | Sw (%) |
| --- | --- |
| 4232.4 | 66.64 |
| 4232.9 | 57.75 |
| 4233.4 | 56.36 |
| 4233.9 | 57.60 |
| 4234.4 | 56.03 |
| 4234.9 | 53.34 |
| 4235.4 | 50.50 |
| 4235.9 | 47.36 |
| 4236.4 | 47.38 |
| 4236.9 | 50.12 |
| 4237.4 | 54.63 |
| 4237.9 | 51.30 |
| 4238.4 | 50.87 |
| 4238.9 | 50.44 |
| 4239.4 | 50.71 |
| 4239.9 | 49.57 |
| 4240.4 | 48.51 |
| 4240.9 | 47.60 |
| 4241.4 | 45.84 |
| 4241.9 | 45.32 |
| 4242.4 | 47.80 |
| 4242.9 | 50.37 |
| 4243.4 | 55.60 |
| 4243.9 | 62.93 |
| 4244.4 | 69.78 |
| 4244.9 | 76.94 |
| 4245.4 | 81.46 |
| 4245.9 | 84.31 |
| 4246.4 | 81.74 |
| 4246.9 | 79.52 |
| 4247.4 | 82.95 |
| 4247.9 | 79.42 |
| 4248.4 | 76.43 |
| 4248.9 | 74.13 |
| 4249.4 | 76.46 |
| 4249.9 | 75.55 |
| 4250.4 | 71.56 |
| 4250.9 | 69.73 |
| 4251.4 | 66.95 |
| 4251.9 | 65.16 |
| 4252.4 | 59.16 |
| 4252.9 | 58.41 |
| 4253.4 | 59.07 |
| 4253.9 | 63.29 |
| 4254.4 | 61.53 |
| 4254.9 | 58.08 |
| 4255.4 | 55.79 |
| 4255.9 | 59.32 |
| 4256.4 | 63.75 |
| 4256.9 | 67.20 |
| 4257.4 | 76.12 |
| 4257.9 | 91.74 |
| 4258.4 | 123.97 |
| 4258.9 | 156.44 |
| 4259.4 | 173.78 |
| 4259.9 | 154.40 |
| 4260.4 | 114.28 |
| 4260.9 | 95.04 |
| 4261.4 | 92.38 |
| 4261.9 | 96.68 |
| 4262.4 | 100.59 |
| 4262.9 | 89.62 |
| 4263.4 | 78.97 |
| 4263.9 | 73.73 |
| 4264.4 | 72.23 |
| 4264.9 | 71.67 |
| 4265.4 | 72.74 |
| 4265.9 | 70.97 |
| 4266.4 | 74.56 |
| 4266.9 | 74.85 |
| 4267.4 | 84.22 |
| 4267.9 | 91.21 |
| 4268.4 | 103.69 |
| 4268.9 | 106.83 |
| 4269.4 | 113.17 |
| 4269.9 | 112.45 |
| 4270.4 | 115.10 |
| 4270.9 | 102.73 |
| 4271.4 | 92.67 |
| 4271.9 | 94.10 |
| 4272.4 | 114.30 |
| 4272.9 | 146.62 |
| 4273.4 | 153.32 |
| 4273.9 | 115.70 |
| 4274.4 | 78.87 |
| 4274.9 | 65.38 |
| 4275.4 | 64.26 |
| 4275.9 | 70.84 |
| 4276.4 | 77.16 |
| 4276.9 | 74.57 |
| 4277.4 | 71.11 |
| 4277.9 | 67.78 |
| 4278.4 | 71.24 |
| 4278.9 | 78.09 |
| 4279.4 | 80.12 |
| 4279.9 | 76.26 |
| 4280.4 | 71.03 |
| 4280.9 | 65.65 |
| 4281.4 | 64.32 |
| 4281.9 | 61.13 |
| 4282.4 | 56.40 |
| 4282.9 | 55.25 |
| 4283.4 | 55.28 |
| 4283.9 | 60.23 |
| 4284.4 | 58.19 |
| 4284.9 | 55.95 |
| 4285.4 | 58.86 |
| 4285.9 | 63.60 |
| 4286.4 | 71.57 |
| 4286.9 | 69.35 |
| 4287.4 | 64.68 |
| 4287.9 | 56.88 |
| 4288.4 | 51.20 |
| 4288.9 | 51.04 |
| 4289.4 | 55.52 |
| 4289.9 | 58.49 |
| 4290.4 | 56.15 |
| 4290.9 | 50.64 |
| 4291.4 | 48.40 |
| 4291.9 | 46.80 |
| 4292.4 | 47.13 |
| 4292.9 | 45.64 |
| 4293.4 | 45.12 |
| 4293.9 | 44.64 |
| 4294.4 | 45.66 |
| 4294.9 | 46.75 |
| 4295.4 | 47.24 |
| 4295.9 | 48.85 |
| 4296.4 | 49.40 |
| 4296.9 | 50.99 |
| 4297.4 | 50.82 |
| 4297.9 | 50.62 |
| 4298.4 | 51.40 |
| 4298.9 | 52.69 |
| 4299.4 | 52.35 |
| 4299.9 | 51.71 |
| 4300.4 | 49.00 |
| 4300.9 | 46.48 |
| 4301.4 | 44.87 |
| 4301.9 | 44.69 |
| 4302.4 | 46.20 |
| 4302.9 | 48.48 |
| 4303.4 | 47.83 |
| 4303.9 | 44.07 |
| 4304.4 | 43.06 |
| 4304.9 | 41.33 |
| 4305.4 | 43.20 |
| 4305.9 | 44.09 |
| 4306.4 | 47.09 |
| 4306.9 | 48.95 |
| 4307.4 | 47.40 |
| 4307.9 | 45.70 |
| 4308.4 | 44.87 |
| 4308.9 | 47.46 |
| 4309.4 | 48.18 |
| 4309.9 | 47.27 |
| 4310.4 | 45.63 |
| 4310.9 | 47.75 |
| 4311.4 | 51.22 |
| 4311.9 | 51.26 |
| 4312.4 | 50.19 |
| 4312.9 | 48.63 |
| 4313.4 | 48.38 |
| 4313.9 | 45.88 |
| 4314.4 | 44.81 |
| 4314.9 | 45.08 |
| 4315.4 | 44.97 |
| 4315.9 | 45.21 |
| 4316.4 | 43.75 |
| 4316.9 | 44.77 |
| 4317.4 | 42.57 |
| 4317.9 | 42.58 |
| 4318.4 | 43.52 |
| 4318.9 | 46.47 |
| 4319.4 | 46.74 |
| 4319.9 | 47.22 |
| 4320.4 | 46.53 |
| 4320.9 | 48.95 |
| 4321.4 | 54.06 |
| 4321.9 | 72.27 |
| 4322.4 | 96.80 |
| 4322.9 | 110.33 |
| 4323.4 | 83.23 |
| 4323.9 | 74.76 |
| 4324.4 | 75.09 |
| 4324.9 | 87.26 |
| 4325.4 | 97.62 |
| 4325.9 | 99.47 |
| 4326.4 | 102.37 |
| 4326.9 | 101.80 |
| 4327.4 | 96.19 |
| 4327.9 | 91.02 |
| 4328.4 | 87.84 |
| 4328.9 | 86.02 |
| 4329.4 | 83.03 |
| 4329.9 | 78.62 |
| 4330.4 | 76.14 |
| 4330.9 | 77.11 |
| 4331.4 | 76.61 |
| 4331.9 | 78.21 |
| 4332.4 | 77.01 |
| 4332.9 | 76.46 |
| 4333.4 | 72.83 |
| 4333.9 | 71.93 |
| 4334.4 | 72.22 |
| 4334.9 | 75.08 |
| 4335.4 | 76.17 |
| 4335.9 | 78.21 |
| 4336.4 | 80.29 |
| 4336.9 | 87.19 |
| 4337.4 | 91.62 |
| 4337.9 | 92.48 |
| 4338.4 | 89.88 |
| 4338.9 | 89.35 |
| 4339.4 | 85.92 |
| 4339.9 | 83.40 |
| 4340.4 | 83.14 |
| 4340.9 | 84.27 |
| 4341.4 | 87.17 |
| 4341.9 | 83.13 |
| 4342.4 | 80.19 |
| 4342.9 | 81.33 |
| 4343.4 | 82.70 |
| 4343.9 | 83.27 |
| 4344.4 | 81.35 |
| 4344.9 | 88.75 |
| 4345.4 | 90.55 |
| 4345.9 | 90.47 |
| 4346.4 | 84.30 |
| 4346.9 | 84.77 |
| 4347.4 | 83.65 |
| 4347.9 | 84.78 |
| 4348.4 | 91.01 |
| 4348.9 | 96.12 |
| 4349.4 | 98.76 |
| 4349.9 | 91.68 |
| 4350.4 | 94.53 |
| 4350.9 | 99.45 |
| 4351.4 | 103.54 |
| 4351.9 | 95.31 |
| 4352.4 | 90.98 |
| 4352.9 | 92.92 |
| 4353.4 | 98.73 |
| 4353.9 | 90.32 |
| 4354.4 | 82.62 |
| 4354.9 | 83.83 |
| 4355.4 | 91.70 |
| 4355.9 | 93.79 |
| 4356.4 | 92.06 |
| 4356.9 | 92.89 |
| 4357.4 | 103.22 |
| 4357.9 | 102.09 |
| 4358.4 | 94.78 |
| 4358.9 | 83.70 |
| 4359.4 | 76.23 |
| 4359.9 | 78.13 |
| 4360.4 | 84.85 |
| 4360.9 | 99.66 |
| 4361.4 | 110.00 |
| 4361.9 | 104.21 |
| 4362.4 | 93.92 |
| 4362.9 | 87.68 |
| 4363.4 | 89.12 |
| 4363.9 | 95.03 |
| 4364.4 | 99.84 |
| 4364.9 | 105.10 |
| 4365.4 | 108.56 |
| 4365.9 | 107.22 |
| 4366.4 | 102.76 |
| 4366.9 | 93.83 |
| 4367.4 | 93.85 |
| 4367.9 | 99.75 |
| 4368.4 | 107.20 |
| 4368.9 | 109.30 |
| 4369.4 | 102.19 |
| 4369.9 | 102.05 |
| 4370.4 | 104.30 |
| 4370.9 | 104.70 |
| 4371.4 | 97.86 |
| 4371.9 | 88.34 |
| 4372.4 | 81.16 |
| 4372.9 | 85.04 |
| 4373.4 | 92.53 |
| 4373.9 | 101.78 |
| 4374.4 | 95.74 |
| 4374.9 | 85.10 |
| 4375.4 | 82.61 |
| 4375.9 | 95.26 |
| 4376.4 | 113.47 |
| 4376.9 | 112.38 |
| 4377.4 | 95.72 |
| 4377.9 | 84.88 |
| 4378.4 | 91.08 |
| 4378.9 | 99.52 |
| 4379.4 | 98.54 |
| 4379.9 | 91.41 |
| 4380.4 | 93.90 |
| 4380.9 | 100.53 |
| 4381.4 | 95.26 |
| 4381.9 | 80.67 |
| 4382.4 | 76.73 |
| 4382.9 | 83.04 |
| 4383.4 | 89.31 |
| 4383.9 | 85.15 |
| 4384.4 | 76.84 |
| 4384.9 | 77.12 |
| 4385.4 | 82.43 |
| 4385.9 | 89.27 |
| 4386.4 | 96.22 |
| 4386.9 | 97.92 |
| 4387.4 | 96.05 |
| 4387.9 | 94.55 |
| 4388.4 | 92.69 |
| 4388.9 | 94.58 |
| 4389.4 | 100.95 |
| 4389.9 | 105.65 |
| 4390.4 | 110.65 |
| 4390.9 | 108.21 |
| 4391.4 | 103.93 |
| 4391.9 | 96.17 |
| 4392.4 | 92.75 |
| 4392.9 | 89.04 |
| 4393.4 | 89.89 |
| 4393.9 | 91.91 |
| 4394.4 | 94.91 |
| 4394.9 | 93.57 |
| 4395.4 | 91.04 |
| 4395.9 | 91.62 |
| 4396.4 | 91.49 |
| 4396.9 | 87.43 |
| 4397.4 | 83.26 |
| 4397.9 | 84.11 |
| 4398.4 | 85.58 |
| 4398.9 | 88.25 |
| 4399.4 | 87.95 |
| 4399.9 | 85.91 |
| 4400.4 | 83.98 |
| 4400.9 | 82.10 |
| 4401.4 | 79.14 |
| 4401.9 | 77.06 |
| 4402.4 | 75.67 |
| 4402.9 | 75.42 |
| 4403.4 | 73.49 |
| 4403.9 | 72.29 |
| 4404.4 | 72.89 |
| 4404.9 | 75.40 |
| 4405.4 | 70.83 |
| 4405.9 | 69.19 |
| 4406.4 | 67.03 |
| 4406.9 | 70.52 |
| 4407.4 | 68.84 |
| 4407.9 | 68.04 |
| 4408.4 | 67.83 |
| 4408.9 | 69.75 |
| 4409.4 | 72.56 |
| 4409.9 | 70.91 |
| 4410.4 | 71.77 |
| 4410.9 | 70.09 |
| 4411.4 | 75.22 |
| 4411.9 | 75.62 |
| 4412.4 | 80.10 |
| 4412.9 | 80.58 |
| 4413.4 | 79.73 |
| 4413.9 | 77.48 |
| 4414.4 | 78.18 |
| 4414.9 | 77.76 |
| 4415.4 | 77.76 |
| 4415.9 | 78.95 |
| 4416.4 | 78.00 |
| 4416.9 | 76.93 |
| 4417.4 | 73.55 |
| 4417.9 | 74.56 |
| 4418.4 | 75.14 |
| 4418.9 | 76.50 |
| 4419.4 | 76.27 |
| 4419.9 | 77.80 |
| 4420.4 | 79.78 |
| 4420.9 | 82.19 |
| 4421.4 | 86.12 |
| 4421.9 | 87.10 |
| 4422.4 | 92.69 |
| 4422.9 | 88.82 |
| 4423.4 | 87.67 |
| 4423.9 | 81.46 |
| 4424.4 | 87.88 |
| 4424.9 | 90.00 |
| 4425.4 | 91.27 |
| 4425.9 | 86.05 |
| 4426.4 | 83.34 |
| 4426.9 | 86.48 |
| 4427.4 | 89.01 |
| 4427.9 | 92.30 |
| 4428.4 | 92.17 |
| 4428.9 | 96.54 |
| 4429.4 | 93.96 |
| 4429.9 | 93.21 |
| 4430.4 | 86.35 |
| 4430.9 | 89.76 |
| 4431.4 | 97.13 |
| 4431.9 | 101.31 |
| 4432.4 | 103.22 |
| 4432.9 | 80.88 |
| 4433.4 | 71.77 |
| 4433.9 | 67.69 |
| 4434.4 | 76.34 |
| 4434.9 | 86.39 |
| 4435.4 | 95.28 |
| 4435.9 | 101.65 |
| 4436.4 | 101.49 |
| 4436.9 | 93.53 |
| 4437.4 | 88.46 |
| 4437.9 | 92.32 |
| 4438.4 | 100.68 |
| 4438.9 | 106.89 |
| 4439.4 | 95.35 |
| 4439.9 | 88.77 |
| 4440.4 | 88.22 |
| 4440.9 | 97.14 |
| 4441.4 | 97.34 |
| 4441.9 | 94.73 |
| 4442.4 | 91.38 |
| 4442.9 | 79.44 |
| 4443.4 | 75.28 |
| 4443.9 | 76.44 |
| 4444.4 | 91.04 |
| 4444.9 | 101.95 |
| 4445.4 | 79.44 |

Table A2.8: Water saturation data (calculated using Archie formula, Archie 1942) for the Great Oolite Formation in the Storrington-2 well.

| TVDSS(ft) | Sw (%) |
| --- | --- |
| 3889.1 | 42.37 |
| 3889.6 | 43.05 |
| 3890.1 | 43.64 |
| 3890.6 | 42.59 |
| 3891.1 | 41.82 |
| 3891.6 | 40.95 |
| 3892.1 | 41.65 |
| 3892.5 | 41.56 |
| 3893.0 | 42.22 |
| 3893.5 | 43.54 |
| 3894.0 | 46.47 |
| 3894.5 | 47.96 |
| 3895.0 | 45.38 |
| 3895.5 | 41.79 |
| 3895.9 | 40.34 |
| 3896.4 | 40.36 |
| 3896.9 | 41.93 |
| 3897.4 | 42.99 |
| 3897.9 | 45.16 |
| 3898.4 | 46.97 |
| 3898.9 | 50.13 |
| 3899.3 | 51.04 |
| 3899.8 | 52.28 |
| 3900.3 | 48.45 |
| 3900.8 | 41.33 |
| 3901.3 | 35.28 |
| 3901.8 | 32.27 |
| 3902.3 | 31.65 |
| 3902.7 | 32.55 |
| 3903.2 | 34.73 |
| 3903.7 | 40.07 |
| 3904.2 | 49.50 |
| 3904.7 | 63.27 |
| 3905.2 | 62.91 |
| 3905.7 | 54.31 |
| 3906.2 | 46.90 |
| 3906.6 | 41.98 |
| 3907.1 | 41.69 |
| 3907.6 | 45.33 |
| 3908.1 | 48.28 |
| 3908.6 | 44.71 |
| 3909.1 | 40.30 |
| 3909.6 | 36.92 |
| 3910.0 | 35.42 |
| 3910.5 | 34.80 |
| 3911.0 | 35.45 |
| 3911.5 | 36.22 |
| 3912.0 | 38.63 |
| 3912.5 | 41.63 |
| 3913.0 | 44.38 |
| 3913.4 | 44.18 |
| 3913.9 | 41.95 |
| 3914.4 | 40.65 |
| 3914.9 | 39.96 |
| 3915.4 | 39.68 |
| 3915.9 | 39.50 |
| 3916.4 | 39.57 |
| 3916.8 | 41.74 |
| 3917.3 | 43.24 |
| 3917.8 | 42.76 |
| 3918.3 | 40.98 |
| 3918.8 | 38.65 |
| 3919.3 | 37.43 |
| 3919.8 | 36.76 |
| 3920.3 | 38.02 |
| 3920.7 | 38.62 |
| 3921.2 | 41.04 |
| 3921.7 | 43.62 |
| 3922.2 | 46.11 |
| 3922.7 | 51.08 |
| 3923.2 | 57.62 |
| 3923.7 | 75.06 |
| 3924.1 | 78.96 |
| 3924.6 | 85.94 |
| 3925.1 | 89.51 |
| 3925.6 | 96.02 |
| 3926.1 | 94.40 |
| 3926.6 | 93.50 |
| 3927.1 | 97.79 |
| 3927.5 | 97.79 |
| 3928.0 | 90.34 |
| 3928.5 | 82.38 |
| 3929.0 | 77.61 |
| 3929.5 | 72.72 |
| 3930.0 | 73.52 |
| 3930.5 | 66.44 |
| 3930.9 | 63.80 |
| 3931.4 | 55.29 |
| 3931.9 | 50.00 |
| 3932.4 | 43.80 |
| 3932.9 | 39.89 |
| 3933.4 | 35.45 |
| 3933.9 | 32.13 |
| 3934.3 | 30.85 |
| 3934.8 | 30.58 |
| 3935.3 | 30.69 |
| 3935.8 | 30.41 |
| 3936.3 | 30.89 |
| 3936.8 | 31.65 |
| 3937.3 | 32.13 |
| 3937.8 | 32.32 |
| 3938.2 | 30.04 |
| 3938.7 | 30.58 |
| 3939.2 | 31.62 |
| 3939.7 | 36.22 |
| 3940.2 | 39.90 |
| 3940.7 | 34.65 |
| 3941.2 | 33.06 |
| 3941.6 | 32.49 |
| 3942.1 | 33.32 |
| 3942.6 | 33.03 |
| 3943.1 | 32.11 |
| 3943.6 | 34.27 |
| 3944.1 | 38.10 |
| 3944.6 | 38.14 |
| 3945.0 | 39.45 |
| 3945.5 | 41.21 |
| 3946.0 | 40.56 |
| 3946.5 | 38.33 |
| 3947.0 | 36.36 |
| 3947.5 | 36.60 |
| 3948.0 | 38.84 |
| 3948.4 | 40.36 |
| 3948.9 | 40.00 |
| 3949.4 | 41.20 |
| 3949.9 | 45.22 |
| 3950.4 | 53.86 |
| 3950.9 | 59.31 |
| 3951.4 | 59.73 |
| 3951.9 | 63.20 |
| 3952.3 | 59.81 |
| 3952.8 | 52.77 |
| 3953.3 | 51.26 |
| 3953.8 | 51.25 |
| 3954.3 | 56.63 |
| 3954.8 | 59.45 |
| 3955.3 | 55.89 |
| 3955.7 | 50.65 |
| 3956.2 | 46.43 |
| 3956.7 | 48.77 |
| 3957.2 | 59.04 |
| 3957.7 | 78.73 |
| 3958.2 | 82.34 |
| 3958.7 | 73.66 |
| 3959.1 | 60.31 |
| 3959.6 | 47.26 |
| 3960.1 | 39.53 |
| 3960.6 | 39.44 |
| 3961.1 | 43.44 |
| 3961.6 | 43.21 |
| 3962.1 | 40.57 |
| 3962.5 | 40.97 |
| 3963.0 | 44.93 |
| 3963.5 | 47.39 |
| 3964.0 | 42.33 |
| 3964.5 | 37.49 |
| 3965.0 | 35.42 |
| 3965.5 | 35.83 |
| 3966.0 | 36.65 |
| 3966.4 | 37.70 |
| 3966.9 | 38.43 |
| 3967.4 | 39.37 |
| 3967.9 | 40.73 |
| 3968.4 | 41.50 |
| 3968.9 | 41.42 |
| 3969.4 | 41.03 |
| 3969.8 | 41.19 |
| 3970.3 | 42.98 |
| 3970.8 | 45.23 |
| 3971.3 | 45.74 |
| 3971.8 | 44.39 |
| 3972.3 | 42.55 |
| 3972.8 | 42.32 |
| 3973.2 | 42.40 |
| 3973.7 | 42.32 |
| 3974.2 | 42.12 |
| 3974.7 | 41.29 |
| 3975.2 | 41.79 |
| 3975.7 | 42.84 |
| 3976.2 | 44.72 |
| 3976.6 | 45.76 |
| 3977.1 | 46.43 |
| 3977.6 | 48.10 |
| 3978.1 | 49.69 |
| 3978.6 | 51.55 |
| 3979.1 | 53.43 |
| 3979.6 | 56.26 |
| 3980.1 | 57.90 |
| 3980.5 | 58.78 |
| 3981.0 | 58.11 |
| 3981.5 | 57.26 |
| 3982.0 | 56.11 |
| 3982.5 | 54.86 |
| 3983.0 | 54.92 |
| 3983.5 | 55.78 |
| 3983.9 | 56.61 |
| 3984.4 | 56.97 |
| 3984.9 | 57.12 |
| 3985.4 | 58.08 |
| 3985.9 | 58.55 |
| 3986.4 | 59.09 |
| 3986.9 | 59.96 |
| 3987.3 | 60.73 |
| 3987.8 | 59.87 |
| 3988.3 | 58.88 |
| 3988.8 | 58.99 |
| 3989.3 | 58.55 |
| 3989.8 | 58.86 |
| 3990.3 | 59.85 |
| 3990.7 | 61.39 |
| 3991.2 | 61.12 |
| 3991.7 | 61.24 |
| 3992.2 | 61.50 |
| 3992.7 | 61.92 |
| 3993.2 | 61.77 |
| 3993.7 | 61.69 |
| 3994.2 | 61.95 |
| 3994.6 | 62.40 |
| 3995.1 | 63.57 |
| 3995.6 | 64.83 |
| 3996.1 | 66.02 |
| 3996.6 | 65.10 |
| 3997.1 | 65.72 |
| 3997.6 | 65.04 |
| 3998.0 | 65.43 |
| 3998.5 | 65.36 |
| 3999.0 | 66.76 |
| 3999.5 | 66.19 |
| 4000.0 | 63.64 |
| 4000.5 | 62.32 |
| 4001.0 | 63.13 |
| 4001.4 | 65.04 |
| 4001.9 | 65.51 |
| 4002.4 | 64.88 |
| 4002.9 | 66.14 |
| 4003.4 | 67.35 |
| 4003.9 | 70.30 |
| 4004.4 | 71.37 |
| 4004.8 | 72.90 |
| 4005.3 | 72.27 |
| 4005.8 | 70.99 |
| 4006.3 | 71.02 |
| 4006.8 | 69.70 |
| 4007.3 | 69.68 |
| 4007.8 | 69.20 |
| 4008.2 | 71.15 |
| 4008.7 | 70.20 |
| 4009.2 | 70.20 |
| 4009.7 | 70.42 |
| 4010.2 | 72.44 |
| 4010.7 | 72.15 |
| 4011.2 | 71.36 |
| 4011.7 | 69.84 |
| 4012.1 | 70.36 |
| 4012.6 | 70.06 |
| 4013.1 | 71.65 |
| 4013.6 | 73.26 |
| 4014.1 | 74.96 |
| 4014.6 | 75.19 |
| 4015.1 | 75.06 |
| 4015.5 | 75.71 |
| 4016.0 | 76.44 |
| 4016.5 | 75.97 |
| 4017.0 | 74.74 |
| 4017.5 | 72.17 |
| 4018.0 | 69.87 |
| 4018.5 | 67.75 |
| 4018.9 | 66.03 |
| 4019.4 | 67.37 |
| 4019.9 | 70.70 |
| 4020.4 | 75.96 |
| 4020.9 | 75.92 |
| 4021.4 | 73.20 |
| 4021.9 | 69.10 |
| 4022.3 | 65.90 |
| 4022.8 | 61.11 |
| 4023.3 | 57.38 |
| 4023.8 | 54.31 |
| 4024.3 | 54.29 |
| 4024.8 | 54.67 |
| 4025.3 | 55.32 |
| 4025.7 | 53.58 |
| 4026.2 | 52.19 |
| 4026.7 | 50.98 |
| 4027.2 | 51.29 |
| 4027.7 | 51.54 |
| 4028.2 | 53.27 |
| 4028.7 | 54.78 |
| 4029.2 | 56.54 |
| 4029.6 | 57.25 |
| 4030.1 | 56.65 |
| 4030.6 | 56.92 |
| 4031.1 | 56.26 |
| 4031.6 | 56.56 |
| 4032.1 | 56.47 |
| 4032.6 | 57.37 |
| 4033.0 | 57.37 |
| 4033.5 | 56.03 |
| 4034.0 | 53.19 |
| 4034.5 | 50.93 |
| 4035.0 | 49.43 |
| 4035.5 | 49.74 |
| 4036.0 | 49.31 |
| 4036.4 | 48.98 |
| 4036.9 | 47.78 |
| 4037.4 | 48.15 |
| 4037.9 | 47.99 |
| 4038.4 | 48.14 |
| 4038.9 | 47.53 |
| 4039.4 | 48.12 |
| 4039.8 | 48.96 |
| 4040.3 | 50.19 |
| 4040.8 | 51.10 |
| 4041.3 | 51.70 |
| 4041.8 | 50.80 |
| 4042.3 | 49.77 |
| 4042.8 | 48.04 |
| 4043.2 | 47.64 |
| 4043.7 | 46.83 |
| 4044.2 | 46.69 |
| 4044.7 | 46.41 |
| 4045.2 | 47.08 |
| 4045.7 | 48.03 |
| 4046.2 | 50.50 |
| 4046.6 | 52.03 |
| 4047.1 | 53.16 |
| 4047.6 | 53.22 |
| 4048.1 | 53.40 |
| 4048.6 | 51.94 |
| 4049.1 | 50.18 |
| 4049.6 | 46.92 |
| 4050.1 | 45.33 |
| 4050.5 | 41.99 |
| 4051.0 | 40.92 |
| 4051.5 | 40.07 |
| 4052.0 | 41.04 |
| 4052.5 | 42.51 |
| 4053.0 | 43.63 |
| 4053.5 | 45.20 |
| 4053.9 | 45.01 |
| 4054.4 | 45.72 |
| 4054.9 | 45.96 |
| 4055.4 | 46.18 |
| 4055.9 | 45.44 |
| 4056.4 | 44.85 |
| 4056.9 | 45.24 |
| 4057.3 | 43.51 |
| 4057.8 | 42.48 |
| 4058.3 | 41.49 |
| 4058.8 | 42.31 |
| 4059.3 | 42.92 |
| 4059.8 | 44.02 |
| 4060.3 | 45.34 |
| 4060.7 | 46.14 |
| 4061.2 | 46.94 |
| 4061.7 | 45.90 |
| 4062.2 | 45.12 |
| 4062.7 | 44.82 |
| 4063.2 | 45.90 |
| 4063.7 | 46.54 |
| 4064.1 | 46.72 |
| 4064.6 | 47.09 |
| 4065.1 | 47.51 |
| 4065.6 | 48.16 |
| 4066.1 | 48.33 |
| 4066.6 | 47.60 |
| 4067.1 | 46.19 |
| 4067.5 | 45.79 |
| 4068.0 | 45.57 |
| 4068.5 | 46.34 |
| 4069.0 | 46.48 |
| 4069.5 | 45.66 |
| 4070.0 | 44.50 |
| 4070.5 | 43.52 |
| 4071.0 | 44.08 |
| 4071.4 | 45.14 |
| 4071.9 | 45.03 |
| 4072.4 | 46.43 |
| 4072.9 | 45.40 |
| 4073.4 | 45.84 |
| 4073.9 | 44.37 |
| 4074.4 | 44.74 |
| 4074.8 | 44.75 |
| 4075.3 | 45.35 |
| 4075.8 | 45.53 |
| 4076.3 | 45.91 |
| 4076.8 | 45.26 |
| 4077.3 | 45.38 |
| 4077.8 | 45.38 |
| 4078.2 | 45.70 |
| 4078.7 | 45.05 |
| 4079.2 | 43.97 |
| 4079.7 | 47.02 |
| 4080.2 | 44.20 |
| 4080.7 | 48.36 |
| 4081.2 | 51.30 |
| 4081.6 | 52.15 |
| 4082.1 | 53.87 |
| 4082.6 | 55.31 |
| 4083.1 | 57.82 |
| 4083.6 | 57.78 |
| 4084.1 | 68.98 |
| 4084.6 | 79.63 |
| 4085.0 | 87.37 |
| 4085.5 | 87.02 |
| 4086.0 | 99.89 |
| 4086.5 | 97.20 |
| 4087.0 | 94.09 |
| 4087.5 | 92.70 |
| 4088.0 | 92.81 |
| 4088.5 | 93.17 |
| 4088.9 | 88.88 |
| 4089.4 | 80.80 |
| 4089.9 | 76.84 |
| 4090.4 | 74.51 |
| 4090.9 | 60.85 |
| 4091.4 | 50.49 |
| 4091.9 | 43.71 |
| 4092.3 | 42.39 |
| 4092.8 | 44.00 |
| 4093.3 | 43.17 |
| 4093.8 | 43.51 |
| 4094.3 | 40.07 |
| 4094.8 | 37.23 |
| 4095.3 | 35.22 |
| 4095.7 | 34.01 |

Table A2.9: Water saturation data (calculated using Archie formula, Archie 1942) for the Great Oolite Formation in the Hesters Copse-1 well.

| TVDSS (ft) | Sw (%) |
| --- | --- |
| 3551.0 | 78.12 |
| 3551.5 | 88.85 |
| 3552.0 | 96.19 |
| 3552.5 | 90.30 |
| 3553.0 | 84.99 |
| 3553.5 | 83.71 |
| 3554.0 | 84.91 |
| 3554.5 | 84.47 |
| 3555.0 | 84.96 |
| 3555.5 | 84.70 |
| 3556.0 | 85.88 |
| 3556.5 | 85.00 |
| 3557.0 | 87.13 |
| 3557.5 | 88.65 |
| 3558.0 | 91.74 |
| 3558.5 | 92.41 |
| 3559.0 | 91.49 |
| 3559.5 | 90.37 |
| 3560.0 | 89.20 |
| 3560.5 | 88.91 |
| 3561.0 | 88.77 |
| 3561.5 | 88.39 |
| 3562.0 | 88.67 |
| 3562.5 | 88.94 |
| 3563.0 | 88.42 |
| 3563.5 | 88.17 |
| 3564.0 | 87.74 |
| 3564.5 | 86.00 |
| 3565.0 | 85.21 |
| 3565.5 | 85.28 |
| 3566.0 | 85.84 |
| 3566.5 | 85.45 |
| 3567.0 | 83.57 |
| 3567.5 | 84.59 |
| 3568.0 | 84.86 |
| 3568.5 | 87.12 |
| 3569.0 | 86.59 |
| 3569.5 | 85.84 |
| 3570.0 | 84.77 |
| 3570.5 | 83.91 |
| 3571.0 | 84.95 |
| 3571.5 | 84.67 |
| 3572.0 | 84.98 |
| 3572.5 | 83.94 |
| 3573.0 | 83.82 |
| 3573.5 | 84.71 |
| 3574.0 | 85.30 |
| 3574.5 | 84.19 |
| 3575.0 | 86.26 |
| 3575.5 | 88.07 |
| 3576.0 | 89.33 |
| 3576.5 | 88.26 |
| 3577.0 | 89.22 |
| 3577.5 | 92.25 |
| 3578.0 | 92.25 |
| 3578.5 | 91.59 |
| 3579.0 | 90.30 |
| 3579.5 | 89.79 |
| 3580.0 | 88.87 |
| 3580.5 | 89.19 |
| 3581.0 | 89.78 |
| 3581.5 | 93.41 |
| 3582.0 | 93.98 |
| 3582.5 | 94.57 |
| 3583.0 | 92.47 |
| 3583.5 | 91.30 |
| 3584.0 | 93.83 |
| 3584.5 | 98.57 |
| 3585.0 | 104.35 |
| 3585.5 | 95.53 |
| 3586.0 | 83.58 |
| 3586.5 | 79.69 |
| 3587.0 | 80.30 |
| 3587.5 | 85.72 |
| 3588.0 | 86.36 |
| 3588.5 | 84.44 |
| 3589.0 | 82.29 |
| 3589.5 | 84.60 |
| 3590.0 | 85.49 |
| 3590.5 | 86.30 |
| 3591.0 | 86.57 |
| 3591.5 | 88.53 |
| 3592.0 | 90.19 |
| 3592.5 | 90.34 |
| 3593.0 | 90.77 |
| 3593.5 | 91.24 |
| 3594.0 | 90.69 |
| 3594.5 | 91.37 |
| 3595.0 | 90.68 |
| 3595.5 | 91.96 |
| 3596.0 | 91.20 |
| 3596.5 | 91.01 |
| 3597.0 | 91.51 |
| 3597.5 | 92.05 |
| 3598.0 | 93.91 |
| 3598.5 | 94.67 |
| 3599.0 | 95.05 |
| 3599.5 | 94.93 |
| 3600.0 | 93.63 |
| 3600.5 | 93.23 |
| 3601.0 | 91.44 |
| 3601.5 | 92.51 |
| 3602.0 | 93.48 |
| 3602.5 | 94.92 |
| 3603.0 | 94.71 |
| 3603.5 | 95.14 |
| 3604.0 | 95.20 |
| 3604.5 | 97.21 |
| 3605.0 | 97.09 |
| 3605.5 | 98.56 |
| 3606.0 | 97.94 |
| 3606.5 | 96.45 |
| 3607.0 | 97.31 |
| 3607.5 | 97.04 |
| 3608.0 | 99.84 |
| 3608.5 | 102.37 |
| 3609.0 | 106.62 |
| 3609.5 | 109.96 |
| 3610.0 | 114.29 |
| 3610.5 | 109.74 |
| 3611.0 | 98.72 |
| 3611.5 | 92.09 |
| 3612.0 | 94.22 |
| 3612.5 | 103.35 |
| 3613.0 | 111.89 |
| 3613.5 | 107.44 |
| 3614.0 | 96.19 |
| 3614.5 | 90.03 |
| 3615.0 | 86.46 |
| 3615.5 | 85.60 |
| 3616.0 | 86.89 |
| 3616.5 | 86.88 |
| 3617.0 | 87.03 |
| 3617.5 | 86.34 |
| 3618.0 | 87.33 |
| 3618.5 | 86.11 |
| 3619.0 | 84.14 |
| 3619.5 | 83.19 |
| 3620.0 | 84.84 |
| 3620.5 | 85.18 |
| 3621.0 | 84.09 |
| 3621.5 | 83.72 |
| 3622.0 | 83.25 |
| 3622.5 | 83.20 |
| 3623.0 | 82.61 |
| 3623.5 | 83.36 |
| 3624.0 | 83.94 |
| 3624.5 | 84.08 |
| 3625.0 | 85.60 |
| 3625.5 | 87.25 |
| 3626.0 | 88.35 |
| 3626.5 | 88.58 |
| 3627.0 | 87.62 |
| 3627.5 | 87.86 |
| 3628.0 | 87.31 |
| 3628.5 | 87.71 |
| 3629.0 | 88.81 |
| 3629.5 | 89.32 |
| 3630.0 | 89.37 |
| 3630.5 | 89.39 |
| 3631.0 | 88.95 |
| 3631.5 | 88.80 |
| 3632.0 | 89.84 |
| 3632.5 | 92.06 |
| 3633.0 | 93.27 |
| 3633.5 | 92.72 |
| 3634.0 | 93.27 |
| 3634.5 | 93.25 |
| 3635.0 | 94.13 |
| 3635.5 | 91.48 |
| 3636.0 | 86.71 |
| 3636.5 | 82.37 |
| 3637.0 | 82.42 |
| 3637.5 | 84.52 |
| 3638.0 | 86.17 |
| 3638.5 | 85.45 |
| 3639.0 | 84.58 |
| 3639.5 | 83.64 |
| 3640.0 | 83.11 |
| 3640.5 | 83.53 |
| 3641.0 | 83.25 |
| 3641.5 | 84.88 |
| 3642.0 | 84.40 |
| 3642.5 | 84.81 |
| 3643.0 | 84.04 |
| 3643.5 | 84.73 |
| 3644.0 | 83.57 |
| 3644.5 | 83.22 |
| 3645.0 | 81.97 |
| 3645.5 | 83.66 |
| 3646.0 | 83.40 |
| 3646.5 | 82.22 |
| 3647.0 | 81.47 |
| 3647.5 | 82.07 |
| 3648.0 | 83.81 |
| 3648.5 | 84.42 |
| 3649.0 | 83.68 |
| 3649.5 | 83.74 |
| 3650.0 | 82.60 |
| 3650.5 | 80.56 |
| 3651.0 | 78.74 |
| 3651.5 | 78.67 |
| 3652.0 | 80.80 |
| 3652.5 | 81.48 |
| 3653.0 | 83.17 |
| 3653.5 | 82.08 |
| 3654.0 | 83.79 |
| 3654.5 | 83.37 |
| 3655.0 | 85.85 |
| 3655.5 | 86.08 |
| 3656.0 | 85.57 |
| 3656.5 | 84.84 |
| 3657.0 | 83.39 |
| 3657.5 | 83.59 |
| 3658.0 | 82.83 |
| 3658.5 | 82.73 |
| 3659.0 | 82.03 |
| 3659.5 | 82.62 |
| 3660.0 | 82.46 |
| 3660.5 | 82.34 |
| 3661.0 | 81.12 |
| 3661.5 | 82.33 |
| 3662.0 | 81.70 |
| 3662.5 | 81.08 |
| 3663.0 | 81.20 |
| 3663.5 | 82.72 |
| 3664.0 | 84.32 |
| 3664.5 | 83.64 |
| 3665.0 | 79.86 |
| 3665.5 | 78.39 |
| 3666.0 | 78.48 |
| 3666.5 | 79.96 |
| 3667.0 | 82.60 |
| 3667.5 | 86.20 |
| 3668.0 | 92.19 |
| 3668.5 | 97.20 |
| 3669.0 | 100.65 |
| 3669.5 | 105.42 |

APPENDIX 3 – Core analysis data

Table A3.1: Core analysis porosity and core permeability data for the Great Oolite Formation in the Singleton-1 well.

| TVDSS (ft) | POR. (%) | PERM. (mD) |
| --- | --- | --- |
| 4218.1 | 8.70 | 0.60 |
| 4218.7 | 9.70 | 1.72 |
| 4219.4 | 11.70 | 1.00 |
| 4220.0 | 9.40 | 0.28 |
| 4220.6 | 12.90 | 0.24 |
| 4221.3 | 10.90 | 0.10 |
| 4221.9 | 13.30 | 0.17 |
| 4222.5 | 12.00 | 0.49 |
| 4223.2 | 10.30 | 0.37 |
| 4223.8 | 9.00 | 0.23 |
| 4224.5 | 9.90 | 0.91 |
| 4225.1 | 10.30 | 0.08 |
| 4225.7 | 12.80 | 0.18 |
| 4226.4 | 12.90 | 1.18 |
| 4227.0 | 11.60 | 0.11 |
| 4227.6 | 11.30 | 0.15 |
| 4228.3 | 14.80 | 0.44 |
| 4228.9 | 7.10 | 0.06 |
| 4229.6 | 12.20 | 0.24 |
| 4230.2 | 18.10 | 2.48 |
| 4230.8 | 12.50 | 0.12 |
| 4231.5 | 8.50 | 0.08 |
| 4232.1 | 12.70 | 2.50 |
| 4232.7 | 19.90 | 4.58 |
| 4233.4 | 12.50 | 1.18 |
| 4234.0 | 18.60 | 3.82 |
| 4234.6 | 8.50 | 0.06 |
| 4235.3 | 13.70 | 1.47 |
| 4235.9 | 13.60 | 1.03 |
| 4236.6 | 12.80 | 0.34 |
| 4237.2 | 14.10 | 0.21 |
| 4237.8 | 10.80 | 0.91 |
| 4238.5 | 9.70 | 0.17 |
| 4239.1 | 10.30 | 0.12 |
| 4239.7 | 14.00 | 0.23 |
| 4240.4 | 11.70 | 0.15 |
| 4241.0 | 9.60 | 0.52 |
| 4241.7 | 11.70 | 0.16 |
| 4242.3 | 9.80 | 0.20 |
| 4242.9 | 11.00 | 0.45 |
| 4243.6 | 11.70 | 0.11 |
| 4244.2 | 12.90 | 0.15 |
| 4244.8 | 10.50 | 0.27 |
| 4245.5 | 10.80 | 0.40 |
| 4246.1 | 17.20 | 0.90 |
| 4246.7 | 13.00 | 0.87 |
| 4247.4 | 15.80 | 0.21 |
| 4248.0 | 15.60 | 2.28 |
| 4248.7 | 16.50 | 2.35 |
| 4249.3 | 21.10 | 5.17 |
| 4249.9 | 22.80 | 23.00 |
| 4250.6 | 15.70 | 0.13 |
| 4251.2 | 13.50 | 1.28 |
| 4251.8 | 16.70 | 0.99 |
| 4252.5 | 12.10 | 0.11 |
| 4253.1 | 14.20 | 0.18 |
| 4253.7 | 12.70 | 0.13 |
| 4254.4 | 12.90 | 0.13 |
| 4255.0 | 12.90 | 1.18 |
| 4255.6 | 12.10 | 0.09 |
| 4256.3 | 11.40 | 0.09 |
| 4256.9 | 15.50 | 0.43 |
| 4257.5 | 14.70 | 0.25 |
| 4258.2 | 10.80 | 0.15 |
| 4258.8 | 9.40 | 0.41 |
| 4259.4 | 8.50 | 0.13 |
| 4260.1 | 14.60 | 0.31 |
| 4260.7 | 10.50 | 0.11 |
| 4261.3 | 12.30 | 1.34 |
| 4262.0 | 9.60 | 0.04 |
| 4262.6 | 6.90 | 0.10 |
| 4263.2 | 8.20 | 0.10 |
| 4263.9 | 4.10 | 0.09 |
| 4264.5 | 4.90 | 0.11 |
| 4265.1 | 6.30 | 0.35 |
| 4265.8 | 3.20 | 0.26 |
| 4266.4 | 5.40 | 0.10 |
| 4267.0 | 4.40 | 0.24 |
| 4267.7 | 6.80 | 0.02 |
| 4268.3 | 4.10 | 0.02 |
| 4268.9 | 3.10 | 0.02 |
| 4269.6 | 2.70 | 0.02 |
| 4270.2 | 3.50 | 0.10 |
| 4270.8 | 8.20 | 0.81 |
| 4271.5 | 6.40 | 0.04 |
| 4272.1 | 14.80 | 7.08 |
| 4272.7 | 7.60 | 0.06 |
| 4273.3 | 11.60 | 0.13 |
| 4274.0 | 10.30 | 0.12 |
| 4274.6 | 11.30 | 0.70 |
| 4275.2 | 8.90 | 0.25 |
| 4275.9 | 17.90 | 4.15 |
| 4277.1 | 14.40 | 0.93 |
| 4277.7 | 12.40 | 0.43 |
| 4278.4 | 18.40 | 1.01 |
| 4279.0 | 17.00 | 1.78 |
| 4279.6 | 10.00 | 0.08 |
| 4280.3 | 15.90 | 0.59 |
| 4280.9 | 16.50 | 6.30 |
| 4281.5 | 14.90 | 1.79 |
| 4282.1 | 17.50 | 2.04 |
| 4282.8 | 12.10 | 0.20 |
| 4283.4 | 20.20 | 9.26 |
| 4284.0 | 20.10 | 9.59 |
| 4284.7 | 23.20 | 28.00 |
| 4285.3 | 17.60 | 6.17 |
| 4285.9 | 22.10 | 15.00 |
| 4286.5 | 17.90 | 6.92 |
| 4287.2 | 19.30 | 2.61 |
| 4288.4 | 14.90 | 0.78 |
| 4289.0 | 10.40 | 0.08 |
| 4289.7 | 17.40 | 1.47 |
| 4290.3 | 16.60 | 1.08 |
| 4290.9 | 11.20 | 0.09 |
| 4291.6 | 13.00 | 0.15 |
| 4292.2 | 13.00 | 0.20 |
| 4292.8 | 15.70 | 0.68 |
| 4293.4 | 18.30 | 1.72 |
| 4294.1 | 20.60 | 5.73 |
| 4295.3 | 15.80 | 0.32 |
| 4295.9 | 20.30 | 1.13 |
| 4296.6 | 19.60 | 3.34 |
| 4297.2 | 20.40 | 1.30 |
| 4298.4 | 10.90 | 0.04 |
| 4299.1 | 10.90 | 0.08 |
| 4299.7 | 10.40 | 0.15 |
| 4300.3 | 16.30 | 1.37 |
| 4300.9 | 18.70 | 1.90 |
| 4301.5 | 19.60 | 2.81 |
| 4302.2 | 13.50 | 0.25 |
| 4302.8 | 18.10 | 0.07 |
| 4304.0 | 14.40 | 0.45 |
| 4305.3 | 21.80 | 1.04 |
| 4306.5 | 23.50 | 5.31 |
| 4307.8 | 21.20 | 6.39 |
| 4308.4 | 19.50 | 0.27 |
| 4309.0 | 21.90 | 2.75 |
| 4309.6 | 18.30 | 1.00 |
| 4310.3 | 17.30 | 1.36 |
| 4310.9 | 12.50 | 0.47 |
| 4311.5 | 12.50 | 0.50 |
| 4312.1 | 14.70 | 0.49 |
| 4312.7 | 17.00 | 0.33 |
| 4313.4 | 12.80 | 0.44 |
| 4314.0 | 13.80 | 0.47 |
| 4314.6 | 21.70 | 0.31 |
| 4315.2 | 20.10 | 0.42 |
| 4315.8 | 21.50 | 0.55 |
| 4316.5 | 18.60 | 1.20 |
| 4317.1 | 20.10 | 0.67 |
| 4317.7 | 17.90 | 1.04 |
| 4318.3 | 19.30 | 0.34 |
| 4318.9 | 17.10 | 0.26 |
| 4319.5 | 12.70 | 0.29 |
| 4320.2 | 17.80 | 0.15 |
| 4320.8 | 16.10 | 0.12 |
| 4321.1 | 16.50 | 0.18 |
| 4322.3 | 16.90 | 1.26 |
| 4322.6 | 15.70 | 0.13 |
| 4323.3 | 13.50 | 0.10 |
| 4323.9 | 15.70 | 0.28 |
| 4324.8 | 15.60 | 0.12 |
| 4325.1 | 15.90 | 0.18 |
| 4325.7 | 19.70 | 0.55 |
| 4326.3 | 13.80 | 1.21 |
| 4327.0 | 20.50 | 0.61 |
| 4327.6 | 18.20 | 0.48 |
| 4328.2 | 14.50 | 0.21 |
| 4328.8 | 13.30 | 0.12 |
| 4329.4 | 11.50 | 0.15 |
| 4330.0 | 11.50 | 0.41 |
| 4331.3 | 16.60 | 0.17 |
| 4331.9 | 14.70 | 0.46 |
| 4332.5 | 12.60 | 0.88 |
| 4333.1 | 15.10 | 0.82 |
| 4333.7 | 12.90 | 0.26 |
| 4334.3 | 13.00 | 0.73 |
| 4334.9 | 12.70 | 0.39 |
| 4335.6 | 19.70 | 1.22 |
| 4336.2 | 17.30 | 1.32 |
| 4336.8 | 16.90 | 1.04 |
| 4337.4 | 15.30 | 0.83 |
| 4338.0 | 15.70 | 0.07 |
| 4338.6 | 16.80 | 1.18 |
| 4339.8 | 19.90 | 0.74 |
| 4340.5 | 14.80 | 0.63 |
| 4341.1 | 16.70 | 0.70 |
| 4343.5 | 16.40 | 0.44 |
| 4344.1 | 14.90 | 0.31 |
| 4344.7 | 14.70 | 0.21 |
| 4345.4 | 16.00 | 0.39 |
| 4346.6 | 14.50 | 0.18 |
| 4347.2 | 12.90 | 0.26 |
| 4347.8 | 15.30 | 0.35 |
| 4348.4 | 14.50 | 0.34 |
| 4349.0 | 12.70 | 0.30 |
| 4349.6 | 12.50 | 0.36 |
| 4350.2 | 6.80 | 0.02 |
| 4350.8 | 13.30 | 0.56 |
| 4352.7 | 15.70 | 1.15 |
| 4353.3 | 13.50 | 1.01 |
| 4353.9 | 14.00 | 0.75 |
| 4354.5 | 16.80 | 0.18 |
| 4355.1 | 17.40 | 2.39 |
| 4355.7 | 11.60 | 0.05 |
| 4356.3 | 10.50 | 0.02 |
| 4356.9 | 19.10 | 0.19 |
| 4357.5 | 16.90 | 0.16 |
| 4358.1 | 16.90 | 1.60 |
| 4358.7 | 12.10 | 0.06 |
| 4359.3 | 15.90 | 0.14 |
| 4359.6 | 14.80 | 0.09 |
| 4360.0 | 12.80 | 1.00 |
| 4360.6 | 13.10 | 1.00 |
| 4361.2 | 15.50 | 0.26 |
| 4361.8 | 17.40 | 1.31 |
| 4362.4 | 16.90 | 2.21 |
| 4363.0 | 12.50 | 0.06 |
| 4363.6 | 12.30 | 0.44 |
| 4364.2 | 12.20 | 0.58 |
| 4364.8 | 16.20 | 1.10 |
| 4365.4 | 14.90 | 0.09 |
| 4366.0 | 13.80 | 0.10 |
| 4366.6 | 13.10 | 0.60 |
| 4367.8 | 15.30 | 0.78 |
| 4368.4 | 16.40 | 1.20 |
| 4369.0 | 12.60 | 0.42 |
| 4369.6 | 12.40 | 0.17 |
| 4370.2 | 12.70 | 0.37 |
| 4370.9 | 15.70 | 0.91 |
| 4371.5 | 15.50 | 0.38 |
| 4372.1 | 17.30 | 1.34 |
| 4372.7 | 13.60 | 0.27 |
| 4373.3 | 13.40 | 0.09 |
| 4373.9 | 12.90 | 0.49 |
| 4374.5 | 18.60 | 0.81 |
| 4375.1 | 18.40 | 0.90 |
| 4375.7 | 17.70 | 0.59 |
| 4376.3 | 14.80 | 0.93 |
| 4376.9 | 14.90 | 0.51 |
| 4377.5 | 14.30 | 0.31 |
| 4378.1 | 12.80 | 0.33 |
| 4378.7 | 15.20 | 0.46 |
| 4379.3 | 14.80 | 0.45 |
| 4380.5 | 16.30 | 1.08 |
| 4381.1 | 9.90 | 0.08 |
| 4381.7 | 15.10 | 0.43 |
| 4382.3 | 16.00 | 0.36 |
| 4382.9 | 11.80 | 0.16 |
| 4383.5 | 13.40 | 0.50 |
| 4384.1 | 14.90 | 1.01 |
| 4384.7 | 14.20 | 0.56 |
| 4385.4 | 12.20 | 0.33 |
| 4386.0 | 14.00 | 0.51 |
| 4386.6 | 15.40 | 0.66 |
| 4387.2 | 15.70 | 0.16 |
| 4387.8 | 11.40 | 0.25 |
| 4388.4 | 9.60 | 0.04 |
| 4389.0 | 13.50 | 0.57 |
| 4389.6 | 12.60 | 0.27 |
| 4390.8 | 9.40 | 0.03 |
| 4391.4 | 8.70 | 0.04 |
| 4392.0 | 9.20 | 0.07 |
| 4392.6 | 6.70 | 0.02 |

Table A3.2: Core analysis porosity and core permeability data for the Great Oolite Formation in the Storrington-2 well.

| TVDSS (ft) | POR. (%) | PERM. (mD) |
| --- | --- | --- |
| 3889.1 | 10.55 | 0.21 |
| 3889.6 | 12.00 | 0.28 |
| 3890.1 | 12.00 | 0.23 |
| 3890.6 | 12.00 | 0.17 |
| 3891.1 | 11.55 | 0.18 |
| 3891.6 | 11.10 | 0.19 |
| 3892.1 | 10.15 | 0.23 |
| 3892.5 | 9.20 | 0.26 |
| 3893.0 | 11.90 | 0.22 |
| 3893.5 | 13.40 | 51.00 |
| 3894.0 | 11.15 | 11.37 |
| 3894.5 | 11.70 | 22.00 |
| 3895.0 | 13.30 | 44.00 |
| 3895.5 | 12.00 | 0.23 |
| 3895.9 | 11.90 | 0.25 |
| 3896.4 | 11.80 | 0.26 |
| 3896.9 | 11.00 | 0.24 |
| 3897.4 | 10.20 | 0.21 |
| 3897.9 | 7.55 | 0.12 |
| 3898.4 | 4.90 | 0.02 |
| 3898.9 | 5.00 | 0.02 |
| 3899.3 | 3.10 | 0.11 |
| 3899.8 | 5.45 | 0.03 |
| 3900.3 | 5.80 | 0.04 |
| 3900.8 | 5.00 | 0.08 |
| 3901.3 | 4.20 | 0.11 |
| 3901.8 | 3.75 | 0.06 |
| 3902.3 | 3.30 | 0.06 |
| 3902.7 | 4.40 | 0.05 |
| 3903.2 | 5.50 | 0.04 |
| 3903.7 | 2.30 | 0.07 |
| 3904.2 | 2.50 | 0.02 |
| 3904.7 | 3.10 | 0.03 |
| 3905.2 | 3.70 | 0.04 |
| 3905.7 | 3.65 | 0.03 |
| 3906.2 | 3.60 | 0.03 |
| 3906.6 | 4.60 | 0.04 |
| 3907.1 | 5.60 | 0.04 |
| 3907.6 | 6.80 | 0.04 |
| 3908.1 | 8.00 | 0.05 |
| 3908.6 | 7.90 | 0.05 |
| 3909.1 | 7.80 | 0.06 |
| 3909.6 | 7.95 | 0.04 |
| 3910.0 | 8.10 | 0.03 |
| 3910.5 | 11.30 | 29.00 |
| 3911.0 | 11.90 | 27.00 |
| 3911.5 | 16.00 | 99.50 |
| 3912.0 | 12.30 | 5.72 |
| 3912.5 | 12.40 | 15.00 |
| 3913.0 | 9.70 | 0.08 |
| 3913.4 | 9.90 | 0.07 |
| 3913.9 | 13.90 | 33.00 |
| 3914.4 | 9.90 | 0.10 |
| 3914.9 | 9.70 | 0.14 |
| 3915.4 | 9.60 | 0.15 |
| 3915.9 | 9.50 | 0.16 |
| 3916.4 | 10.80 | 0.14 |
| 3916.8 | 12.10 | 0.12 |
| 3917.3 | 12.30 | 0.16 |
| 3917.8 | 12.50 | 0.19 |
| 3918.3 | 12.80 | 0.15 |
| 3918.8 | 14.50 | 37.00 |
| 3919.3 | 11.90 | 0.12 |
| 3919.8 | 10.70 | 0.12 |
| 3920.3 | 9.00 | 0.33 |
| 3920.7 | 7.30 | 0.54 |
| 3921.2 | 6.65 | 0.28 |
| 3921.7 | 6.50 | 0.14 |
| 3922.2 | 4.25 | 0.02 |
| 3922.7 | 2.50 | 0.02 |
| 3923.2 | 2.15 | 0.03 |
| 3923.7 | 1.80 | 0.04 |
| 3924.1 | 1.80 | 0.03 |
| 3924.6 | 1.80 | 0.02 |
| 3925.1 | 1.90 | 0.02 |
| 3925.6 | 2.00 | 0.02 |
| 3926.1 | 1.85 | 0.02 |
| 3926.6 | 1.70 | 0.01 |
| 3927.1 | 2.30 | 0.02 |
| 3927.5 | 2.90 | 0.03 |
| 3928.0 | 2.65 | 0.05 |
| 3928.5 | 2.40 | 0.06 |
| 3929.0 | 10.00 | 1.00 |
| 3929.5 | 9.00 | 1.10 |
| 3930.0 | 10.20 | 0.98 |
| 3930.5 | 8.80 | 1.54 |
| 3930.9 | 9.90 | 1.62 |
| 3931.4 | 10.30 | 1.30 |
| 3931.9 | 11.00 | 1.20 |
| 3932.4 | 10.40 | 1.20 |
| 3932.9 | 8.00 | 1.50 |
| 3933.4 | 9.80 | 1.90 |
| 3933.9 | 10.30 | 1.00 |
| 3934.3 | 7.20 | 0.06 |
| 3934.8 | 8.45 | 0.05 |
| 3935.3 | 11.50 | 25.50 |
| 3935.8 | 12.50 | 25.00 |
| 3936.3 | 6.60 | 0.15 |
| 3936.8 | 5.00 | 0.05 |
| 3937.3 | 6.00 | 0.04 |
| 3937.8 | 6.70 | 0.05 |
| 3938.2 | 6.40 | 0.12 |
| 3938.7 | 4.90 | 0.03 |
| 3939.2 | 5.50 | 0.03 |
| 3939.7 | 3.10 | 0.06 |
| 3940.2 | 5.70 | 0.05 |
| 3940.7 | 8.10 | 0.08 |
| 3941.2 | 7.80 | 0.08 |
| 3941.6 | 6.90 | 0.06 |
| 3942.1 | 9.10 | 0.07 |
| 3942.6 | 8.20 | 0.06 |
| 3943.1 | 7.00 | 0.08 |
| 3943.6 | 5.00 | 0.10 |
| 3944.1 | 5.80 | 0.14 |
| 3944.6 | 5.00 | 0.08 |
| 3945.0 | 1.80 | 0.06 |
| 3945.5 | 13.00 | 0.87 |
| 3946.0 | 5.00 | 1.71 |
| 3946.5 | 12.00 | 0.87 |
| 3947.0 | 3.70 | 0.03 |
| 3947.5 | 2.15 | 0.05 |
| 3948.0 | 2.45 | 0.05 |
| 3948.4 | 3.30 | 0.03 |
| 3948.9 | 3.30 | 0.03 |
| 3949.4 | 3.30 | 0.04 |
| 3949.9 | 3.30 | 0.04 |
| 3950.4 | 13.00 | 4.41 |
| 3950.9 | 12.70 | 8.77 |
| 3951.4 | 12.60 | 4.40 |
| 3951.9 | 2.50 | 0.02 |
| 3952.3 | 2.20 | 0.03 |
| 3952.8 | 1.90 | 0.03 |
| 3953.3 | 2.00 | 0.05 |
| 3953.8 | 2.10 | 0.07 |
| 3954.3 | 1.95 | 0.06 |
| 3954.8 | 1.80 | 0.05 |
| 3955.3 | 1.85 | 0.05 |
| 3955.7 | 1.90 | 0.04 |
| 3956.2 | 2.05 | 0.03 |
| 3956.7 | 2.20 | 0.05 |
| 3957.2 | 2.65 | 0.05 |
| 3957.7 | 3.10 | 0.05 |
| 3958.2 | 2.50 | 0.03 |
| 3958.7 | 1.90 | 0.01 |
| 3959.1 | 2.35 | 0.02 |
| 3959.6 | 2.80 | 0.02 |
| 3960.1 | 2.95 | 0.07 |
| 3960.6 | 5.10 | 0.02 |
| 3961.1 | 7.10 | 0.88 |
| 3961.6 | 11.10 | 1.64 |
| 3962.1 | 10.85 | 1.09 |
| 3962.5 | 10.60 | 0.53 |
| 3963.0 | 10.60 | 0.63 |
| 3963.5 | 10.60 | 0.73 |
| 3964.0 | 14.85 | 0.17 |
| 3964.5 | 15.10 | 0.15 |
| 3965.0 | 9.70 | 0.04 |
| 3965.5 | 9.75 | 0.03 |
| 3966.0 | 11.40 | 0.04 |
| 3966.4 | 8.25 | 0.03 |
| 3966.9 | 11.45 | 12.81 |
| 3967.4 | 10.40 | 0.62 |
| 3967.9 | 11.28 | 8.72 |
| 3968.4 | 12.15 | 16.81 |
| 3968.9 | 13.03 | 24.91 |
| 3969.4 | 10.10 | 0.05 |
| 3969.8 | 13.60 | 38.50 |
| 3970.3 | 13.55 | 0.19 |
| 3970.8 | 15.15 | 205.00 |
| 3971.3 | 17.00 | 366.00 |
| 3971.8 | 16.35 | 207.00 |
| 3972.3 | 15.70 | 48.00 |
| 3972.8 | 11.95 | 0.06 |
| 3973.2 | 16.30 | 151.00 |
| 3973.7 | 15.75 | 269.00 |
| 3974.2 | 15.20 | 387.00 |
| 3974.7 | 16.40 | 225.00 |
| 3975.2 | 17.60 | 63.00 |
| 3975.7 | 18.30 | 38.50 |
| 3976.2 | 19.00 | 14.00 |
| 3976.6 | 16.75 | 25.50 |
| 3977.1 | 13.10 | 0.11 |
| 3977.6 | 16.05 | 41.00 |
| 3978.1 | 17.60 | 45.00 |
| 3978.6 | 18.20 | 39.00 |
| 3979.1 | 18.80 | 33.00 |
| 3979.6 | 18.50 | 23.50 |
| 3980.1 | 18.20 | 14.00 |
| 3980.5 | 15.80 | 32.50 |
| 3981.0 | 14.60 | 0.18 |
| 3981.5 | 15.25 | 33.00 |
| 3982.0 | 17.10 | 15.00 |
| 3982.5 | 16.60 | 14.50 |
| 3983.0 | 16.10 | 14.00 |
| 3983.5 | 14.65 | 7.37 |
| 3983.9 | 13.20 | 0.73 |
| 3984.4 | 13.25 | 0.85 |
| 3984.9 | 13.30 | 0.97 |
| 3985.4 | 15.60 | 3.44 |
| 3985.9 | 17.90 | 5.90 |
| 3986.4 | 17.50 | 6.39 |
| 3986.9 | 17.10 | 6.88 |
| 3987.3 | 17.75 | 22.44 |
| 3987.8 | 18.40 | 38.00 |
| 3988.3 | 18.20 | 25.50 |
| 3988.8 | 18.00 | 13.00 |
| 3989.3 | 12.95 | 6.57 |
| 3989.8 | 7.90 | 0.14 |
| 3990.3 | 12.45 | 3.73 |
| 3990.7 | 17.00 | 7.32 |
| 3991.2 | 17.25 | 6.36 |
| 3991.7 | 17.50 | 5.39 |
| 3992.2 | 14.90 | 5.56 |
| 3992.7 | 12.50 | 0.07 |
| 3993.2 | 14.95 | 13.86 |
| 3993.7 | 17.60 | 22.00 |
| 3994.2 | 18.40 | 16.50 |
| 3994.6 | 19.20 | 11.00 |
| 3995.1 | 18.40 | 11.00 |
| 3995.6 | 17.60 | 11.00 |
| 3996.1 | 17.90 | 29.00 |
| 3996.6 | 18.20 | 47.00 |
| 3997.1 | 19.70 | 56.50 |
| 3997.6 | 21.20 | 66.00 |
| 3998.0 | 19.25 | 41.50 |
| 3998.5 | 17.30 | 17.00 |
| 3999.0 | 18.58 | 39.00 |
| 3999.5 | 19.85 | 61.00 |
| 4000.0 | 21.13 | 83.00 |
| 4000.5 | 22.40 | 105.00 |
| 4001.0 | 21.55 | 81.50 |
| 4001.4 | 20.70 | 58.00 |
| 4001.9 | 19.20 | 49.75 |
| 4002.4 | 17.70 | 41.50 |
| 4002.9 | 18.75 | 33.25 |
| 4003.4 | 19.80 | 25.00 |
| 4003.9 | 19.20 | 37.50 |
| 4004.4 | 18.60 | 50.00 |
| 4004.8 | 20.35 | 52.50 |
| 4005.3 | 22.10 | 55.00 |
| 4005.8 | 19.65 | 38.50 |
| 4006.3 | 17.20 | 22.00 |
| 4006.8 | 19.85 | 72.50 |
| 4007.3 | 22.50 | 45.00 |
| 4007.8 | 20.20 | 64.18 |
| 4008.2 | 17.90 | 5.35 |
| 4008.7 | 20.40 | 50.68 |
| 4009.2 | 22.90 | 96.00 |
| 4009.7 | 21.15 | 53.50 |
| 4010.2 | 19.40 | 11.00 |
| 4010.7 | 18.75 | 17.50 |
| 4011.2 | 18.10 | 24.00 |
| 4011.7 | 17.50 | 20.00 |
| 4012.1 | 16.90 | 16.00 |
| 4012.6 | 16.05 | 15.75 |
| 4013.1 | 15.20 | 15.50 |
| 4013.6 | 14.35 | 15.25 |
| 4014.1 | 13.50 | 15.00 |
| 4014.6 | 16.80 | 18.50 |
| 4015.1 | 20.10 | 22.00 |
| 4015.5 | 21.15 | 37.50 |
| 4016.0 | 22.20 | 53.00 |
| 4016.5 | 17.30 | 34.00 |
| 4017.0 | 11.10 | 0.08 |
| 4017.5 | 14.10 | 8.36 |
| 4018.0 | 15.80 | 1.71 |
| 4018.5 | 14.30 | 0.96 |
| 4018.9 | 12.80 | 0.21 |
| 4019.4 | 13.45 | 0.70 |
| 4019.9 | 14.10 | 1.19 |
| 4020.4 | 15.00 | 1.88 |
| 4020.9 | 15.90 | 2.57 |
| 4021.4 | 13.85 | 1.51 |
| 4021.9 | 11.80 | 0.44 |
| 4022.3 | 12.65 | 1.19 |
| 4022.8 | 13.50 | 1.93 |
| 4023.3 | 14.50 | 2.88 |
| 4023.8 | 15.50 | 3.83 |
| 4024.3 | 15.00 | 2.45 |
| 4024.8 | 14.50 | 1.06 |
| 4025.3 | 12.98 | 0.84 |
| 4025.7 | 11.45 | 0.63 |
| 4026.2 | 9.93 | 0.41 |
| 4026.7 | 8.40 | 0.19 |
| 4027.2 | 11.70 | 0.32 |
| 4027.7 | 15.00 | 0.45 |
| 4028.2 | 13.40 | 0.38 |
| 4028.7 | 11.80 | 0.30 |
| 4029.2 | 12.60 | 0.37 |
| 4029.6 | 13.40 | 0.43 |
| 4030.1 | 11.70 | 0.32 |
| 4030.6 | 10.00 | 0.21 |
| 4031.1 | 10.00 | 0.23 |
| 4031.6 | 10.00 | 0.25 |
| 4032.1 | 11.95 | 0.34 |
| 4032.6 | 13.90 | 0.43 |
| 4033.0 | 14.50 | 0.37 |
| 4033.5 | 15.10 | 0.30 |
| 4034.0 | 15.00 | 0.42 |
| 4034.5 | 14.90 | 0.54 |
| 4035.0 | 15.00 | 0.43 |
| 4035.5 | 15.10 | 0.32 |
| 4036.0 | 13.95 | 0.40 |
| 4036.4 | 12.80 | 0.48 |
| 4036.9 | 13.05 | 0.47 |
| 4037.4 | 13.30 | 0.46 |
| 4037.9 | 12.10 | 0.35 |
| 4038.4 | 10.90 | 0.23 |
| 4038.9 | 11.75 | 0.27 |
| 4039.4 | 12.60 | 0.31 |
| 4039.8 | 12.50 | 0.63 |
| 4040.3 | 12.40 | 0.95 |
| 4040.8 | 12.20 | 0.60 |
| 4041.3 | 12.00 | 0.24 |
| 4041.8 | 11.40 | 0.66 |
| 4042.3 | 10.80 | 1.07 |
| 4042.8 | 10.55 | 0.76 |
| 4043.2 | 10.30 | 0.44 |
| 4043.7 | 10.35 | 0.69 |
| 4044.2 | 10.40 | 0.93 |
| 4044.7 | 8.40 | 0.53 |
| 4045.2 | 6.40 | 0.02 |
| 4045.7 | 6.00 | 0.02 |
| 4046.2 | 6.80 | 0.02 |
| 4046.6 | 7.75 | 0.15 |
| 4047.1 | 8.90 | 0.15 |
| 4047.6 | 8.55 | 0.11 |
| 4048.1 | 8.20 | 0.06 |
| 4048.6 | 9.45 | 0.12 |
| 4049.1 | 10.70 | 0.18 |
| 4049.6 | 9.85 | 0.17 |
| 4050.1 | 9.00 | 0.16 |
| 4050.5 | 9.55 | 0.15 |
| 4051.0 | 10.10 | 0.13 |
| 4051.5 | 9.00 | 0.11 |
| 4052.0 | 7.90 | 0.09 |
| 4052.5 | 7.90 | 0.08 |
| 4053.0 | 7.90 | 0.06 |
| 4053.5 | 7.75 | 0.07 |
| 4053.9 | 7.60 | 0.08 |
| 4054.4 | 9.50 | 0.10 |
| 4054.9 | 11.40 | 0.12 |
| 4055.4 | 11.38 | 0.17 |
| 4055.9 | 11.35 | 0.22 |
| 4056.4 | 11.33 | 0.26 |
| 4056.9 | 11.30 | 0.31 |
| 4057.3 | 11.20 | 0.23 |
| 4057.8 | 11.10 | 0.15 |
| 4058.3 | 10.50 | 0.20 |
| 4058.8 | 9.90 | 0.24 |
| 4059.3 | 11.75 | 0.18 |
| 4059.8 | 13.60 | 0.12 |
| 4060.3 | 13.00 | 0.14 |
| 4060.7 | 12.40 | 0.16 |
| 4061.2 | 11.85 | 0.15 |
| 4061.7 | 11.30 | 0.14 |
| 4062.2 | 12.05 | 0.15 |
| 4062.7 | 12.80 | 0.16 |
| 4063.2 | 11.55 | 0.13 |
| 4063.7 | 10.30 | 0.10 |
| 4064.1 | 10.80 | 0.11 |
| 4064.6 | 11.30 | 0.12 |
| 4065.1 | 11.85 | 0.15 |
| 4065.6 | 12.40 | 0.17 |
| 4066.1 | 11.40 | 0.16 |
| 4066.6 | 10.40 | 0.14 |
| 4067.1 | 11.55 | 0.17 |
| 4067.5 | 12.70 | 0.19 |
| 4068.0 | 12.25 | 0.18 |
| 4068.5 | 11.80 | 0.16 |
| 4069.0 | 11.30 | 0.15 |
| 4069.5 | 10.80 | 0.13 |
| 4070.0 | 10.65 | 0.13 |
| 4070.5 | 10.50 | 0.12 |
| 4071.0 | 10.58 | 0.12 |
| 4071.4 | 10.65 | 0.12 |
| 4071.9 | 10.73 | 0.11 |
| 4072.4 | 10.80 | 0.11 |
| 4072.9 | 10.15 | 0.09 |
| 4073.4 | 9.50 | 0.07 |
| 4073.9 | 8.90 | 0.07 |
| 4074.4 | 8.30 | 0.06 |
| 4074.8 | 8.90 | 0.08 |
| 4075.3 | 9.50 | 0.10 |
| 4075.8 | 8.90 | 0.09 |
| 4076.3 | 8.30 | 0.08 |
| 4076.8 | 7.80 | 0.08 |
| 4077.3 | 7.30 | 0.08 |
| 4077.8 | 6.15 | 0.06 |
| 4078.2 | 5.00 | 0.04 |
| 4078.7 | 5.30 | 0.05 |
| 4079.2 | 5.60 | 0.05 |
| 4079.7 | 5.30 | 0.05 |
| 4080.2 | 5.00 | 0.06 |
| 4080.7 | 4.70 | 0.06 |
| 4081.2 | 4.40 | 0.06 |
| 4081.6 | 5.60 | 0.03 |
| 4082.1 | 4.20 | 0.02 |
| 4082.6 | 2.05 | 0.04 |
| 4083.1 | 2.30 | 0.02 |
| 4083.6 | 2.10 | 0.02 |
| 4084.1 | 1.90 | 0.02 |
| 4084.6 | 1.95 | 0.02 |
| 4085.0 | 2.00 | 0.02 |
| 4085.5 | 3.50 | 0.03 |
| 4086.0 | 4.00 | 0.02 |
| 4086.5 | 3.30 | 0.02 |
| 4087.0 | 2.60 | 0.03 |
| 4087.5 | 2.10 | 0.03 |
| 4088.0 | 1.60 | 0.03 |
| 4088.5 | 12.75 | 1.23 |
| 4088.9 | 13.90 | 2.42 |
| 4089.4 | 12.85 | 1.22 |
| 4089.9 | 1.80 | 0.01 |
| 4090.4 | 1.90 | 0.02 |
| 4090.9 | 2.00 | 0.02 |
| 4091.4 | 2.50 | 0.03 |
| 4091.9 | 3.00 | 0.03 |
| 4092.3 | 2.00 | 0.01 |
| 4092.8 | 1.80 | 0.01 |
| 4093.3 | 1.60 | 0.01 |
| 4093.8 | 1.50 | 0.01 |
| 4094.3 | 1.60 | 0.01 |
| 4094.8 | 1.30 | 0.01 |
| 4095.3 | 1.00 | 0.01 |
| 4095.7 | 1.20 | 0.01 |

Table A3.3: Core analysis porosity and core permeability data for the Great Oolite Formation in the Hesters Copse-1 well.

| TVDSS (ft) | POR. (%) | PERM. (mD) |
| --- | --- | --- |
| 3551.5 | 12.70 | 0.17 |
| 3552.5 | 10.50 | 0.38 |
| 3553.5 | 14.50 | 0.15 |
| 3554.5 | 11.80 | 0.19 |
| 3555.5 | 14.50 | 0.23 |
| 3556.5 | 11.40 | 0.19 |
| 3557.5 | 8.50 | 0.16 |
| 3558.5 | 12.00 | 0.25 |
| 3559.5 | 10.70 | 0.15 |
| 3560.5 | 12.10 | 0.12 |
| 3561.5 | 12.30 | 0.52 |
| 3562.5 | 11.00 | 0.26 |
| 3563.5 | 10.30 | 0.26 |
| 3564.5 | 12.10 | 0.28 |
| 3565.5 | 12.60 | 0.33 |
| 3566.5 | 15.50 | 0.65 |
| 3567.5 | 12.30 | 0.27 |
| 3568.5 | 12.70 | 0.35 |
| 3569.5 | 12.50 | 0.39 |
| 3570.5 | 13.20 | 0.34 |
| 3571.5 | 8.60 | 0.14 |
| 3572.5 | 7.60 | 0.11 |
| 3573.5 | 8.30 | 0.06 |
| 3574.5 | 6.50 | 0.05 |
| 3575.5 | 9.10 | 0.11 |
| 3576.5 | 8.10 | 0.80 |
| 3582.5 | 7.30 | 1.60 |
| 3583.5 | 5.60 | 0.03 |
| 3584.5 | 6.80 | 0.05 |
| 3585.5 | 5.00 | 0.01 |
| 3586.5 | 6.70 | 9.00 |
| 3587.5 | 9.00 | 9.00 |
| 3588.5 | 10.70 | 2.40 |
| 3589.5 | 15.70 | 1.60 |
| 3590.5 | 10.00 | 0.27 |
| 3591.5 | 12.10 | 0.60 |
| 3592.5 | 11.50 | 0.21 |
| 3593.5 | 12.70 | 0.46 |
| 3594.5 | 9.00 | 9.00 |
| 3595.5 | 10.30 | 0.20 |
| 3596.5 | 10.50 | 0.26 |
| 3597.5 | 12.00 | 0.32 |
| 3598.5 | 12.50 | 0.13 |
| 3599.5 | 9.00 | 0.08 |
| 3600.5 | 8.70 | 0.10 |
| 3601.5 | 10.40 | 0.08 |
| 3602.5 | 10.50 | 0.01 |
| 3603.5 | 10.50 | 0.04 |
| 3604.5 | 11.10 | 0.03 |
| 3605.5 | 11.20 | 0.05 |
| 3606.5 | 6.70 | 0.08 |
| 3607.5 | 9.10 | 0.02 |
| 3608.5 | 9.80 | 0.03 |
| 3609.5 | 7.60 | 0.01 |
| 3610.5 | 5.40 | 0.01 |
| 3611.5 | 4.30 | 0.01 |
| 3612.5 | 8.80 | 7.10 |
| 3613.5 | 4.90 | 0.01 |
| 3614.5 | 4.40 | 0.01 |
| 3615.5 | 6.90 | 0.01 |
| 3616.5 | 10.00 | 0.15 |
| 3617.5 | 10.10 | 0.31 |
| 3618.5 | 12.90 | 0.31 |
| 3619.5 | 17.70 | 0.45 |
| 3620.5 | 9.00 | 9.00 |
| 3621.5 | 16.40 | 0.58 |
| 3622.5 | 16.10 | 0.69 |
| 3623.5 | 18.00 | 0.52 |
| 3624.5 | 16.80 | 4.30 |
| 3625.5 | 16.70 | 0.69 |
| 3626.5 | 13.10 | 1.80 |
| 3627.5 | 15.30 | 0.73 |
| 3628.5 | 7.00 | 0.60 |
| 3629.5 | 13.20 | 0.77 |
| 3630.5 | 13.10 | 0.47 |
| 3631.5 | 12.30 | 0.32 |
| 3632.5 | 10.80 | 0.35 |
| 3633.5 | 9.30 | 0.33 |
| 3634.5 | 8.80 | 0.34 |
| 3635.5 | 6.00 | 0.03 |
| 3636.5 | 14.30 | 0.33 |
| 3637.5 | 12.80 | 0.30 |
| 3638.5 | 12.40 | 0.24 |
| 3639.5 | 14.70 | 1.70 |
| 3640.5 | 18.10 | 0.42 |
| 3643.5 | 19.60 | 0.72 |
| 3644.5 | 19.90 | 0.47 |
| 3645.5 | 18.00 | 0.43 |
| 3646.5 | 19.30 | 0.21 |
| 3647.5 | 18.00 | 0.48 |
| 3648.5 | 17.30 | 0.51 |
| 3649.5 | 9.40 | 0.51 |
| 3650.5 | 12.40 | 0.52 |
| 3651.5 | 14.00 | 0.46 |
| 3652.5 | 14.20 | 0.80 |
| 3653.5 | 16.20 | 0.55 |
| 3654.5 | 15.30 | 0.69 |
| 3655.5 | 17.70 | 0.63 |
| 3656.5 | 19.20 | 0.58 |
| 3657.5 | 19.90 | 0.69 |
| 3658.5 | 15.90 | 0.68 |
| 3659.5 | 17.70 | 0.82 |
| 3660.5 | 15.80 | 0.35 |
| 3661.5 | 18.20 | 0.64 |
| 3662.5 | 15.50 | 0.69 |
| 3663.5 | 16.70 | 0.45 |
| 3664.5 | 16.30 | 0.37 |
| 3665.5 | 13.90 | 0.18 |
| 3666.5 | 16.60 | 0.16 |
| 3667.5 | 13.10 | 0.11 |
| 3668.5 | 7.70 | 0.01 |
| 3669.5 | 3.60 | 0.01 |

APPENDIX 4 – XRD data

Table A4.1: Quantitative XRD data for all samples (whole rock) of the Great Oolite Formation analysed in Singleton-1, Horndean-1A, Hesters Copse-1, Chilgrove-1 and Ashington-1 wells.

| Sample | TVDSS (ft) | DBTF (ft) | Calcite (%) | Dolomite (%) | Quartz (%) | Pyrite (%) | Clay (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S-25 | 4218.7 | 0.7 | 94.8 | 3.4 | 1.4 | 0.4 | 0 |
| S-24 | 4220.6 | 2.6 | 98.1 | 1.2 | 0.7 | 0 | 0 |
| S-23 | 4228.3 | 10.3 | 53.5 | 38.2 | 3.7 | 2.4 | 2.2 |
| S-22 | 4233.7 | 15.7 | 98 | 0.8 | 0.7 | 0.5 | 0 |
| S-21 | 4241 | 23 | 62.6 | 33.9 | 1.9 | 0.8 | 0.8 |
| S-20 | 4251.8 | 33.8 | 98.4 | 0 | 0.7 | 0.4 | 0.5 |
| S-19 | 4269.6 | 51.6 | 94.8 | 3.1 | 2.1 | 0 | 0 |
| S-18 | 4279 | 61 | 99.6 | 0 | 0.4 | 0 | 0 |
| S-17 | 4284.3 | 66.3 | 99.5 | 0 | 0.5 | 0 | 0 |
| S-16 | 4296 | 78 | 99.4 | 0 | 0.6 | 0 | 0 |
| S-15 | 4301.2 | 83.2 | 100 | 0 | 0 | 0 | 0 |
| S-14 | 4303.1 | 85.1 | 100 | 0 | 0 | 0 | 0 |
| S-13 | 4305 | 87 | 100 | 0 | 0 | 0 | 0 |
| S-12 | 4306.5 | 88.5 | 100 | 0 | 0 | 0 | 0 |
| S-11 | 4307.6 | 89.6 | 100 | 0 | 0 | 0 | 0 |
| S-10 | 4308.2 | 90.2 | 100 | 0 | 0 | 0 | 0 |
| S-9 | 4308.9 | 90.9 | 99.4 | 0 | 0.6 | 0 | 0 |
| S-8 | 4309.3 | 91.3 | 99.5 | 0 | 0.5 | 0 | 0 |
| S-7 | 4310.9 | 92.9 | 99.4 | 0 | 0.6 | 0 | 0 |
| S-6 | 4332.2 | 114.2 | 91.9 | 5.6 | 2 | 0.5 | 0 |
| S-5 | 4357.6 | 139.6 | 99.3 | 0 | 0.7 | 0 | 0 |
| S-4 | 4372.9 | 154.9 | 90.1 | 5.9 | 3.6 | 0.4 | 0 |
| S-3 | 4383.9 | 165.9 | 98.1 | 0.7 | 1.2 | 0 | 0 |
| HO-25 | 4244.9 | 12.9 | 99.5 | 0 | 0.5 | 0 | 0 |
| HO-24 | 4251.8 | 19.8 | 99.4 | 0 | 0.6 | 0 | 0 |
| HO-23 | 4252.7 | 20.7 | 98.2 | 1 | 0.8 | 0 | 0 |
| HO-22 | 4260.5 | 28.5 | 99.4 | 0 | 0.6 | 0 | 0 |
| HO-21 | 4261.5 | 29.5 | 96.4 | 0 | 0.7 | 1.9 | 1 |
| HO-20 | 4266.6 | 34.6 | 99.2 | 0 | 0.8 | 0 | 0 |
| HO-19 | 4275.4 | 43.4 | 100 | 0 | 0 | 0 | 0 |
| HO-18 | 4280.4 | 48.4 | 99.6 | 0 | 0.4 | 0 | 0 |
| HO-17 | 4285.9 | 53.9 | 99.5 | 0 | 0.5 | 0 | 0 |
| HO-16 | 4300.9 | 68.9 | 100 | 0 | 0 | 0 | 0 |
| HO-15 | 4311.4 | 79.4 | 99.6 | 0 | 0.4 | 0 | 0 |
| HO-14 | 4317.4 | 85.4 | 97.7 | 0 | 1.2 | 0.5 | 0.6 |
| HO-13 | 4321 | 89 | 98 | 1.1 | 0.9 | 0 | 0 |
| HO-12 | 4323.6 | 91.6 | 96.9 | 1.3 | 1.3 | 0.5 | 0 |
| HO-11 | 4326 | 94 | 99.5 | 0 | 0.5 | 0 | 0 |
| HO-10 | 4329.4 | 97.4 | 98.4 | 0 | 0.9 | 0 | 0.7 |
| HO-9 | 4368.3 | 136.3 | 94.2 | 3.2 | 2.1 | 0 | 0.5 |
| HO-8 | 4406.4 | 174.4 | 99.3 | 0 | 0.7 | 0 | 0 |
| HO-7 | 4412.9 | 180.9 | 99.2 | 0 | 0.8 | 0 | 0 |
| HO-6 | 4417 | 185 | 98.4 | 0 | 1.6 | 0 | 0 |
| HO-5 | 4422.9 | 190.9 | 98.9 | 0 | 1.1 | 0 | 0 |
| Sample | TVDSS (ft) | DBTF (ft) | Calcite (%) | Dolomite(%) | Quartz (%) | Pyrite (%) | Clay (%) |
| HO-4 | 4425.4 | 193.4 | 97 | 1.6 | 1.4 | 0 | 0 |
| HO-3 | 4430.1 | 198.1 | 99.3 | 0 | 0.7 | 0 | 0 |
| HO-2 | 4431.5 | 199.5 | 94.1 | 3.7 | 2.2 | 0 | 0 |
| HE-23 | 3557 | 6 | 92 | 4.5 | 0.6 | 2.9 | 0 |
| HE-22 | 3586.1 | 35.1 | 94 | 4.9 | 1.1 | 0 | 0 |
| HE-21 | 3600 | 49 | 95.5 | 3.7 | 0.8 | 0 | 0 |
| HE-20 | 3635 | 84 | 94.1 | 4.6 | 1.3 | 0 | 0 |
| HE-19 | 3640 | 89 | 99.2 | 0 | 0.8 | 0 | 0 |
| HE-18 | 3645 | 94 | 99.4 | 0 | 0.6 | 0 | 0 |
| HE-17 | 3647.5 | 96.5 | 99.1 | 0 | 0.9 | 0 | 0 |
| HE-16 | 3651 | 100 | 99.2 | 0 | 0.8 | 0 | 0 |
| HE-15 | 3653.5 | 102.5 | 99.1 | 0 | 0.9 | 0 | 0 |
| HE-14 | 3655.7 | 104.7 | 99.2 | 0 | 0.8 | 0 | 0 |
| HE-13 | 3659 | 108 | 99.3 | 0 | 0.7 | 0 | 0 |
| HE-12 | 3660.5 | 109.5 | 96.6 | 2.4 | 1 | 0 | 0 |
| HE-11 | 3662.9 | 111.9 | 96.2 | 2.8 | 1 | 0 | 0 |
| HE-10 | 3666 | 115 | 95.9 | 3.1 | 1 | 0 | 0 |
| HE-9 | 3667.5 | 116.5 | 92 | 5.3 | 1.6 | 1.1 | 0 |
| HE-8 | 3669 | 118 | 89.7 | 7.3 | 3 | 0 | 0 |
| C-21 | 4229 | 40 | 87.3 | 7.6 | 2.4 | 0.9 | 1.8 |
| C-20 | 4244.6 | 55.6 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-19 | 4255.8 | 66.8 | 84.5 | 12.2 | 1.9 | 0.5 | 0.9 |
| C-18 | 4258.6 | 69.6 | 52.1 | 38.8 | 4.4 | 2.1 | 2.6 |
| C-17 | 4262 | 73 | 98.6 | 0.8 | 0.6 | 0 | 0 |
| C-16 | 4272 | 83 | 98.3 | 1.1 | 0.6 | 0 | 0 |
| C-15 | 4273.5 | 84.5 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-14 | 4276.5 | 87.5 | 96.2 | 2.7 | 1.1 | 0 | 0 |
| C-13 | 4280.6 | 91.6 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-12 | 4284 | 95 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-11 | 4287 | 98 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-10 | 4289.5 | 100.5 | 99.4 | 0 | 0.6 | 0 | 0 |
| C-9 | 4299.5 | 110.5 | 99.3 | 0 | 0.7 | 0 | 0 |
| C-8 | 4306 | 117 | 99.4 | 0 | 0.6 | 0 | 0 |
| C-7 | 4311 | 122 | 99.4 | 0 | 0.6 | 0 | 0 |
| C-6 | 4313.1 | 124.1 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-5 | 4316 | 127 | 98.6 | 0.7 | 0.7 | 0 | 0 |
| C-4 | 4317.5 | 128.5 | 99.6 | 0 | 0.4 | 0 | 0 |
| C-3 | 4319 | 130 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-2 | 4320 | 131 | 99.5 | 0 | 0.5 | 0 | 0 |
| C-1 | 4321 | 132 | 99.3 | 0 | 0.7 | 0 | 0 |
| A-25 | 4243.2 | 13.2 | 98.4 | 0.8 | 0.8 | 0 | 0 |
| A-24 | 4250.3 | 20.3 | 94.6 | 3.2 | 2.2 | 0 | 0 |
| A-23 | 4260.3 | 30.3 | 98.6 | 0.6 | 0.8 | 0 | 0 |
| A-22 | 4262.4 | 32.4 | 99.3 | 0 | 0.7 | 0 | 0 |
| A-21 | 4265.6 | 35.6 | 99.4 | 0 | 0.6 | 0 | 0 |
| A-20 | 4267.1 | 37.1 | 99.3 | 0 | 0.7 | 0 | 0 |
| Sample | TVDSS (ft) | DBTF (ft) | Calcite (%) | Dolomite(%) | Quartz (%) | Pyrite (%) | Clay (%) |
| A-19 | 4269.8 | 39.8 | 97.5 | 1.6 | 0.9 | 0 | 0 |
| A-18 | 4273 | 43 | 99.4 | 0 | 0.6 | 0 | 0 |
| A-17 | 4283.9 | 53.9 | 98.3 | 0 | 0.7 | 1 | 0 |
| A-16 | 4298.4 | 68.4 | 96.9 | 1.7 | 1.4 | 0 | 0 |
| A-15 | 4302.5 | 72.5 | 53.3 | 39.9 | 2.7 | 1.7 | 2.4 |
| A-14 | 4303.8 | 73.8 | 93.4 | 5.4 | 0.5 | 0.7 | 0 |
| A-13 | 4306.8 | 76.8 | 98.5 | 0 | 0.5 | 1 | 0 |
| A-12 | 4308.1 | 78.1 | 98.1 | 0 | 0.6 | 1.3 | 0 |
| A-11 | 4310 | 80 | 96.8 | 2.6 | 0.6 | 0 | 0 |
| A-10 | 4310.5 | 80.5 | 98.3 | 1.2 | 0.5 | 0 | 0 |
| A-9 | 4311 | 81 | 96.6 | 1.9 | 0.6 | 0.9 | 0 |
| A-8 | 4313.3 | 83.3 | 99.5 | 0 | 0.5 | 0 | 0 |
| A-7 | 4314.5 | 84.5 | 97.7 | 1.2 | 0.5 | 0.6 | 0 |
| A-6 | 4328.1 | 98.1 | 99.5 | 0 | 0.5 | 0 | 0 |
| A-5 | 4340.8 | 110.8 | 98.2 | 1.2 | 0.6 | 0 | 0 |
| A-4 | 4347.9 | 117.9 | 99.2 | 0 | 0.8 | 0 | 0 |
| A-3 | 4361.1 | 131.1 | 98.5 | 0.9 | 0.6 | 0 | 0 |
| A-2 | 4369.5 | 139.5 | 67 | 29.3 | 1.6 | 0.8 | 1.3 |
| A-1 | 4370.1 | 140.1 | 98.9 | 0 | 1.1 | 0 | 0 |

APPENDIX 5 – Isotope data

Table A5.1: Isotope data (δ13C and δ18O) for each sample (whole rock) of the Great Oolite Formation analysed in Singleton-1, Horndean-1A, Hesters Copse-1, Chilgrove-1, Ashington-1 and Storrington-2 wells.

| Sample | TVDSS (ft) | DBTF (ft) | δ13C (‰PDB) | δ18O (‰PDB) |
| --- | --- | --- | --- | --- |
| S-25 | 4218.7 | 0.7 | 0.25 | -3.78 |
| S-24 | 4220.6 | 2.6 | 1.29 | -4.38 |
| S-23 | 4228.3 | 10.3 | 1.13 | -4.08 |
| S-22 | 4233.7 | 15.7 | 1.03 | -4.75 |
| S-21 | 4241.0 | 23.0 | 1.22 | -3.72 |
| S-20 | 4251.8 | 33.8 | 1.31 | -3.79 |
| S-19 | 4269.6 | 51.6 | 1.05 | -5.66 |
| S-18 | 4279.0 | 61.0 | 1.51 | -5.30 |
| S-17 | 4284.3 | 66.3 | 1.51 | -5.27 |
| S-16 | 4296.0 | 78.0 | 1.69 | -4.71 |
| S-15 | 4301.2 | 83.2 | 1.66 | -5.31 |
| S-14 | 4303.1 | 85.1 | 1.71 | -5.34 |
| S-13 | 4305.0 | 87.0 | 1.78 | -4.44 |
| S-12 | 4306.5 | 88.5 | 1.80 | -5.22 |
| S-11 | 4307.6 | 89.6 | 1.72 | -5.34 |
| S-10 | 4308.2 | 90.2 | 1.77 | -5.88 |
| S-9 | 4308.9 | 90.9 | 1.67 | -5.48 |
| S-8 | 4309.3 | 91.3 | 1.73 | -5.44 |
| S-7 | 4310.9 | 92.9 | 1.72 | -4.59 |
| S-6 | 4332.2 | 114.2 | 1.65 | -4.87 |
| S-5 | 4357.6 | 139.6 | 1.79 | -5.14 |
| S-4 | 4372.9 | 154.9 | 1.74 | -5.33 |
| S-3 | 4383.9 | 165.9 | 1.67 | -4.59 |
| HO-25 | 4244.9 | 12.9 | 1.03 | -4.51 |
| HO-24 | 4251.8 | 19.8 | 1.05 | -5.67 |
| HO-23 | 4252.7 | 20.7 | 1.09 | -5.52 |
| HO-22 | 4260.5 | 28.5 | 1.38 | -5.13 |
| HO-21 | 4261.5 | 29.5 | 1.38 | -5.02 |
| HO-20 | 4266.6 | 34.6 | 1.17 | -5.84 |
| HO-19 | 4275.4 | 43.4 | 1.51 | -5.16 |
| HO-18 | 4280.4 | 48.4 | 1.49 | -4.92 |
| HO-17 | 4285.9 | 53.9 | 1.64 | -5.33 |
| HO-16 | 4300.9 | 68.9 | 1.68 | -5.65 |
| HO-15 | 4311.4 | 79.4 | 1.57 | -5.88 |
| HO-14 | 4317.4 | 85.4 | 1.48 | -5.66 |
| HO-13 | 4321.0 | 89.0 | 1.70 | -4.93 |
| HO-12 | 4323.6 | 91.6 | 1.70 | -4.81 |
| HO-11 | 4326.0 | 94.0 | 1.74 | -5.15 |
| HO-10 | 4329.4 | 97.4 | 1.69 | -5.20 |
| HO-9 | 4368.3 | 136.3 | 1.53 | -5.46 |
| HO-8 | 4406.4 | 174.4 | 2.24 | -5.35 |
| HO-7 | 4412.9 | 180.9 | 2.21 | -5.23 |
| HO-6 | 4417.0 | 185.0 | 2.08 | -5.41 |
| Sample | TVDSS (ft) | DBTF (ft) | δ13C (‰PDB) | δ18O (‰PDB) |
| HO-5 | 4422.9 | 190.9 | 1.92 | -4.91 |
| HO-4 | 4425.4 | 193.4 | 1.84 | -5.60 |
| HO-3 | 4430.1 | 198.1 | 2.11 | -5.21 |
| HO-2 | 4431.5 | 199.5 | 1.76 | -4.91 |
| HE-23 | 3557.0 | 6.0 | 1.21 | -4.04 |
| HE-22 | 3586.1 | 35.1 | 1.51 | -4.29 |
| HE-21 | 3600.0 | 49.0 | 1.86 | -4.82 |
| HE-20 | 3635.0 | 84.0 | 2.16 | -4.50 |
| HE-19 | 3640.0 | 89.0 | 2.04 | -5.34 |
| HE-18 | 3645.0 | 94.0 | 2.14 | -5.02 |
| HE-17 | 3647.5 | 96.5 | 2.06 | -5.16 |
| HE-16 | 3651.0 | 100.0 | 2.07 | -5.42 |
| HE-15 | 3653.5 | 102.5 | 2.13 | -4.84 |
| HE-14 | 3655.7 | 104.7 | 2.13 | -5.07 |
| HE-13 | 3659.0 | 108.0 | 2.07 | -5.13 |
| HE-12 | 3660.5 | 109.5 | 2.10 | -5.22 |
| HE-11 | 3662.9 | 111.9 | 2.18 | -4.61 |
| HE-10 | 3666.0 | 115.0 | 2.09 | -4.79 |
| HE-9 | 3667.5 | 116.5 | 2.11 | -4.29 |
| HE-8 | 3669.0 | 118.0 | 2.04 | -5.31 |
| C-21 | 4229.0 | 40.0 | 1.14 | -4.08 |
| C-20 | 4244.6 | 55.6 | 1.20 | -4.43 |
| C-19 | 4255.8 | 66.8 | 1.48 | -4.23 |
| C-18 | 4258.6 | 69.6 | 1.54 | -3.90 |
| C-17 | 4262.0 | 73.0 | 1.61 | -4.53 |
| C-16 | 4272.0 | 83.0 | 1.54 | -5.26 |
| C-15 | 4273.5 | 84.5 | 1.40 | -5.70 |
| C-14 | 4276.5 | 87.5 | 1.39 | -4.86 |
| C-13 | 4280.6 | 91.6 | 1.37 | -4.87 |
| C-12 | 4284.0 | 95.0 | 1.23 | -5.49 |
| C-11 | 4287.0 | 98.0 | 1.01 | -5.37 |
| C-10 | 4289.5 | 100.5 | 1.20 | -4.62 |
| C-9 | 4299.5 | 110.5 | 1.07 | -5.07 |
| C-8 | 4306.0 | 117.0 | 1.07 | -4.77 |
| C-7 | 4311.0 | 122.0 | 1.20 | -5.55 |
| C-6 | 4313.1 | 124.1 | 1.20 | -5.97 |
| C-5 | 4316.0 | 127.0 | 1.30 | -6.11 |
| C-4 | 4317.5 | 128.5 | 1.45 | -6.01 |
| C-3 | 4319.0 | 130.0 | 1.51 | -5.00 |
| C-2 | 4320.0 | 131.0 | 1.51 | -6.12 |
| C-1 | 4321.0 | 132.0 | 1.60 | -4.60 |
| A-25 | 4243.2 | 13.2 | 0.21 | -4.11 |
| A-24 | 4250.3 | 20.3 | 0.55 | -4.15 |
| A-23 | 4260.3 | 30.3 | 0.77 | -4.39 |
| A-22 | 4262.4 | 32.4 | 0.81 | -4.94 |
| A-21 | 4265.6 | 35.6 | 0.87 | -4.84 |
| Sample | TVDSS (ft) | DBTF (ft) | δ13C (‰PDB) | δ18O (‰PDB) |
| A-20 | 4267.1 | 37.1 | 1.04 | -5.60 |
| A-19 | 4269.8 | 39.8 | 1.11 | -4.45 |
| A-18 | 4273.0 | 43.0 | 1.04 | -5.62 |
| A-17 | 4283.9 | 53.9 | 0.87 | -6.08 |
| A-16 | 4298.4 | 68.4 | 0.86 | -4.98 |
| A-15 A-14 | 4302.5 4303.8 | 72.5 73.8 | 1.84 1.30 | -3.86 -6.02 |
| A-13 | 4306.8 | 76.8 | 1.32 | -6.03 |
| A-12 | 4308.1 | 78.1 | 1.28 | -5.84 |
| A-11 | 4310.0 | 80.0 | 1.49 | -5.37 |
| A-10 | 4310.5 | 80.5 | 1.53 | -4.87 |
| A-9 | 4311.0 | 81.0 | 1.49 | -5.24 |
| A-8 | 4313.3 | 83.3 | 1.58 | -4.79 |
| A-7 | 4314.5 | 84.5 | 1.64 | -4.54 |
| A-6 | 4328.1 | 98.1 | 1.76 | -6.08 |
| A-5 | 4340.8 | 110.8 | 1.67 | -4.99 |
| A-4 | 4347.9 | 117.9 | 1.76 | -5.67 |
| A-3 | 4361.1 | 131.1 | 1.75 | -6.05 |
| A-2 | 4369.5 | 139.5 | 2.00 | -4.34 |
| A-1 | 4370.1 | 140.1 | 1.65 | -6.14 |
| ST-20 | 3891.0 | 2.1 | 0.66 | -4.05 |
| ST-19 | 3893.0 | 4.1 | 0.95 | -4.32 |
| ST-18 | 3918.0 | 29.1 | 1.36 | -5.65 |
| ST-17 | 3921.3 | 32.4 | 1.44 | -4.16 |
| ST-16 | 3927.8 | 38.9 | 1.30 | -4.94 |
| ST-15 | 3938.4 | 49.5 | 1.30 | -6.09 |
| ST-14 | 3966.0 | 77.1 | 1.66 | -3.95 |
| ST-13 | 3985.9 | 97.0 | 2.03 | -3.92 |
| ST-12 | 3992.0 | 103.1 | 1.62 | -4.60 |
| ST-11 | 4011.0 | 122.1 | 2.12 | -3.98 |
| ST-10 | 4013.0 | 124.1 | 1.95 | -4.06 |
| ST-9 | 4024.0 | 135.1 | 1.72 | -4.80 |
| ST-8 | 4031.0 | 142.1 | 1.82 | -5.23 |
| ST-7 | 4035.0 | 146.1 | 1.85 | -5.07 |
| ST-6 | 4040.0 | 151.1 | 1.97 | -4.91 |
| ST-5 | 4045.0 | 156.1 | 1.72 | -5.38 |
| ST-4 | 4054.0 | 165.1 | 1.99 | -4.08 |
| ST-3 | 4064.0 | 175.1 | 1.63 | -4.67 |
| ST-2 | 4077.5 | 188.6 | 1.77 | -4.54 |
| ST-1 | 4092.0 | 203.1 | 2.06 | -4.91 |

Table A5.2: Isotope data (δ13C and δ18O) for each separate late cement sample of the Great Oolite Formation analysed in Horndean-1A, Singleton-1, Chilgrove-1, Ashington-1 and Storrington-2 wells.

| Sample | TVDSS (ft) | DBTF (ft) | Cement type | Sampling point | δ13C (‰PDB) | δ18O (‰PDB) |
| --- | --- | --- | --- | --- | --- | --- |
| HO-23(a) | 4252.7 | 20.7 | Ferroan calcite | Fracture | 1.26 | -6.97 |
| HO-23(b) | 4252.7 | 20.7 | Ferroan calcite | Intergranular | 1.38 | -7.62 |
| HO-20 | 4266.6 | 34.6 | Ferroan calcite | Intergranular | 1.50 | -7.17 |
| HO-18 | 4280.4 | 48.4 | Ferroan calcite | Intergranular | 1.42 | -7.40 |
| HO-17 | 4285.9 | 53.9 | Ferroan calcite | Intergranular | 1.40 | -7.57 |
| HO-14 | 4317.4 | 85.4 | Ferroan calcite | Intergranular | 1.86 | -7.35 |
| HO-8 | 4406.4 | 174.4 | Ferroan calcite | Intergranular | 2.20 | -7.08 |
| HO-7 | 4412.9 | 180.9 | Ferroan calcite | Intergranular | 2.22 | -7.01 |
| S-24 | 4220.6 | 2.6 | Ferroan calcite | Intergranular | 1.34 | -6.81 |
| S-23 | 4228.3 | 10.3 | Ferroan calcite | Intergranular | 0.53 | -7.40 |
| S-23(a) | 4228.3 | 10.3 | Coarse dolomite | Intergranular | 1.08 | -8.95 |
| S-23(b) | 4228.3 | 10.3 | Coarse dolomite | Intergranular | 1.15 | -9.18 |
| S-19 | 4269.6 | 51.6 | Ferroan calcite | Intergranular | 1.18 | -7.42 |
| S-17(a) | 4284.3 | 66.3 | Ferroan calcite | Intergranular | 1.38 | -7.21 |
| S-17(b) | 4284.3 | 66.3 | Ferroan calcite | Intergranular | 1.42 | -7.45 |
| S-10(a) | 4308.2 | 90.2 | Ferroan calcite | Intergranular | 1.41 | -8.22 |
| S-10(b) | 4308.2 | 90.2 | Ferroan calcite | Intergranular | 1.45 | -6.77 |
| S-4 | 4372.9 | 154.9 | Ferroan calcite | Intergranular | 1.72 | -6.81 |
| C-17 | 4262.0 | 73.0 | Ferroan calcite | Intergranular | 1.63 | -6.34 |
| C-16 | 4272.0 | 83.0 | Ferroan calcite | Intergranular | 1.55 | -7.25 |
| C-14 | 4276.5 | 87.5 | Ferroan calcite | Intergranular | 1.21 | -7.12 |
| C-11 | 4287.0 | 98.0 | Ferroan calcite | Intergranular | 1.29 | -6.51 |
| C-10 | 4289.5 | 100.5 | Ferroan calcite | Intergranular | 1.16 | -6.67 |
| C-9 | 4299.5 | 110.5 | Ferroan calcite | Intergranular | 0.96 | -7.62 |
| C-5 | 4316.0 | 127.0 | Ferroan calcite | Fracture | 1.24 | -8.33 |
| A-21 | 4265.6 | 35.6 | Ferroan calcite | Intergranular | 0.90 | -7.79 |
| A-11 | 4310.0 | 80.0 | Ferroan calcite | Intergranular | 1.47 | -8.07 |
| A-8 | 4313.3 | 83.3 | Ferroan calcite | Intergranular | 1.56 | -8.01 |
| A-5 | 4340.8 | 110.8 | Ferroan calcite | Intergranular | 1.62 | -7.97 |
| ST-20(a) | 3891.0 | 2.1 | Coarse dolomite | Fracture | 0.55 | -9.30 |
| ST-20(b) | 3891.0 | 2.1 | Coarse dolomite | Fracture | 0.61 | -8.84 |
| ST-17 | 3921.3 | 32.4 | Ferroan calcite | Intergranular | 1.45 | -6.84 |
| ST-12 | 3992.0 | 103.1 | Ferroan calcite | Intergranular | 1.63 | -7.03 |
| ST-10 | 4013.0 | 124.1 | Ferroan calcite | Intergranular | 1.91 | -6.98 |